Understanding Energy Loss in Organic Solar Cells: Towards a New Efficiency Regime

S. Matthew Menke,1 Niva A. Ran,2 Guillermo C. Bazan,2 Richard H. Friend1

1SMM and RHF

Department of Physics, Cavendish Laboratory, University of Cambridge, J.J. Thompson Avenue, Cambridge, CB3 0HE, United Kingdom

2NAR and GCB

Center for Polymers and Organic Solids, University of California, Santa Barbara, Santa Barbara, CA, 93106, USA

# Abstract

Reducing energy and voltage loss is an imperative area of improvement for the design of organic solar cells (OSCs). Both in the context of charge generation and charge recombination, significant amounts of energy are lost even in state-of-the-art OSCs compared to their inorganic counterparts. Through a set of recent examples, however, we show that (1) charge generation can proceed with a high quantum efficiency even in the absence of an offset energy at the donor-acceptor interface and (2) non-radiative charge recombination may be mitigated by considering systems with distinct properties of the interfacial charge-transfer state. To capitalize on these recent advances in understanding, we provide three actionable paths forward that aim to better identify, process, and characterize low energy loss systems: incorporating consistent and accurate measurements for energy levels, moving away from photoluminescence quenching, and exploring blends with reduced miscibility.

# Keywords

Organic Solar Cell; Energy Loss; Charge Generation; Charge Recombination; Charge Transfer States

# Introduction

Energy loss (Eloss) in a solar cell is embodied by the difference between the optical energy gap of a semiconductor (Eg) and its open-circuit voltage (eVOC). In the thermodynamic limit of solar to electrical energy conversion for an ideal semiconductor, several factors contribute to a minimum amount of energy loss that always exists: (1) Imperfect absorption, (2) Carnot loss, and (3) éntendue expansion.1,2 The first factor signals that unabsorbed photons will limit the available number of carriers in the cell, while the other two factors are additive entropic losses due to the finite temperature of the sun and the irreversibility in the direction of photon absorption versus emission. In practice, inorganic semiconductors such as GaAs and hybrid Pb-halide perovskites are approaching this fundamental limit with power conversion efficiencies exceeding 25% and 20%, respectively.3

For state-of-the-art organic solar cells (OSCs), there are additional pathways that further increase energy loss and, presently, limit power conversion efficiencies to less than 15%.4 Primarily, the excitonic nature of photogenerated electron-hole pairs in an organic semiconductor fundamentally alters the nature of carrier generation. The binding energy for an exciton varies depending on both the chemical nature of the molecule and its surroundings. Values are on the order of 0.5 eV or larger.5,6 An electron donor-acceptor (DA) interface is considered to be required in order to overcome the binding energy of the exciton by providing a driving force for electron-hole separation.

One observation is that efficient systems typically have a ~300 meV offset in molecular orbital energy levels between the donor and acceptor. This sets up an interfacial charge-transfer (CT) state with an energy ECT<Eg. In terms of the thermodynamics of organic solar cells, the interfacial CT state plays the role of the semiconductor energy gap in the system. This situation is visualized in Figure 1a. We define energy loss incurred during charge generation as the difference between Eg and ECT and energy loss incurred during charge recombination as the difference between ECT and eVOC (Fig. 1b). As these interfacial CT states are weakly absorbing and also show low luminescence efficiencies due to their small oscillator strengths, additional energy is lost due to incomplete absorption and non-radiative recombination. Altogether, most organic solar cells typically demonstrate energy losses ranging from 0.7–1 eV.7

In order for organic solar cells to move beyond 15% efficiency and capitalize on their promised advantages such as compatibility with lightweight substrates, scalable manufacturing processes, and abundant chemical feedstocks, energy loss values must be reduced below 0.5 eV. In this perspective, we begin by capturing our current understanding of energy loss pathways in organic solar cells and highlight some general observations that would appear to confer organic solar cells with an intrinsically higher degree of energy loss than their inorganic counterparts. We then provide a series of illustrative examples that suggest that these may not be intrinsic limitations and make the case that implicit measurement bias may have, to date, precluded the discovery of more efficient systems with lower energy losses.

# Current Understanding of Energy Loss in Organic Solar Cells

It has been suggested, and often assumed, that the energetic offsets between the electron affinities (or lowest unoccupied molecular orbitals, LUMO) as well as the ionization potentials (or highest occupied molecular orbitals, HOMO) of the donor and acceptor must be above a certain minimum value to achieve good quantum efficiency for charge generation. The evidence for this is relatively straightforward: by mixing donor and acceptor materials with varying energy levels, the offset energy can be tuned. For small offsets, the short-circuit current density (JSC) and fill factor (FF) decrease sharply, and consequently the power conversion efficiency (ηPCE) of the devices decreases. This is illustrated in a recent study by Li et al., who reported on a series of a four DPP-based polymers with varying bandgap values  in combination with fullerene acceptors.8 Li et al. find a correlation between reducing the energy loss, Eloss and the maximum external quantum efficiency (ηEQE), with a sharp drop in ηEQE for Eloss<0.6 eV. They illustrate this behaviour in the context of literature data using a number of polymer-based solar cells, reproduced here in Fig. 2. As will be discussed in the next section, this review has been, in part, motivated by the discovery of systems which populate the upper left region in Fig. 2, requiring the field to reconsider this category of design rule.

As noted above, we divide the energy loss into two parts: energy lost due to charge generation (Eg−ECT) and energy lost due to charge recombination (ECT−eVOC). Below, we provide a snapshot of our current understanding of these two energy loss components.

## Charge Generation

Eg−ECT correlates with the energetic offsets between the donor and acceptor components—larger offsets typically result in larger Eg−ECT. By modifying the chemical structure of either the donor or acceptor, and thus the energy levels, Eg−ECT can be tuned.9 For example, we can consider the case of two high-efficiency, structurally-related copolymers: PNTz4T and PNOz4T, blended with PC71BM. The Eloss of PNTz4T solar cells, 0.77 eV, is significantly higher than the Eloss of PNOz4T, 0.56 eV. PNTz4T was first reported on the merits of its high JSC=19.4 mA cm-2 (VOC=0.71 V, FF=73%), and consequently its high ηPCE=9.8%.10 PNOz4T, on the other hand, was able to achieve ηPCE=8.5% with a very high VOC=0.97 V (JSC=14.6 mA cm-2, FF=62%).11 Between the two systems, PNTz4T:PC71BM has an Eg−ECT=1.55−1.07=0.49 eV, while PNOz4T:PC71BM has Eg−ECT=1.52−1.38 eV=0.14 eV. The difference in Eg−ECT between the two systems accounts for the large difference in energy loss: 1.0–0.96 eV in the case of PNTz4T blends, and 0.71–0.74 eV in the case of PNOz4T blends. However, we know that modifying the chemical structure to tune Eg−ECT can change more than just the energy landscape.

Several reports have addressed properties besides the degree of offset energy that may affect the efficiency of charge carrier generation: the dissociation of hot excitons,12 vibronic coupling,13 access to delocalized accepting states,14,15 high local charge mobility,16 interfacial dipoles,17,18 and energy cascades, among others. As charge generation has been known to occur efficiently even when a CT state is directly excited,19 the efficiency of charge generation is likely tied to the nature of the CT state wavefunction as well as to that of the exciton. Recently, the contribution of entropy has been highlighted and it follows that if the entropic energy gain can outweigh the enthalpic energy change determined by the CT state binding energy, then the free energy of the process can favour the separated state.20–24 The degree of entropic gain is therefore correlated to the number of states accessible by each carrier as dictated by the interfacial morphology at the nanoscale.21,25 Efficient charge separation is achievable if the carriers can access these states on a timescale shorter than the CT state recombination timescale.

## Charge Recombination

ECT−eVOC reflects the energy lost to charge recombination and the consequent decrease in quasi-Fermi level splitting. ECT−eVOC can be divided into radiative and non-radiative recombination. Detailed balance analysis shows that all solar cells must lose some voltage to radiative recombination.1,26,27 A certain amount of energy loss due to radiative recombination is therefore intrinsic, and sets the upper limit for the VOC. In the Shockley-Queisser framework, the maximum achievable VOC is ~0.3 eV lower than the optical energy gap due to radiative recombination (note that the exact value will depend on the assumed properties of an idealized semiconductor).2 However, any additional voltage (energy) that is lost by non-radiative recombination is superfluous and should be curtailed. The amount of voltage loss due to non-radiative recombination is quantified by extending the description from Ross:28

∆VOC,NR=-kBTqln⁡(ϕ)	(1)

where kB is the Boltzmann constant, T is the temperature, q is the charge of an electron and  is the radiative efficiency of the system.  Commonly,  is represented as either the photoluminescence quantum yield or external electroluminescence quantum efficiency. While there has been a strong effort in identifying non-radiative recombination pathways in OSC blends, only modest progress has been made in their suppression. As we will discuss later, an implicit screening bias during material selection may be the culprit.

Non-radiative recombination can be geminate or non-geminate, and includes recombination through triplet states, structural defects or energetic traps, and Auger recombination. A recent report has suggested that the high non-radiative recombination in OSC is intrinsic to the C-C bond (and thus to all organic-based materials).29 Benduhn et al. have published a comprehensive analysis which shows an inverse relation between the ECT and the non-radiative energy loss for a wide range of OSC blends and device architectures, following the energy gap law,30 or the transition rate in the Marcus inverted regime (which decreases as the free energy of the process increases).31 Note that increases in non-radiative recombination with smaller ECT will increase the difference between ECT and eVOC, resulting in a lower overall VOC.

# Systems that Break Trends

Recent results have highlighted systems that are able to achieve high performance with very small energy loss.11,32–36 According to empirically-derived guidelines reported in previous studies, OSC devices with such small Eloss should have negligible ηPCE. As this is clearly not the case, these examples make one question the accuracy of these guidelines. In fact, ηEQE vs. Eloss data collected for the most recent examples of high performance solar cells suggest that efforts to decrease Eloss have managed to break the trends observed in older examples (such as what was shown by Li et al., Figure 2), as illustrated in Figure 3. Note that ηEQE can also vary due to extrinsic factors such as optical interference. A better metric might be the internal quantum efficiency (ηIQE) which normalizes for differences in the absorption efficiency of the device. However, consistent values for ηIQE are not readily available.

## Charge Generation

The ability to generate charges efficiently in the absence of a large energy offset at the DA interface has the potential to greatly reduce charge generation-incurred energy loss. In one recent example, Liu et. al. demonstrated that a blend of P3TEA and SF-PDI2 can generate charges (ηEQE > 60%) with a negligible difference between Eg and ECT.37  Indeed, our own work has demonstrated efficient charge generation in a blend of PIPCP and PC61BM with Eg−ECT~50 meV.36 At face value, there are very few chemical similarities between these two systems, and work is needed to understand what underlying physical mechanisms allow these systems reach such high ηEQE. In yet another striking example, Tabachnyk et. al. have shown that it is even possible to achieve near unity efficiency for electron-hole separation from triplet excitons at the interface between pentacene and C60 for which the pentacene triplet and initially-generated CT state are isoenergetic and generation of the long-range separated electron hole pair has an overall endothermicity of 220 meV.25

Photovoltaic operation requires that electrons and holes separate to distances greater than their Langevin recombination radius (generally considered to be >5 nm).15 The initial exciton ionisation at the DA interface needs therefore to be followed by separation of the electron from hole across a significant Coulomb barrier or binding energy (Fig. 4) that is generally found to be around 200-300 meV.15  Two models for this second process are considered in the literature. The first invokes carriers accessing delocalized states within, for example, fullerene clusters or nanocrystalline donor or acceptor domains, and their rapid motion as the ‘band velocity’ is higher within these regions.15 The second invokes the incoherent motion of carriers between localized states with a sufficiently high local mobility.  Indirect measurements for the rise time of the Coulomb barrier (through observation of Stark electroabsorption generated between a separating electron and hole) can show extremely fast charge separation, as fast as <100 fs for systems with large offset energies.38 In systems with smaller offset energies or direct excitation of CT states, there is insufficient energy for the electron and hole to move against their mutual Coulomb attraction, and the mechanism for charge separation has been more speculative, though there are now indications that in some of these systems, where the overall long range charge photogeneration process is endothermic, there is a significant waiting time of up to 100 ps following charge generation before full separation.25 This is considered to arise from the time for thermal excitation to overcome the long-range Coulomb barrier (W) (Fig. 4).

Open questions still remain about the precise nature of charge separation including the degree to which coherent charge motion and high local mobility can describe the same phenomenon. More work is required to answer these questions, in particular for non-fullerene acceptors and in low energy loss systems. For this reason, we have opted here to keep the discussion to a high level. Regardless of the mechanism, it is apparent that free carriers can be generated in purely organic heterojunctions with zero exothermicity (energy loss) and even to upwards of ~200 meV of endothermicity.

## Charge Recombination

Charge recombination poses a larger problem for reducing energy loss in OSCs. As many groups have noted, there exists no organic solar cell which displays ECT–eVOC<0.5 eV and many cells exhibit values of 0.5-0.7 eV. This potential loss is made up of radiative and non-radiative recombination, as discussed above. In order to reduce this energy loss contribution, CT states with significantly weaker non-radiative decay pathways are required.

One possible avenue is the continued optimization of new non-fullerene acceptors. Nearly all the experimental results used in the study by Benduhn et al. utilize fullerenes as the acceptor material. Indeed, some recent reports on non-fullerene acceptors suggest much higher electroluminescence quantum efficiencies (ηEL) are possible, a proxy for the degree of non-radiative recombination (see Eq. 1), resulting in a reduction in non-radiative energy loss of ~200–300 meV.32,37,39 It remains unclear, however, (1) which non-radiative pathways have been mitigated in these non-fullerene systems and (2) if there is a fundamental advantage of using a non-fullerene instead of a fullerene acceptors. Nonetheless, further attention should be placed on understanding the chemical and physical origin of non-radiative recombination in systems that exhibit low non-radiative decay.

Recent reports have also shown that non-radiative recombination is a function of molecular orientation at the donor-acceptor interface, with edge-on interfaces losing more voltage to non-radiative recombination than face-on interfaces.40 These results complement theoretical calculations of face-on and edge-on pentacene films with C60, which predict that the edge-on configuration will suffer more non-radiative recombination.41 The greater calculated non-radiative recombination is the consequence of a reduced vibronic coupling between the CT state and the ground state, which is a result of a decrease in electron-hole density overlap. Interestingly, due to differences in electrostatic interactions, hole delocalization and hole migration in the pentacene films, the edge-on configuration is also characterized with a smaller ECT (and therefore VOC), in agreement with the trend highlighted by Benduhn et al. We also note that reductions to the electron-hole density overlap will also reduce the radiative rate, and more research is needed to understand how to positively affect the balance between radiative and non-radiative recombination (increase ).

In the radiative limit of charge recombination, every recombination event would lead to the emission of photon. While the VOC is increased due to longer charge lifetimes, the VOC can be further increased if the emitted photon is reabsorbed in the active layer and undergoes, once again, charge separation to reform free charges.42 Photon recycling has been shown for Pb-halide perovskite solar cells43 and GaAs solar cells.44 It is estimated that photon recycling can increase the VOC by up to 100 mV.45 Recall that in an OSC blend, the CT state acts as the renormalized energy gap. In order to achieve photon recycling within an OSC, the Stokes shift between the CT states emission and absorption would have to be small, necessitating systems with small reorganization energies and low electronic disorder.46,47 Achieving these feats in an OSC may be additionally challenging due to the fact the CT state is characterized by a very low oscillator strength due to the separated, intermolecular nature of the wavefunction. For this reason, it may be further advantageous to develop OSC systems where Eg and ECT are very close in energy, especially if the CT state may borrow some oscillator strength from the singlet. Recently, theoretical calculations have suggested that the CT state in a system with very low energetic offsets, PIPCP:PC61BM, has electron density on the donor and acceptor LUMO levels.48

# Moving forward: three possible pathways to find better systems

Taken together, these examples of exceptional behaviour point to a promising future for the design of OSCs. If a system was able to combine zero charge generation energy loss with even a modest charge recombination energy loss, Eloss values of 0.4–0.5 eV are achievable. If Eloss could be reduced to 0.3 eV, and the solar cell were to retain a high JSC and FF, power conversion efficiencies between 15–20% are possible. Below, we outline three routes towards uncovering low Eloss, high efficiency systems.

## (1) Detailed Characterization of Energy Levels

The need to reduce the variability and error in the measurements of energy levels is now increasingly essential. We propose that energetic offsets should be characterized by Eg−ECT as measured in the blend, instead of the offset between HOMO or LUMO energy levels measured separately for the donor and acceptor materials. This is for several reasons. Primarily, the measured energy levels depend on the chosen experimental method, cyclic voltammetry and ultraviolet photoelectron spectroscopy for example, and it is difficult to accurately compare energy levels from the literature, obtained from different methods. As we try to understand charge generation and recombination in OSCs, it is preferable to use consistent methodology so that reports across the literature are comparable. Furthermore, energy levels depend on the solid-state morphology and local environment and will vary between neat films and blended films.

Eg should be determined by the low energy onset of the absorption spectra, as is already standard in most research labs.  Measuring ECT is more challenging, especially as we reduce the energetic offset between donor and acceptor materials and ECT approaches Eg. In most cases, it will be necessary to measure both absorption and emission from the blend film, using techniques that favour signal from the donor/acceptor interface (such as high-sensitivity photothermal deflection spectroscopy or external quantum efficiency for absorption, and electroluminescence for emission). The absorption and emission spectra can be fit to Marcus theory equations to extract the ECT. Since bimolecular recombination is temperature-dependent, it may be possible to estimate ECT by measuring eVOC as a function of temperature, and extrapolating to eVOC at 0K. At 0K all non-radiative recombination pathways are expected to be turned off, and thus the extrapolation will give an estimate of recombination losses to the eVOC at room temperature.

## (2) Radiative CT states: Moving away from PL quenching

It is now evident that non-radiative CT state decay pathways can severely limit the VOC and increase energy loss, and almost all organic solar cell blends exhibit exceedingly low luminescence quantum efficiencies. This behaviour directly manifests from using photoluminescence quenching as a technique to screen the quality of a donor or acceptor material before the more laborious task of device fabrication is undertaken. It may therefore be unsurprising that most materials fall into the non-radiative category. To un-bias the measurement, we propose that research groups refrain from using photoluminescence quenching to determine the photovoltaic potential of a blend, and, instead use alternative techniques to monitor the presence and amount of charges formed.

Film-based techniques offer obvious advantages as they can be performed more rapidly than device-based techniques and rely on less variables.  Quasi-steady state photo-induced absorption measurements can be performed with simple instrumentation, high sensitivity, and allow for the presence of charges to be determined. In the limit of even weakly radiative CT states, transient or gated luminescence techniques can also be used to measure the intensity of delayed luminescence as a metric for blend quality.

## (3) Blends with reduced miscibility

The amount of interfacial area between the donor and acceptor domains can affect the degree of non-geminate recombination and therefore the VOC. It is also generally observed that systems with low energy loss also have a low FF.  The low FF and JSC in low Eloss systems is strongly correlated to the nanoscale morphology of the blend.49 In fact, aggregation and domain purity have been correlated with improved performance and reduced losses via a multitude of loss pathways, including triplet recombination, geminate recombination, and bimolecular recombination.50–53 The FF, specifically, has been correlated with average domain purity,50,54–58 so long as there still exist sufficient percolation pathways for both hole and electron transport.59,60

It may be that the currently limited FF values are a result of suboptimal morphologies or transport properties (due to the competition between extraction and recombination), rather than the energetic offsets (due to field-dependent generation). It would thus be fruitful to direct our efforts on material development and device engineering focused at these issues, also when developing solar cells with low Eloss values.

Efforts to achieve optimal morphologies are well appreciated in the literature, with many studies focused on the interplay between morphology and solar cell performance (independent of energetic offsets).50,61 However, we would like to emphasize a few of the recent successful efforts to control morphology by molecular design or deposition method. Controlling the temperature-dependent solubility of donor polymers has enabled the use of a range of acceptor materials, because the final morphology does not depend on self-assembly of the donor and acceptor materials out of solution.62 Depending on the miscibility between donor and acceptor molecules, it may also be possible to arrive at optimal morphologies by sequential processing: casting donor and acceptor films from different solvents, and annealing the resultant ‘bilayer’ to achieve a bulk heterojunction morphology.63,64

# Conclusions

Overall, we are optimistic that OSCs can achieve power conversion efficiencies >15% within the optimisation paradigm of reducing energy loss. Within the context we have put forward, we believe that charge generation-incurred energy loss can be reduced to zero and charge recombination incurred energy loss can be mitigated to 0.4–0.5 eV (0.1–0.2 eV above the radiative limit). Part of this goal may be achieved through serendipity, especially with the diversity of non-fullerene acceptors increasing daily, but the larger part may only be achieved once informed strategies such as those outlined above are put into action.

# Acknowledgements

SMM and RHF acknowledge support from the KAUST Competitive Research Grant Program. NAR and GCB acknowledge support from the Department of the Navy, Office of Naval Research (Award Nos. N00014-14-1-0580 and N00014-16-1-25200).

References

1.	Rau, U., Paetzold, U.W. and Kirchartz, T. (2014). Thermodynamics of light management in photovoltaic devices. Phys. Rev. B 90, 35211.

2.	Shockley, W. and Queisser, H.J. (1961). Detailed Balance Limit of Efficiency of p-n Junction Solar Cells. J. Appl. Phys. 32, 510.

3.	Shin, S.S., Yeom, E.J., Yang, W.S., Hur, S., Kim, M.G., Im, J., Seo, J., Noh, J.H. and Seok, S. Il (2017). Colloidally prepared La-doped BaSnO 3 electrodes for efficient, photostable perovskite solar cells. Science 356, 167–171.

4.	Zhao, W., Li, S., Yao, H., Zhang, S., Zhang, Y., Yang, B. and Hou, J. (2017). Molecular Optimization Enables over 13% Efficiency in Organic Solar Cells. J. Am. Chem. Soc. 139, 7148–7151.

5.	Brédas, J.-L., Norton, J.E., Cornil, J. and Coropceanu, V. (2009). Molecular Understanding of Organic Solar Cells: The Challenges. Acc. Chem. Res. 42, 1691–1699.

6.	Seo, J.H., Jin, Y., Brzezinski, J.Z., Walker, B. and Nguyen, T.-Q. (2009). Exciton Binding Energies in Conjugated Polyelectrolyte Films. ChemPhysChem 10, 1023–1027.

7.	Burke, T.M., Sweetnam, S., Vandewal, K. and McGehee, M.D. (2015). Beyond Langevin Recombination: How Equilibrium Between Free Carriers and Charge Transfer States Determines the Open-Circuit Voltage of Organic Solar Cells. Adv. Energy Mater. 5, 1500123.

8.	Li, W., Hendriks, K.H., Furlan, A., Wienk, M.M. and Janssen, R.A.J. (2015). High Quantum Efficiencies in Polymer Solar Cells at Energy Losses below 0.6 eV. J. Am. Chem. Soc. 137, 2231–2234.

9.	Walker, B., Liu, J., Kim, C., Welch, G.C., Park, J.K., Lin, J., Zalar, P., Proctor, C.M., Seo, J.H., Bazan, G.C., et al. (2013). Optimization of energy levels by molecular design: evaluation of bis-diketopyrrolopyrrole molecular donor materials for bulk heterojunction solar cells. Energy Environ. Sci. 6, 952.

10.	Vohra, V., Kawashima, K., Kakara, T., Koganezawa, T., Osaka, I., Takimiya, K. and Murata, H. (2015). Efficient inverted polymer solar cells employing favourable molecular orientation. Nat. Photonics 9, 403–408.

11.	Kawashima, K., Tamai, Y., Ohkita, H., Osaka, I. and Takimiya, K. (2015). High-efficiency polymer solar cells with small photon energy loss. Nat. Commun. 6, 10085.

12.	Jailaubekov, A.E., Willard, A.P., Tritsch, J.R., Chan, W.-L., Sai, N., Gearba, R., Kaake, L.G., Williams, K.J., Leung, K., Rossky, P.J., et al. (2013). Hot charge-transfer excitons set the time limit for charge separation at donor/acceptor interfaces in organic photovoltaics. Nat. Mater. 12, 66–73.

13.	Falke, S.M., Rozzi, C.A., Brida, D., Maiuri, M., Amato, M., Sommer, E., De Sio, A., Rubio, A., Cerullo, G., Molinari, E., et al. (2014). Coherent ultrafast charge transfer in an organic photovoltaic blend. Science 344, 1001–1005.

14.	Bakulin, A.A., Rao, A., Pavelyev, V.G., van Loosdrecht, P.H.M., Pshenichnikov, M.S., Niedzialek, D., Cornil, J., Beljonne, D. and Friend, R.H. (2012). The Role of Driving Energy and Delocalized States for Charge Separation in Organic Semiconductors. Science 335, 1340–1344.

15.	Gelinas, S., Rao, A., Kumar, A., Smith, S.L., Chin, A.W., Clark, J., van der Poll, T.S., Bazan, G.C., Friend, R.H., Gélinas, S., et al. (2014). Ultrafast Long-Range Charge Separation in Organic Semiconductor Photovoltaic Diodes. Science 343, 512–516.

16.	Burke, T.M. and McGehee, M.D. (2014). How High Local Charge Carrier Mobility and an Energy Cascade in a Three-Phase Bulk Heterojunction Enable >90% Quantum Efficiency. Adv. Mater. 26, 1923–1928.

17.	Ryno, S.M., Fu, Y.-T., Risko, C. and Brédas, J.-L. (2016). Polarization Energies at Organic–Organic Interfaces: Impact on the Charge Separation Barrier at Donor–Acceptor Interfaces in Organic Solar Cells. ACS Appl. Mater. Interfaces 8, 15524–15534.

18.	Schwarz, C., Tscheuschner, S., Frisch, J., Winkler, S., Koch, N., Bässler, H. and Köhler, A. (2013). Role of the effective mass and interfacial dipoles on exciton dissociation in organic donor-acceptor solar cells. Phys. Rev. B 87, 155205.

19.	Vandewal, K., Albrecht, S., Hoke, E.T., Graham, K.R., Widmer, J., Douglas, J.D., Schubert, M., Mateker, W.R., Bloking, J.T., Burkhard, G.F., et al. (2014). Efficient charge generation by relaxed charge-transfer states at organic interfaces. Nat Mater 13, 63–68.

20.	Hood, S.N. and Kassal, I. (2016). Entropy and Disorder Enable Charge Separation in Organic Solar Cells. J. Phys. Chem. Lett. 7, 4495–4500.

21.	Gao, F., Tress, W., Wang, J. and Inganas, O. (2015). Temperature dependence of charge carrier generation in organic photovoltaics. Phys. Rev. Lett. 114, 128701.

22.	Gregg, B.A. (2011). Entropy of charge separation in organic photovoltaic cells: The benefit of higher dimensionality. J. Phys. Chem. Lett. 2, 3013–3015.

23.	Monahan, N.R., Williams, K.W., Kumar, B., Nuckolls, C. and Zhu, X.Y. (2015). Direct Observation of Entropy-Driven Electron-Hole Pair Separation at an Organic Semiconductor Interface. Phys. Rev. Lett. 114, 247003.

24.	Ono, S. and Ohno, K. (2016). Combined impact of entropy and carrier delocalization on charge transfer exciton dissociation at the donor-acceptor interface. Phys. Rev. B 94, 75305.

25.	Tabachnyk, M., Smith, S.L., Weiss, L.R., Sadhanala, A., Chin, A.W., Friend, R.H. and Rao, A. (2017). Energy Efficient Dissociation of Excitons to Free Charges http://arxiv.org/abs/1704.03780.

26.	Miller, O.D., Yablonovitch, E. and Kurtz, S.R. (2012). Strong Internal and External Luminescence as Solar Cells Approach the Shockley Queisser Limit. IEEE J. Photovoltaics 2, 303–311.

27.	Rau, U. (2007). Reciprocity relation between photovoltaic quantum efficiency and electroluminescent emission of solar cells. Phys. Rev. B 76, 85303.

28.	Ross, R.T. (1967). Some Thermodynamics of Photochemical Systems. J. Chem. Phys. 46, 4590–4593.

29.	Benduhn, J., Tvingstedt, K., Piersimoni, F., Ullbrich, S., Fan, Y., Tropiano, M., McGarry, K.A., Zeika, O., Riede, M.K., Douglas, C.J., et al. (2017). Intrinsic non-radiative voltage losses in fullerene-based organic solar cells. Nat. Energy 2, 17053.

30.	Nitzan, A., Mukamel, S. and Jortner, J. (1975). Energy gap law for vibrational relaxation of a molecule in a dense medium. J. Chem. Phys. 63, 200–207.

31.	Marcus, R.A. (1997). Electron transfer reactions in chemistry theory and experiment. J. Electroanal. Chem. 438, 251–259.

32.	Baran, D., Kirchartz, T., Wheeler, S., Dimitrov, S., Abdelsamie, M., Gorman, J., Ashraf, R.S., Holliday, S., Wadsworth, A., Gasparini, N., et al. (2016). Reduced voltage losses yield 10% efficient fullerene free organic solar cells with >1 V open circuit voltages. Energy Environ. Sci. 9, 3783–3793.

33.	Cheng, P., Zhang, M., Lau, T.-K., Wu, Y., Jia, B., Wang, J., Yan, C., Qin, M., Lu, X. and Zhan, X. (2017). Realizing Small Energy Loss of 0.55 eV, High Open-Circuit Voltage >1 V and High Efficiency >10% in Fullerene-Free Polymer Solar Cells via Energy Driver. Adv. Mater. 29, 1605216.

34.	Gao, K., Li, L., Lai, T., Xiao, L., Huang, Y., Huang, F., Peng, J., Cao, Y., Liu, F., Russell, T.P., et al. (2015). Deep Absorbing Porphyrin Small Molecule for High-Performance Organic Solar Cells with Very Low Energy Losses. J. Am. Chem. Soc. 137, 7282–7285.

35.	Li, Y., Liu, X., Wu, F.-P., Zhou, Y., Jiang, Z.-Q., Song, B., Xia, Y., Zhang, Z.-G., Gao, F., Inganäs, O., et al. (2016). Non-fullerene acceptor with low energy loss and high external quantum efficiency: towards high performance polymer solar cells. J. Mater. Chem. A 4, 5890–5897.

36.	Ran, N.A., Love, J.A., Takacs, C.J., Sadhanala, A., Beavers, J.K., Collins, S.D., Huang, Y., Wang, M., Friend, R.H., Bazan, G.C., et al. (2016). Harvesting the Full Potential of Photons with Organic Solar Cells. Adv. Mater. 28, 1482–1488.

37.	Liu, J., Chen, S., Qian, D., Gautam, B., Yang, G., Zhao, J., Bergqvist, J., Zhang, F., Ma, W., Ade, H., et al. (2016). Fast charge separation in a non-fullerene organic solar cell with a small driving force. Nat. Energy 1, 16089.

38.	Jakowetz, A.C., Böhm, M.L., Zhang, J., Sadhanala, A., Huettner, S., Bakulin, A.A., Rao, A. and Friend, R.H. (2016). What Controls the Rate of Ultrafast Charge Transfer and Charge Separation Efficiency in Organic Photovoltaic Blends. J. Am. Chem. Soc. 138, 11672–11679.

39.	Zhao, W., Qian, D., Zhang, S., Li, S., Inganäs, O., Gao, F. and Hou, J. (2016). Fullerene-Free Polymer Solar Cells with over 11% Efficiency and Excellent Thermal Stability. Adv. Mater. 28, 4734–4739.

40.	Ran, N.A., Roland, S., Love, J.A., Savikhin, V., Takacs, C.J., Fu, Y.-T., Li, H., Coropceanu, V., Liu, X., Brédas, J.-L., et al. (2017). Impact of interfacial molecular orientation on radiative recombination and charge generation efficiency. Nat. Commun. 8, 79.

41.	Chen, X.-K., Ravva, M.K., Li, H., Ryno, S.M. and Brédas, J.-L. (2016). Effect of Molecular Packing and Charge Delocalization on the Nonradiative Recombination of Charge-Transfer States in Organic Solar Cells. Adv. Energy Mater. 6, 1601325.

42.	Martı́, A., Balenzategui, J.L. and Reyna, R.F. (1997). Photon recycling and Shockley’s diode equation. J. Appl. Phys. 82, 4067–4075.

43.	Pazos-Outon, L.M., Szumilo, M., Lamboll, R., Richter, J.M., Crespo-Quesada, M., Abdi-Jalebi, M., Beeson, H.J., Vru ini, M., Alsari, M., Snaith, H.J., et al. (2016). Photon recycling in lead iodide perovskite solar cells. Science 351, 1430–1433.

44.	Kayes, B.M., Nie, H., Twist, R., Spruytte, S.G., Reinhardt, F., Kizilyalli, I.C. and Higashi, G.S. (2011). 27.6% Conversion efficiency, a new record for single-junction solar cells under 1 sun illumination. 2011 37th IEEE Photovolt. Spec. Conf., 4–8 doi:10.1109/PVSC.2011.6185831.

45.	Kirchartz, T., Staub, F. and Rau, U. (2016). Impact of Photon Recycling on the Open-Circuit Voltage of Metal Halide Perovskite Solar Cells. ACS Energy Lett. 1, 731–739.

46.	De Wolf, S., Holovsky, J., Moon, S.-J., Löper, P., Niesen, B., Ledinsky, M., Haug, F.-J., Yum, J.-H. and Ballif, C. (2014). Organometallic Halide Perovskites: Sharp Optical Absorption Edge and Its Relation to Photovoltaic Performance. J. Phys. Chem. Lett. 5, 1035–1039.

47.	Wehrenfennig, C., Liu, M., Snaith, H.J., Johnston, M.B. and Herz, L.M. (2014). Homogeneous Emission Line Broadening in the Organo Lead Halide Perovskite CH3NH3PbI3–xClx. J. Phys. Chem. Lett. 5, 1300–1306.

48.	Menke, S.M., Sadhanala, A., Nikolka, M., Ran, N.A., Ravva, M.K., Abdel-Azeim, S., Stern, H.L., Wang, M., Sirringhaus, H., Nguyen, T.-Q., et al. (2016). Limits for Recombination in a Low Energy Loss Organic Heterojunction. ACS Nano 10, 10736–10744.

49.	Jiao, X., Ye, L. and Ade, H. (2017). Quantitative Morphology-Performance Correlations in Organic Solar Cells: Insights from Soft X-Ray Scattering. Adv. Energy Mater. 7, 1700084.

50.	Love, J.A., Collins, S.D., Nagao, I., Mukherjee, S., Ade, H., Bazan, G.C. and Nguyen, T.-Q. (2014). Interplay of Solvent Additive Concentration and Active Layer Thickness on the Performance of Small Molecule Solar Cells. Adv. Mater. 26, 7308–7316.

51.	Proctor, C.M., Albrecht, S., Kuik, M., Neher, D. and Nguyen, T.-Q. (2014). Overcoming Geminate Recombination and Enhancing Extraction in Solution-Processed Small Molecule Solar Cells. Adv. Energy Mater. 4, 1400230.

52.	Rao, A., Chow, P.C.Y., Gélinas, S., Schlenker, C.W., Li, C.-Z., Yip, H.-L., Jen, A.K.-Y.K.Y., Ginger, D.S. and Friend, R.H. (2013). The role of spin in the kinetic control of recombination in organic photovoltaics. Nature 500, 435–439.

53.	Ye, L., Zhao, W., Li, S., Mukherjee, S., Carpenter, J.H., Awartani, O., Jiao, X., Hou, J. and Ade, H. (2017). High-Efficiency Nonfullerene Organic Solar Cells: Critical Factors that Affect Complex Multi-Length Scale Morphology and Device Performance. Adv. Energy Mater. 7, 1602000.

54.	Gao, K., Miao, J., Xiao, L., Deng, W., Kan, Y., Liang, T., Wang, C., Huang, F., Peng, J., Cao, Y., et al. (2016). Multi-Length-Scale Morphologies Driven by Mixed Additives in Porphyrin-Based Organic Photovoltaics. Adv. Mater. 28, 4727–4733.

55.	Guo, X., Zhang, M., Ma, W., Ye, L., Zhang, S., Liu, S., Ade, H., Huang, F. and Hou, J. (2014). Enhanced Photovoltaic Performance by Modulating Surface Composition in Bulk Heterojunction Polymer Solar Cells Based on PBDTTT-C-T/PC71BM. Adv. Mater. 26, 4043–4049.

56.	Mukherjee, S., Proctor, C.M., Bazan, G.C., Nguyen, T.-Q. and Ade, H. (2015). Significance of Average Domain Purity and Mixed Domains on the Photovoltaic Performance of High-Efficiency Solution-Processed Small-Molecule BHJ Solar Cells. Adv. Energy Mater. 5, 1500877.

57.	Mukherjee, S., Jiao, X. and Ade, H. (2016). Charge Creation and Recombination in Multi-Length Scale Polymer:Fullerene BHJ Solar Cell Morphologies. Adv. Energy Mater. 6, 1600699.

58.	Zhao, J., Li, Y., Yang, G., Jiang, K., Lin, H., Ade, H., Ma, W. and Yan, H. (2016). Efficient organic solar cells processed from hydrocarbon solvents. Nat. Energy 1, 15027.

59.	Bartelt, J.A., Beiley, Z.M., Hoke, E.T., Mateker, W.R., Douglas, J.D., Collins, B.A., Tumbleston, J.R., Graham, K.R., Amassian, A., Ade, H., et al. (2013). The importance of fullerene percolation in the mixed regions of polymer-fullerene bulk heterojunction solar cells. Adv. Energy Mater. 3, 364–374.

60.	Ko, S.J., Walker, B., Nguyen, T.L., Choi, H., Seifter, J., Uddin, M.A., Kim, T., Kim, S., Heo, J., Kim, G.H., et al. (2016). Photocurrent Extraction Efficiency near Unity in a Thick Polymer Bulk Heterojunction. Adv. Funct. Mater. 26, 3324–3330.

61.	Love, J.A., Proctor, C.M., Liu, J., Takacs, C.J., Sharenko, A., van der Poll, T.S., Heeger, A.J., Bazan, G.C. and Nguyen, T.-Q. (2013). Film Morphology of High Efficiency Solution-Processed Small-Molecule Solar Cells. Adv. Funct. Mater. 23, 5019–5026.

62.	Liu, Y., Zhao, J., Li, Z., Mu, C., Ma, W., Hu, H., Jiang, K., Lin, H., Ade, H. and Yan, H. (2014). Aggregation and morphology control enables multiple cases of high-efficiency polymer solar cells. Nat. Commun. 5, 5293.

63.	Aguirre, J.C., Hawks, S.A., Ferreira, A.S., Yee, P., Subramaniyan, S., Jenekhe, S.A., Tolbert, S.H. and Schwartz, B.J. (2015). Sequential Processing for Organic Photovoltaics: Design Rules for Morphology Control by Tailored Semi-Orthogonal Solvent Blends. Adv. Energy Mater. 5, 1402020.

64.	Moon, J.S., Takacs, C.J., Sun, Y. and Heeger, A.J. (2011). Spontaneous Formation of Bulk Heterojunction Nanostructures: Multiple Routes to Equivalent Morphologies. Nano Lett. 11, 1036–1039.

Figure Captions

Figure 1 Energetics of Organic Solar Cells | (a) Orbital energy diagram for a typical donor-acceptor pairing. The optical energy gap of the blend can be generalized as the smallest optical energy gap of the two constituent materials, and the CT state energy can be generalized as the difference between the ionization potential of the donor and the electron affinity of the acceptor. Note that our schematic does not intend to represent the absolute values for Eg and ECT. (b) Energy loss for organic solar cells can be separated as that which is incurred during charge generation (Eg−ECT) and that which is incurred during charge recombination (ECT−eVOC). Charge recombination energy loss results from both radiative and non-radiative CT state decay.

Figure 2 First Generation of Low Energy Loss Organic Solar Cells | Maximum external quantum efficiency (EQE) as a function of energy loss (Eg−eVOC) for various polymer-based organic solar cells. It has been empirically observed that the EQE drops sharply for energy loss values <0.6 eV. The color code indicates the electron deficient unit in the polymer: BT = benzothiadiazole, DPP = diketopyrrolopyrrole, II = isoindigo, TPD = thieno[3,4-c]pyrrole-4,6-dione, TT = thieno[3,4-b]thiophene. Reprinted with permission from Ref. 8. Copyright 2015 American Chemical Society.

Figure 3 High Quantum Efficiency and Low Energy Loss Organic Solar Cells | Updated maximum ηEQE vs. Energy Loss (Eg−eVOC) for a range of high-performance OSC systems, focused primarily on systems with ηPCE>6%. Shown as a dashed line is the radiative limit for energy loss set at 0.3 eV.

Figure 4 Two Charge Generation Pathways | Schematic for charge generation in systems with a large offset energy such that the difference between the lowest singlet exciton energy (S1 or equivalently Eg) and the charge transfer state (ECT) is greater (case A) or less (case B) than the long-range Coulomb potential (W) which needs to be overcome in order to separate charge and create free carriers beyond their Langevin recombination radius (> 5 nm). For low Eloss systems, case B will dominate. Free carriers can be generated from localized CT states either by thermal promotion to delocalized states or by successive hopping.