Microplastic fibre releases from industrial wastewater effluent: a textile wet processing mill in China

Carmen KM Chan1, Curie Park2, King Ming Chan3, Daniel CW Mak3,4, James KH Fang4, Denise M. Mitrano5

1. Cambridge Institute for Sustainability Leadership, University of Cambridge, United Kingdom

2. Institute for Manufacturing, University of Cambridge, United Kingdom

3. School of Life Sciences, The Chinese University of Hong Kong, Hong Kong

4. Department of Applied Biology and Chemical Technology, The Hong Kong Polytechnic University, Hong Kong

5. Department of Environmental Systems Science, ETH Zurich, Switzerland

ABSTRACT

Microplastic fibres (MPFs) released from textiles are routinely found throughout the environment indicating the human impacts on natural systems. The most common release pathways for MPFs to the environment investigated are laundering textiles in domestic settings, transport through/retention in municipal wastewater treatment plants and subsequent application of processed sludge onto agricultural fields as a soil amendment. A less studied source, but potentially equally relevant, are releases further upstream in the textile production chain such as industrial wastewater effluents from textile processing mills. In this context, the industrial wastewater from a typical textile wet processing mill in China was sampled to estimate MPF release. Effluent was sampled where MPFs were quantified by stereomicroscope in terms of fibre number and length. An average of 361.6±24.5MPF/L were identified in the mill effluent. MPF length was highly variable (451.0+/-509.1µm; n=17,392), yet 92% of all fibres were shorter than 1,000µm. Additionally, the sampling strategy was used to identify optimal volume necessary to adequately sub-sample the effluent. We found that total fibre counts were linearly correlated to sample volumes between 1 and 10L, but a sampling volume of 5L is suggested for adequate reproducibility, low standard deviation and ease of working volume. The significant abundance of MPFs in the industrial wastewater effluent should emphasize that attention should not only be placed on domestic releases, but that the production stage of textiles can also be responsible for microplastic fibre pollution. The ability to target and treat industrial effluents may significantly reduce a potentially major point source.

Keywords: microplastic, microplastic fibres, wastewater treatment, industrial wastewater, textile wet processing

INTRODUCTION

Synthetic textiles have the largest share of the global textile fibre production market, with 62% of the market share in 2018 (Opperskalski et al., 2019). Commonly released from petrochemicals–based synthetic-based textiles, microplastic fibres (MPFs) are one of the most ubiquitous form of microplastics in the marine environment (Henry et al., 2018; Xu et al, 2018),  with up to 85% of all microplastic particles being  MPFs (Browne et al., 2011). MPFs are extensively distributed across various environments, including freshwater, rivers, oceans, landfill and air, and once they are in the environment they will likely be impossible to remove. It was estimated that over 22 million tonnes of MPFs were released to the ocean between 2015 and 2050 based on domestic laundry studies (Ellen MacArthur Foundation, 2017).  Consequently, Boucher & Friot (2017) suggested that household activities cause about 75% of the shedding of MPFs, which ultimately shifts the responsibility of reducing MPF releases to the consumer, domestic laundry, and municipal wastewater treatment: all of which are end-of-pipe solutions (Sancroft, 2018). At the textile production stage, garment shedding can be reduced if MPFs are removed from fabric production stage (Roos et al.,2017). Understanding which textile manufacturing process leads to increased MPF release (Cai et al., 2020) could help produce garments less likely to shed MPF and subsequently could reduce the number of MPF releases in domestic washing (Hernandez et al., 2017). Therefore, understanding how to reduce their emissions to the envionment through earlier phases of the textile life cycle is essential (Henry et al., 2018). Most studies focused on aspects of the MPF later in the life cycle such as domestic laundering of MPF and subsequent release from wastewater treatment plants (WWTP) (e.g. Magnusson and  Norén 2014; Carr, 2017; Hernandez et al., 2017; Frehland et al., 2020), yet the importance of industrial stage releases at industrial WWTPs from textile mills is less understood.

A comparison between industrial textile effluents (Xu et al., 2018) and municipal wastewater treatment effluents (Yang et al., 2019; Lv et al., 2019) in China suggests that 28–1,310 times higher concentrations of MPFs are in the industrial effluent, which are directly discharged to aquatic environments. Although the reported MPFs removal efficiency of 80.2–97.2% at municipal WWTPs are relatively high, (Conley et al., 2019) the volume of daily discharge from WWTPs may result in large releases of MPFs to the aquatic environment. Advanced treatment processes have the potential to improved removal efficiency even of small-sized MPs <100µm (Talvitie et al., 2017), but these solutions are expensive, and may only be realistic for (some) municipal WWTPs, not all industrial facilities. The higher retention efficiency of WWTPs implies a higher concentration of MPFs in the sludge. Notably, the majority of sludge from industrial WWTPs is incinerated or processed as solids for other uses such as bricks, opposed to municipal WWTP where sludge is often applied to agricultural soil as a nutrient amendment and thus may inadvertently pollute the environment with MPFs (Nizzetto et al.,2016). These divergent sludge pathways suggest that if the textile industry could exercise better control in capturing MPF in their WWTPs, the number of MPFs released into the environment at the production stage of the textile life cycle could be drastically reduced.

To date, however, it has been difficult to put precise numbers on how many MPFs follow each release pathway. Most MPF monitoring studies suffer from inconsistencies and comparability issues in their sampling and extraction techniques, a lack of standardised analysis methods and standard reporting units. Due to the wide variations employed by different researchers, the comparison of reported MPF concentrations between studies often greatly varies and is highly inconsistent (Mishra et al., 2019). For example, mesh filters of 100µm sieve size or larger results in fewer MPFs being identified, irrespective of the analytical methodology which follows the sampling protocol (Pirc et al., 2016; Roos et al., 2017). Even seemingly small changes can be relevant: sampling with an 80µm mesh size increased the probability of capturing fibres by 250 times compared to a mesh size of 300µm (Dris et al., 2018). MPFs are often being underestimated in most studies (Barrows et al., 2018), which leads to inconsistencies when comparing current modelling and ﬁeld approaches (Boucher and Billard, 2019).

Data available for estimating the abundance of MPFs directly released from industrial WWTPs is sparse, and this figure is needed in order to put relative MPF sources in context so that we can tackle those sources which are releasing the highest number of MPFs into the environment first. This research aims to measure the releases of MPFs originating from industrial-scale textile production by developing test protocol to accurately measure the quantity and size of MPFs in industrial WWTP effluent. In particular, we aim to 1) assess sampling protocols and procedures, particularly sample size, 2) innumerate MPF  quantity and length distribution in industrial WWTP samples, and 3) relate these findings to the magnitude of MPF releases which have been reported from other types of WWTP. The scope of this study is focused on the industrial effluent pathway from a typical textile wet processing mill in China

MATERIALS AND METHODS

Study site

China is the global hub for polyester (PET) production, accounting for approximately 69% of total polyester fibre production (Henry et al., 2018) and with one-third of its fibre processing concentrated in the Jiangsu region (Fibre2fashion.com, 2018).  Therefore, a typical factory located in Changzhou, Jiangsu region was chosen for this study. It has a reasonably stable production level, primarily producing polyester fleece all year round at 3,000 tonnes/month on average, approximately 95% of its production is warp-knitted base fabric from FDY 75D/36F multi-filament yarn (2.31dtex), and the loop pile is DTY 150D/288F (0.58dtex) multi-filament yarn which is cut and raised to a loop height of approximately 4.5–5.0mm.  The mechanical and chemical processes are used for turning warp and weft-knitted polyester greige fabrics into fleece of various colours. Pattern and effects printing also takes place in this mill. An average of approximately 3,000 tonnes of wastewater is treated daily at the mill’s secondary biochemical WWTP. 95-96% of influent is from the production process, with the rest from non-production source at the mill (e.g. dormitories). Effluent is produced in the dyeing and finishing processes and then treated. The treatment chain in this WWTP included: neutralization, equalisation, flocculation, primary sedimentation, biological oxidation, secondary sedimentation, coagulation and finally filtration before effluent before being discharged to the common effluent treatment plant (CETP). At the CETP, the effluent is further treated before released into receiving waters.

Sampling

The key procedures of the test protocol for quantifying MPF from industrial effluent are shown in Figure 1. The effluent samples were collected from the factory discharge point, which was at the end of the treatment process chain before the effluent was released to the CETP.

Sample collection was made directly from the effluent stream, which was a continuously flowing tank, a 2L metal measuring jar was used to collect water just below the water surface level at the opening of the effluent stream. Samples were then transferred to clean brown glass bottles for ≤1L or ethylene-vinyl acetate (EVA) buckets for larger sample volumes. A large volume composite sample is important for sampling MPFs, especially for treated effluent, to limit the intra-day influence of source loading and peak flows (Talvitie et al., 2017). Samples were collected hourly for six hours, with each sample mixed to create a composite sample on the sampling day which was on 28th December 2018. (modified from ZDHC Foundation 2019 and ISO - ISO 5667-10:1992 Water quality - Sampling - Part 10: Guidance on sampling of waste waters). The six-hour time blocks we sampled over corresponded to two to three production cycles. Five batches of various composited volumes (0.5L, 1L, 3L, 5L and 10L) were collected in triplicate at each sampling site to assess how sample volume effects the number of MPFs in the sampling campaign. All samples were filtered through a 10µm metal sieve and backwashed into brown glass bottles using 250-300 mL MilliQ water per litre for pre-concentration on-site. Samples were treated with small volume of H2O2 (approximately 250 – 300 mL per sample) to destroy trace amounts of organic matter and supress sequential biological growth, the brown bottles were kept in concealed boxes while transferring samples to the laboratory and were stored at −4 °C until analysis.

The concentrated samples were transferred to a glass Duran® flask and treated with 30% H2O2 for 30 minutes on a preheated plate at 70oC to remove the remaining organic matter. Following a cool-down period, each sample was vacuum filtered through a 1.5µm pore size, 47mm diameter borosilicate glass-fibre filter (Whatman, 934-AH), with a maximum of 1L effluent per filter and dried at 105oC in a glass petri dish in modification to Masura et al. (2015) and Dyachenko et al. (2017), the test condition was suggested as an effective setting with insignificant impact on polymer degradation of the MPFs.

A spike recovery study to assess our extraction protocol using reference MPFs from production was conducted. Spiked MPFs were prepared by cutting the production fabric into fibres of various lengths by microtome into 36-3,498µm., 89% were below 1,000µm, which resembles the length distribution of the test samples. An average of 98 MPFs were counted and then mixed in 1L of MilliQ water in duplicate. The solutions were then filtered and dried, and visually assessed by the stereomicroscope in the same way as the effluent samples (see section 2.3). MPF recovery was on average 89.1% from duplicate samples.

Figure 1:  Key procedures of the test protocol for quantifying microplastic fibres from industrial WWTP effluent.

MPF Visual Number and Length Quantification

Adapting methods from a combination of various published studies (Tsang et al., 2017;   Norin and Ab, 2018; De Falco et al., 2018), we examined the treated and filtered MPFs by visually counting them by stereomicroscope (Euromex CMEX-18 PRO) at 20x magnification. Photo imaging and recordings were made with an 18-Mpix connected digital camera. The entire filter surface was subdivided into 64 grids to ensure comprehensive analysis and imaging. All images were analysed using the ImageFocus Alpha software V1.3.7 for counting and measuring the length of each MPF. A set of criteria was developed to determine the MPF length detection limit of our technique (Figure S1). Given the magnification and image quality of the microscope, the detection limit was 20m. Objects that had a width to length ratio greater than 1.5 were counted as MPF. (e.g. Zhao et al., 2014; Fischer et al., 2016; Barrows, et al., 2017). Fibres which were not able to be measured accurately in terms of length due to e.g. entanglement or other visual obstructions were omitted. This represented a small fraction of fibres from the total number of fibres which were measured (approximately <1%).

Fibre length was calculated based on the overall average of all sample volumes by assuming they are homogenous as production was stable between all sample collection periods. Length distribution analysis was based on the quantity count of each size bin in 100µm increments for lengths <1,000µm and 1,000µm increments for lengths of 1,000–4,999µm. Since the most fibres were shorter than 1,000µm, smaller size bins in this range enabled a more detailed analysis of length distribution.

MPF Visual Characterisation

MPFs were taken directly from the production process and a subset of MPF samples from the effluent were chosen randomly to assess if there were any identifying characteristics through a light microscope at 400x resolution. Two separate and distinct measurements were made on these fibres: fibre diameter and fibre morphology. The average diameter of the reference fibre from the production of 14.6µm with a standard deviation of 1.6µm and a range of 10.5–17.4µm.The diameter of fibres can support that the 10µm sieve in pre-concentration samples should be able to retain majority of the MPFs.The longitudinal morphology of the production fibres (n=18) was compared to that of the fibres found in the effluent (n=18) using an industry standard fibre identification methodology (ISO - ISO/TR 11827:2012 - Textiles -- Composition testing -- Identification of fibres,” 2012). The morphology of the longitudinal images including circularity of shape, smoothness and uniformity, were evaluated. When compared to the standard, these characteristics can suggest that fibres are synthetic or organic in nature.  Both the fibres originating from production and from the effluent had similar characteristics to the standard polyester fibres used in the ISO method. In this way, suspected MPFs from the effluent were synthetic origin and likely polyester which came from the production process. A further validation step was made with chemical methodology described in 2.5.

Fibre Chemical Characterisation

A subset of MPFs (n=18) were randomly selected to analyse their chemical composition using a Renishaw inVia confocal micro-Raman spectrometer (Wotton-under Edge, England) with a Leica 50× objective (numerical aperture = 0.75; Wetzlar, Germany). Calibration was carried out using the vibrational band of 520cm-1 of a silicon wafer reference. Excitation was obtained using a 785nm laser source. Raman spectra in the range of 300–3,200cm-1, with a spectral resolution of 1cm-1, were acquired at 0.1–1% laser power and 20s integration time. Baseline correction and smoothing of the acquired spectra were performed with the Renishaw WiRE 4.2 software. Polymer types of the samples were identified by matching their Raman spectra with polymer standards provided in the Renishaw Polymeric Materials Database. Since many MPFs may not be pure polymer, and traces of other compounds were present either from the production process or through sorption of chemicals in the effluent, three different areas on each fibre were measured to achieve a positive confirmation, as recommended by Dyachenko et al. (2017). Representative samples of suspected MPFs and non-MPFs were also tested and the results were consistent with those from the high-resolution microscope analysis.

Contamination control (blanks)

MPFs contamination is a serious concern when collecting and measuring MPF, as there may be cross-contamination if clean working procedures are not ensured. The steps taken to minimise this risk were as follows:

- All equipment, including collection bottles, were triple rinsed with MilliQ water and capped immediately following sample collection,

- All laboratory apparatus used were washed and rinsed with MilliQ, or equivalent quality water,

- Limited usage of plastic materials; the utilisation of aluminium containers or foil for covering the samples during collection, transfer and storage was practiced. Glass petri dishes were used to store filters,

- During sampling and in laboratories, researchers only wore clothes made exclusively of natural fabrics and clean laboratory coats,

- Control filter papers (i.e. blanks) were used during all laboratory steps where specimens might become exposed.

Statistical analysis

All statistical analyses were performed using standard statistical software, including GraphPad, Prism 8.2.1 and Excel (Microsoft® Excel® for Office 365 MSO).  The data were tested for normality and correlation. The mean, standard deviation and relative standard deviation (coefficient of variance) were calculated for each set of volumes and were expressed as items per litre. The abundance counts of MPFs and volumes are continuous variables to test for linear relationship, R squares value larger than 0.95 indicate a positive correlation and abundance count can be derived from the best-fit slope formula. The optimum sample volume was identified as the minimum volume with least variance in the sampling groups. The calculated abundance by count and the average length of MPFs were rounded up to the one decimal place with a ‘±’ standard deviation (SD) throughout the study.

RESULTS and Discussion

Chemical characterisation of fibres

- A subset of MPFs from the production quality fibres and the filtered samples were evaluated using high-resolution microscopy. All fibres displayed the same morphology, which was indicative of polyester fibres, according to industry standard assessment method (Figure S2). The subset of MPFs analysed in the effluent and from processed fabrics (n=18) showed a similar chemical signature as determined by micro-Raman spectroscopy, with 7 to 8 peaks matching in each of the points measured against polyester standard (examples in Figure S3). The Raman shift graphs, suggesting that the MPFs collected from the industrial wastewater treatment effluent were polyester and likely from those which were processed in the mill.

MPF number in industrial wastewater effluent

The results from microscopic counting are presented in Table 1. A linear relationship existed between MPF count and volume of effluent collected from 1L to 10L (Figure 2A), but sample volumes below 5L show high MPF number variance (Figure 2B). The average number of fibres measured was relatively similar across all sample volumes. However, the MPF number variance is reduced when the sample volume increases, and the relative standard deviation drops to less than 5% for sample sizes 5L and above (Table 1). Ultimately, this means that more precise MPF number concentrations will be obtained with higher sample volumes. Therefore, we propose that 5L is the optimum volume for the sampling of industrial wastewater effluent to work with the lowest volume while maintaining accurate and precise results.

Table 1:  Summary of microplastic fibres identified in all volumes of wastewater effluent samples.

| Sample Volume (Litre) | Microplastic fibre number |  |  | Microplastic fibres number per litre |  |  | Average MPF per litre | Standard deviation | Relative standard deviation |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | A | B | C | A | B | C |  |  |  |
| 0.5* |  | 134 | 183 |  | 268.0 | 366.0 | 317.0 | 69.3 | 21.9% |
| 1 | 284 | 187 | 255 | 284.0 | 187.0 | 255.0 | 242.0 | 49.8 | 20.6% |
| 3 | 1,086 | 893 | 891 | 362.0 | 297.7 | 297.0 | 319.6 | 36.8 | 11.5% |
| 5 | 1,672 | 1,675 | 1,611 | 334.4 | 335.0 | 322.2 | 335.6 | 15.4 | 4.6% |
| 10 | 2,957 | 2,615 | 2,949 | 295.7 | 261.5 | 294.9 | 284.0 | 19.5 | 6.9% |

*The 0.5L volume only consisted of 2 samples.

Although precautions were taken to reduce contamination, on average 0.375 MPF was found on each control per filter. This was 0.16–0.44% of the total number of MPFs counted for each data set, and thus does not significantly affect the results. The average MPFs released from the polyester wet processing mill in the effluent is 361.6±24.5MPF/L, we estimated the total daily release of MPF from this mill. With an average of 3,000 tonnes of effluent produced daily, the total quantity of MPFs released as effluent equates to 1.1x109 MPF per day. Since the effluent undergoes further processing at the CETP, the efficiency of this can be calculated by referencing the study carried out by Xu et al. (2018) in the same region which operated at 95.1% efficiency. Therefore, it can be estimated that 17.7±1.2MPF/L are potentially released from this mill into the aquatic environment. These values are consistent with the study by Xu et al. (2018) which found that an average abundance of small fibres (both natural and synthetic) in the influent and effluent amounted to 334.1±24.3items/L and 16.3±1.2items/L respectively.

Figure 2. A) Linear regression analysis of abundance of microplastic fibres in different sample volumes of the effluent. Standard deviation is variance between triplicate samples. B) Number of MPF per litre variance in different sample volumes of the effluent

.

Average MPF length and length distribution

Over 92% of the MPFs identified were shorter than 1,000µm (n=17,392). We assumed that all sample volumes were homogenous in terms of MPF length distribution, since collection occurred in the same period and they were mixed into composite samples. The average sample lengths measured was 451.0±509.1µm. The average number of MPF per litre were plotted against each length size bins and a secondary y-axis were plotted against the percentage of total MPFs (Figure 3). The largest size bin by MPF number was <100µm. MPFs in the size range of 30-499µm constituted 81% of the total count and 92% of all fibres measured were <1,000µm (Figure 3).

Figure 3. MPF abundance by length. Note that the x-axis is not a linear scale: size bins are 100m for bins <1,000m and 1,000m for bins >1,000m.  Proportion of MPF in each size bin to the total MPF count in percentage is also indicated by the diamond points along each bar, referenced by the right y-axis.

The most abundant fibre length measured in the WWTP effluent were those below 100µm. A few studies also have observed <100µm as the most abundant length as a result of using finer meshes for sampling. These findings reinforce the results produced by Hartline et al. (2016) that demonstrated how finer mesh or filter size gives rise to higher apparent concentrations of MPs, as the smaller mesh size in this research enabled finer and shorter fibres being retained for quantification.

Consistent and standardised sample processing and analysis procedures are essential to estimate the abundance of MPFs. Currently, a standardised test does not exist for the evaluation of MPFs released from textiles or WWTPs. The concentration of microplastic particles and MPFs are measured in different units from per volume (items/m3), per area (items/m2), per weight (items/kg), or the percentage of the total mass (Hidalgo-Ruz et al., 2012 ). Setting up a standard testing methodology is a recognised priority (Henry et al., 2018; Hu et al., 2019). It has been suggested that the best MPF sampling protocols should rely on large sample volumes (≥1m3) and a small mesh size for filtration (<10µm) to capture a representative number of MPF in a sample (Eunomia et al., 2017). However, to date many studies continue to use small sample volumes, as low as 1L (Ziajahromi et al., 2017).  Since our work has shown we can have lower sample volumes and still have a low standard deviation in sampling, this indicates that sampling regimes may be dependent on microplastic concentrations in the sampled environment and/or size of microplastics which are being targeted.

Retention efficiency of solid particles in industrial wastewater treatment

The mill analysed in this present study had a relatively efficient WWTP in removing solid particulates. The total suspended solids (TSS) load in the effluent was 9mg/L, which is lower than the Chinese standard of 100mg/L (National Standard of the People’s Republic of China, 2012) for indirect discharge. This is also lower than the legal requirements for many various countries globally, i.e. a value of 25-150mg/L (ZDHC Foundation 2016). Removal of TSS has been positively correlated with removal of MPF, and thus those treatment plants which are efficient at removing TSS may also be predicted to effectively reduce MPF release (Frehland et al., 2020). Unfortunately, according to UNEP 2018, the performance standard of WWTPs at other mills in textile producing regions often have a lower removal performance than we have documented at the textile processing mill in this study. Consequently, this could mean the MPF release from WWTP would be worse in those areas.

Effectiveness of wastewater treatment in reducing MPF environmental pollution

Since industrial WWTPs are a point source of MPF to the environment which could be mitigated, developing and implementing technologies to reduce MPF in the effluent may be warranted. In particular, there may be a strong demand for better treatment technologies to retain shorter fibres.  In municipal WWTP, installation of a new post-filtration system e.g. tertiary WWTP could reduce the total MPs discharge can retain MPs >500µm completely and increase MPFs <500µm at 98% removal efficiency (Mintenig et al., 2017). Whereas Talvitie et al., (2017) showed various tertiary treatment technologies can improve the retention efficiency of MPs, it can even achieve 99.9% with membrane bioreactor (MBA) type. Later research conducted by Sun et al., (2019) based on 25 published studies suggested that advanced tertiary treatment generally showed a lower MPs concentration than secondary treatment process only WWTPs. The drawbacks are the high investment and operational costs and energy demands. How these studies with municipal WWTP can be related to industrial WWTP also still needs to be seen. Both further research and development and forward-thinking governmental policy implementation are required for a more affordable and effective mean of managing effluent and sewage sludge.

In particular, in China, where global polyester production is currently concentrated, a tertiary treatment of the effluent at the national/regional industrial WWTPs will reduce the MPF release to the aquatic environment from the production process. At the moment, most of the industrial WWTPs are operating primary and secondary treatment (Zhang et al., 2016).  The complication is that the private mills outside the industrial parks are supposed to pay for their own on-site WWTP, as opposed to the national/regional industrial parks where the government funding is concentrated. Consequently, the extremely high price pressure of the industry is experiencing constantly makes these private, smaller mills more likely to reduce water treatment processes. Among 83,227 industrial WWTPs in China (as of 2015), with an annual treatment capacity of 90 billion tonnes of wastewater, the penetration rate of WWTPs remains low. 44 billion tonnes of wastewater were treated in 2015 means that lower than 50% of the full capacity of available industrial WWTPs were utilised in China (Soh, 2018). It is logical to presume that a tertiary treatment of the effluent at the national and regional industrial WWTPs within industrial parks will spread the cost for the individual mills, increase the wastewater treatment penetration rate, and eventually reduce substantial amount of MPF release into the aquatic environments.

Transferability to industry – potential of routine monitoring at industrial wastewater treatment sites

Practically, micro-Raman or micro-FTIR spectroscopy require specialised, highly trained users to operate, and hence are not widely available in commercial laboratories. Scanning microscopic imaging is also used which can be more accurate, but it is highly labour-intensive which makes it difficult to scale up. While high-resolution light microscopic analysis may be an alternative, the obvious drawback is the inability to chemically differentiate between MPFs from varies material types. To improve the reliability and robustness in fibre identification on a larger scale, we suggest win-win academia-industry collaboration: the industry opens their WWTP facilities for MPF researchers to take samples and conduct studies, and researchers can provide the textile mills with MPF detection expertise. In this way, the textile mills can benefit from the expertise which has been generated in an academic setting, while researchers can gain access to primary samples from the industry.

Ultimately, the industry-academia collaboration can help to increase the possibility to set up monitoring regimes at industrial WWTPs which are scientifically sound. In the long run, however, it will be up to the industry to find a way to monitor and control MPF emissions from their mills as academic partners do not have the capacity to run standardised sampling campaigns indefinitely. It is anticipated that once a given mill can set up a standardised operating procedure, they may be able to incorporate MPF analysis into existing monitoring routines for the WWTP effluent.

For textile manufacturers, reporting on and mitigating this source of MPF pollution will increase their transparency and help to promote environmentally sustainable practices. There is currently a lot of international pressure for more sustainable manufacturing practices, especially directed towards the textile industry, and thus shifting efforts to reduce the MPF during the textile production processes could be a responsible and welcome direction for the industry.

Conclusions

This study suggests that the release of MPFs from industrial WWTPs is regularly occurring and thus should be studied and assessed to the same extent as municipal WWTPs. The constant growth of the synthetic textile production would imply an increase of the MPF pollution issue. The protocols developed in this study is considered suitable to be employed by other synthetic textile mills beyond the wet processing units. Our study may be used as the beginning for exploring the potential for including MPFs release as a parameter in monitoring effluent discharge quality. This will help to establish an impact assessment standard for the efficacy of improvements introduced at different stages of textile production. Ultimately, we encourage industry to help reduce MPFs emissions at the production stage, where may account for a substantial proportion of MPF pollution, especially locally. As significant quantities of synthetic textiles are produced in China, measures taken in China will have a large impact. Suggestions for allocation of the public fund from the China’s 14th Five-Year plan to improve the situation for the Chinese polyester production and wastewater treatment specifically is threefold: a) invest in developing affordable and effective MPF filtration system within the WWTPs, b) invest in installing the advanced WWTP within the national/ regional industrial parks, and c)  support private textile mills which cannot afford their own WWTP to relocate within the park to benefit from the centralised pollution control facilities. The benefits and improvements which are developed in Chinese textile mills from these new plans in terms of finding solutions for MPF removal from industrial WWTP could also be used in other textile production facilities as well. This could be particularly relevant for regions which are now developing increased textile production capabilities, as they would have the opportunity to directly implement improved industrial wastewater treatment in relation to MPF removal. These indicators can support industry and regulatory bodies alike to define the maximum threshold for releases of MPFs in effluents of textile processing mills and elsewhere.

DECLARE OF CONFLICT OF INTEREST: We declare no conflict of interests.

Acknowledgements: We thank the School of Technology Fieldwork Fund, University of Cambridge in subside the fieldwork cost. We acknowledge the University Research Facility in Chemical and Environmental Analysis, The Hong Kong Polytechnic University, for the technical support in micro-Raman spectrometry. We thank the facility support from the School of Life Sciences, Chinese University of Hong Kong, to this project. We also thank the Chinatesta (Shenzhen) Testing Services Co., Ltd. for facility and technical support in high-resolution microscopic fibre identification. The factory management to provide access, samples and production data.

Author contributions statement: CKMC designed the experiment, carried out the field trips and sample collection, conducted experiments, produced the results and analysis. KMC helped to design the experiments and characterisation of MPF. JKHF and CWM provided technical support and guidance of sample treatments, and MPF identifications. DMM guided development of sampling protocol, analysis of results, and identifying the goals of the study. CKMC, CP and DMM drafted the manuscript. All co-authors edited and approved it before submission.

REFERENCES

Barrows, A. P. W., Neumann, C. A., Berger, M. L., & Shaw, S. D. (2017). Grab: Vs. neuston tow net: A microplastic sampling performance comparison and possible advances in the field. Analytical Methods, 9(9), 1446–1453. https://doi.org/10.1039/c6ay02387h

Barrows, A. P. W. P. W., Cathey, S. E. E., & Petersen, C. W. W. (2018). Marine environment microfiber contamination: Global patterns and the diversity of microparticle origins. Environmental Pollution, 237, 275–284. https://doi.org/10.1016/j.envpol.2018.02.062

Boucher, J., & Friot, D. (2017). Primary microplastics in the oceans: A global evaluation of sources. Primary Microplastics in the Oceans: A Global Evaluation of Sources, 43. https://doi.org/10.2305/iucn.ch.2017.01.en

Boucher, Julien, & Billard, G. (2019). the Challenges of Measuring. Field Actions Science Reports. The Journal of Field Actions, (19), 68–75. Retrieved from https://journals.openedition.org/factsreports/5319

Browne, M. A., Crump, P., Niven, S. J., Teuten, E., Tonkin, A., Galloway, T., & Thompson, R. (2011). Accumulation of microplastic on shorelines woldwide: Sources and sinks. Environmental Science and Technology, 45(21), 9175–9179. https://doi.org/10.1021/es201811s

Cai, Y., Yang, T., Mitrano, D. M., Heuberger, M., Hufenus, R., & Nowack, B. (2020). Systematic Study of Microplastic Fiber Release from 12 Different Polyester Textiles during Washing. Environmental Science and Technology. https://doi.org/10.1021/acs.est.9b07395

Carr, S. A. (2017). Sources and dispersive modes of micro-fibers in the environment. Integrated Environmental Assessment and Management, 13(3), 466–469. https://doi.org/10.1002/ieam.1916

Conley, K., Clum, A., Deepe, J., Lane, H., & Beckingham, B. (2019). Wastewater treatment plants as a source of microplastics to an urban estuary: Removal efficiencies and loading per capita over one year. Water Research X, 3, 100030. https://doi.org/10.1016/j.wroa.2019.100030

De Falco, F., Gentile, G., Di Pace, E., Avella, M., & Cocca, M. (2018). Quantification of microfibres released during washing of synthetic clothes in real conditions and at lab scale⋆. European Physical Journal Plus, 133(7). https://doi.org/10.1140/epjp/i2018-12123-x

Dris, R., Gasperi, J., & Tassin, B. (2018). Sources and fate of microplastics in urban areas: A focus on Paris megacity. In Handbook of Environmental Chemistry (Vol. 58, pp. 69–83). https://doi.org/10.1007/978-3-319-61615-5_4

Dyachenko, A., Mitchell, J., & Arsem, N. (2017). Extraction and identification of microplastic particles from secondary wastewater treatment plant (WWTP) effluent. Analytical Methods, 9(9), 1412–1418. https://doi.org/10.1039/c6ay02397e

Ellen MacArthur Foundation. (2017). A new textiles economy: redesigning fashion’s future. Retrieved August 16, 2019, from Ellen MacArthur Foundation website: https://www.ellenmacarthurfoundation.org/assets/downloads/publications/A-New-Textiles-Economy_Full-Report_Updated_1-12-17.pdf

Fibre2fashion.com. (2018). Surplus Polyester Production in China. Retrieved November 18, 2018, from https://www.fibre2fashion.com/industry-article/7406/surplus-polyester-production-in-china?page=2

Fischer, E. K., Paglialonga, L., Czech, E., & Tamminga, M. (2016). Microplastic pollution in lakes and lake shoreline sediments e A case study on Lake Bolsena and Lake Chiusi ( central Italy ) *. Environmental Pollution, 213, 648–657. https://doi.org/10.1016/j.envpol.2016.03.012

Frehland, S., Kaegi, R., Hufenus, R., & Mitrano, D. M. (2020). Long-term assessment of nanoplastic particle and microplastic fiber flux through a pilot wastewater treatment plant using metal-doped plastics. Water Research, 182. https://doi.org/10.1016/j.watres.2020.115860

Hann, S., Sherrington, C., Jamieson, O., Hickman, M., Kershaw, P., Bapasola, A., … Eunomia. (2017). Investigating options for reducing releases in the aquatic environment of microplastics emitted by (but not intentionally added in) products - Interim Report. Report for DG Env EC, Vol. 62, N(February), 1596–1605. https://doi.org/10.1002/lsm.22016

Hartline, N. L., Bruce, N. J., Karba, S. N., Ruff, E. O., Sonar, S. U., & Holden, P. A. (2016). Microfiber Masses Recovered from Conventional Machine Washing of New or Aged Garments. Environmental Science and Technology, 50(21), 11532–11538. https://doi.org/10.1021/acs.est.6b03045

Henry, B., Laitala, K., & Klepp, I. G. (2018). Microplastic pollution from textiles : A literature review. Consumption Research Norway - SIFO, Oslo and Akershus University College of Applied Sciences.

Hernandez, E., Nowack, B., Mitrano, D. M., & Empa, †. (2017). Polyester Textiles as a Source of Microplastics from Households: A Mechanistic Study to Understand Microfiber Release during Washing. Environmental Science and Technology, 51(12), 7036–7046. https://doi.org/10.1021/acs.est.7b01750

Hidalgo-Ruz, V., Gutow, L., Thompson, R. C., & Thiel, M. (2012). Microplastics in the marine environment: A review of the methods used for identification and quantification. Environmental Science and Technology, 46(6), 3060–3075. https://doi.org/10.1021/es2031505

Hu, Y., Gong, M., Wang, J., & Bassi, A. (2019). Current research trends on microplastic pollution from wastewater systems: a critical review. Reviews in Environmental Science and Biotechnology, 18(2), 207–230. https://doi.org/10.1007/s11157-019-09498-w

International Organization for Standardisation. (1992). ISO 5667-10:1992 Water quality: Sampling. Part 10: Guidance on sampling of waste waters (Vol. 00). Retrieved from https://www.iso.org/standard/11773.html

ISO - ISO/TR 11827:2012 - Textiles -- Composition testing -- Identification of fibres. (2012). Retrieved August 25, 2019, from Insternational Standard Organisation website: https://www.iso.org/standard/50853.html

Lv, X., Dong, Q., Zuo, Z., Liu, Y., Huang, X., & Wu, W. M. (2019). Microplastics in a municipal wastewater treatment plant: Fate, dynamic distribution, removal efficiencies, and control strategies. Journal of Cleaner Production, 225, 579–586. https://doi.org/10.1016/j.jclepro.2019.03.321

Magnusson, K., & Norén, F. (2014). Screening of microplastic particles in and down-stream a wastewater treatment plant. In IVL Swedish Environmental Research Institute. https://doi.org/naturvardsverket-2226

Masura, J., Baker, J., Foster, G., & Arthur, C. (2015). Laboratory Methods for the Analysis of Microplastics in the Marine Environment. In NOAA Marine Debris Program National. https://doi.org/10.1016/j.jjcc.2016.11.011

Mintenig, S. M., Int-Veen, I., Löder, M. G. J., Primpke, S., & Gerdts, G. (2017). Identification of microplastic in effluents of waste water treatment plants using focal plane array-based micro-Fourier-transform infrared imaging. Water Research, 108(1), 365–372. https://doi.org/10.1016/j.watres.2016.11.015

Mishra, S., Rath, C. charan, & Das, A. P. (2019, March). Marine microfiber pollution: A review on present status and future challenges. Marine Pollution Bulletin, Vol. 140, pp. 188–197. https://doi.org/10.1016/j.marpolbul.2019.01.039

National Standard of the People’s Republic of China. (2012). GB 4287-2012 Discharge standards of water pollutants for dyeing and finishing of textile industry. Retrieved from https://www.chinesestandard.net/PDF.aspx/GB4287-2012

Nizzetto, L., Futter, M., & Langaas, S. (2016, October 18). Are Agricultural Soils Dumps for Microplastics of Urban Origin? Environmental Science and Technology, Vol. 50, pp. 10777–10779. https://doi.org/10.1021/acs.est.6b04140

Norin, H., & Ab, E. (2018). Microplastics from industrial laundries - A laboratory study of laundry effluents. Retrieved from http://www.naturvardsverket.se/Documents/publ-kompl/1003-10 Report Microplastics from industrial laundries.pdf

Opperskalski, S., Siew, S., Tan, E., & Truscott, L. (2019). Preferred Fiber & Materials Market Report 2019. Retrieved from https://store.textileexchange.org/product/2019-preferred-fiber-materials-report/

Pirc, U., Vidmar, M., Mozer, A., & Kržan, A. (2016). Emissions of microplastic fibers from microfiber fleece during domestic washing. Environmental Science and Pollution Research, 23(21), 22206–22211. https://doi.org/10.1007/s11356-016-7703-0

Roos, S., Arturin, O. L., & Hanning, A.-C. (2017). Microplastics shedding from polyester fabrics. 15. Retrieved from www.mistrafuturefashion.com

Sancroft. (2018). Microfibres Pollution: Current State Assessment Report.

Sun, J., Dai, X., Wang, Q., van Loosdrecht, M. C. M., & Ni, B. J. (2019). Microplastics in wastewater treatment plants: Detection, occurrence and removal. Water Research, 152, 21–37. https://doi.org/10.1016/j.watres.2018.12.050

Talvitie, J., Mikola, A., Koistinen, A., & Setälä, O. (2017). Solutions to microplastic pollution – Removal of microplastics from wastewater effluent with advanced wastewater treatment technologies. Water Research, 123, 401–407. https://doi.org/10.1016/j.watres.2017.07.005

Talvitie, J., Mikola, A., Setälä, O., Heinonen, M., & Koistinen, A. (2017). How well is microlitter purified from wastewater? – A detailed study on the stepwise removal of microlitter in a tertiary level wastewater treatment plant. Water Research, 109, 164–172. https://doi.org/10.1016/j.watres.2016.11.046

Tsang, Y. Y., Mak, C. W., Liebich, C., Lam, S. W., Sze, E. T. P., Chan, K. M., … Chan, K. M. (2017). Microplastic pollution in the marine waters and sediments of Hong Kong. Marine Pollution Bulletin, 115(1–2), 20–28. https://doi.org/10.1016/j.marpolbul.2016.11.003

UNEP. (2018). Mapping of global plastics value chain and plastics losses to the environment (with a particular focus on marine environment). 1–99. Retrieved from https://gefmarineplastics.org/files/2018 Mapping of global plastics value chain and hotspots - final version r181023.pdf

Xu, X., Hou, Q., Xue, Y., Jian, Y., & Wang, L. P. (2018). Pollution characteristics and fate of microfibers in the wastewater from textile dyeing wastewater treatment plant. Water Science and Technology, 78(10), 2046–2054. https://doi.org/10.2166/wst.2018.476

Yang, L., Li, K., Cui, S., Kang, Y., An, L., & Lei, K. (2019). Removal of microplastics in municipal sewage from China’s largest water reclamation plant. Water Research, 155, 175–181. https://doi.org/10.1016/j.watres.2019.02.046

ZDHC Foundation. (2016). Textile Industry Wastewater Discharge Quality Standard: Literature Review Rev 1. Retrieved from https://www.roadmaptozero.com/fileadmin/pdf/WastewaterQualityGuidelineLitReview.pdf

ZDHC Foundation. (2019). ZDHC Wastewater Guidelines V1.1. Retrieved from https://www.roadmaptozero.com/post/updated-zdhc-wastewater-guidelines-v1-1-released

Zhang, Q. H., Yang, W. N., Ngo, H. H., Guo, W. S., Jin, P. K., Dzakpasu, M., … Ao, D. (2016). Current status of urban wastewater treatment plants in China. Environment International, 92–93(July), 11–22. https://doi.org/10.1016/j.envint.2016.03.024

Zhao, S., Zhu, L., Wang, T., & Li, D. (2014). Suspended microplastics in the surface water of the Yangtze Estuary System, China: First observations on occurrence, distribution. Marine Pollution Bulletin, 86(1–2), 562–568. https://doi.org/10.1016/j.marpolbul.2014.06.032

Ziajahromi, S., Neale, P. A., Rintoul, L., & Leusch, F. D. L. (2017). Wastewater treatment plants as a pathway for microplastics: Development of a new approach to sample wastewater-based microplastics. Water Research, 112, 93–99. https://doi.org/10.1016/j.watres.2017.01.042

Tables and Figures Legend

Table 1. Summary of microplastic fibres identified in all volumes of wastewater effluent samples

Figure 1. Key procedures of the test protocol for quantifying microplastic fibres from industrial effluent

Figure 2. A) Linear regression analysis of abundance of microplastic fibres in different sample volumes of the effluent. Standard deviation is variance between triplicate samples. B) Number of MPF per litre variance in different sample volumes of the effluent

Figure 3. MPF abundance by length. Note that the x-axis is not a linear scale: size bins are 100µm for bins <1,000µm and 1,000µm for bins >1,000µm. Standard deviation is variance between sample volumes. Proportion of MPF in each size bin to the total MPF count in percentage is also indicated by the diamond points along each bar, referenced by the right y-axis.

Figure S1. Stereomicroscope images from ImageFocus Alpha illustrating how count and measurements were taken and counting criteria were applied A) Fibrous shape which was organic (natural) was excluded B) Microplastic fibre at width (>20µm) was excluded C) Microplastics were excluded

Figure S2. High-resolution microscopic images A) Microplastic fibres from production fabric base yarn fibres FDY75D/36F B) Microplastic fibres from production fabric pile yarn DTY 150D/288F. C & D) Microplastic fibres from effluent

Figure S3. Micro-Raman spectrophotometer images with matching polyester standard spectrum against microplastic fibres specimens found in production and effluent.