Dataset Description

Fig2_In situ pseudo-2D 1H NMR

Zip folder containing 1) online 1H spectra of the anolyte obtained from a 100 mM DHAQ against 300 mM K4Fe(CN)6 full cell acquired while charging with a current of 100 mA; 2) the voltage profile of the cell.

Fig3_Electron transfer

Zip folder containing variable-temperature NMR spectra of 5 mM DHAQ3•− in a DHAQ solution of total concentration 100 mM, and in situ 1H NMR spectra and voltage of the cell comprising 100 mM DHAQ and 300 mM K4Fe(CN)6, obtained with a low current of 1 mA so as to capture the initial stages of charging.

Fig4_In situ NMR and MS

Zip folder containing 1) 1H NMR spectra of 100 mM DHAQ during a potential hold at 1.2 V and 1.7 V, following charging at 100 mA, and the voltage profile of the cell; 2) 1H NMR spectra, voltage and current of a 100 mM 2,6-DHAQ in D2O in a charge–rest experiment in N2 (flow) atmosphere. 3) In situ mass spectrometry signals of D2 (mass-to-charge ratio, m/z = 4) during a stepped potential-hold experiment.

Efig2_In situ pseudo-2D 1H NMR

Zip folder containing 1) Operando NMR spectra of 10 cm3 of 100 mM DHAQ, against 20 cm3 of 150 mM potassium ferrocyanide; 2) On-line NMR spectra of 20 cm3 of 100 mM DBEAQ (anolyte), against 20 cm3 of 300 mM potassium ferrocyanide (catholyte).

Efig3_EPR

Zip folder containing EPR spectra of 100 mM and 1 mM DHAQ solution reduced to 50% SOC.

Efig4_CV and radical concentration

Zip folder containing 1) CV of 5 mM DHAQ and 5 mM DBEAQ in D2O with 1 M KOH. The potential was scanned at 20 mV s−1, starting from positive to negative potentials. 2) Fraction of DHAQ3•− radicals calculated on the basis of the Evans method as a function of SOC for DHAQ

(100 mM) under a charging current of 100 mA and a flow rate of 13.6 cm3 min−1, and a charging current of 150 mA and a flow rate of 33.3 cm3 min−1.

Efig5_Multiplecycs

Zip folder containing 1) 20 cm3 of 100 mM DHAQ against 40 cm3 of 150 mM potassium hexacyanoferrate(ii)/50 mM potassium hexacyanoferrate(iii). The flow rate is 33.3 cm3 min−1 and the current is 150 mA. With d1 = 20 s, an acquisition time (aq) = 1.5 s and ns = 4, each spectrum is a snapshot of the electrochemical processes averaged over 2.5% of the SOC; 2) 20 cm3 of 200 mM DHAQ against 40 cm3 of 250 mM potassium hexacyanoferrate(ii)/50 mM potassium hexacyanoferrate(iii). The flow rate is 13.6 cm3 min−1 and the current is 150 mA. With d1 = 15 s, aq = 1.5 s and ns = 8, each spectrum is a snapshot of the electrochemical processes averaged over 2.9% of the SOC. 3) 20 cm3 of 100 mM DBEAQ against 40 cm3 of 150 mM potassium hexacyanoferrate(ii)/50 mM potassium hexacyanoferrate(iii). The flow rate is 13.6 cm3 min−1 and the current is 100 mA. With d1 = 7 s, aq = 1.5 s and ns = 8, each spectrum is a snapshot of the electrochemical processes averaged over 2.1% of the SOC.

Efig6_VT NMR

Zip folder containing variable-temperature NMR spectra acquired from a solution containing a radical concentration of 5 mM in 100 mM DHAQ. As the experiments were performed by locking the magnetic field on the shift of the water resonance (which is temperature dependent),

the shift of peak A of DHAQ was manually set to 7.3 ppm so as to more readily compare the different spectra.

Efig7_Electron transfer rate

Zip folder containing on-line 1H NMR spectra performed to quantify the electron-transfer rates at 30 mM, 50 mM, 100 mM 2,6-DHAQ, and 100 mM 2,6-DBEAQ during charge/reduction at 1 mA.

Efig8_NMR of decomposition product

Zip folder containing 1) DOSY 2) COSY 3) HSQC NMR spectra of the aliquot extracted from the H cell at 470 h (see Method section ‘H-cell experiments in an argon glovebox’ in the article for details) in an airtight NMR tube; 4) In situ NMR during the galvanostatic cycling at 100 mA after the potential-hold (1.7 V) step.

Efig9_Decomposition under different cycling condition

Zip folder containing in situ 1H NMR study of the decomposition reaction

under different cycling conditions at 1.4 V and 1.7 V for DHAQ and DBEAQ molecules, respectively.

Efig10_Relaxation

Zip folder containing the NMR spectra acquired by t1ir and CPMG pulse sequences. These spectra were used to extract the longitudinal and transverse relaxation times of DHAQ and HOD at different SOC.