# First UK commercial deployment of microcapsule-based self-healing reinforced concrete

Chrysoula Litina*, Benyi Cao, Jingtao Chen, Zijing Li, Ioanna Papanikolaou, Abir Al-Tabbaa

*Corresponding author

# Abstract

Consolidating previous research on the development of novel microcapsules for self-healing in cementitious systems, this work forms a base for developing an implementation strategy and guidance for microcapsule-based self-healing technology. The study presents details of the first commercial deployment of this technology, as a ready-mix self-healing additive for commercial application. This involved the on-site construction of two slabs in a new development at the University of Cambridge. This paper describes the optimisation of the mix, the structural concept and design, and processing and casting procedures. Prior to application, investigations of the compliance and compatibility of the healing additive with the concrete according to specifications and requirements of the design were completed, validating the use of the developed system. These were further complemented by large-scale laboratory testing of the healing efficiency under damage scenarios identified as critical for the on-site application. The performance of the site installation was monitored over 12 months through a combination of NDT methods. Results are presented with durability indicators confirming the in situ enhanced performance of the proposed self-healing system.

# Introduction

Increasing population and living standards in both developing and developed countries impose an ever-increasing demand for infrastructure. This translates to a growing volume of civil engineering activities and in turn a construction market. It is not surprising that within the EU28, the total output of these construction activities, amounts to over €1278 billion and employs over 14 million people (FIEC 2019). Concrete structures have been the main driver of these activities as concrete remains the most versatile, cost effective and widely produced building material. However, concrete structures are becoming more and more strained by increasingly unpredictable and severe damaging environments and performance requirements. Concrete structures built in the 1960s and 1970s, are failing to meet their expected service life not due to lack of intrinsic strength but due to gradual deterioration. This is mirrored in the increasing share of the construction activities associated with rehabilitation and maintenance. In the UK this corresponds to half the annual construction budget (ONS 2016). Looking towards addressing future societal needs, strategic investments such as for energy generation, climate change management, data security (European Commission 2014; i3P 2017; UK Treasury 2016) will require large infrastructure to be built in the next decade that is able to deliver enhanced safety, less structural failures and reduced maintenance.

Now more than ever the scope of new technologies to provide a higher level of confidence in the reliability of our infrastructure materials is considerable (European Commission 2014). Amongst these technologies self-healing materials have been acknowledged as a technological breakthrough able to shape the future of the construction industry sector (World Economic Forum and The Boston Consulting Group 2016). Self-healing is a long known property of biological materials. Concrete is considered as an intrinsic self-healing material itself, since it exhibits self-regenerating properties due to the mineral composition of the cementitious matrix. The main mechanisms that induce this so-called autogenous healing however are efficient only for small cracks and can only be activated in the presence of water (de Rooij et al. 2013). During the last decade, several concepts for self-healing concrete have been explored to enhance this autogenous process based on engineering the concrete mix by addition of crystalline admixtures or bacteria to enhance carbonate precipitation, fibres to control the crack width, or hydrogels to seal cracks and supply water for further hydration (De Belie et al. 2018; de Rooij et al. 2013). At the same time, to address healing of larger cracks (> than few hundreds of µm), it was early identified that additional healing material must be supplied (Dry 1994a; b). Therefore, a mechanism was needed that could sense the damage and trigger repair. The latter has been achieved by encapsulating polymeric or mineral agents that imbue the ability of a localised response to damage upon rupture and release and activation of their healing core (De Belie et al. 2018; de Rooij et al. 2013). Microencapsulation is a particular category of encapsulation that involves the coating of finely ground solids, liquid droplets or gaseous components, with protective walls (Ghosh 2009). Microcapsule-based technologies are powerful adjuncts to the construction industry’s existing toolbox of chemical admixtures, being employed already for heat proofing and air-entraining applications (Boh et al. 2008). More and more research in self-healing cementitious systems has focused on the development of microcapsules aiming at reducing permeability and/or restoring the mechanical properties of the cementitious materials after the damage has occurred (De Belie et al. 2018; de Rooij et al. 2013) as their relative benefits in terms of ease of handling and direct incorporation to construction practices are identified.

# Self-healing infrastructure materials: The commercial tipping point

Self-healing technologies are poised to become successful commercial products if the enthusiasm and high level engagement from client organisations and companies across the construction supply chain are any indication (Gardner et al. 2018; Lychgate 2016). Concurrently, the successful commercialisation of self-healing materials in other sectors has been promising (eg. “epion | self-healing asphalt” n.d.). But even if it is, for the wider industry to take note and adopt in normal practices, that success will have to be repeated many times over in relevant to the construction sector applications. Over the recent years, first demonstrators with self-healing concrete for commercial deployment have been constructed through national and international projects. In the Netherlands significant advances have been made on the development of biological healing for concrete (Jonkers 2010). Researchers at Delft University of Technology (TU Delft) were first to implement a bacteria self-healing technology in a new structure (Stewart 2016). Since then more large scale field applications of bacteria-based self-healing systems (Tziviloglou et al. 2016; Wiktor and Jonkers 2015, 2016) aiming to provide confidence in the proposed technologies. Other sporadic exhibitions of self-healing concrete in scale have been realised (Sierra-Beltran et al. 2015; Wang et al. 2019) with promising results.

In the UK, as part of the EPSRC funded project Materials for Life (M4L) in 2013-2016, a more systematic approach for the delivery of self-healing systems to address cracks across many length scales was realised (Al-Tabbaa et al. 2019; Davies et al. 2018b; Kanellopoulos et al. 2017; Teall et al. 2016, 2018). This project focused on developing complementary technologies for healing damage, amongst these were also microcapsules, and how these could be combined in the concrete scale. The extensive system development and material testing in the laboratory was successfully culminated by scaling up, and using and evaluating the performance in full-scale field trials (Al-Tabbaa et al. 2019; Davies et al. 2018b; Teall et al. 2016).

The work reported herein aims to consolidate the extensive previous research activities and field trials (Al-Tabbaa et al. 2018, 2019; Alghamri et al. 2016; Davies et al. 2018a; Kanellopoulos et al. 2015, 2017; Souza 2017; Teall et al. 2016), enabling the first commercial deployment of microcapsule-based self-healing concrete in the UK. This included validation, optimisation and creation of a selection matrix, proposing the appropriate dosage for the expected service conditions and expected damage. The optimisation of the mix design in terms of compatibility, the structural concept and design, the location of healing agents, processing and casting procedures, were also considered. Finally, the durability and self-healing performance of the proposed microcapsule-based concrete was investigated by relevant simulation testing in the lab and non-destructive monitoring. This study forms a base for developing a sound implementation strategy and guidance for microcapsule-based self-healing concrete.

# Commercial application background: University of Cambridge, West Cambridge Engineering Campus

The commercial installation forms part of the new Civil Engineering Building of the proposed Department of Engineering Campus in West Cambridge. This is a £36M project to provide a world-class building to house the UK Collaboratorium for Research on Infrastructure and Cities (UKCRIC), National Research Facility for Infrastructure Sensing (NRFIS) and the research activities of the Civil Engineering Division. The building incorporates a number of pioneering and innovative aspects of construction design, design for deconstruction, the installation of building sensors and elements of innovative concrete.

Within the project’s site compound two external concrete slabs were specified for the application. These are grade PAV2 concrete slabs with brushed finish (200mm thick, 4.25m long and 2.822m wide) that form part of the permanent structure. The base case concrete requirements are defined in Table 1.

A concept model of the structure is shown in Fig. 1. For all elements of this structure, the detailed structural design was completed according to the provisions of BS EN 1992. A concrete air entrained mix design was specified, referred to as the control mix, and is detailed in Table 2. For consideration of the appropriateness of the self-healing additions as part of the permanent installation, a preliminary round of testing was agreed with the contractor and critical performance parameters had to be met. Upon approval of the material for site use, the pouring sequence and construction programme was agreed to accommodate the application of the self-healing concrete cover. The slabs were constructed over a 4-week period with the control base slabs initially cast and allowed to cure for 28 days before pouring in the self-healing cover concrete.

# Materials and Methods

## Self-healing additives

The microcapsules used and reported here were the result of industrial collaboration, which led to the design and production, using complex coacervation, of gelatine/gum Arabic shell microcapsules containing sodium silicate as the cargo. Details on the production, characteristics and properties are presented elsewhere (Kanellopoulos et al. 2017). The microcapsules had a mean diameter of 290µm (SD ~120µm) (Fig. 2)(Kanellopoulos et al. 2017). Based on the results from related laboratory studies on the effect of the microcapsules on the fresh and hardened material properties and healing potential of mortars  and concrete, (Kanellopoulos et al. 2016), and building on the promising findings of the previous field trials (Al-Tabbaa et al. 2019), a selection matrix was developed and two microcapsule dosages, 12% and 16%  by volume of cement were proposed for the commercial deployment. These dosages were selected to provide an increased level of healing whilst preliminary studies identified a high compatibility with traditional mortar matrices with negligible  detrimental effects on the workability, setting time and strength development (Giannaros et al. 2016; Kanellopoulos et al. 2016).

## Critical compatibility assessment

The critical parameters were defined by the contractor for the application. These included minimum compressive strength and workability in accordance with BS EN 12390 and BS EN12350-2 respectively. Thus, samples were initially prepared in the lab to establish the compliance of the self-healing microcapsules at the two proposed dosages of 12% and 16% by vol of the cement, with the ready mix design for the PAV2 concrete slab according to the contractor’s specification. For comparison, a control mix was also cast following the specified ready mix design. Moreover, the mix sequence was considered to optimise the mix for site application. The mixtures were prepared using a rotating pan mixer. The production started with the dry mixing of the cement and aggregates for 5 minutes. The water was added in two parts into the mixer. Half of the water was added in the mix as is and the rest was used to disperse the microcapsules to ensure optimum distribution during mixing. Following the completion of mixing slump test was conducted on the fresh mix and the workability was evaluated. Subsequently the material was moulded in 100×100×100 mm cubes and Ø100x200mm cylinders necessary for the strength assessment at 7 and 28 days. The samples were compacted on a vibration table, levelled during casting and no further surface adjustment was needed prior to testing. The samples were then demoulded at 1 day and placed in water for curing until testing. All tests were conducted in triplicates.

## Commercial deployment of the self-healing concrete

### Field installation

The ready mix concrete was delivered on site and the two control concrete slabs poured in the base leaving a rebate out with dimensions of 1.42m wide, 2.822m long and 60mm deep in each for the self-healing topping concrete to be applied. The construction sequence is presented in Fig. 3. The self-healing deep topping was poured as an infill of 0.34m3 in each precast slab (Fig. 3d). For the preparation of the two self-healing topping concrete sections, the microcapsules were first washed with water and filtered from their preserving solution before being added, in their slurry form, directly into the ready-mix C32/40 concrete. These were mechanically hand mixed in 250 Litre concrete mixers on site and cast in place. The microcapsules were added at 12 and 16% by volume of the cement, corresponding to ~4 and 5.3% by weight of the cement and ~0.66% and 0.88% of the total concrete mix, respectively. Casting, compaction and finishing were carried out in accordance with standard construction practice. The workability was assessed upon delivery of the ready mix concrete and further evaluated upon the addition of the microcapsules in the mix. Moreover, concrete cubes (100mmx100mmx100mm) and cylinders (Ø100mmx200mm) were cast on site for the mix for 7 and 28days strength characterisation as well as for calibration of the NDT techniques and to determine SonReb curb coefficients for all mixes with and without self-healing additives.

### NDT testing and continuous performance monitoring on site

Non-destructive testing (NDT) methods were applied on site to monitor the performance of the self-healing slabs sections and provide further information about internal densification, compressive strength development, durability and corrosion potential (Fig. 4). Reference readings were taken on the control concrete sections for comparison. Herein, a rebound hammer complying to EN 13791 for the non-destructive assessment of strength was employed at multiple locations on both the control and self-healing concrete slabs. A ultrasonic pulse velocity test (UPV) instrument complying with European standard EN12504-4 and BS1881:Part 203 was used to assess the compressive strength of the applied self-healing concrete sections. The ultrasonic probes were placed on the concrete surface and ultrasonic couplant was used between the surfaces to facilitate transmission. Ultrasonic measurements were carried out with 54 kHz transducers on site on the selected grid measuring the time (T) required for the pulse to transverse a length L in μs according to:

V=LT, in km/s					    (Eq. 1)

where V is the velocity of the pulse. High pulse velocity readings are generally indicative of good quality concrete.

Prior to testing calibration measurements were done on cylinders of the same cement and aggregate as used on site and correlated to compressive strength values in the lab at 7, 28 and 365 days.  The concrete compressive strength test was conducted on cylindrical specimen taken from the site, which were kept in wet conditions till 7 days and then at ambient RH~65% conditions till tested. The ultrasonic pulse velocity test was performed at first, then specimen was placed between the plates of a universal testing machine. A constant 5 kN load was applied to fix its position and rebound hammer test was performed in horizontal direction. On three equidistant locations (at 120o angle), 9 readings by rebound hammer were taken per specimen. Finally, the cylinder was loaded until crushed and the failure load was recorded in the evaluation of compressive strength. Both tests were combined through regression analysis to propose a prediction formula to assess the compressive strength in situ.

Concrete permeability is a good indicator of the long-term durability of a concrete section. Air permeability testing allows a non-destructive assessment of the quality of the concrete cover on site and is in good agreement with laboratory methods such as oxygen permeability, capillary suction and chloride penetration (Torrent 1992). As part of the long-term assessment of the on-site performance of the installed self-healing concrete section, air permeability measurements were taken at various locations on the surfaces of both the control and self-healing topping sections using a Torrent Permeability Tester (Fig. 5), as per SN 505 252/1, Annex E. Data was collected automatically by the display unit and the permeability coefficient (kT) and the depth of penetration (L) of the vacuum was then calculated.

To further establish the durability and robustness of the self-healing concrete installation compared to the control reference section, resistivity measurements were undertaken. Empirical tests and theory have shown that resistivity is directly linked to both the likelihood of corrosion due to chloride diffusion and to the corrosion rate once depassivation of the steel has taken place (Hornbostel et al. 2013; Polder et al. 2000). A resistivity meter was employed to measure the electrical resistivity of the concrete. A current was applied to the two outer probes and the potential difference was measured between the two inner probes. The current is carried by ions in the pore liquid. The calculated resistivity depends on the spacing (a) of the probes.

ρ=2πaV l (kΩcm) 					      (Eq. 2)

where ρ is the resistivity of the concrete, V is the voltage measured between the two inner probes (in volts) and I the current injected in the two outer probes (in amps). When the electrical resistivity (ρ) of the concrete is low, the likelihood of corrosion increases.

## Self-healing potential evaluation

### Evaluation of crack sealing by optical microscopy and ultrasonic measurements

To assess the healing performance of the self-healing concrete proposed for the commercial deployment, prisms with dimensions of 80mmx80mmx300mm were prepared. A Ø1.6 diameter reinforcement bar was introduced on the top half of the specimen to control the cracking of the samples and prevent complete separation into two pieces. All specimens were demoulded after 1 day of curing and then cured in a water tank at 20 ± 2 °C until the designated testing age. The mechanical loading of the prisms was performed on a 30 kN static testing frame. Prior to cracking, all specimens were notched to depth of 3 mm with a rotating diamond blade. A clip gauge was used to monitor crack mouth opening displacement (CMOD). The prisms were three-point-loaded over a span of 240 mm, at a rate of 0. 25 mm/min to a crack width of 0.30 (± 0.02) mm, controlled by the CMOD. Two different ages (7 and 28 days) of initial cracking were selected to establish base-line self-healing. After cracking, all samples were kept in high moisture environment (~RH 98%) to activate the healing mechanism for 28 days.

To monitor crack initiation, opening and closure of the crack faces, all the specimens were monitored over time using a Leica S6D digital stereoscope microscope. Digital microscope images were taken from at least five observation locations along the crack length. Crack width healing values were also calculated in order to quantify crack closure. The crack width healing percentage compares measured crack width values with the initial crack opening at that point following cracking and unloading. It is noteworthy that despite the specimens being cracked for a controlled width of 0.30 mm, upon load removal all specimens had remaining crack width of 0.22 and 0.35 mm at 7 and 28 days of initial cracking, respectively. The visual observations on the specimen were complemented by crack depth measurements to assess the overall crack volume reduction. Ultrasonic wave transmission was used to measure the crack depth evolution at each of the crack locations during the monitoring events. A ultrasonic testing equipment was employed following a similar setup to (Al-Tabbaa et al. 2019; Alghamri et al. 2016; Kanellopoulos et al. 2015).

### Evaluation of freeze-thaw resistance and immunity to damage

To emulate better the primary type of damage expected on site, cube specimens were prepared for the control and the two self-healing concrete mixes proposed and subjected to freeze-thaw cycles. 100mmx100mmx100mm cubes were prepared and cured according to CEN/TS 12390-9:2006 and then immersed in 3% sodium chloride solution. Their freeze-thaw resistance was evaluated by measurement of mass loss of the cubes after 28 freeze-thaw cycles. During the freeze-thaw curing, each freeze-thaw cycle consisted of 16 h of all-round freezing at -18°C (±1°C) and 8 h of thawing at 20°C (±2°C). These measurements were coupled with compressive strength and sorptivity testing to assess further the strength retention potential and immunity to damage.

### Capillary water absorption as a durability indicator

Sorptivity test was used to evaluate the durability recovery potential for the healed prismatic and cube samples. The liquid capillary absorption coefficient was obtained for cracked and healed specimens. At the end of the healing period the samples were removed from their curing condition and left for 14 days in ambient conditions (60% RH and 20 oC). Subsequently, the bottom and side faces of the prisms, were insulated with adhesive aluminium tape leaving only the crack area exposed; thus ensuring that the capillary absorption can only take place through the crack itself. For the freeze-thaw samples the side faces of the cubes were insulated with adhesive aluminium tape leaving only the bottom face of cube exposed. Weight changes of the specimens due to capillary water uptake were monitored for 4 h and 16 min in all specimens. The sorptivity coefficient of concrete was then estimated according to (Hall and Tse 1986).

# Field performance of the microcapsule-based concrete

## Compatibility assessment

Slump test results are available in Table 3. The slump requirement according to the design specification was S2 with an expected slump range varying from 50 to 90mm. All mixes consistently reported a higher slump value outside of the designated range. This was even more pronounced for the ready mix delivered on site. The latter was expected as further water was added in the bulk load delivered on site to improve the workability. Nevertheless the recorded values, 100mm and 110mm for the lab and on site testing respectively, are within the maximum allowable range for the S2 class and were considered acceptable. Comparatively, the use of self-healing additives overall, did not affect the slump performance and workability of the fresh mix, yielding similar slump to the control mix.

Samples of the control mix and the two applied self-healing concrete slabs were collected during the site application for compatibility and quality assessment. Compressive strength results at 7 and 28 days are presented in Fig. 6. Overall the measured strength values from site samples were lower than the equivalent lab prepared samples. This reduction could be attributed to the addition of extra water in the ready mix delivered on site to improve the workability. However, CTRL samples reported a compressive strength above the C32/40 characteristic strength designation. Considering the effects of the addition of self-healing materials, results confirmed a negative influence on strength development, and that effect was dependent on the volumetric content and the age of the specimens. This is in agreement with our previous work on the same microcapsules (Giannaros et al. 2016; Kanellopoulos et al. 2016) where the lowest volume fraction of microcapsules at which the effect of microcapsule addition becomes noticeably detrimental is 12% Vf with a reported loss of ∼17% (Kanellopoulos et al. 2016).  In lab results, this was indeed reported here but only at 7 days, with a 12.5% loss in strength compared to the control observed for RMC12 and 19% for RMC16 respectively. However, this was reduced at 28 days reaching ~12% for RMC16 compared to the control while in the case of RMC12 (12% by volume addition) it became negligible. A similar trend can be seen for the site samples, with the final 28 days strength reporting a 15.2% and 13% reduction compared to the control for RMC12 and RMC16 respectively. However, the impact of self-healing additions is smaller at 7 days. In fact, a relative strength increase of ~2% can be observed at RMC12. In all cases the reported values are above the designated strength requirement at 28 days. Moreover, the small variation of the reported values confirms the good distribution of the self-healing additions achieved both in the lab and in the concrete on site and the compatibility with the other additives used in the mix. This further implies that for normal construction practices the addition of microcapsules doesn’t practically hinder strength development.

The presence of microcapsules seemed to improve the flexural strength and fracture toughness at both 7 and 28 days, as identified by 3-point bending results (Fig. 7). The improvement is not however proportional to the microcapsule content. Results show an optimum for RMC12, with a more than 50% improvement at 7 days and ~13% at 28 days respectively. Increasing the microcapsule concentration further although improved the measured values compared to the control resulted in a reduction of both flexural strength and fracture toughness. These observations are consistent with previous findings in mortar and concrete prisms (Kanellopoulos et al. 2016, 2017).

## In situ performance

### Monitoring mechanical performance

The long-term performance of the slabs was assessed through a combination of NDT tests. To assess the strength development rebound hammer tests, combined with ultrasonic pulse velocity measurements were undertaken at two monitoring events; 4 months and 12 months from the time of installation. Average measurements from 9 different locations were used to profile the surface hardness of the concrete slabs and are presented in Fig. 8. The rebound number can be used as an indicator of strength in situ (Breysse 2012; Pucinotti 2015). A consistent increase in recorded rebound values can be seen for all slabs with time, indicating the progress of hydration and strength development. At 12 months the overall surface hardness for all slabs is similar, within the range of 31-32. This confirms our lab assessment of concrete cubes and cylinders at 28 days suggesting that any strength effects on the concrete are short-termed and do not affect the long-term performance. On the other hand, at 4 months observations suggest a higher rebound index for both the RMC12 and RMC16 slabs compared to the control. This could be the result of a densifying effect of the microcapsules in the concrete mix. Moreover, it could be an early indication of an immunity of the microcapsule system to the environmental conditions. As the measurements at 4 months were performed over the winter, with low temperatures (below freezing) over night and thawing through the day.

Average values of UPV are presented in Fig. 9. At least 3 readings were recorded. Error bars present the standard deviation, all values lie in the range of 3.2-3.95 km/s. The general trend shows an increase of measured UPV values with time, confirming the strength development of the concrete in situ. Overall the recorded values are lower than other data from literature (Breysse 2012). This could be attributed to the increased air content of the air entrained mixes, which could increase the time for traveling of the ultrasonic pulse wave, reducing the measured velocity. The effect of both the addition and fraction of microcapsules on the UPV measurements seems to be beneficial. At 4 months the variations are negligible but comparatively after 12 months both self-healing slabs recorded higher UPV than the CTRL. This effect seems dependent on the microcapsule content. This contradicts previous findings on the effect of microcapsule content on UPV predicted strength of mortars (Kanellopoulos et al. 2016). A higher fraction of microcapsule addition in this concrete matrix could lead to a denser structure due to a filler effect of small particles in the matrix thus reducing the time needed for the pulse to travel through the matrix. It should be noted, here that the texture (uneven brushed finish) rendered the application of the probes problematic. Measurements were possible in only some locations, and only after effort was taken to sufficiently smooth the surface.

Both NDTs were used in combination to assess and predict the compressive strength in situ. Cylinders from the site were used to determine SonReB curve coefficients for the three investigated mixes. Eq. 3 is the general equation which has been used to correlate compressive strength with UPV and rebound hammer values.

F=aVbNc										(Eq. 3)

Where, F is the compressive strength, V is the ultra-sonic pulse velocity, N the Rebound hammer index value, and a, b, c are constants depended on the material. The natural logarithms of the V versus F and F versus N were initially calculated, and subsequently the ‘least squares’ method to best fit the data was employed following the procedure proposed by Proceq (Proceq n.d.). Based on these analyses, appropriate values for coefficients a, b, c were determined (Table 4) and used for evaluating the compressive strength on site from rebound hammer and UPV values. Several relationships have been proposed in literature, in which both NDTs are combined to predict the compressive strength (Ali-Benyahia et al. 2017; Alwash et al. 2015; Breysse 2012; RILEM TC 43-CND 1993). It is not within the scope of this work to propose an overall model but rather to better describe and predict the material performance in situ. Results show that the trend of the models is similar for all the examined mixes but the exact values are highly affected by an increase in microcapsule content. As the microcapsule content increases a gradual drop can be seen in the N values as UPV is increased. From the combined SonReb analysis the in situ compressive strength was estimated (Fig. 10). Although the values presented are predicted values the results confirm an improved performance for the microcapsule-based cover-concrete compared to the control in situ and are very promising as an indication of the long term durability of the system.

### Concrete Durability Indicators

The coefficient of air permeability values measured on site are presented in Fig. 11. The measurements from the site show similar values in the range of ~10-16kT, typical of concrete of good quality (Bjegović et al. 2016). The permeability of the two microcapsule slabs was 7.3ˑ10-17kT (±1.51ˑ10-17) and 3.3ˑ10-18kT (±3.2 ˑ10-18) for the RMC12 and RMC16 slabs respectively compared to 2.2ˑ10-16kT (±2.2ˑ10-16) for the CTRL. These suggest that the microcapsule content did not negatively affect the porosity of the concrete. These results are in agreement with previous observations from the site application of microcapsule additives in a self-healing concrete panel  (Al-Tabbaa et al. 2019). Moreover, a further reduction of the permeability with increasing microcapsule content can be seen. Similar results were observed in the laboratory using sorptivity tests to assess the permeability of concrete and mortar samples (Kanellopoulos et al. 2016). It should be noted here that it was not possible to obtain air permeability measurements at both monitoring events. Considerable efforts were devoted to establish appropriate conditions  as recommended by literature (Ebensperger and Torrent 2011; Romer 2005; Torrent et al. 2012). Only one monitoring event was possible, after 12 months, as there were a number of challenges when attempting to test the slab surfaces at 4 months. Concrete that is too cold, and/or with too high degree of saturation should be avoided. As the latter is known to have a strong effect on the measured values (Romer 2005). During the first monitoring event (January 2019) temperature measurements of the surface of the concrete indicated a temperature of 4oC and a thin layer of ice was visible on the surface.

As a further indicator of the durability of the slab in terms of corrosion potential the surface resistivity of the concrete applied on site, including CTRL, RMC12 and RMC16 mixes, was assessed at 28 days on concrete cylinders sampled from the site according to AASHTO T358-19. Moreover, a concrete resistivity array probe was employed on site to determine the resistivity of the concrete slabs in situ with time. Results are presented in Table 5. According to empirical reference values and classification of concrete permeability for Portland cement at 20oC assessed by the Wenner four-probe system (AASHTO 2017; Azarsa and Gupta 2017; LANGFORD and BROOMFIELD 1987) cylinders for all mixes report a low corrosion rate (>20 kΩcm) and a very low chloride ion penetration potential. Results from site assessment also confirm a very low chloride ion permeability compared with measured empirical data for real (semi-infinite) slab applications (Azarsa and Gupta 2017), showing similarly lower overall measured values. This could be a result of the effect on temperature and humidity/saturation variation on site. The resistivity of the concrete is expected to increase when the concrete is drying out and when the concrete ages (as a result of carbonation), while the resistivity significantly decreases in wet, saturated concrete and with larger and connected pores (Polder et al. 2000). Yet an effect on surface resistivity by the addition of microcapsules can be seen, confirming previous observations on the potential influence of higher microcapsule fractions on the corrosion durability of cementitious composites (Wang et al. 2013). However, literature is scarce on the effect of healing additives on the durability characteristics of cementitious composites. Further assessment is needed to ascertain the long-term performance.

## Laboratory investigation of self-healing potential of applied microcapsule-based concrete

Parallel to assessing the performance in situ further testing was undertaken to identify the self-healing potential of the proposed mixes under appropriate simulated damage environments in the laboratory. Crack mouth healing results of concrete prisms cracked under 3-point bending testing at lab scale, are presented in Fig. 12. Typical images of the crack patterns and morphology can be seen in Fig. 13. Crack mouth healing results for samples cracked at both 7 and 28 days confirm the superior performance of self-healing microcapsule-based concrete. Moreover for early age damage the healing performance improvement is proportional to the increase of microcapsule content. It is noteworthy that the healing environment adopted provided minimum water to further promote autogenic healing through further hydration and carbonate precipitation, thus any observed crack recovery is due to the complementary action of the microcapsules cracking and releasing their healing agent. This is more evident at samples cracked at 28 days, where hydration process has further progressed and the availability of unhydrated particles contributing to crack sealing is limited. This is the case of the control prisms where the presence of microcapsules significantly enhances the healing process, yielding CMH up to 62% and 70% for RMC16 and RMC12 respectively. These results not only are consistent with preliminary investigation for mortars specimen (Kanellopoulos et al. 2016) but also were in good agreement with microscopic crack width healing reported in the full scale trials at 28 days (Al-Tabbaa et al. 2019).

Assessment of the crack depth recovery confirms the improved crack filling ability of the microcapsule concrete (Fig. 14). It is worth noting that even for considerably deeper cracks, for the same crack width crack filling was more pronounced. Particularly when samples were cracked at 28 days. The average crack depth reduced by 48% and ~39% in the RMC12 and RMC16 samples after 28 days of healing for early age cracking respectively. Concurrently negligible improvement was observed at the control specimen. A consistent improvement was also observed for samples cracked at 28 days, reaching 33% for RMC12 and exceeding ~75% for RMC16. Similarly, the reduction for the control was minimal.

Yet, the overall sealing efficiency potential of the microcapsule concrete seemed impaired compared to the control (Fig. 15). Although microscopic healing observations and crack depth measurements confirm the crack filling and recovery, the sorptivity results (as seen in Fig. 16) report increased water uptake by the microcapsule-based concretes compared to the control. Previous investigations in mortars and concrete (Kanellopoulos et al. 2016) on the same microcapsule system reported that higher microcapsule fraction has a higher potential for water update. This is related to the nature of the shell of the microcapsules. The gelatine/gum Arabic shell has been found to absorb water and swell as it transitions from rigid to flexible/rubbery shell properties (Kanellopoulos et al. 2017). An increased content of microcapsules would mean an increased capacity of the system to absorb water. However, this effect seems counteracted partially by the healing contribution of the microcapsules, as the fraction of microcapsules increases from 12 to 16% by volume. The latter could explain the better performance of the RMC16.

The concrete mix used in the slabs is designed for exposure environment with high risk of frost damage. The results for laboratory testing for scaling resistance with deicing salts are given in Fig.17. All concrete samples are more or less deteriorated due to scaling. A closer look at Fig. 18 shows that the specimens developed with self-healing concrete had lower mass loss (scaling) compared to the control. RMC16 exhibited significant immunity to scaling even after 28 f-t cycles. It is implied that the microcapsules themselves may be acting as flexible voids, not yet ruptured and releasing their core material, but still allowing the dissipation of the stress build up due to the volume increase of the frozen water. Their size falls within an optimum proposed pore size range for higher resistance to frost scaling as suggested by  (Sommer 1979).

Frost deterioration is also expected to lead to reduction in compressive strength. Previous investigations in self-healing concrete for frost damage have shown reductions in strength of up to 29% (Jacobsen and Sellevold 1996).  Compressive strength results after 28 cycles of f-t are presented in Fig. 19 and further confirm the superior performance of the samples prepared with microcapsule additions. After 28 cycles of damage RMC12 and RMC16 reported relatively smaller reduction in strength (~32%) or even complete immunity compared to CTRL which reported a loss of 37.5% in compressive strength. Self-healing between f-t cycles can be an important factor improving the durability against frost damage for concrete on site (Jacobsen and Sellevold 1996). Water uptake is related to the degree of internal damage (Jacobsen and Sellevold 1996). An increased uptake, and as a result increased sorptivity coefficient values, would be expected after damage has occurred. The reduction in water uptake in RMC12 and RMC16 signifies not only an enhanced immunity of the matrix against damage but also the healing of internal cracking and overall improved frost durability. Although healing wasn’t evident for the RMC12 samples the increase microcapsule content reported a significantly improved performance and strength retention/immunity even under the most aggressive environment. Of course monitoring of the performance on site should be taken into account when attempting to interpret the long term durability of the installation. However, the results so far suggest that the healing additions not only are compatible with the concrete as designed for the specific application but also further improve the resistance of the concrete to f-t, increasing the long term durability.

# Conclusions

The work reported herein aims to consolidate the extensive previous research activities enabling the first commercial deployment of microcapsule-based self-healing technology in the UK. The self-healing concrete using microencapsulated sodium silicate was cast on-site as part of the permanent slab pavement work of the new Civil Engineering Building of the University of Cambridge in West Cambridge. Two self-healing topping concrete sections were poured as infills (0.34m3). Based on previous results on performance of these microcapsules a selection matrix was developed, and two microcapsule contents, 12% and 16% by volume of cement were selected for the application. Initial compatibility assessment was undertaken considering compressive strength and workability. The physical implementation was shown to be a relatively straightforward process with the self-healing additives directly introduced and mixed in batches in the ready mix concrete upon delivery on site. Non-destructive testing methods were applied on site to monitor the performance of the self-healing slabs sections providing further information about internal densification, compressive strength development, durability and corrosion potential. In particular:

- A consistent increase in recorded rebound values can be seen for all slabs with time, suggesting a negligible effect of the self-healing additions on the progress of hydration and strength development.

- The effect of both the addition and fraction of microcapsules on the UPV measurements seems to be beneficial. After 12 months both self-healing slabs recorded higher UPV than the CTRL.

- Combined SonReb analysis was used to further assess the in situ performance. Results confirmed an improved strength for the microcapsule-based cover-concrete compared to the CTRL.

- A further reduction of the permeability with increasing microcapsule content was observed, namely 7.3ˑ10-17kT (±1.51ˑ10-17) and 3.3ˑ10-18kT (±3.2 ˑ10-18) for the RMC12 and RMC16 slabs respectively compared to 2.2ˑ10-16kT (±2.2ˑ10-16) for the CTRL.

- Surface resistivity results identified very low chloride ion penetration potential for all slabs but a negative effect from the addition of microcapsules was observed. Yet environmental conditions could have affected the observed values. Testing is ongoing to assess the long-term durability of all slabs.

In parallel, lab testing to assess the self-healing performance of the concrete under relevant to the application damage scenarios identified:

- The enhanced performance of self-healing microcapsule-based concrete in terms of crack mouth healing at both investigated ages, reaching up to 62% and 70% crack closure for RMC16 and RMC12 respectively.

- An improved crack volume recovery for both proposed microcapsule contents with average crack depth reductions reaching 48% and ~39% in the RMC12 and RMC16 samples after 28 days of healing for early age cracking. A consistent improvement was also observed for samples cracked at 28 days, reaching 33% for RMC12 and exceeding ~75% for RMC16. Control samples showed no visible healing at the assessed times.

- A significant improvement in the freeze-thaw resistance of concrete that had been designed with self-healing additives. The self-healing samples had lower reported mass loss (scaling) and compressive strength loss compared to the control. In particular RMC16 exhibited significant immunity to scaling with no strength loss reported even after 28 f-t cycles.

This work comprised the first use of microcapsule based self-healing in a permanent structural application not only demonstrating the maturity of the technology and the ease with which such commercial deployment can be made possible through close collaboration with the industry but also offers invaluable insight in the real time performance. This study forms a base for developing a sound implementation strategy and guidance for microcapsule-based self-healing concrete.

# Data availability statement

All data, models, and code generated or used during the study appear in the submitted article.

# Acknowledgements

The financial support from EPSRC for the Resilient Materials for Life (RM4L) Programme Grant (EP/P02081X/1) is gratefully acknowledged. The authors are also particularly grateful to Paul Astle of Ramboll, Cambridge, Tom Fenner of SDC, Andy Dunlop from AECOM, Simon Smith from Smith and Wallwork and Rachel Williams from Cambridge University Building Projects for their part in supporting and facilitating this commercial deployment.

# References

AASHTO. (2017). T358 Standard Method of Test for Surface Resistivity Indication of Concrete’s Ability to Resist Chloride Ion Penetration.

Al-Tabbaa, A., Lark, B., Paine, K., Jefferson, T., Litina, C., Gardner, D., and Embley, T. (2018). “Biomimetic Cementitious Construction Materials for Next Generation Infrastructure.” Proceedings of the Institution of Civil Engineers - Smart Infrastructure and Construction,  Thomas Telford Ltd , 1–35.

Al-Tabbaa, A., Litina, C., Giannaros, P., Kanellopoulos, A., and Souza, L. (2019). “First UK field application and performance of microcapsule-based self-healing concrete.” Construction and Building Materials, Elsevier, 208, 669–685.

Alghamri, R., Kanellopoulos, A., and Al-Tabbaa, A. (2016). “Impregnation and encapsulation of lightweight aggregates for self-healing concrete.” Construction and Building Materials, 124, 910–921.

Ali-Benyahia, K., Sbartaï, Z.-M., Breysse, D., Kenai, S., and Ghrici, M. (2017). “Analysis of the single and combined non-destructive test approaches for on-site concrete strength assessment: General statements based on a real case-study.” Case Studies in Construction Materials, Elsevier, 6, 109–119.

Alwash, M., Breysse, D., and Sbartaï, Z. M. (2015). “Non-destructive strength evaluation of concrete: Analysis of some key factors using synthetic simulations.” Construction and Building Materials, Elsevier, 99, 235–245.

Azarsa, P., and Gupta, R. (2017). “Electrical Resistivity of Concrete for Durability Evaluation: A Review.” Advances in Materials Science and Engineering, Hindawi, 2017, 1–30.

De Belie, N., Gruyaert, E., Al-Tabbaa, A., Antonaci, P., Baera, C., Bajare, D., Darquennes, A., Davies, R., Ferrara, L., Jefferson, T., Litina, C., Miljevic, B., Otlewska, A., Ranogajec, J., Roig-Flores, M., Paine, K., Lukowski, P., Serna, P., Tulliani, J. M., Vucetic, S., Wang, J., and Jonkers, H. M. (2018). “A Review of Self-Healing Concrete for Damage Management of Structures.” Advanced Materials Interfaces, 1800074, 1–28.

Bjegović, D., Serdar, M., Oslaković, I. S., Jacobs, F., Beushausen, H., Andrade, C., Monteiro, A. V., Paulini, P., and Nanukuttan, S. (2016). “Test Methods for Concrete Durability Indicators.” 51–105.

Boh, B., Boštjan Šumiga, and Šumiga, B. (2008). “Microencapsulation technology and its applications in building construction materials.” RMZ - Materials and Geoenvironment, 55(3), 329–344.

Breysse, D. (2012). “Nondestructive evaluation of concrete strength: An historical review and a new perspective by combining NDT methods.” Construction and Building Materials, Elsevier, 33, 139–163.

Davies, R., Teall, O., Pilegis, M., Kanellopoulos, A., Sharma, T., Jefferson, A., Gardner, D., Al-Tabbaa, A., Paine, K., and Lark, B. (2018a). “Large scale application of self-healing concrete: Design, construction and testing.” Frontiers in Materials, (accepted).

Davies, R., Teall, O., Pilegis, M., Kanellopoulos, A., Sharma, T., Jefferson, A., Gardner, D., Al-Tabbaa, A., Paine, K., and Lark, R. J. (2018b). “Large Scale Application of Self-Healing Concrete: Design, Construction and Testing.” Frontiers in Materials, Frontiers, 5, 51.

Dry, C. (1994a). “Matrix cracking repair and filling using active and passive modes for smart timed release of chemicals from fibers into cement matrices.” Smart Material Structure, 118(3).

Dry, C. (1994b). “Smart multiphase composite materials which repair themselves by a release of liquids which become solids.” Proceedings of Symposium on Smart Structures and Materials, Orlando, USA, 62–70.

Ebensperger, L., and Torrent, R. (2011). “Concrete air permeability ‘in situ’ test: status quo.” Revista Ingeniería de Construcción, 25(3), 371–382.

“epion | self-healing asphalt.” (n.d.). <http://www.epionasphalt.com/> (Oct. 18, 2019).

European Commission. (2014). Business Innovation Observatory - Smart Living: Advanced Building Materials.

Ferrara, L. (2018). “Self-healing cement-based materials: an asset for sustainable construction industry.” IOP Conference Series: Materials Science and Engineering, IOP Publishing, 442(1), 012007.

FIEC. (2019). Key Figures Activity 2018, Construction in Europe.

Gardner, D., Lark, R., Jefferson, T., and Davies, R. (2018). “A survey on problems encountered in current concrete construction and the potential benefits of self-healing cementitious materials.” Case Studies in Construction Materials, Elsevier, 8, 238–247.

Ghosh, S. K. (2009). “Self-healing Materials: Fundamentals, Design Strategies, and Applications.” Self-healing Materials Fundamentals, Design Strategies, and Applications, S. K. Ghosh, ed., WILEY-VCH Verlag GmbH & Co. KGaA, 1–25.

Giannaros, P., Kanellopoulos, A., and Al-Tabbaa, A. (2016). “Sealing of cracks in cement using microencapsulated sodium silicate.” Smart Materials and Structures, 25(8), 084005.

Hall, C., and Tse, T. K.-M. (1986). “Water movement in porous building materials—VII. The sorptivity of mortars.” Building and Environment, 21(2), 113–118.

Hornbostel, K., Larsen, C. K., and Geiker, M. R. (2013). “Relationship between concrete resistivity and corrosion rate - A literature review.” Cement and Concrete Composites.

i3P. (2017). Technology Roadmap for UK Construction &amp; National Infrastructure.

Jacobsen, S., and Sellevold, E. J. (1996). “Self healing of high strength concrete after deterioration by freeze/thaw.” Cement and Concrete Research, 26(1), 55–62.

Jonkers, H. M. (2010). “BioConcrete : A novel bio-based material.” Engineering, 1–3.

Kanellopoulos, A., Giannaros, P., and Al-Tabbaa, A. (2016). “The effect of varying volume fraction of microcapsules on fresh, mechanical and self-healing properties of mortars.” Construction and Building Materials, 122, 577–593.

Kanellopoulos, A., Giannaros, P., Palmer, D., Kerr, A., and Al-Tabbaa, A. (2017). “Polymeric microcapsules with switchable mechanical properties for self-healing concrete: synthesis, characterisation and proof of concept.” Smart Materials and Structures, IOP Publishing, 26(4), 045025.

Kanellopoulos, A., Qureshi, T., and Al-Tabbaa, A. (2015). “Encapsulated mineral precursors for self-healing cement based composites.” 5th International Conference on Self-Healing Materials, Durham, USA.

LANGFORD, P., and BROOMFIELD, J. (1987). “MONITORING THE CORROSION OF REINFORCING STEEL.” Construction Repair, Palladian Publications, 1(2).

Lychgate. (2016). Self-healing concrete – potential applications and benefits.

ONS. (2016). “Construction output in Great Britain: May 2016.” <https://www.ons.gov.uk/>.

Polder, R., Andrade, C., Eslener, B., Vennesland, O., Gulikers, J., Weidert, R., and Raupach, M. (2000). “RILEM TC 154-EMC: ELECTROCHEMICAL TECHNIQUES FOR MEASURING METALLIC CORROSION.” Materials and Structures, 33, 603–6011.

Proceq. (n.d.). Proceq, Using EXCEL to determine SONREB curve coefficients. Switzerland.

Pucinotti, R. (2015). “Reinforced concrete structure: Non destructive in situ strength assessment of concrete.” Construction and Building Materials, Elsevier, 75, 331–341.

RILEM TC 43-CND. (1993). “Draft recommendation for in situ concrete strength determination by combined non-destructive methods.” Materials and Structures, 26, 43–49.

Romer, M. (2005). “Effect of moisture and concrete composition on the torrent permeability measurement.” Materials and Structures, Kluwer Academic Publishers, 38(5), 541–547.

de Rooij, M., Van Tittelboom, K., De Belie, N., and Schlangen, E. (2013). Self-Healing Phenomena in Cement-Based Materials State-of-the-Art Report of RILEM Technical Committee 221-SHC: Self-Healing Phenomena in Cement-Based Materials. RILEM 2013.

Sierra-Beltran, M. G., Jonkers, H. M., and Ortiz, M. (2015). “Field application of self-­healing concrete with natural fibres as linings for irrigation canals in Ecuador.” Fifth International Conference on Self-Healing Materials, 32.

Sommer, H. (1979). “The Precision o| the Micro-seopleal Determination of the Air-Void System in Hardened Concrete.” Cement, Concrete and Aggregates, CCAGDP, 1(2), 49–55.

Souza, L. R. L. R. (2017). “Design and synthesis of microcapsules using microfluidics for autonomic self-healing in cementitious materials.” Cambridge University Engineering Department.

Stewart, A. (2016). “The ‘living concrete’ that can heal itself.” CNN, <https://edition.cnn.com/2015/05/14/tech/bioconcrete-delft-jonkers/index.html>.

Teall, O., Davies, R., Pilegis, M., Kanellopoulos, A., Sharma, T., Paine, K., Jefferson, A., Lark, R., Gardner, D., and Al-Tabbaa, A. (2016). “Self-healing concrete full-scale site trials.” Proceedings of the 11th fib International PhD Symposium in Civil Engineering, K. Maekawa, A. Kasuga, and J. Yamazaki, eds., Tokyo, Japan, 639–646.

Teall, O., Pilegis, M., Davies, R., Sweeney, J., Jefferson, T., Lark, R., and Gardner, D. (2018). “A shape memory polymer concrete crack closure system activated by electrical current.” Smart Materials and Structures, IOP Publishing, 27(7), 075016.

Torrent, R., Denarie, E., Jacobs, F., Leemann, A., and Teruzzi, T. (2012). “Specification and site control of the permeability of the cover concrete: The Swiss approach.” Materials and Corrosion, 63(12).

Torrent, R. J. (1992). “A two-chamber vacuum cell for measuring the coefficient of permeability to air of the concrete cover on site.” Materials and Structures, 25(6), 358–365.

Tziviloglou, E., Wiktor, V., Jonkers, H. M., and Schlangen, E. (2016). “Bacteria-based self-healing concrete to increase liquid tightness of cracks.” Construction and Building Materials, 122, 118–125.

UK Treasury. (2016). National Infrastructure Delivery Plan 2016–2021. HM Treasury, London.

Wang, X., Huang, Y., Huang, Y., Zhang, J., Fang, C., Yu, K., Chen, Q., Li, T., Han, R., Yang, Z., Xu, P., Liang, G., Su, D., Ding, X., Li, D., Han, N., and Xing, F. (2019). “Laboratory and field study on the performance of microcapsule-based self-healing concrete in tunnel engineering.” Construction and Building Materials, Elsevier, 220, 90–101.

Wang, X., Xing, F., Zhang, M., Han, N., and Qian, Z. (2013). “Experimental Study on Cementitious Composites Embedded with Organic Microcapsules.” Materials, 6(9), 4064–4081.

Wiktor, V., and Jonkers, H. M. (2015). “Field performance of bacteria-based repair system: Pilot study in a parking garage.” Case Studies in Construction Materials, Elsevier Ltd., 2, 11–17.

Wiktor, V., and Jonkers, H. M. (2016). “Bacteria-based concrete: From concept to market.” Smart Materials and Structures, Institute of Physics Publishing, 25(8).

World Economic Forum, and The Boston Consulting Group. (2016). A Breakthrough in Mindset and Technology - Shaping the Future of Construction.

Table 1 The base case concrete requirements as defined by the contractor for the field application.

| Concrete Grade | PAV 2 with brushed finish |
| --- | --- |
| Type of reinforcement | A393 mesh top with 50mm cover |
| Mix Type | AE |
| Cement Type | CEMI |
| Max Aggregate size (mm) | 20 |
| Target Slump (mm) | S2 |
| Max w/c ratio | 0.45 |
| Min cement content (kg/m3) | 340 |
| Chloride class | 0.40 |
| Exposure class | XF4 |

Table 2 Composition by % weight of the ready mix C32/40 concrete (supplied by Tarmac UK)

| Material | Quantity for ready mix slab (kg/m³ unless noted otherwise) |
| --- | --- |
| Cement (CEM I_52.5R) | 376 |
| 10/20mm Granite aggregates | 733 |
| 4/10mm Granite | 387 |
| 0/4mm Sand | 617 |
| Water | 169 (w/c 0.45) |
| Admix: ChrysoAIR D /air entraining agent | 0.56 |
| Admix: Chrysoplast /RMD plasticizer | 2.22 |

Table 3 Slump test results in the lab

| # | Samples | Slump (mm) | Field measurement (mm) |
| --- | --- | --- | --- |
| CTRL | Designated design mix | 100 | 110 |
| RMC12 | 12% vol. by cement |  |  |
| RMC16 | 16% vol. by cement |  |  |

Table 4 SonReb coefficients a,b,c of the correlation curve F=aVbNc relating compressive strength (F) with UPV (V) and rebound hammer values (N) for each of the three investigated mixes. Values have been calculated through regression analysis to best-fit experimental data. The relevant R-square value of the fit is also presented.

| Coefficient | CTRL | RMC12 | RMC16 |
| --- | --- | --- | --- |
| a | 0.0177 | 0.0039 | 0.0407 |
| b | 0.476 | 0.52 | 0.152 |
| c | 1.126 | 1.472 | 1.62 |
| R2 | 0.989 | 0.845 | 0.839 |

Table 5 Average surface resistivity values for CTRL, RMC12 and RMC16 concrete cylinders (Ø100x200mm) at 28 days and equivalent values from in situ assessment of the slabs after 4 months and 12 months.

|  | Surface resistivity ρ (kΩcm) |  |  |
| --- | --- | --- | --- |
|  | 28 days | 4 months | 12 months |
| CTRL | 147.6 (±16.7) | 55.5 (±2.7) | 49.3 (±3.0) |
| RMC12 | 145.1 (±7) | 34.7 (±2.6) | 32.2 (±2.3) |
| RMC16 | 142.3 (±5.1) | 38.4 (±0.8) | 37.2 (±1.6) |

## FIGURES

Fig. 1. The New Cambridge University Civil Engineering Building; Concept model of the slabs.

Fig. 2. A microscopic image of the microcapsules used in the commercial deployment work presented here.

Fig. 3. Field installation process stages, (a) ready mix concrete was delivered on site; (b) the microcapsules were added and mixed in situ before (c) samples were taken for further compliance assessment; (d) the self-healing concrete was applied as top coating in the preformed rebates.

Fig. 4. Location of permeability, rebound hammer, ultrasonic pulse velocity and surface resistivity measurements.

Fig. 5. Air-permeability testing device obtaining measurements on the RMC12 slab.

Fig. 6. Lab and field result for compressive strength with increasing volume fraction (Vf) of microcapsules at 7 and 28days respectively.

Fig. 7. Flexural strength and fracture toughness variation with increasing volume fraction (Vf) of microcapsules at 7 and 28 days.

Fig. 8. Surface hardness characterisation of (a) CTRL, (b) RMC12 and (c) RMC16 slab areas through rebound hammer test. Scale indicates rebound index values.

Fig. 9. Average ultrasonic pulse velocity values measured in situ for all three slabs CTRL, RMC12, RMC16 at 4 and 12 months.

Fig. 10. Evaluated compressive strength from combined NDT measurements at two monitoring events.

Fig. 11. Average air permeability coefficient values measured in situ.

Fig. 12. Crack mouth healing (%) of laboratory samples after 28 days, with respect to microcapsules volume fraction (Vf) for samples cracked at 7 and 28 days.

Fig. 13. Typical digital stereoscope images of crack mouth taken on the day of cracking (top) of laboratory samples and after 28 days of healing (bottom) for: (a) samples cracked at 7 days  and  (b) samples cracked at 28 days (Note: solid bars correspond to 500 μm).

Fig. 14. Average ultrasonic crack depth measurements at the date of cracking of the laboratory samples and after 28 days healing; for cracking at  7 and 28 days.

Fig. 15. Estimated sealing efficiency in the laboratory samples after 28 days healing.

Fig. 16. Measured sorptivity coefficients with increasing concentration of microcapsules measurements in the laboratory samples on the date of cracking and after 28 days healing; for cracking at 7 and 28 days.

Fig. 17. Observation of the laboratory samples of CTRL, RMC12 and RMC16 after (a) 7 and (b) 28 freeze/thaw cycles(a)(a)

Fig. 18. Total material lost after 28 cycles of freeze-thaw damage for the laboratory CTRL, and microcapsules-based concrete RMC12 and RMC16.

Fig. 19. Compressive strength before and after 28 cycles of freeze-thaw damage and after healing for the laboratory samples CTRL, and microcapsules-based concrete RMC12 and RMC16.

Dr Chrysoula Litina, Ph.D., Research Associate, University of Cambridge, Department of Engineering, Civil Engineering Building, JJ Thompson Avenue 7a, Cambridge, CB3 0FA, email: cl519@cam.ac.uk

Benyi Cao, PhD Researcher, University of Cambridge, Department of Engineering, Civil Engineering Building, JJ Thompson Avenue 7a, Cambridge, CB3 0FA,

Jingtao Chen, PhD Researcher, University of Cambridge, Department of Engineering, Civil Engineering Building, JJ Thompson Avenue 7a, Cambridge, CB3 0FA,

Zijing Li, PhD Researcher, University of Cambridge, Department of Engineering, Civil Engineering Building, JJ Thompson Avenue 7a, Cambridge, CB3 0FA,

Ioanna Paanikolaou, Ieng, MICE, PhD Researcher, University of Cambridge, Department of Engineering, Civil Engineering Building, JJ Thompson Avenue 7a, Cambridge, CB3 0FA

Professor Abir Al-Tabbaa, PhD CEng FICE, University of Cambridge, Department of Engineering, Civil Engineering Building, JJ Thompson Avenue 7a, Cambridge, CB3 0FA