Supplementary Material

High-Pressure Phase Transitions of Nitinol, NiTi, to a Semiconductor with Unusual Topological Structure

Guangtao Liu1, Hanyu Liu2 , Xiaolei Feng3 and Simon A. T. Redfern3,4 *

1 National Key Laboratory of Shock Wave and Detonation Physics, Institute of Fluid Physics, China Academy of Engineering Physics, Mianyang 621900, China

2 Geophysical Laboratory, Carnegie Institution of Washington, Washington, DC 20015, USA

3 Department of Earth Sciences, University of Cambridge, Downing Street, Cambridge, CB2 3EQ, UK

4 Center for High Pressure Science and Technology Advanced Research, Shanghai 201203, China

Corresponding author: satr@cam.ac.uk (Simon A. T. Redfern)

Contents

1. Parameter Convergence Test

2. Elastic Constants Cij (GPa)

3. Equation of states of all phases in NiTi.

4. Band structures of NiTi.

1. Parameter Convergence Test

The selected Pbcm and B32 (Fd-3m) structure are shown as examples here.

a) When Monkhorst-Pack grid is 2π×0.05 Å−1 in reciprocal space,

| Energy cutoff (eV) | Pbcm, Energy (eV/atom) | B32, Energy (eV/atom) |
| --- | --- | --- |
| 200 | -6.7282 | -6.4148 |
| 300 | -6.9699 | -6.6487 |
| 400 | -6.9654 | -6.6440 |
| 450 | -6.9648 | -6.6434 |
| 500 | -6.9649 | -6.6435 |
| 600 | -6.9647 | -6.6433 |
| 700 | -6.9646 | -6.6432 |
| 800 | -6.9646 | -6.6432 |

we set energy cutoff with 450 eV in structural optimization, enthalpy and electronic structure calculations.

b) When energy cutoff is 450 eV,

| Monkhorst-Pack grid | Pbcm, Energy (eV/atom) | B32, Energy (eV/atom) |
| --- | --- | --- |
| 1.0 | -7.0872 | -6.6342 |
| 0.8 | -6.9887 | -6.6018 |
| 0.6 | -6.9898 | -6.6552 |
| 0.5 | -6.9835 | -6.6552 |
| 0.4 | -6.9623 | -6.6438 |
| 0.3 | -6.9648 | -6.6434 |
| 0.2 | -6.9658 | -6.6430 |
| 0.15 | -6.9649 | -6.6419 |
| 0.1 |  | -6.6425 |

we set Monkhorst-Pack grid with 2π×0.05 (~ 0.3) Å−1 in structural optimization, enthalpy and electronic structure calculations.

2. Elastic Constants Cij (GPa)

Pbcm phase at 20 GPa

301.99414   151.45338   186.80861     0.00000     0.00000     0.00000

151.45338   376.57869   192.37652     0.00000     0.00000     0.00000

186.80861   192.37652   357.17950     0.00000     0.00000     0.00000

0.00000     0.00000     0.00000    80.18312     0.00000     0.00000

0.00000     0.00000     0.00000     0.00000    81.51821     0.00000

0.00000     0.00000     0.00000     0.00000     0.00000    22.79107

It satisfies the criteria for mechanical stability (orthorhombic phase):

Cii > 0, C11 + C22 + C33 + 2(C12 + C13 + C23) > 0,

C11 + C22 - 2C12 > 0, C11 + C33 - 2C13 >0, C22 + C33 - 2C23 >0.

B32 (Fd-3m) phase at 40 GPa

392.36040   255.38702   255.38702     0.00000     0.00000     0.00000

255.38702   392.36040   255.38702     0.00000     0.00000     0.00000

255.38702   255.38702   392.36040     0.00000     0.00000     0.00000

0.00000     0.00000     0.00000   171.01783     0.00000     0.00000

0.00000     0.00000     0.00000     0.00000   171.01783     0.00000

0.00000     0.00000     0.00000     0.00000     0.00000   171.01783

It satisfies the criteria for mechanical stability (cubic phase):

C11 >0, C44 >0, C11 > |C12|, C11 + 2C12 > 0.

3. Equation of states of all phases in NiTi

4. Band structures of NiTi

Band structures along high symmetry path.

(a) B2 structure at 0 GPa, (b) B33 structure at 0 GPa and (c) Pbcm structure at 30 GPa.