Advances in Dielectric Thin Films for Energy Storage Applications, Revealing the Promise of group IV binary oxides

J. P. B. Silvaa*, K. C. Sekharb, Hao Panc,d, J. L. MacManus-Driscolld+*, M. Pereira+a

aCentre of Physics of University of Minho and Porto (CF-UM-UP), Campus de Gualtar, 4710-057 Braga, Portugal

bDepartment of Physics, School of Basic and Applied Science, Central University of Tamil Nadu, Thiruvarur-610 101, India

cDivision of Physics and Applied Physics, School of Physical and Mathematical Science, Nanyang Technological University, 21 Nanyang Link, 04-01, 637371, Singapore

d Dept. of Materials Science and Metallurgy, 27 Charles Babbage Rd., Cambridge, CB3 OFS, U.K

+Joint last authors

*Corresponding authors’ e-mails: josesilva@fisica.uminho.pt and jld35@cam.ac.uk

ABSTRACT

Among currently available energy storage (ES) devices, dielectric capacitors are optimal systems owing to their highest power density, high operating voltages, and long lifetime. Standard, high-performance ferroelectric-based ES compositions are formed of complex-composition perovskites, and require precision, high temperature thin film fabrication. The discovery of ferroelectricity in doped HfO2 in 2011 at the nanoscale was potentially game-changing for many modern technologies such as field effect transistors, non-volatile memory, and ferroelectric tunnel junctions. This is because HfO2 is a well-established material in the semiconductor industry where it is used as a gate dielectric. On the other hand, (pseudo-)binary HfO2 and ZrO2-based materials have received much less attention for ES capacitors, even though antiferroelectric HfO2 and ZrO2-based thin films show strong promise. This focus review summarizes the current status of conventional polymer and perovskite ferroic-based energy storage. It then discusses recent developments in, and proposes new directions for, antiferroelectric and ferroelectric group IV oxides, namely HfO2 and ZrO2-based thin films.

The demand for reducing both CO2 emission and the consumption of fossil fuels requires the long-term pursuit of renewable and sustainable energy sources such as solar, wind, hydroelectric and tide energy. However, these energy sources are intermittent, and thus, there is a pressing need to develop high-power-density, efficient, low-cost and environmentally friendly ES devices.

There is a significant difference in the energy storage density, power density and the charge-discharge time of batteries, electrochemical capacitors (i.e. supercapacitors), and dielectric capacitors.1,2 Among them, dielectric capacitors realize energy storage via a physical charge-displacement mechanism, with ultra-high-power density (MW kg-1) and higher operation voltages than electrochemical capacitors2,3 where the electrolytes are unstable at higher voltages.4

Key advantages of dielectric capacitors over electrochemical capacitors include low self-discharge, higher thermal and mechanical stability, which make them important for high power/pulse power technologies in medical equipment (defibrillators, pacemakers), commercial systems (camera flash, food sterilization), energy systems (grid-connected photovoltaics and wind turbine generators, and high-frequency inverters), communication and sensing devices in the internet of things, and transportation (electric vehicles and trains).1,2 Advantages of dielectric capacitors over batteries includes faster charge and discharge rates because the chemical reactions that take place within batteries take longer time to release electrons than the electrical discharge in dielectric capacitors. In addition, batteries have the disadvantage that chemical reactions need to take place to store and release energy. However, the application of dielectric capacitors is currently limited by their low energy storage density (ESD) in circumstances requiring large capacitances and small packaging size. Hence, compared to batteries the ESD is typically three orders of magnitude lower.5

The ESD of a dielectric is determined by two factors: the polarization (P) induced by external electric field (E) and the highest sustainable E in the dielectric (also denoted as dielectric breakdown field (EBD), as given by the equation  , where Pm and Pr are the maximum and remnant polarization, respectively.1,2 Moreover, the ES efficiency of the capacitor is quantified by the ratio between the recoverable energy density (Urec) and the stored energy density (Ust), as given by the equation η=UrecUst.1,2

To achieve high ESD and for it to be stable at high temperatures, to obtain superior ES performance, it is important to aim for a low coercive field Ec, high Pm, low Pr, large EBD, slim hysteresis, and low leakage current.1,2

Table 1 gives examples of the best performance ES parameters for different types in the family of dielectric materials. Throughout the paper, we contrast the performance parameters of the different dielectrics. We begin with more traditional systems and then move to the more recently discovered HfO2 and ZrO2-based systems where there is great promise for future improvements. We also provide a view on the ways to further improve their performance.

| Material | Type | Film thickness (nm) | ESD (J cm-3) | EBD (MV/cm) | Efficiency (%) | Ref no |
| --- | --- | --- | --- | --- | --- | --- |
| Polymer dielectric-based |  |  |  |  |  |  |
| BOPP | Polymer | 3000 | 2-3 | 6 | >90 | 9 |
| Oxide perovksite ferroic-based |  |  |  |  |  |  |
| 0.25BiFeO3-0.3BaTiO3-0.45SrTiO3 | RFE | 200-800 | 112 | 4.9 | 80 | 27 |
| Mn-doped BiFeO3–BaTiO3 | RFE | 350 | >80 | 3.0 | 90 | 28 |
| 0.5Ba(Zr0.2Ti0.8)O3–0.5(Ba0.7Ca0.3)TiO3/HfO2:Al2O3 | RFE | 160 | 99.8 | 0.8 | 71 | 28 |
| Ba(Zr0.2Ti0.8)O3 | RFE | 350 | 133 | 5.7 | 80 | 29 |
| 0.99(0.94Bi0.5Na0.5TiO3–0.06BaTiO3)–0.01BiMnO3 | RFE | 400 | 57 | 2.7 | 79 | 30 |
| PbZr0.52Ti0.48O3/Al2O3/PbZr0.52Ti0.48O3 | FE | 330 | 64 | 5.5 | 81 | 31 |
| Pb0.99Nb0.02(Zr0.55Sn0.40Ti0.05)0.98O3 | AFE | 700 | 39 | 1.0 | 62 | 38 |
| Pb0.88Ca0.12ZrO3 | AFE | 300 | 50 | 2.8 | 83 | 33 |
| (Pseudo-)binary HfO2/ZrO2-based |  |  |  |  |  |  |
| Si:Hf0.5Zr0.5O2 | AFE | 10 | >50 | 4 | >80 | 71 |
| Si:HfO2 | AFE | 10 | 61.2 | 4.5 | 65 | 68 |
| ZrO2 | AFE | 9.6 | 37 | ~4 | 51 | 67 |
| Al2O3:HfO2/ZrO2 | FE | 7 | 54.3 | 5 | 51.3 | 24 |
| Ta2O5/Hf0.5Zr0.5O2 | FE | 25 | >100 | ~7 | >95 | 82 |

Table 1: Highest performance data exemplars for dielectric energy storage systems of different materials, including the bulky BOPP, perovskite relaxor ferroelectric (RFE) and antiferroelectric (AFE) thin films, and ferroelectric (FE) and AFE HfO2 and ZrO2-based thin films. ESD =energy storage density; EBD = dielectric breakdown field.

Polymer based dielectrics

Polymer based dielectrics are attractive for capacitor applications, in particular because of they are flexible. Recent developments on polymer based capacitors and strategies implemented to enhance their performance are reported in several papers.6-8 The best-performing commercial dielectric capacitor is BOPP, which has an ESD of <5 J cm−3.9-11 In order to achieve desirable ESD, a large capacitor bank with many rolls of the polymer film is usually employed. A strategy for improving the performance of BOPP is the incorporation of ferroelectric ceramic nanoparticles in the polymer matrix to achieve higher energy density with lower dielectric loss and great flexibility.12,13 Challenges for these composites include improving interfaces between the different materials for enhancing the exchange coupling,12,14,15  and creating  hierarchical nanocomposites.14 Even with extensive investigations, BOPP nanocomposites still exhibit insufficient ES response with ESD of ≤20 J cm−3 and efficiencies of <80%. In addition, the ES performance of the BOPP capacitor is limited by the low maximum operating temperature, which is typically below 160 0C.16 For example, with an operating temperature of 105 oC in a hybrid-electric vehicle (HEV), a cooling system is needed, bringing an extra weight, volume, and complexity in the design of power systems.9-11

Perovskite ferroics

Materials with more promising advantages than BOPP in terms of ESD are non-linear dielectrics in the form of ferroelectrics (FE), relaxor ferroelectrics (RFE), and antiferroelectrics (AFE). These materials have spontaneous polarization Ps and higher dielectric permittivities (K) than linear dielectric (LD) capacitors, and they can work both as DC and AC devices.17 However, ESD in FE is compromised by large hysteresis loss and the thickness-dependent EBD, which limit their application. Also, the robustness of FE polarization in conventional FE materials at the nanoscale is a big challenge due to the presence of a critical thickness (or dead layer) effect. This is limiting for energy storage in miniaturized electronic devices.

- Relaxor ferroelectrics (RFEs): RFE materials are more advantageous over FE in that they display weak temperature dependence with ultra-slim P-E hysteresis loops, which enable high energy recovery upon voltage cycling. They have the merits of synergistically exhibiting large Pm and small hysteresis loss and thus have strong potential for next-generation ES capacitors.18 Different strategies have been adopted to improve the ES performance of RFEs, typically such as doping, microstructure tailoring, use of  semiconductor/relaxor 0-3 type composite, local random field strategy, nanodomain engineering, layer-by-layer engineering, and implementation of multi-layered capacitors.1,19,20 One of the most attractive RFE material classes for ES applications is Pb-based perovskite dielectrics, including PbTiO3, PbZrO3 and Pb(Mg1/3Nb2/3)O3 due to ultrahigh Pm  (~ 80 μC cm-2).21

However, since Pb is toxic, wide-ranging practical applications are unlikely to emerge owing to the ever-increasing environmental concerns. On the other hand, Pb-free perovskite ceramics such as Bi0.5Na0.5TiO3-based relaxors, and BaTiO3 (BTO) -based systems show promise, although their ESD values are low than <2.5 J cm−3, owing to large Pr and/or small EBD.22,23 Recently, weakly coupled relaxor Pb-free FE of BTO-Bi(M)O3 (M is single trivalent cation or two cations with an average of + 3 valence) show ESD and efficiency values of >10 J cm−3 and ~90%, respectively.24-26 RFE thin films usually exhibit significantly higher ES performance than RFE ceramics due to their high EBD and so different strategies have been employed to enhance the ES performance of lead-free RFE thin films.10,21,25

In this context, RFE films of 0.25BiFeO3-0.3BaTiO3-0.45SrTiO3 and Ba(Zr0.2Ti0.8)O3 can exhibit ESD and efficiency values of >110 J cm−3 and ~80-90%, as shown in Table 1.27-31 This is attributed to the elimination of the macroscopic domain walls and the formation of polymorphic nanodomains. The highest ES performance in RFE films was achieved for films with a thickness of ≥350 nm, which limits the miniaturization of the devices. We note that Ps is significantly suppressed for perovskite FE films of <∼4 nm thickness, owing to the dead layer effect.32

b) Antiferroelctrics (AFEs): AFEs such as AgNbO3-based and PbZrO3-based systems are also promising candidates for high-performance energy storage. A field-induced AFE-FE transition results in a high Pm and low Pr and composition tuning greatly reduces the hysteresis loss and improves the EBD.33,34 ESD values of >6 J cm−3  (>10 J cm-3) and efficiencies of ~90% (90%) have been achieved at fields of >300 kV cm−1 (400 kV cm-1) for AgNbO3-based (PbZrO3-based) systems.35-37 Again, the ES performance of these ceramics is <20 J cm-3, limits their application.

In the case of AFE thin films, as shown in Table 1, ESD values of >50 J cm−3  (>39 J cm-3) and efficiencies of ~83% (62%) have been obtained at fields of >2800 kV cm−1 (988 kV cm-1) for Pb1-xCaxZrO3 (bilayer-like Pb0.99Nb0.02(Zr0.55Sn0.40Ti0.05)0.98O3) thin films.33,38 On the other hand, it was theoretically demonstrated that Bi1-xRxFeO3 systems (R being a lanthanide) can potentially allow high energy densities (100–150 J cm−3) with an efficiency of ~80% for electric fields in the range 2–3 MV cm−1, but still there is no experimental evidence of this performance.34 Overall, it can be concluded that RFE films exhibit higher ES performance when compared to AFE ones. However, perovskite-based FE films usually experience a large internal stress under flexure, which limits their application in flexible ES devices. Furthermore, perovskite thin films typically need to be grown above 600°C and they also suffer leakage problems.

For more detailed reviews on complex oxide FE materials, especially perovskites for ES and strategies implemented to enhance their performance, we recommend several papers.1,2,19,20,25

HfO2 and ZrO2-based materials

Binary oxides based on HfO2 and ZrO2 systems are much less complex in terms of composition than the aforementioned dielectric materials and they can also exhibit ferroelectricity. We bear in mind the important challenges of the current systems, namely the need to improve ESD, the need to increase the working temperature, and the need to reduce the size, weight, and cost of the capacitor structures for cutting-edge pulse power technologies.

As already mentioned, the strong interest in FE HfO2 and ZrO2 and HfxZr1-xO2 (HZO) systems stems from their compatibility of with complementary metal oxide semiconductor (CMOS) technology. Critically, the scalable industry method, atomic layer deposition (ALD) is suitable for fabricating high-quality films of these (pseudo-)binary systems, as well as 3D structured nanoscale capacitors,39 at as low as 400 oC.40,41 It should also be mentioned that ALD has severe limitations for growth of complex perovskite dielectrics, in particular high post-annealing deposition temperatures of >600 oC are typically required.42,43

Table 1 shows that even after a short period of research FE (pseudo-)binary thin films comprised of HfO2 and ZrO2 have higher ES performance than other RFE and AFE thin films and BOPP. However, to compete with optimal RFE thin films (of Ba(Zr0.2Ti0.8)O3), more work is still needed to simultaneously optimize ESD and efficiency.

The field of ES capacitors based on (pseudo-)binary HfO2 and ZrO2 thin films is growing quite rapidly. Recently, F. Ali et al. reviewed the polarization behavior and ES properties of these materials, including the influences of doping, temperature, electric field, and the creation of negative-capacitance (NC) electrostatic capacitors by interfacing dielectric layers with the HfO2 and ZrO2 thin films.44 In addition, the ESD values of FE and AFE (pseudo-)binary HfO2 and ZrO2 thin films were compared with other composition systems, including linear dielectrics, paraelectrics, FEs, RFEs and AFEs.

This focus review provides additional insight to this important field: it first analyses how and why, in comparison to standard perovksite ferroic and polymeric materials systems, FE and AFE HfO2 and ZrO2-based thin films are attractive for ES applications. It also considers the methods currently being explored to enhance the FE and ES performance to meet real-world applications, e.g. doping, strain, orientation and dead-layer engineering to tune Pm and Pr and consequently enhance the ES performance of FE HfO2 and ZrO2-based thin films. New ways of thinking are then presented towards enhancing the ES performance of these materials. Different strategies towards achieving enhanced ES performance such as defect, strain, orientation and multilayer engineering are proposed. The readers attention is then called to the fact that good FE performance can be achieved even at thicknesses as low as ~1 nm, which is advantageous for device miniaturization.

Different strategies that can be used to achieve wake-up free FE behavior in orthorhombic HfO2 and ZrO2-based thin films are discussed and the importance of performing further ES studies on rhombohedral phase ZrO2 and HZO films, where it appears there is no wake-up effect, are noted. Also, the importance of investigating and optimizing FE and ES performance at temperatures above 150°C is stressed in order to achieve adequate capacitor performance in the automotive, power transmission, aerospace and oil and gas industries. New ways for achieving such improved higher temperature performance are proposed. Finally, the importance of measurement protocols for cross-comparing data from different groups and for the implementation of materials in real time device applications is stressed, and the need to undertake measurements up to high frequencies is noted. Overall, in terms of improved properties and easier processing, the excellent prospects of HfO2 and ZrO2-based thin films for wide-ranging ES applications compared to perovskite RFE and AFE films are revealed.

- Origin of ferroelectricity in HfO2 and ZrO2-based thin films: The discovery of ferroelectricity in doped HfO2 in 2011 was originally unexpected because its phase diagram shows only centrosymmetric crystal structures.45,46 Yet, the FE phase in doped and undoped HfO2, ZrO2 and HZO is accepted as the metastable orthorhombic phase with non-centrosymmetric space group Pca21,47 in which a relative displacement of O from the center of Hf tetrahedron is seen. The orthorhombic phase is believed to be transformed from a high-temperature tetragonal phase due to its structure similarity and close lattice parameters. The orthorhombic phase is stabilized by a series of effects, including doping, strain, capping layer, oxygen vacancies, thermal expansion mismatch, surface energy, etc.20,45,48 However, the aforementioned parameters are often coupled (e.g. strain and oxygen vacancies) and so future work will require careful decoupling of these parameters. Recently, a polar rhombohedral phase was also reported in ZrO2 and Hf0.5Zr0.5O2 thin films.49-52 There is promise also for HfO2 and ZrO2 materials in non-volatile memory, multiferroics, FE tunnel junctions, and field effect transistors.53-58 However, there is limited work on energy storage capacitors. Thus we focus the rest of this review on the current status and prospects of using HfO2, ZrO2 and HZO in ES capacitors.

b) Performance Attributes of HfO2 and ZrO2-based materials: As already mentioned, a material with low Ec, high Pm, low Pr, large EBD and slim hysteresis is imperative to obtain superior ES performance. In this context, owing to their large bandgaps of >5 eV and large conduction band offset when contacting with Nitride-based electrodes,47,50 HfO2, ZrO2 and HZO FE thin films exhibit ultralow leakage current. This means the EBD is very high, up to ∼5 MV cm-1, which is superior to the values (typically < 4 MV cm-1)17, for perovskite-based FE films. In addition, a Pm up to ∼50 µC cm−2 can be achieved in polycrystalline HZO films, while the Pr can be tuned from ∼5 up to ∼30 µC cm−2, by adjusting the thickness of the HZO film.57 HfO2 and ZrO2-based FEs also resist polarization degradation during annealing. The degradation is less than in conventional perovskite-based FEs, due to the strong Hf-O and Zr-O bonds.58 Moreover, stemming from the higher Ecs (1-5 MV cm-1)42,50 these (pseudo-) binary materials offer the dual advantage of enabling a higher gate length scaling in FE field effect transistors, while also providing a high resilience toward internal depolarization of the FE.59  We note that achieving  low switching voltages is crucial not only for memory applications,60 but also for ES devices.

Additional positive attributes of HfO2 and ZrO2 films is that they exhibit fast FE switching times in the ns range.49 Furthermore, Hf0.8Zr0.2O2 films exhibit good FE performance even at thicknesses as low as ~1 nm,61 which is not the case for conventional perovskite-based FE films where interfacial dead layers kill the FE effect. From a technological point-of-view, direct monolithic integration of ultrathin doped HfO2 on silicon paves the way for polarization-driven low-power memories and ultra-scaled FE-based transistors.61 A reduction in the required space occupied by the ES material is also necessary to enable the design of nanocapacitors for applications in miniaturized energy-autonomous systems, e.g. electric vehicles. As already mentioned, a large capacitor bank with many rolls of the polymer film is usually employed for achieve high ESD but this is disadvantageous in terms of space minimization.  Hence, the ability to grow pseudo- binary oxide thin films with strong performance is highly beneficial for miniaturized devices.

Reliable FE performance up to 150°C has also been achieved in flexible Hf0.6Zr0.4O2 films62. This therefore makes this material attractive for flexible ES capacitors. In fact, conferring flexibility to electronics can dramatically enhance applications for the emerging Internet of Things fields.63 Thus, the integration of capacitors in flexible devices has become one of the most important trends in the development of the next-generation ES devices.64,65 The ability to grow at as low as 400°C is highly beneficial for growth on flexible substrates.66 More developments of these (pseudo-)binary FEs on flexible substrates is highly anticipated in future and is an important field of future research. Challenges will likely be in growth without a need for any rapid thermal annealing steps, and ability to create reproducible behavior.

c) AFE HfO2 and ZrO2-based materials:  Besides the aforementioned advantages of FE HfO2 and ZrO2-based thin films, AFE films have begun to be investigated for ES with promising results. Pešić and co-workers have shown that the ESD of 37 J cm-3 with an efficiency of 51% could be achieved with AFE ZrO2 films in a planar configuration.67 It was also demonstrated that Al and Si doped HfO2 film capacitors exhibited an ESD of <65 J cm-3 with an efficiency of  ≤80%. 44,68-70 AFE doped HfO2 thin films exhibit higher ES performance than ZrO2 films, although the large annealing temperature (~1000oC) is undesirable for integrated applications.71 In this sense, HZO materials are particularly interesting for the applications due to its low annealing temperature, robustness to H-annealing and fully miscible compositional range.71

Following this trend, the ES performance of AFE HZO films has also been tuned by controlling the composition of HZO. In this work, a 46 J cm−3 energy storage density with 51% efficiency could be achieved in a Hf0.3Zr0.7O2 film.72

Moreover, an AFE Hf0.5Zr0.5O2 film has been found to show a thickness dependent ESD performance, as shown in Figure 1. The 7.1 nm-thick Hf0.5Zr0.5O2 film displays an ESD of 55 J cm-3 with an efficiency of ∼60%, which can be cycled up to 1010 times while maintaining an energy storage density of ∼40 J cm-3.73

Figure 1. Ferroelectric behaviour and energy storage performance of  Hf0.5Zr0.5O2 thin films capacitors. (a) Polarization-electric field curves for films with different thickness. (b) Energy storage density and efficiency as a function of the film thickness. Reprinted from Ref. 73, with permission from Elsevier.

Si-doped Hf0.5Zr0.5O2 thin films have been found to give an ESD of nearly 50 J cm-3 with an efficiency of over 80%, as shown in Figure 2. Moreover, these Si-doped Hf0.5Zr0.5O2 thin films have been cycled 109 times at up to 125 °C and maintained a robust ESD of 35  J cm-3 and efficiency of greater than 80%.71 It is worth mentioning that (pseudo-)binary oxide thin film capacitors exhibit a higher working temperature when compared to commercial BOPP (∼105 ºC),11 and therefore the need for a secondary cooling system can be removed in wind pitch control devices (which operate at ~125 ºC).16 However, the annealing temperature required to make Si-doped Hf0.5Zr0.5O2 thin films have strong performance is still too high (900oC) for their integration in applications.

Figure 2. Ferroelectric behaviour and energy storage performance of Si-doped Hf0.5Zr0.5O2 thin films capacitors.  (a) Polarization-electric field hysteresis curves under electric field cycling. (b) Energy storage density and efficiency as a function of electric field. Reprinted from Ref. 71, with the permission of AIP Publishing.

d) FE HfO2 and ZrO2-based thin films: Even though AFE HfO2 and ZrO2 film capacitors have mainly been investigated for ES, FE films could be more advantageous for improved ES devices since they can exhibit several advantages, as already discussed, namely high Ps, low Pr, robust FE even at 1 nm thickness and low annealing temperature (400 oC). To the best of our knowledge, these materials only started to be investigated for ES capacitors in 2018. Therefore, more detailed investigations exploring the aforementioned advantages of FE HfO2 and ZrO2 should be conducted in order to optimize their performance for potentially very high-performance ES devices.

Progress since 2018 includes work which has shown in 2% La-doped Hf0.5Zr0.5O2-based thin film capacitors a transition from FE to AFE-like behavior, accompanied by a significant increase of energy storage density value and efficiency.74 ESD values of >40 J cm-3 were achieved with an efficiency of 70%, as shown in Figure 3.

Figure 3. Ferroelectric behaviour and energy storage performance of La:Hf0.5Zr0.5O2-based thin film capacitors. (a) Polarization-electric field hysteresis loops with different La contents. (b) ESD and efficiency as a function of La content. The inset shows the dielectric permittivity (K) as a function of La content. Reprinted from Ref. 74, with the permission of AIP Publishing.

More interestingly, a further increase of efficiency to ~80% along with a decrease of the hysteresis was noticed as the film underwent 109 electric field cycles. The efficiency improvement was attributed to charged defects redistribution across the dielectric film, consequent change in the local domain environment, and phase transitions near the AFE/electrode interfaces.74

Challenges, Potential Solutions and Future Opportunities for FE HfO2 and ZrO2-based materials

HfO2 and ZrO2-based materials are still far away from ES applications requirements, and to meet these applications. To compete with optimal RFE thin films of 0.25BiFeO3-0.3BaTiO3-0.45SrTiO3 and Ba(Zr0.2Ti0.8)O3,27,29 it will be necessary to increase ESD by ~50% to ~150 J cm-3, while keeping an efficiency of ~95%. It will also be important to decrease the annealing temperature of AFE thin films. The way to achieve these aims is by defect engineering of films via a variety of means, e.g. ion bombardment, using doping additives, or via careful process control, in particular the effect of oxygen partial pressure (PO2) and substrate temperature during growth and post-annealing conditions, such as temperature and environment (air, N2, Ar, O2).

Ion bombardment has been shown to be an efficient way to improving the ESD of RFE films75 and therefore, we believe this could be an important area for future research in the ES field of (pseudo-)binary FE HfO2 and ZrO2-based thin films. There are many factors reported so far to affect the FE orthorhombic-phase in ZrO2 and HfO2-based films, such as composition, thickness, surface energy effect, thermal expansion mismatch, capping layer effect and forming of defects (e.g., oxygen vacancies).48 This also offers rich opportunities for ES performance optimization. The modification of composition and thickness of HfO2 and ZrO2-based thin films is an efficient way to tune the polarization behavior and hence its impact on the ES performance should be evaluated. Moreover, strain and orientation engineering by choosing the appropriate substrate offers a unique opportunity to stabilize the FE phase in these materials to control the FE and ES performance. Also, multilayered thin films should be investigated since the interfaces in them acts as media to generate space charges that serve as traps for injected electrons from the metal electrodes under the application of a high electric field. This is another route to improving the polarization and thus ES performance.

One important challenge for orthorhombic HfO2 and ZrO2-based thin films is the need for a wake-up effect before FE switching is obtained. Hence an initial pre-cycling is needed to induce FE behavior, but this is technologically inconvenient. Several different strategies have been used to overcome the wake-up problem, such as La-doping, NH3 plasma treatment and ozone dosage during atomic layer deposition of films.76-79 On the other hand, the rhombohedral phases of ZrO2 and HZO films are typically FE without the need for any wake-up cycling and thus rhombohedral structures are currently more interesting for ES capacitor applications.

Recently, the insertion of a thin Al2O3:HfO2 (HAO) dielectric layer was shown to modify the FE properties by increasing the depolarization field which leads to the increase of Pm - Pr value and in doing so enhance the ES performance of ZrO2 film capacitors, as shown in Figure 4.24 An optimum combination of high ESD of 54.3 J cm-3 and good storage efficiency of 51.3% was obtained for the ZrO2 film capacitors with a 2 nm-thick HAO insert layer. These values correspond to an increase of ~ 55% and ~ 92%, from the respective values of pure ZrO2 film capacitors.24 The inclusion of a thin dielectric layer also proved to be useful to modify the FE behavior of Hf0.5Zr0.5O2/Al2O3 capacitors. On the other hand, the ES performance has not yet been evaluated.80 In addition, a dead-layer engineering approach has also proven to be useful for enhancing the ES performance of RFE thin film capacitors.28,31

Figure 4. Ferroelectric behaviour and energy storage performance of  ZrO2 and ZrO2/ HAO film capacitors. (a) Polarization-electric field hysteresis loops. (b) Variation of Pmax-Pr, energy storage and efficiency () with change in the HAO layer thickness. Reprinted from Ref. 24 with permission from The Royal Society of Chemistry.

Also, recently it was also shown that the ESD and efficiency of TiN/HfxZr1-xO2/TiN capacitors with x = 0.25, 0.33 and 0.50, can be improved with the insertion of an Al2O3 interlayer in the middle of the HZO layer. By introducing a 1 Å thick Al2O3 interlayer in a TiN/HZO/TiN capacitor with x = 0.33, the ESD and efficiency were optimized up to ~55 J cm -3 and ~68%, respectively, with a robust thermal stability up to 200 ºC. These values corresponds to ~35% and ~55% enhancements when compared to the capacitor without the interlayer.81 The origin of the improvements is believed to be the inclusion of the Al2O3 interlayer that controls the grain size of the HZO film resulting in lower energy dissipation by controlling the linearity of the hysteresis loop.

A new concept of negative-capacitance (NC) has also been proposed to increase ESD. This can be achieved by combining, in a single structure, a FE layer of Hf0.5Zr0.5O2 having a NC, with a linear-dielectric layer (e.g., Al2O3 and Ta2O5) having a positive capacitance. This results in nonlinear charge–voltage characteristics with enhanced ES performance. In this case, a giant ESD of >100 J cm-3 has been demonstrated82, which is the highest ESD of all the state-of-the-art (pseudo-)binary FE HfO2 and ZrO2-based thin film capacitors, as shown in Figure 5. It is observed that combining FE films with dielectric layers gives rise to significantly enhanced ES performances over standard AFE films. This is a very exciting result and there is much scope for further optimization by exploring different dielectric materials, such as SiO2 and HfO2. The selection of the proper architecture of the device by placing the dielectric layer between the FE layer and the top/bottom electrode or even between two FE layers needs to be studied in more detail in the future.

We predict that (pseudo-)binary FE HfO2 and ZrO2-based thin films should be combined with AFE ones to boost the ES performance. This approach will benefit from the advantages of each individual layer, similar to the one already observed in RFE/AFE perovskite ceramics and thin films.83,84

Figure 5. Comparison of the ES performance obtained in AFE and FE HfO2 and ZrO2-based films.

Also, 3D capacitors should be explored in more detail since they allow much higher ESD when compared to the 2D ones. 3D nanostructured capacitors are made using nanoporous templates into which thin films of metals and insulators are deposited. Enhancements from 37 J cm-3 up to 937 J cm-3 per projected 2D capacitor area have been obtained in a 3D capacitor based on ZrO2 films.67

While, as mentioned earlier, stable FE performance in (pseudo-)binary oxide thin films has been shown up to 150 ºC in flexible Hf0.6Zr0.4O2 thin films62, and the ES performance of TiN/Hf0.33Zr0.66O2/Al2O3/Hf0.33Zr0.66O2/TiN capacitors is thermally stable up to 200 ºC,81 it is imperative to also achieve strong ES performance in the range 150-250 °C. In this way, it will be possible to meet the requirements of the automotive (150–200 ºC), power transmission (150–250 ºC), aerospace (180-250 ºC) and oil and gas industries (175-250 ºC).16 Since the ferroelectric Curie temperature (Tc) of these materials is up to 450 ºC,85  there are strong possibilities to reach these higher temperature operation targets. In the perovskite systems, 3D straining approaches and careful compositional tuning have led to the aforementioed property improvements.86 This success could potentially also be also translated to the HfO2 and ZrO2-based systems.

As an aside, we stress the importance of measurement protocols for cross-comparing data from different groups, as well as for carefully assessing whether a particular material is well matched to a given application. Hence, we invoke using transient methods for evaluating energy storage performance, since the ESD value obtained using quasi-static methods, where the P-E loop is measured at lower frequency (few hundred Hz), is usually larger than the ones obtained from transient methods where measurements are done at ultrahigh frequencies (MHz).87,88 We also invoke that charge/discharge speed needs to be investigated in ES capacitors, since this allows important information to be obtained regarding the application of ES capacitors. Also, performance of capacitors at a range of frequencies is necessary since many applications are at high frequencies, e.g., high-frequency inverters. The different loss mechanisms operating at the different frequencies also need to be elucidated.

Finally for HfO2 and ZrO2-based thin films, if there is success in improving the ESD by ~50% while maintaining a very high efficiency (~95%), using a variety of materials engineering approaches, e.g. strain, orientation and dead-layer control, as well as judicious multilayering, there is much promise for the aforementioned applications in electric vehicles, IoT applications, medical equipment, etc.

In conclusion, while the discovery of ferroelectricity in HfO2 and ZrO2-based thin films has revolutionized the research in the FE field, the impact of these materials in energy storage capacitors is still incipient. Promisingly, there are many possibilities for engineering these simple binary materials to achieving high-performance ES capacitors for a wide range of devices where the need for low-weight, small-size and fast-discharge energy storage devices is critical, e.g., in electric vehicles and beyond.

Author biographies

Dr. José Pedro Basto da Silva is a junior researcher at Centre of Physics of University of Minho and Porto (CF-UM-UP). His current research interests focuses on understanding the relationship between structure and functionality of ferroelectric oxide thin films for memory and energy storage applications.

https://www.cf-um-up.pt/index.php/people/minho-university/effective-members/10-team/153-jose-pedro-basto-da-silva

Dr. Koppole Chandra Sekhar is working as UGC-Assistant Professor at department of physics, Central University of Tamil Nadu; Thiruvarur since 2015. He has contributed around 60 journal articles and his current h-index is 17. His research interests focuses on ferroelectric- semiconductor heterostructures for memory, energy, environmental and photovoltaic applications.

https://cutn.ac.in/teams/k-chandra-sekhar/

Dr. Hao Pan is a research fellow at School of Physical and Mathematical Science, Nanyang Technological University, Singapore. He received his Ph.D. degree in Materials Science and Engineering from Tsinghua University, China, in 2020. He worked as a visiting scholar in Department of Materials Science and Metallurgy, University of Cambridge, in 2019. His research focuses on functional complex oxide films, dielectrics and ferroelectrics for energy storage and conversion.

# Prof. Judith MacManus-Driscoll is a Professor in the Materials Science at the University of Cambridge. She is also Royal Academy of Engineering Chair in Emerging Technologies. She is fellow of IOP, IOM3, WES, APS, MRS, and the Royal Academy of Engineering.  He research work is in the area of oxide thin film engineering for low power electronic and energy devices. She is interested in both understanding of basic functionalities and in engineering new interfacial-driven properties. For this purpose, she designs, fabricates and analyses novel nanostructured films. https://driscoll.msm.cam.ac.uk

Dr. Mario Pereira is Assistant Professor at the Physics Department (University of Minho-Portugal). He received his Ph. D in Ceramic Materials Science in 1994 (University of Limoges - France). His main research interest is the production of ferroelectric thin films for the development of new smart Materials as Memories, Batteries…

Acknowledgements

This work was supported by the Portuguese Foundation for Science and Technology (FCT) in the framework of the Strategic Funding Contract UIDB/04650/2020 and by DST-SERB, Govt. of India through Grant Nr. ECR/2017/00006.  J.L.M.-D. thanks the Royal Academy of Engineering, grant CIET 1819 24. H.P. thanks the China Scholarship Council (No. 201806210299).

References

(1) Palneedi, H.; Peddigari, M.; Upadhyay, A.; Silva, J. P. B.; Hwang, G.-T.; Ryu, J. (2020). “Lead-based and lead-free ferroelectric ceramic capacitors for electrical energy storage” in Ferroelectric Materials for Energy Harvesting and Storage (Woodhead Publishing, Elsevier) (https://doi.org/10.1016/B978-0-08-102802-5.00009-1).

(2) Palneedi, H.; Peddigari, M; Hwang, G.-T.; Jeong, D.-Y.; Ryu, J. High‐performance dielectric ceramic films for energy storage capacitors: progress and outlook. Adv. Funct. Mater. 2018, 28, No. 1803665.

# (3) Meng, N.; Ren, X.; Santagiuliana, G.; Ventura, L.; Zhang, H.; Wu, J.; Yan, H.; Reece, M. J.; Bilotti, E. Ultrahigh β-phase content poly(vinylidene fluoride) with relaxor-like ferroelectricity for high energy density capacitors. Nat. Commun. 2019, 10, No. 4535.

(4) Li, Q.; Chen, J.; Fan, L.; Kong, X.; Lu, Y. Progress in electrolytes for rechargeable Li-based batteries and beyond. Green Energy Environ. 2016, 1, 18-42.

(5) Zhang, Y.; Jiang, J.; An, Y.; Wu, L.; Dou, H.; Zhang, J.; Zhang, Y.; Wu, S.; Dong, M.; Zhang, X.; Guo, Z. Sodium-ion capacitors: materials, mechanism, and challenges. ChemSusChem 2020, 13, 2522-2539.

(6) Jiang, Y.; Zhou, M.; Shen, Z.; Zhang, X.; Pan, H.; Lin, Y.-H. Ferroelectric polymers and their nanocomposites for dielectric energy storage applications. APL Materials 2021, 9, No. 020905.

(7) Prateek; Thakur, V. K.; Gupta, R. K. Recent progress on ferroelectric polymer-based nanocomposites for high energy density capacitors: synthesis, dielectric properties, and future aspects. Chem. Rev. 2016, 116, 4260–4317.

(8) Hu, X.; Yi, K.; Liu, J.; Chu, B. High energy density dielectrics based on PVDF‐based polymers. En. Techn. 2018, 6, 849-864.

(9) Xiong, J.; Wang, X.; Zhang, X.; Xie, Y.; Lu, J.; Zhang, Z. How the biaxially stretching mode influence dielectric and energy storage properties of polypropylene films. J. Appl. Polym. Sci. 2021, 138, No. 50029.

(10) Xu, X.; Liu, W.; Li, Y.; Wang, Y.; Yuan, Q.; Chen, J.; Ma, R.; Xiang, F.; Wang, H. Flexible mica films for high-temperature energy storage. J. Materiomics 2018, 4, 173-178.

(11) Li, Q.; Yao, F.-Z.; Liu, Y.; Zhang, G.; Wang, H.; Wang, Q. High-temperature dielectric materials for electrical energy storage. Annu. Rev. Mater. Res. 2018, 48, 219–243.

(12) Luo, S.; Yu, J.; Yu, S.; Sun, R.; Cao, L.; Liao, W.-H.; Wong, C.-P. Significantly enhanced electrostatic energy storage performance of flexible polymer composites by introducing highly insulating‐ferroelectric microhybrids as fillers. Adv. Energy Mater. 2019, 9, No. 1803204.

(13) Li, H.; Ai, D.; Ren, L.; Yao, B.; Han, Z.; Shen, Z.; Wang, J.; Chen, L.-Q.; Wang, Q. Scalable polymer nanocomposites with record high‐temperature capacitive performance enabled by rationally designed nanostructured inorganic fillers. Adv. Mater. 2019, 31, No. 1900875.

(14) Luo, B.; Shen, Z.; Cai, Z.; Tian, E.; Yao, Y.; Li, B.; Kursumovic, A.; MacManus‐Driscoll, J. L.; Li, L.; Chen, L.-Q.; Wang, X. Superhierarchical inorganic/organic nanocomposites exhibiting simultaneous ultrahigh dielectric energy

(15) Zhang, X.; Shen, Y.; Xu, B.; Zhang, Q.; Gu, L.; Jiang, J.; Ma, J.; Lin, Y.; Nan, C.-W. Giant energy density and improved discharge efficiency of solution-processed polymer nanocomposites for dielectric energy storage. Adv. Mater. 2016, 28, No. 2055.

(16) Hassan, Y. A.; Hu, H. Current status of polymer nanocomposite dielectrics for high-temperature applications. Composites Part A Appl. Sci. Manufact. 2020, 138, No. 106064.

(17) Kursumovic, A.; Li, W.-W., Cho, S.; Curran, P. J.; Tjhe, D. H. L.; MacManus-Driscoll, J. L. Lead-free relaxor thin films with huge energy density and low loss for high temperature applications, Nano Energy 2020, 71, No. 104536.

(18) Zhao, P.; Wang, H.; Wu, L.; Chen, L.; Cai, Z.; Li, L.; Wang, X. High‐performance relaxor ferroelectric materials for energy storage applications. Adv. Energy Mater. 2019, 9, No. 1803048.

(19) Sun, Z.; Wang, Z.; Tian, Y.; Wang, G.; Wang, W.; Yang, M.; Wang, X.; Zhang, F.; Pu, Y. Progress, outlook, and challenges in lead‐free energy‐storage ferroelectrics, Adv. Electron. Mater. 2020, 6, No. 1900698.

(20) Yang, L.; Kong, X.; Li, F.; Hao, H.; Cheng, Z.; Liu, H.; Li, J. F.; Zhang, S. Perovskite lead-free dielectrics for energy storage applications, Prog. Mater. Sci. 2019, 102, 72-108.

(21) Kim, J.; Saremi, S.; Acharya, M.; Velarde, G.; Parsonnet, E.; Donahue, P.; Qualls, A.; Garcia, D.; Martin, L. W. Ultrahigh capacitive energy density in ion-bombarded relaxor ferroelectric films, Science 2020, 369 81-84.

(22) Lin, Y.; Li, D.; Zhang, M.; Zhan, S.; Yang, Y.; Yang, H.; Yuan Q. Excellent energy-storage properties achieved in BaTiO3-based lead-free relaxor ferroelectric ceramics via domain engineering on the nanoscale. ACS Appl. Mater. Interfaces 2019, 11, 36824–36830.

(23) Liu, X. Y.; Yang, H. B.; Yan, F.; Qin, Y.; Lin, Y.; Wang, T. Enhanced energy storage properties of BaTiO3-Bi0.5Na0.5TiO3 lead-free ceramics modified by SrY0.5Nb0.5O3. J. Alloys Compd. 2019, 778, 97−104.

(24) Silva, J. P. B.; Silva, J. M. B.; Sekhar, K. C.; Palneedi, H.; Istrate, M. C.; Negrea, R. F.; Ghica, C.; Chahboun, A.; Pereira, M.; Gomes, M. J. M., Energy storage performance of ferroelectric ZrO2 film capacitors: effect of HfO2:Al2O3 dielectric insert layer, J. Mater. Chem. A 2020, 8, 14171-14177.

(25) Pan, H.; Kursumovic, A.; Lin, Y.-H.; Nan, C.-W.; MacManus-Driscoll, J. L. Dielectric films for high performance capacitive energy storage: multiscale engineering, Nanoscale 2020, 12, 19582-19591.

(26) Hu, Q.; Tian, Y.; Zhu, Q.; Bian, J.; Jin, L.; Du, H.; Alikin, D. O.; Shur, V. Y.; Feng, Y.; Xu, Z.; Wei, X. Achieve ultrahigh energy storage performance in BaTiO3–Bi(Mg1/2Ti1/2)O3 relaxor ferroelectric ceramics via nano-scale polarization mismatch and reconstruction. Nano Energy 2020, 67, No.104264.

(27) Pan, H.; Li, F.; Liu, Y.; Zhang, Q; Wang, M.; Lan, S.; Zheng, Y.; Ma, J.; Gu, L.; Shen, Y.; Yu, P.; Zhang, S.; Chen, L.-Q.; Lin, Y.-H.; Nan, C.-W. Ultrahigh–energy density lead-free dielectric films via polymorphic nanodomain design, Science, 2019, 365, 578-582.

(28) Silva, J. P. B.; Silva, J. M. B.; Oliveira, M. J. S.; Weingärtner, T.; Sekhar, K. C.; Pereira, M.; Gomes, M. J. M. High‐performance ferroelectric–dielectric multilayered thin films for energy storage capacitors, Adv. Funct. Mater. 2019, 29, No. 1807196.

(29) Cheng, H.; Ouyang, J.; Zhang, Y.-X.; Ascienzo, D.; Li, Y.; Zhao Y.-Y.; Ren, Y. Demonstration of ultra-high recyclable energy densities in domain-engineered ferroelectric films Nat. Commun. 2017, 8, No. 1999.

(30) Wu, S.; Xu, L.; Zhu, K.; Song, B.; Yan, H.; Shen, B.; Zhai, J. Improved piezoelectricity and energy storage performance simultaneously achieved in [001]-preferentially oriented Bi0.50.5Na0.5TiO3–BaTiO3–BiMnO3 thin films grown on Nb-doped SrTiO3 single-crystalline substrates, J. Eur. Ceram. Soc. 2021, 41, 2539-2547.

(31) Zhang, T.; Li, W.; Zhao, Y.; Yu, Y.; Fei, W. High energy storage performance of opposite double‐heterojunction ferroelectricity–insulators, Adv. Funct. Mater. 2018, 28, No. 1706211.

(32) Gao, P.; Zhang, Z.; Li, M.; Ishikawa, R.; Feng, B.; Liu, H.-J.; Huang, Y.-L.; Shibata, N.; Ma, X.; Chen, S.; Zhang, J.; Liu, K.; Wang, E.-G.; Yu, D.; Liao, L.; Chu, Y.-H.; Ikuhara, Y. Possible absence of critical thickness and size effect in ultrathin perovskite ferroelectric films. Nat. Commun. 2017, 8, No. 15549.

(33) Li, Y. Z.; Wang, Z. J.; Bai, Y.; Zhang, Z. D. High energy storage performance in Ca-doped PbZrO3 antiferroelectric films. J. Eur. Ceram. Soc. 2019, 40, 1285–1292.

(34) Xu, B.; Iñiguez, J.; Bellaiche, L. Designing lead-free antiferroelectrics for energy storage, Nat. Commun. 2017, 8, No. 15682.

(35) Luo, N.; Han, K.; Cabral, M. J.; Liao, X.; Zhang, S.; Liao, C.; Zhang, G.; Chen, X.; Feng, Q.; Li, J.-F.; Wei, Y. Constructing phase boundary in AgNbO3 antiferroelectrics: pathway simultaneously achieving high energy density and efficiency. Nat Commun. 2020, 11, No. 4824.

(36) Lu, Z.; Bao, W.; Wang, G.; Sun, S.-K.; Li, L.; Li, J.; Yang, H.; Ji, H.; Feteira, A.; Li, D.; Xu, F.; Klepp, A. K.; Wang, D.; Liu, S.-Y.; Reaney, I. M. Mechanism of enhanced energy storage density in AgNbO3-based lead-free antiferroelectrics. Nano Energy 2021, 79, No. 105423.

(37) Wang, H.; Liu, Y.; Yang, T.; Zhang, S. Ultrahigh energy‐storage density in antiferroelectric ceramics with field‐induced multiphase transitions. Adv. Funct Mater. 2019, 29, No. 1807321.

(38) Shen, B.; Li, Y.; Sun, N.; Zhao, Y.; Hao, X. Enhanced energy-storage performance of an all-inorganic flexible bilayer-like antiferroelectric thin film via using electric field engineering. Nanoscale 2020, 12, 8958-8968.

(39) Park, M. H.; Lee, Y. H.; Mikolajick, T.; Schroeder, U.; Hwang, C. S. Review and perspective on ferroelectric HfO2-based thin films for memory applications. MRS Commun. 2018, 8, 795-808.

(40) Onaya, T.; Nabatame, T.; Sawamoto, N.; Ohi, A.; NaokiIkeda, Nagata, T.; Ogura, A. Ferroelectricity of HfxZr1-xO2 thin films fabricated by 300 °C low temperature process with plasma-enhanced atomic layer deposition. Microelectronic Engineering 2019, 215, No. 111013.

(41) Kim, S. J.; Mohan, J.; Lee, J.; Lee, J. S.; Lucero, A. T.; Young, C. D.; Colombo, L.;  Summerfelt, S. R.; San, T.; Kim, J. Effect of film thickness on the ferroelectric and dielectric properties of low-temperature (400 °C) Hf0.5Zr0.5O2 films. Appl. Phys. Lett. 2018, 112, 172902.

(42) Kim, S. J.; Mohan, J.; Summerfelt, S. R.; Kim, J. Ferroelectric Hf0.5Zr0.5O2 thin films: a review of recent advances JOM 2019, 71, 246-255.

(43) Coll, M.; Napari, M. Atomic layer deposition of functional multicomponent oxides. APL Materials 2019, 7, 110901.

(44) Ali, F.; Zhou, D., Ali, M., Ali, H. W.; Daaim, M.; Khan, S.; Hussain, M. M.; Sun, N. Recent progress on energy-related applications of HfO2-based ferroelectric and antiferroelectric materials, ACS Appl. Electron. Mater. 2020, 8, 2301–2317.

(45) Müller, J.; Schröder, U.; Böscke, T. S.; Müller, I.; Böttger, U.; Wilde, L.; Sundqvist, J.; Lemberger, M.; Kücher, P.; Mikolajick, T.; Frey, L. Ferroelectricity in yttrium-doped hafnium oxide, J. Appl. Phys. 2011, 110, 114113.

(46) Park, M. H.; Kim, H. J.; Lee, G.; Park, J.; Lee, Y. H.; Kim, Y. J.; Moon, T.; Kim, K. D; Hyun, S. D.; Park, H. W.; Chang, H. J.; Choi, J.-H.; Hwang, C. S. A comprehensive study on the mechanism of ferroelectric phase formation in hafnia-zirconia nanolaminates and superlattices, Appl. Phys. Rev. 2019, 6, 041403.

(47) Estandía, S.; Dix, N.; Chisholm, M. F.; Fina, I.; Sánchez, F. Domain-matching epitaxy of ferroelectric Hf0.5Zr00.5O2(111) on La2/3Sr1/3MnO3(001). Cryst. Growth Des. 2020, 20, 3801–3806.

(48) Fan, Z.; Chen, J.; Wang, J. Ferroelectric HfO2-based materials for next-generation ferroelectric memories, J. Adv. Dielectrics 2016, 06, No. 1630003.

(49) Silva J. P. B.; Negrea, R. F.; Istrate, M. C.; Dutta, S.; Aramberri, H.; Íñiguez, J.; Figueiras, F. G.; Ghica, C.; Sekhar, K.; Kholkin, A. K. Ferroelectricity in epitaxially strained rhombohedral ZrO2 thin films. arXiv:2011.02728

(50) Wei, Y.; Nukala, P.; Salverda, M.; Matzen, S.; Zhao, H. J.; Momand, J.; Everhardt, A. S.; Agnus, G.; Blake, G. R.; Lecoeur, P.; Kooi, B. J.; Íñiguez, J.; Dkhil, B.; Noheda, B. A rhombohedral ferroelectric phase in epitaxially strained Hf0.5Zr00.5O2 thin films, Nat. Mater. 2018, 17, 1095–1100.

(51) Bégon-Lours, L.; Mulder, M.; Nukala, P.; Graaf, S.; Birkhölzer, Y.; Kooi, B.; Noheda, B.; Koster, G.; Rijnders, G. Stabilization of phase-pure rhombohedral HfZrO4 in pulsed laser deposited thin films, Phys. Rev. Materials 2020, 4, No. 043401.

(52) Nukala, P.; Wei, Y.; Haas, V.; Guo, Q.; Antoja-Lleonart, J.; Noheda, B. Guidelines for the stabilization of a polar rhombohedral phase in epitaxial Hf0.5Zr0.5O2 thin films. Ferroelectrics 2020, 569, 148-163.

(53) Liu, W.-Y.; Liao, J.-J.; Jiang, J.; Zhou, Y.-C.; Chen, Q.; Mo, S.-T.; Yang, Q.; Peng, Q.-X.;Jiang, L.-M. Highly stable performance of flexible Hf0.6Zr0.4O2 ferroelectric thin films under multi-service conditions, J. Mater. Chem. C 2020, 8, 3878-3886.

(54) Wei, Y.; Matzen, S.; Maroutian, T.; Agnus, G.; Salverda, M.; Nukala, P.; Chen, Q.; Ye, J.; Lecoeur, P.; Noheda, B. Magnetic tunnel junctions based on ferroelectric Hf0.5Zr0.5O2 tunnel barriers, Phys. Rev. Applied 2019, 12, 031001.

(55) Halter, M.; Bégon-Lours, L.; Bragaglia, V.; Sousa, M.; Offrein, B. J.; Abel, S.; Luisier, M.; Fompeyrine, J. Back-end, CMOS-compatible ferroelectric field-effect transistor for synaptic weights, ACS Appl. Mater. Interfaces 2020, 12, 17725–17732.

(56) Chen, L.; Wang, T.-Y.; Dai, Y.-W.; Cha, M.-Y.; Zhu, H.; Sun, Q.-Q.; Ding, S.-J.; Zhou, P.; Chua, L.; Zhang, D. W. Ultra-low power Hf0.5Zr0.5O2 based ferroelectric tunnel junction synapses for hardware neural network applications, Nanoscale 2018, 10, 15826-15833.

(57) Lyu, J.; Song, T.; Fina, I.; Sánchez, F. High polarization, endurance and retention in sub-5 nm Hf0.5Zr0.5O2 films, Nanoscale 2020, 12, 11280-11287.

(58) Weeks, S. L.; Pal, A.; Narasimhan, V. K.; Littau, K. A.; Chiang, T. Engineering of ferroelectric HfO2-ZrO2 nanolaminates. ACS Appl. Mater. Interfaces 2017, 9, 13440–13447.

(59) Müller, J.; Polakowski, P.; S. Mueller, S.; Mikolajick, T. Ferroelectric hafnium oxide based materials and devices: assessment of current status and future prospects. ECS J. Solid State Sci. Technol. 2015, 4, N30-N35.

(60) Noheda, B.; Íñiguez, J. A key piece of the ferroelectric hafnia puzzle. Science 2020, 369, 1300-1301.

(61) Cheema,S. S.; Kwon, D.; Shanker, N.; Reis, R.; Hsu, S.-L.; Xiao, J.; Zhang, H.;  Wagner, R.; Datar, A.; McCarter, M. R.; Serrao, C. R., Yadav, A. K.; Karbasian, G.; Hsu, C.-H.; Tan, A. J.; Wang, L.-C.; Thakare, V.; Zhang, X.; Mehta, A.; Karapetrova, E.; Chopdekar, R. V.; Shafer, P.; Arenholz, E.; Hu, C.; Proksch, R.; Ramesh, R.; Ciston, Salahuddin, J. S. Enhanced ferroelectricity in ultrathin films grown directly on silicon, Nature 2020, 580, 478–482.

(62) Liu, W.-Y.; Liao, J.-J.; Kiang, J.; Zhou, Y.-C.; Chen, Q.; Mo, S.-T.; Yang, Q.; Peng, Q.-X.; Jiang, L.-M. Highly stable performance of flexible Hf0.6Zr0.4O2 ferroelectric thin films under multi-service conditions, J. Mater. Chem. C 2020, 8, 3878-3886.

(63) Bao, Z; Chen, X., Flexible and stretchable devices, Adv. Mat. 2016, 28, 4177-4179.

(64) Wang, X.; Lu, X.; Liu, B.; Chen, D.; Tong, Y.; Shen, G. Flexible energy-storage devices: design consideration and recent progress. Adv. Mater. 2014, 26, 4763-4782.

(65) Song, W.-J.; Lee, S.; Song, G.; Son, H. B.; Han, D.-Y.; Jeong, I; Bang, Y.; Park, S. Recent progress in aqueous based flexible energy storage devices. Energy Storage Materials 2020, 30, 260-286

(66) Kim, M.-G.; Kanatzidis, M. G.; Facchetti, A.; Marks, T. J. Low-temperature fabrication of high-performance metal oxide thin-film electronics via combustion processing. Nat. Mater. 2011, 10, 382–388.

(67) Pešić, M.; Hoffmann, M; Richter, C.; Mikolajick, T.; Schroeder, U.; Nonvolatile random access memory and energy storage based on antiferroelectric like hysteresis in ZrO2, Adv. Funct. Mater. 2016, 26, 7486-7494.

(68) Ali, F.; Liu, X.; Zhou, D.; Yang, X.; Xu, J.; Schenk, T.; Müller, J.; Schroeder, U.; Cao, F.; Dong, X. Silicon-doped hafnium oxide anti-ferroelectric thin films for energy storage, J. Appl. Phys. 2017, 122, 144105.

# (69) Hoffmann, M.; Schroeder, U.; Künneth, C.; Kersch, A.; Starschich, S.; Böttger, U.; Mikolajick, T. Ferroelectric phase transitions in nanoscale HfO2 films enable giant pyroelectric energy conversion and highly efficient supercapacitors, Nano Energy 2015, 18, 154-164.

(70) Zhang, W. L.; Mao, Y. H.; Cui, L.; Tang, M. H.; Su, P. Y.; Long, X. J., Xiao, Y. G.; Yan S. A. Impact of the radiation effect on the energy storage density and wake-up behaviors of antiferroelectric-like Al-doped HfO2 thin films, Phys. Chem. Chem. Phys. 2020, 22, 21893-21899.

(71) Lomenzo, P. D.; Chung, C.-C.; Zhou, C.; Jones, J. L.; Nishida, T. Doped Hf0.5Zr0.5O2 for high efficiency integrated supercapacitors, Appl. Phys. Lett. 2017, 110, No. 232904.

(72) Park, M. H.; Kim, H. J.; Kim, Y. J.; Moon, T.; Kim, K.; Hwang, C. S. Thin HfxZr1‐xO2 films: a new lead‐free system for electrostatic supercapacitors with large energy storage density and robust thermal stability, Adv. En. Mater. 2014, 4, No. 1400610.

(73) Kim, K. D.; Lee, Y. H.; Gwon, T.; Kim, Y. J.; Kim, H. J.; Seung, T. M.; Hyeon, D. H.; Park, W.; Park, M. H.; Hwang, C. S. Scale-up and optimization of HfO2-ZrO2 solid solution thin films for the electrostatic supercapacitors, Nano Energy 2017, 39, 390–399.

(74) Kozodaev, M. G.; Chernikova, A. G.; Khakimov, R. R.; Park, M. H.; Markeev, A. M.; Hwang, C. S. La-doped Hf0.5Zr0.5O2 thin films for high-efficiency electrostatic supercapacitors, Appl. Phys. Lett. 2018, 113, No. 123902.

(75) Kim, J.; Saremi, S.; Acharya, M.; Velarde, G.; Parsonnet, E.;Donahue, P.; Qualls, A.; Garcia, D.; Martin, L. W. Ultrahigh capacitive energy density in ion-bombarded relaxor ferroelectric films. Science 2020, 369, 81–84.

(76) Kashir, A.; Oh, S.; Hwang, H. Defect engineering to achieve wake‐up free HfO2‐based ferroelectrics. Adv. Energy Mater 2021, 23, No. 2000791.

(77) Kashir, A.; Kim, H.; Oh, S.; Hwang, H. Large remnant polarization in a wake-up free Hf0.5Zr0.5O2 ferroelectric film through bulk and interface engineering. ACS Appl. Electron. Mater. 2021, 3, 629–638.

(78) Kozodaev, M. G.; Chernikova, A. G.;  Korostylev, E. V.; Park, M. H.; Khakimov, R. R.; Hwang, C. S.; Markeev, A. M. Mitigating wakeup effect and improving endurance of ferroelectric HfO2-ZrO2 thin films by careful La-doping featured. J. Appl. Phys. 2019, 125, No. 034101.

# (79) Chen, K.-Y.; Chen, P.-H.; Wu, Y.-H. Excellent reliability of ferroelectric HfZrOx free from wake-up and fatigue effects by NH3 plasma treatment. IEEE Electron. Dev. Lett. 2021, 42, 331-334.

(80) Si, M.; Lyu, X.; Ye, P. D. Ferroelectric polarization switching of hafnium zirconium oxide in a ferroelectric/dielectric stack, ACS Appl. Electron. Mater. 2019, 1, 745−751.

(81) (IEEE Electron Device Letters 42, 2021, 331 – 334).

(82) Hoffmann, M.; Fengler, F. P. G.; Max, B.; Schroeder, U.; Slesazeck, S.; Mikolajick, T. Negative capacitance for electrostatic supercapacitors. Adv. Energy Mater. 2019, 9, No. 1901154.

(83) Fan, P.; Zhang, S.-T.; Xu, J.; Zang, J.; Samart, C.; Zhang, T.; Tan, H.; Salamon, D.; Zhang, H.; Liu, G. Relaxor/antiferroelectric composites: a solution to achieve high energy storage performance in lead-free dielectric ceramics. J. Mater. Chem. C 2020, 8, 5681-5691.

(84) Nguyen. M. D.; Rijnders, G. Thin films of relaxor ferroelectric/antiferroelectric heterolayered structure for energy storage. Thin Solid Films 2018, 659, 89-93.

(85) Shimizu, T.; Katayama, K.; Kiguchi, T.; Akama, A.; Konno, T. J.; Sakata, O.; Funakubo, H. The demonstration of significant ferroelectricity in epitaxial Y-doped HfO2 film. Sci. Rep. 2016, 6, No. 32931.

(86) MacManus-Driscoll, J. L.: Wells, M. P.; Yun, C.; Lee, J.-W.; Eom, C.-B.; Schlom, D. G. New approaches for achieving more perfect transition metal oxide thin films featured. APL Materials 2020, 8, No. 040904

(87) Hao, X. A review on the dielectric materials for high energy-storage application, J. Adv. Dielectr. 2013, 03, No. 1330001.

(88) Li, F.; Zhai, J.; Shen, B.; Zeng, H. Recent progress of ecofriendly perovskite-type dielectric ceramics for energy storage applications. J Adv. Dielectr. 2018, 8, No. 1830005.