Iron delivery from liquid-core hydrogels within a therapeutic nipple shield

Theresa Maiera,b, Antonina Kerbsa, Ljiljana Fruka, Nigel K. H. Slatera

a University of Cambridge, Department of Chemical Engineering and Biotechnology, West Cambridge Site, Philippa Fawcett Drive, Cambridge CB3 0AS, United Kingdom

b University of Cambridge, Department of Paediatrics, Cambridge Biomedical Campus, Cambridge CB2 0QQ, United Kingdom

Corresponding author

Name: 			Theresa Maier

Address: 	Department of Chemical Engineering and Biotechnology, 
University of Cambridge

West Cambridge Site, Philippa Fawcett Drive, Cambridge CB3 0AS,
UK

Telephone number: 	+44 (0)7778627858

Fax number:		+44 (0)1223 334796

E-mail address: 	tm520@cam.ac.uk

Abstract

To aid oral therapeutic administration to infants, a novel delivery technology, referred to as a Therapeutic Nipple Shield (TNS), was previously developed. It consists of a silicone nipple shield device and a dosage form containing a therapeutic (or Active Pharmaceutical Ingredient (API)) to enable delivery during breastfeeding. A range of dosage forms were investigated in past literature, but sufficient API release into human milk had not been achieved. The presented work illustrates the delivery of iron sulphate pentahydrate from liquid-core sodium alginate hydrogels, inserted into a commercially available ultra-thin silicone nipple shield into human milk during in-vitro breastfeeding simulation. Release of iron was quantified employing absorbance measurements of a salicylic assay. An absolute recovery of 44.35 ± 5.43 % of loaded iron(III)sulphate pentahydrate was obtained after 10.58 ± 0.09 g of human milk had passed through the nipple shield. This finding is superior to previous investigations involving the delivery of zinc from rapidly disintegrating tablets and non-woven fibres within a TNS. Due to their superior delivery properties, ease of fabrication and cost-efficiency, liquid-core sodium alginate hydrogels consequently represent a promising dosage form for use as part of the TNS. Further improvements can be made to enhance handling stability and shelf-life characteristics.

Keywords: pediatrics; oral delivery; breastfeeding; human milk; medication systems; liquid-core hydrogels; spherification

1. Introduction

There is a great need for innovations in infant therapeutic development and administration. The WHO estimates that access to affordable interventions, tailored for use in resource-constraint settings, could help to prevent a large percentage of the 5.9 million child deaths worldwide before the age of five (IGME, 2015; World Health Organization, 2007). Improved infant compliant technologies could also facilitate the process of infant oral administration in both high- and low-resource settings, easing the physical and emotional challenges experienced by many parents. While administration during feeding is recommended to improve acceptability (Helms and Quan, 2006), this is not a feasible approach for the 36% of exclusively breastfed infants aged 0-6 months (World Health Organization, 2017). A novel delivery technology, called Therapeutic Nipple Shield (TNS), could help to address this shortcoming. Designed to enable therapeutic delivery during breastfeeding, it consists of two components: a silicone nipple shield and a therapeutic dosage form contained within the nipple shield’s teat. The TNS is worn by the mother during breastfeeding, and enables therapeutic delivery to her sucking infant through the flow of human milk (see Figure 1). In-vitro testing of the TNS is performed using a breastfeeding simulation apparatus, capable of simulating the process of lactation and infant feeding (Gerrard et al., 2013). Past literature has investigated the use of a modified lip-containing nipple shield to enable drug placement, also referred to as the NSDS design, as well as the release of Sulforhodamine B from rapidly disintegrating tablets (Gerrard et al., 2012), and of zinc sulphate from both non-woven fibres and rapidly disintegrating tablets into human milk (Maier et al., 2018; Scheuerle et al., 2017a). Yet, in all cases, delivery of a full dose within the duration of an average breastfeed was not achieved (Gerrard et al., 2012; Maier et al., 2018; Scheuerle et al., 2017a), encouraging the investigation of liquid-core hydrogels as an alternative dosage form as part of the TNS.

Although iron is a biochemically essential element, involved in a range of metabolic processes and DNA synthesis (Camaschella, 2015), over two billion people are affected by iron deficiency, making it the most common single-nutrient deficiency worldwide (Lanzkowsky, 2016). Affected individuals experience a variety of nonspecific symptoms such a fatigue and weakness (Camaschella, 2015), as well as deficits in mental, behavioural, motor, and neurophysiological function (Agostoni et al., 2010; Berglund et al., 2015; Caglayan et al., 1993; Kazal, 2002; Lozoff et al., 2006). Although iron deficiency is particularly common in low-resource environments, as many as 26% of healthy toddlers aged 1 to 3 years were reported  to be affected (Domelloef et al., 2014; Persson et al., 1998). In infants, deficiency is caused either by a low consumption of iron-containing food, common for healthy term infants aged 6-12 months whose iron stores last approximately until their forth to sixth prenatal month (Baker and Greer, 2010; De Alarcon and Werner, 2005), or due to premature birth, which results in significantly lower amounts of stored iron, resulting in deficiency already within the infants’ first months of age (Baker and Greer, 2010). Because the increased iron requirements of preterm infants cannot be met by human milk alone, which contains only 0.2–0.4 mg l-1 of available iron (Ziegler et al., 2009)), supplementation is recommended (Baker and Greer, 2010). Guidelines suggest 2 mg of elemental iron per kg body weight per day, starting at the beginning of the infants’ fifth postnatal week until the end of their twelfth month of age (Rao and Georgieff, 2009). For developing countries with high prevalence of iron deficient anaemia (40% or higher), a condition in which the blood’s haemoglobin concentration is decreased and the red blood cell’s morphology affected, the World Health Organization recommends a daily dose of 10-12.5 mg of elemental iron for three consecutive months within a year (World Health Organization, 2016). Iron(II)sulphate, is the most commonly used form of iron supplementation, based on its availability, cost-effectiveness, and high bioavailability (Naude et al., 2000; Rao and Georgieff, 2009). It is included in both the WHO Model List of Essential Medicines and the WHO Model List of Essential Medicines for Children (World Health Organization, 2017, 2015), and can be found in fortified food, as well as in formulations of prophylactic and therapeutic purpose (eMC, 2018).

Taking into account the clear need for improved infant iron supplementation during breastfeeding, we embarked on developing an improved TNS system, employing a novel hydrogel based dosage form and a commercially available silicone nipple shield, which enhances its potential for translation from bench into clinical practice.

2. Materials and methods

2.1. Materials

Low viscosity alginic acid sodium salt in FCC grade (G:M ratio in the range of 61-65 : 39-35) was obtained from Alfa Aesar (Lancashire, UK), calcium lactate pentahydrate from Sigma Aldrich (Dorset, UK), salicylic acid and iron(III)sulphate pentahydrate from Fisher Scientific (Leicestershire, UK). Iron(III)sulphate was preferred over iron(II)sulphate to prevent potential competition with Ca2+ during crosslinking and to facilitate subsequent iron analysis. Human milk samples were provided by the Queen Charlotte’s and Chelsea Hospital Milk Bank (Imperial College Healthcare NHS Trust) and characterized to contain a protein content of 43.52 g l-1 and a fat content of 16.51 g l-1 (Maier et al., 2018). These values align with previously reported literature (Emmett and Rogers, 1997; Kent et al., 2006; Maier et al., 2018; Saarela et al., 2005). The experimental use of human milk was approved by the Cambridge Human Biology Research Ethics Committee at the University of Cambridge.

2.2. Methods
2.2.1. Hydrogel fabrication

Liquid-core ferric sulphate hydrogels were prepared using the following procedure. Two solutions were prepared: i) A 0.5% sodium alginate solution of low viscosity alginic acid sodium salt in double deionized water (DDI), which was left to settle at 4°C overnight to remove air bubbles, ii) a solution of 1% calcium lactate pentahydrate and 60 mg mL-1 ferric sulphate pentahydrate in DDI water, of which 500 µL were pipetted into each of the hemispherical impressions of a food-grade silicone mould (impression measuring 2.5 cm in diameter and 1 cm in depth). The filled mould was transferred to -20 °C for at least 5 hours. Gelation was achieved by exposing a frozen calcium lactate ferric sulphate hemisphere for 2.75 min to a 4°C sodium alginate bath, following which access sodium alginate was rinsed off in a DDI water bath. All liquid-core hydrogels were prepared immediately before use in delivery or characterisation measurements.

2.2.2. Compression testing and visual characterisation

To assess the mechanical properties of manufactured liquid-core hydrogels, uniaxial compression testing was performed in octuplicate using a H5Ks electric screw machine (Tinius Olsen, Redhill/UK) fitted with a 5N load cell. Hereby, each hydrogel was placed on a stationary flat surface, while a second flat plate applied vertical compression until the gel's plastic region of formation was reached. An illustration of the setup is provided in Figure 4 a).  The crosshead speed was set at 2 mm/min, and force displacement data recorded. Due to the complex nature of liquid-core hydrogels, other mechanical properties were not evaluated. Visual analysis of the gels’ rupture mechanism and morphology was performed by means of a bespoke optical system to enable real-time image analysis. It consisted of a high-speed camera (Basler, Ahrensburg/Germany) and a National Instruments card (NIC, National Instruments, Austin, TX/USA), controlled via a LabVIEW software programme. Calibration was performed by determining the number of pixels and the distance in mm between both the top and bottom compression plate. This relationship was used to evaluate the hydrogel's average wall thickness, diameter, and height in quadruplicate using images taken before compression testing. Hereby, wall thickness measurements made use of the shell’s and core’s difference in colour strength when visualised via the LabVIEW programme, enabling to identify the solid core’s boundary.

2.2.3. Delivery of iron(III)sulphate during breastfeeding simulation experiments

Delivery of iron(III)sulphate was conducted in triplicate using the breastfeeding simulation apparatus by Gerrard et al. (Gerrard et al., 2013), illustrated in Figure 2. The apparatus transfers human milk within silicone tubing from a stirred reservoir to the fraction collector. Pump 1 enables human milk to reach a silicone breast mimic, on which the hydrogel-containing nipple shield is fixated in an angle of 30° downwards from the vertical axis, while pump 2 transports milk having passed the nipple shield to the fraction collector. Pump 3 is controlled by a computer system linked to a National Instruments Card, enabling temperature and pressure monitoring and the exertion of an oscillating suction pattern similar to those of breastfed infants. In accordance with breastfeeding physiology, an approximate flow rate of 5.0 mL min-1, a suction frequency of 1 suction sec-1, and a temperature range of 33.7 - 35.7°C, mimicking the temperature of human milk in the infant’s mouth, were used during breastfeeding simulation (Black et al., 1998; Geddes et al., 2008; Macias and Meneses, 2011; Moral et al., 2010). Prior to experimental procedures, the apparatus’ pumps were calibrated. To investigate the potential of hydrogel delivery for preterm infants, who commonly require use of an ultrathin contact nipple shields to establish breastfeeding and increase milk transfer (Meier et al., 2000), the pressure values for breastfeeding simulation were adjusted in alignment with literature by Geddes et al. (Geddes et al., 2018, 2017). Mean peak vacuum values of -62.47 ± 1.76 mmHg, mean baseline vacuum values -0.92 ± 0.37 mmHg, and mean average vacuum values of -38.30 ± 9.71 mmHg were recorded. Fractions, each collected for a duration of 10 sec, were weighted before analysis, and recovery into approximately 10 g of human milk investigated.

2.2.4. Quantification of iron in human milk

Iron(III)sulphate pentahydrate in fractions collected during breastfeeding simulation as well as in prepared standards with known concentration was quantified as follows: In order to obtain transparent solutions, 1 M hydrochloric acid was added in a ratio of 1:8 to the sample to trigger the release of transferrin-bound iron and precipitate the human milk’s casein, with its isoelectric point at pH 4.7 (Broyard and Gaucheron, 2015; Phillips and Williams, 2011). All samples were mixed by vortexing and centrifuged for 7 min at 16,112 x g. For each sample 20 µL of the supernatant was transferred to 180 µL of DDI water and 1700 µL of 0.1% salicylic acid solution added. Following mixing, absorbance of ferric salicylate in each sample was measured at room temperature at max = 524 nm. The wavelength of maximum absorbance was determined by means of absorbance scans of all calibration samples over the wavelength range of  = 328-1000 nm, and a calibration curve at ferric salicylate's maximum absorbance in human milk generated (see Figure A.1). A separate calibration curve was constructed in DDI water (see Figure A.2) to determine the total amount of iron loaded within the liquid-core hydrogels. Frozen hemispheres were melted, weighted, diluted 1:1 in DDI water, and their concentration determined through absorbance measurements of ferric salicylate at max = 524 nm as described previously. Triplicate analysis indicated a total of 29.59 ± 0.43 mg ferric sulphate pentahydrate contained within manufactured liquid-core hydrogels, corresponding to 6.75 ± 0.10 g of elemental iron. Absorbance values obtained from fractions collected during breastfeeding simulation experiments were used to generate a release profile, i.e. the cumulative iron(III)sulphate pentahydrate recovery over time, represented as a percentage of the total amount encapsulated within the sodium alginate hydrogels. Hereby, the amount of iron(III)sulphate pentahydrate in each fraction was evaluated based on absorbance measurements at max = 524 nm using the calibration curve (Figure A.1), and normalised to the total amount of ferric sulphate pentahydrate used for liquid-core hydrogel manufacture. A cumulative normalised release graph was obtained by summing up the resulting values of each new fraction with those of previous fractions.

3. Results and discussion

3.1. Hydrogel preparation

Liquid-core hydrogels containing ferric sulphate were prepared by means of frozen reverse spherification, a method that originated from the molecular gastronomy (Barham et al., 2010; Caporaso and Formisano, 2016; Sen, 2017), and is nowadays also applied for formulation preparation and nutrient supplementation (Hudson and Noel, 2014; Messaoud et al., 2016). The protocol was iteratively adapted, choosing frozen reverse spherification over reverse spherification due to the hydrogels’ higher uniformity. Fabrication optimisation variables included the following: i) type of spherification technique used to obtain reproducibly uniform spheres, ii) ratio of iron(III)sulphate pentahydrate to calcium lactate pentahydrate with the objective to minimize precipitation of either compound, iii) duration of gelation to control wall thickness and liquid-core content available for delivery, iv) the gel size in order to maximize its liquid load, but to also enable sufficient milk flow through the nipple shield’s silicone teat. While the first two variables could be assessed visually, the optimal gel size and gelation time were evaluated by means of breastfeeding simulation experiments. Since wall thickness is a function of gelation time, increasing with prolonged gelation duration, fabrication optimisation procedures had the objective to provide sufficient stability for gel handling, while retaining the gel’s mechanical sensitivity for rapid rupture. A range of gelation times between 1 min to 5 min were assessed and those stable enough for handling tested in the breastfeeding simulation apparatus. Less liquid to be encapsulated required shorter gelation times than larger amounts of liquid to achieve the same hydrogel stability. Aqueous solution of calcium lactate pentahydrate and iron(III)sulphate pentahydrate were pipetted into each of the hemispherical impressions of a food-grade silicone mould and subsequently frozen at -20°C. Gelation was achieved by exposing a frozen calcium lactate iron(III)sulphate hemisphere for 2.75 min to a 4°C sodium alginate bath (Figure 3).

3.2. Compression testing and visual characterisation

Average values for wall thickness, diameter, and height of manufactured liquid-core hydrogels, as well as compression force required for gel rupture are summarised in Table 1. Values are compared to previously published data of i) rapidly disintegrating tablets for zinc delivery into human milk, ii) liquid-core alginate hydrogel beads by Tsai et al. (Tsai et al., 2017a, 2017b, 2017c). A typical force-displacement graph is illustrated in Figure 4 b). Two conclusions can be drawn: first, the larger diameter of fabricated liquid-core hydrogels, compared to rapidly disintegrating tablets, allows central positioning of the gels within the nipple shield’s teat, even without a lip for dosage form positioning, as studied previously (Gerrard et al., 2012; Maier et al., 2018; Scheuerle et al., 2017a), and increases the dosage form’s surface area for human milk contact. Moreover, when comparing LHBs by Tsai et al. (Tsai et al., 2017a, 2017b) and liquid-core hydrogels, a five-fold lower compression force can be observed. This can likely be attributed to the comparatively large amount of liquid encapsulated within the manufactured hydrogels and its resulting diminished sphericity. Visual analysis data during compression testing, illustrated in Figure 5, contributes towards this hypothesis, and reveals that the hydrogel’s API-release mechanism merely entails the formation of a pinhole in the hydrogel’s solid shell.

Table 1: Overview of wall thickness, diameter, height, and compression force of liquid-core hydrogels used for ion delivery into human milk. Data obtained was compared to literature by Scheuerle et al. and Tsai et al., using rapidly disintegrating tablets for zinc delivery into human milk (Scheuerle et al., 2017a), and liquid-core hydrogel beads for chlorogenic acid delivery into simulated intestinal fluid (Tsai et al., 2017a, 2017b), respectively.

|  |  | Comparison with literature data |  |
| --- | --- | --- | --- |
|  | Liquid-core hydrogels | Liquid-core alginate hydrogel beads (LHBs) | Rapidly disintegrating tablets (tablet type 2)c |
| Wall thickness [mm] | 0.44 ± 0.10 a | Not provided | N/A |
| Diameter [mm] | 14.28 ± 0.85 a | Range: 4.17-5.84 (Tsai et al., 2017b) | 8.093 ± 0.003 |
| Height [mm] | 4.91 ± 0.28 a |  | 4.65 ± 0.03 |
| Compression force [N] | 0.245 ± 0.103 b | 1.26d (Tsai et al., 2017a) | 22,000 |

a Values were measured in quadruplicate.

b Values were measured in octuplicate.

c Values taken from (Scheuerle et al., 2017a)

d Reverse spherification using a single spherification step

3.3. Release of iron from liquid-core hydrogels

Breastfeeding simulation data, illustrating the cumulative normalized proportion of iron sulphate pentahydrate released over time, can be found in Figure 6. An absolute recovery of 44.35 ± 5.43 % of loaded iron(III)sulphate pentahydrate was achieved after 10.58 ± 0.09 g of human milk had passed through the TNS, highlighting the liquid-core hydrogels’ superior release properties compared to previously studied dosage forms. In comparison: Release of zinc sulphate from rapidly disintegrating tablets and non-woven fibres in approximately 10 g of human milk (equivalent to 2 min of breastfeeding simulation) resulted in only 3-5% and 29-31% recovery, respectively (Maier et al., 2018; Scheuerle et al., 2017a), and proofed even after an additional 18 min of breastfeeding simulation insufficient in delivering the full dose within the 76.0 ± 12.6 g human milk of an infants’ average breastfeed (Kent et al., 2006). While the hydrogel’s rapid release promises sufficient delivery even during short feeds, reduced mixing with human milk over time also necessitates that the therapeutic formulation is design to possess adequate taste, aiming to prevent its impact on the infant’s breastfeeding compliance. The potential to encapsulate commercially available paediatric liquid formulations and syrups, with their already optimised taste masking characteristics for the delivery by means of oral syringes or dosing spoons, provides a potential strategy to mitigate these risks. Although liquid-core hydrogel increase the ratio of API to human milk with a total of 38.16 ± 0.06 % of iron sulphate released within the first minute of breastfeeding simulation, it has to be noted that human milk itself comprises taste masking properties (Bennett et al., 2012), and that breastfed infants are generally used to a wide range of different tastes as a result of the maternal diet (Bravi et al., 2016; Cosmi et al., 2017).

Despite their superior release properties, full release of the loaded dose within the approximately 2 min of breastfeeding simulation experiments was not achieved. The difference between the amount of iron(III)sulphate pentahydrate loaded into the hemispherical silicone mould as part of the hydrogels’ fabrication process, and the amount recovered in human milk during breastfeeding simulation, can be explained by a combination of both iron retention within the hydrogel’s core shell, as well as within the apparatus void space in form of iron-casein precipitates. The former is a direct result of the spherification process, whereby ferric sulphate is enclosed within the crosslinked alginate polymer chains, and the shell’s remainder in the nipple shield teat following delivery of its liquid core. Iron-casein precipitates are caused by neutralization of the casein’s negative charge following binding of Fe3+ to its Pser clusters (Gaucheron, 2000), and can only be re-suspended in fractioned samples by adjusting the pH during pre-analysis processing. While in-vitro experiments yielded only insufficient delivery of the loaded dose, it has to be noted that therapeutic loss due to precipitate formation within the complex apparatus setup would not occur during in-vivo delivery and that the experimental duration chosen only assessed the hydrogel’s rapid release properties within the first two minutes of breastfeeding simulation. A breastfed infant however would be directly latched onto the nipple shield containing the hydrogel, and breastfeeding for a seven times extended period of time (Kent et al., 2006).

In addition to their superior release characteristics, liquid-core hydrogels possess three distinct advantages, suggesting their preferred use as a dosage form as part of the TNS. Firstly, liquid-core hydrogels are the first dosage form studied for delivery into human milk that are characterised by a mechanically induced release mechanism, i.e. the rupture of the hydrogels’ solid shells through suction force and milk flow. It thereby overcomes previous limitations of rapidly disintegrating tablets and non-woven fibres, which involved alteration of the dosage forms’ release efficiency based on the milk’s fat content, the milk’s homogeneity, and the overall milk macromolecule composition (Gerrard et al., 2012). Hereby, the strong dependence of achievable release efficiency on human milk composition, which is known to vary among others based on the maternal diet and the stage of lactation (Vir, 2011), was perceived as particularly problematic for the exploration of suitable dosage forms and the formulation of widely applicable findings.  The use of liquid-core hydrogels within a commercially available ultrathin contact nipple shield is also believed to enhance user acceptability through both, enabling use of the same nipple shield device for normal feeding and therapeutic administration, while at the same time reducing potential discomfort for mother and/or infant during breastfeeding based on the hydrogel’s soft texture. Moreover, sodium alginate hydrogels manufactured via frozen reverse spherification enable the production of low-cost dosage forms, using both a biocompatible and non-toxic polymer, and calcium, one of the 21 essential elements of the human body (Preedy, 2016). While use of calcium lactate or calcium gluconate is beneficial due to its neutral taste (Pathomrungsiyounggul et al., 2010), sodium alginate is a common component of commercially available infant medication, e.g. ‘Gaviscone’ to treat gastric regurgitation in infants aged 1-2 years (Corvaglia et al., 2011b, 2011a; Dhillon and Ewer, 2004), as well as gastroesophageal reflux in preterm infants under medical supervision (Corvaglia et al., 2011b, 2011a; Dhillon and Ewer, 2004). As hydrogel manufacture goes without potentially harmful or problematic excipients used in other infant formulations, the liquid-core hydrogels presented in this study also respond to the consistently emphasized need for more appropriate paediatric formulations and their inclusion into pharmaceutical product portfolios (Lopez et al., 2015; Standing and Tuleu, 2005). Lastly, with regard to the therapeutic delivered as part of this study, the hydrogels’ rapid delivery properties as part of the TNS seem particularly suitable for iron release during breastfeeding, as prolonged exposure of iron to milk products over time, e.g. through supplementation in milk and yoghurt, results in an undesired change of odour and flavour, as well as the milk’s rancidity due to iron-induced lipid oxidation (Gaucheron, 2000).

Areas of further improvement include both the liquid-core hydrogel’s stability and shelf life characteristics, as well as solubility considerations. According to Tsai et al., the hydrogels’ mechanical stability for handling and storage purposes can be improved by means of a secondary gelation step (Tsai et al., 2017a, 2017b, 2017c), involving the introduction of crosslinked hydrogels into a Ca2+ solution to enable the ion’s permeation into the previously unoccupied blocks within the hydrogels’ core shell structure (Tsai et al., 2017c). This approach was shown to increase hardness and storage stability of LHBs produced by means of reverse spherification, while simultaneously decreasing the release rate of the encapsulated API (Tsai et al., 2017a, 2017b, 2017c). Due to the exposure of the TNS’s hydrogels to repetitive mechanical stress during breastfeeding simulation, representing a significantly different environment than during experiments performed by Tsai et al. without agitation (Tsai et al., 2017a, 2017b, 2017c), it can however be hypothesized that a reduction in absolute recovery due to secondary gelation is not to be expected. In fact, findings by Scheuerle et al. give reason to expect an even enhanced API-recovery during in-vivo breastfeeding, as infant tongue peristalsis, shown to be an important driver for dosage form disintegration (Scheuerle et al., 2017b), cannot be mimicked using the breastfeeding simulation apparatus. Solubility considerations relate to the availability of calcium lactate pentahydrate for hydrogel gelation. Soluble calcium lactate might permanently precipitate during the spherification’s freezing step, depending on both the characteristics and amount of dissolved therapeutic within the calcium lactate solution. As calcium ions are essential for gelation, it has to be noticed that both crosslinking protocol and/or the concentration of calcium lactate pentahydrate used for hydrogel fabrication will need to be consistently optimised for the respective type and concentration of therapeutic.

4. Conclusions

This study investigated the delivery of iron(III)sulphate pentahydrate from liquid-core hydrogels, comprised within the teat of a commercially available ultrathin contact nipple shield, into human milk by means of a breastfeeding simulation apparatus. A total recovery of 
44.35 ± 5.43 % was achieved after 10.58 ± 0.09 g human milk had passed through the shield. Compared to previous dosage forms used for delivery into human milk, liquid-core hydrogels within a commercial ultrathin silicone nipple shield were identified as the superior dosage form for delivery during in-vitro breastfeeding. The hydrogel’s delivery strategy, based on the rupture of the hydrogel’s solid membrane, seems particularly feasible for administration during breastfeeding, as the release is not dependent on the complex and varying properties of human milk. Moreover, liquid-core hydrogels are characterised by their low cost, ease of fabrication, and high safety profile of used compounds, as well as their projected enhanced acceptability due to the hydrogel’s soft texture and the possibility of using a commercially available nipple shield for both therapeutic delivery and normal feeding. Further research is required to enhance the hydrogel’s stability characteristics for handling and storage purposes.

Acknowledgements

Theresa Maier (T.M.) was supported through academic scholarships by the WD Armstrong Trust, University of Cambridge, the German Academic Scholarship Foundation, and the Kurt Hahn Trust, University of Cambridge. We would like to thank Gillian Weaver, manager of the Queen Charlotte’s and Chelsea Hospital Milk Bank (Imperial College Healthcare NHS Trust) for providing human milk samples to conduct this study, Dr. Jochen Dreyer (Department of Chemical Engineering and Biotechnology, University of Cambridge) for his support in revising the LabVIEW programme used for breastfeeding simulation, and Andrew Rayment (Department of Materials Science & Metallurgy, University of Cambridge) for assisting in the performed compression testing and visual characterisation.

Competing interests

Declarations of interest: none.

References

Agostoni, C., Buonocore, G., Carnielli, V.P., De Curtis, M., Darmaun, D., Decsi, T., Domellöf, M., Embleton, N.D., Fusch, C., Genzel-Boroviczeny, O., Goulet, O., Kalhan, S.C., Kolacek, S., Koletzko, B., Lapillonne, A., Mihatsch, W., Moreno, L., Neu, J., Poindexter, B., Puntis, J., Putet, G., Rigo, J., Riskin, A., Salle, B., Sauer, P., Shamir, R., Szajewska, H., Thureen, P., Turck, D., van Goudoever, J.B., Ziegler, E.E., 2010. Enteral Nutrient Supply for Preterm Infants: Commentary From the European Society of Paediatric Gastroenterology, Hepatology and Nutrition Committee on Nutrition. J. Pediatr. Gastroenterol. Nutr. 50, 85–91. doi:10.1097/MPG.0b013e3181adaee0

Baker, R.D., Greer, F.R., 2010. Diagnosis and prevention of iron deficiency and iron-deficiency anemia in infants and young children (0-3 years of age). Pediatrics 126, 1040–1050. doi:10.1542/peds.2010-2576

Barham, P., Skibsted, L.H., Bredie, W.L.P., Bom Frost, M., Moller, P., Risbo, J., Snitkjær, P., Mortensen, L.M., 2010. Molecular Gastronomy: A New Emerging Scientific Discipline. Chem. Rev. 110, 2313–2365. doi:10.1021/cr900105w

Bennett, S.M., Zhou, L., Hayes, J.E., 2012. Using milk fat to reduce the irritation and bitter taste of ibuprofen. Chemosens. Percept. 5, 231–236. doi:10.1007/s12078-012-9128-6

Berglund, S.K., Westrup, B., Domellöf, M., 2015. Iron supplementation until 6 months protects marginally low-birth-weight infants from iron deficiency during their first year of life. J. Pediatr. Gastroenterol. Nutr. 60, 390–395. doi:10.1097/MPG.0000000000000633

Black, R.F., Jarman, L., Simpson, J., 1998. The science of breastfeeding, 3rd ed. Jones and Bartlett Publishers, Sudbury.

Bravi, F., Wiens, F., Decarli, A., Pont, A.D., 2016. Impact of maternal nutrition on breast-milk composition: a systematic review. Am. J. 104, 646–662. doi:10.3945/ajcn.115.120881

Broyard, C., Gaucheron, F., 2015. Modifications of structures and functions of caseins: a scientific and technological challenge. Dairy Sci. Technol. 95, 831–862. doi:10.1007/s13594-015-0220-y

Caglayan, S., Candemir, H., Aksit, S., Kansoy, S., Asik, S., 1993. Superiority of oral agar and phototherapy combination in the treatment of neonatal hyperbilirubinemia. Pediatrics 92, 86–89. doi:N/A

Camaschella, C., 2015. Iron-Deficiency Anemia. N. Engl. J. Med. 372, 1832–1843. doi:10.1056/NEJMra1401038

Caporaso, N., Formisano, D., 2016. Developments, applications, and trends of molecular gastronomy among food scientists and innovative chefs. Food Rev. Int. 32, 417–435. doi:10.1080/87559129.2015.1094818

Corvaglia, L., Aceti, A., Mariani, E., 2011a. The efficacy of sodium alginate (Gaviscon) for the treatment of gastro oesophageal reflux in preterm infants. Aliment. Pharmacol. Ther. 33, 466–470. doi:10.1111/j.1365-2036.2010.04545.x

Corvaglia, L., Spizzichino, M., Zama, D., Aceti, A., 2011b. Sodium alginate (Gaviscon®) does not reduce apnoeas related to gastro-oesophageal reflux in preterm infants. Early Hum. Dev. 87, 775–778. doi:10.1016/j.earlhumdev.2011.05.013

Cosmi, V.D., Scaglioni, S., Agostoni, C., 2017. Early taste experiences and later food choices. Nutrients 9, 107. doi:10.3390/nu9020107

De Alarcon, P.A., Werner, E.J., 2005. Neonatal hematology, 4th ed. Cambridge University Press, Cambridge.

Dhillon, A.S., Ewer, A.K., 2004. Diagnosis and management of gastro-oesophageal reflux in preterm infants in neonatal intensive care units. Acta Paediatr. 93, 88–93. doi:10.1111/j.1651-2227.2004.tb00680.x

Domelloef, M., Braegger, C., Campoy, C., Colomb, V., Decsi, T., Fewtrell, M., Hojsak, I., Mihatsch, W., Molgaard, C., Shamir, R., Turck, D., van Goudoever, J., 2014. Iron requirements of infants and toddlers. J. Pediatr. Gastroenterol. Nutr. 58, 119–129. doi:10.1097/MPG.0000000000000206

Electronic medicines compendium, 2018. Search eMC.

Emmett, P.M., Rogers, I.S., 1997. Properties of human milk and their relationship with maternal nutrition. Early Hum. Dev. 49, S7–S28. doi:10.1016/S0378-3782(97)00051-0

Gaucheron, F., 2000. Iron fortification in dairy industry. Trends Food Sci. Technol. 11, 403–409. doi:10.1016/S0924-2244(01)00032-2

Geddes, D., Kok, C., Nancarrow, K., Hepworth, A., Simmer, K., 2018. Preterm infant feeding: a mechanistic comparison between a vacuum triggered novel teat and breastfeeding. Nutrients 10, 376. doi:10.3390/nu10030376

Geddes, D.T., Chooi, K., Nancarrow, K., Hepworth, A.R., Gardner, H., Simmer, K., 2017. Characterisation of sucking dynamics of breastfeeding preterm infants: a cross sectional study. BMC Pregnancy Childbirth 17, 386. doi:10.1186/s12884-017-1574-3

Geddes, D.T., Kent, J.C., Mitoulas, L.R., Hartmann, P.E., 2008. Tongue movement and intra-oral vacuum in breastfeeding infants. Early Hum. Dev. 84, 471–477. doi:10.1016/j.earlhumdev.2007.12.008

Gerrard, S.E., Baniecki, M.L., Sokal, D.C., 2012. A nipple shield delivery system for oral drug delivery to breastfeeding infants: microbicide delivery to inactivate HIV. Int. J. Pharm. 434, 224–234. doi:10.1016/j.ijpharm.2012.05.035

Gerrard, S.E., Orlu-Gul, M., Tuleu, C., Slater, N.K.H., 2013. Modeling the physiological factors that affect drug delivery from a nipple shield delivery system to breastfeeding infants. J. Pharm. Sci. 102, 3773–3783. doi:10.1002/jps.23688

Helms, R.A., Quan, D.J., 2006. Textbook of therapeutics: drug and disease management., 2nd ed. Lippincott Williams & Wilkins, Philadelphia.

Hudson, E.T., Noel, L.S., 2014. Method and system for making customized formulations for individuals. US Pat. App. 14/207 364.

Kazal, L.A., 2002. Prevention of iron deficiency in infants and toddlers. Am. Fam. Physician 66, 1217–1224.

Kent, J.C., Mitoulas, L.R., Cregan, M.D., Ramsay, D.T., Doherty, D.A., Hartmann, P.E., 2006. Volume and frequency of breastfeedings and fat content of breast milk throughout the day. Pediatrics 117, 387–395. doi:10.1542/peds.2005-1417

Lanzkowsky, P., 2016. Iron-deficiency anemia, in: Lanzkowsky’s Manual of Pediatric Hematology and Oncology. Elsevier, pp. 69–83. doi:10.1016/B978-0-12-801368-7.00006-5

Lopez, F.L., Ernest, T.B., Tuleu, C., Gul, M.O., 2015. Formulation approaches to pediatric oral drug delivery: benefits and limitations of current platforms. Expert Opin. Drug Deliv. 12, 1727–1740. doi:10.1517/17425247.2015.1060218

Lozoff, B., Beard, J., Connor, J., Felt, B., Georgieff, M., Schallert, T., 2006. Long-lasting neural and behavioral effects of iron deficiency in infancy. Nutr. Rev. 64, S34–S43. doi:10.1111/j.1753-4887.2006.tb00243.x

Macias, M.E.R., Meneses, G.J.S., 2011. Physiology of nutritive sucking in newborns and infants. Bol. Med. Hosp. Infant. Mex. 68, 296–303. doi:N/A

Maier, T., Scheuerle, R.L., Markl, D., Bruggraber, S., Zeitler, A., Fruk, L., Slater, N.K.H., 2018. Zinc delivery from non-woven fibres within a therapeutic nipple shield. Int. J. Pharm. 537, 290–299. doi:10.1016/j.ijpharm.2017.12.042

Meier, P.P., Brown, L.P., Hurst, N.M., Spatz, D.L., Engstrom, J.L., Borucki, L.C., Krouse, A.M., 2000. Nipple shields for preterm infants: effect on milk transfer and duration of breastfeeding. J. Hum. Lact. 16, 106–114. doi:10.1177/089033440001600205

Messaoud, G.B., Sanchez-Gonzalez, L., Probst, L., 2016. Physico-chemical properties of alginate shellac aqueous-core capsules: Influence of membrane architecture on riboflavin release. Carbohydr. Polym. 144, 428–437. doi:10.1016/j.carbpol.2016.02.081

Moral, A., Bolibar, I., Seguranyes, G., Ustrell, J.M., Sebastiá, G., Martínez-Barba, C., Ríos, J., 2010. Mechanics of sucking: comparison between bottle feeding and breastfeeding. BMC Pediatr. 10, 1–8. doi:10.1186/1471-2431-10-6

Naude, S., Clijsen, S., Naulaers, G., Daniels, H., Vanhole, C., Devlieger, H., 2000. Iron supplementation in preterm infants: a study comparing the effect and tolerance of a Fe2+ and a nonionic FeIII compound. J. Clin. Pharmacol. 40, 1447–1451. doi:10.1177/009127000004001215

Paques, J.P., van der Linden, E., van Rijn, C.J.M., 2014. Preparation methods of alginate nanoparticles. Adv. Colloid Interface Sci. 209, 163–171. doi:10.1016/j.cis.2014.03.009

Pathomrungsiyounggul, P., Grandison, A.S., Lewis, M.J., 2010. Effect of calcium carbonate, calcium citrate, tricalcium phosphate, calcium gluconate and calcium lactate on some physicochemical properties of soymilk. Int. J. Food Sci. Technol. 45, 2234–2240. doi:10.1111/j.1365-2621.2010.02399.x

Persson, L.A., Lundstroem, M., Loennerdal, B., Hernell, O., 1998. Are weaning foods causing impaired iron and zinc status in 1-year-old Swedish infants? A cohort study. Acta Paediatr. 87, 618–622. doi:10.1111/j.1651-2227.1998.tb01518.x

Phillips, G.O., Williams, P.A., 2011. Caseins, in: Handbook of Food Proteins. Woodhead Publishing, Cambridge, pp. 13–29.

Preedy, V.R., 2016. Calcium, in: Caffeine - Chemistry, Analaysis, Function and Effects. Royal Society of Chemistry, London.

Rao, R., Georgieff, M.K., 2009. Iron therapy for preterm infants. Clin. Perinatol. 36, 27–42. doi:10.1016/j.clp.2008.09.013

Saarela, T., Kokkonen, J., Koivisto, M., 2005. Macronutrient and energy contents of human milk fractions during the first six months of lactation. Acta Paediatr. 94, 1176–1181. doi:10.1111/j.1651-2227.2005.tb02070.x

Scheuerle, R.L., Bruggraber, S.F.A., Gerrard, S.E., Kendall, R.A., Tuleu, C., Slater, N.K.H., 2017a. Characterisation of zinc delivery from a nipple shield delivery system using a breastfeeding simulation apparatus. PLoS One 12, e0171624. doi:10.1371/journal.pone.0171624

Scheuerle, R.L., Kendall, R.A., Tuleu, C., Slater, N.K.H., Gerrard, S.E., 2017b. Mimicking the impact of infant tongue peristalsis on behavior of solid oral dosage forms administered during breastfeeding. J. Pharm. Sci. 106, 193–199. doi:10.1016/j.xphs.2016.08.006

Sen, D.J., 2017. Cross linking of calcium ion in alginate produce spherification in molecular gastronomy by pseudoplastic flow. World J. Pharm. Sci. 5, 1–10. doi:N/A

Standing, J.F., Tuleu, C., 2005. Paediatric formulations - getting to the heart of the problem. Int. J. Pharm. 300, 56–66. doi:10.1016/j.ijpharm.2005.05.006

Tsai, F.-H., Chiang, P.-Y., Kitamura, Y., Kokawa, M., Islam, M.Z., 2017a. Producing liquid-core hydrogel beads by reverse spherification: effect of secondary gelation on physical properties and release characteristics. Food Hydrocoll. 62, 140–148. doi:10.1016/j.foodhyd.2016.07.002

Tsai, F.-H., Kitamura, Y., Kokawa, M., 2017b. Liquid-core alginate hydrogel beads loaded with functional compounds of radish by-products by reverse spherification: optimization by response surface methodology. Int. J. Biol. Macromol. 96, 600–610. doi:10.1016/j.ijbiomac.2016.12.056

Tsai, F.-H., Kitamura, Y., Kokawa, M., 2017c. Effect of gum arabic-modified alginate on physicochemical properties, release kinetics, and storage stability of liquid-core hydrogel beads. Carbohydr. Polym. 174, 1069–1077. doi:10.1016/J.CARBPOL.2017.07.031

UNICEF, Wold Health Organization, World Bank Group, United Nations, 2018. Levels and trends in child mortality: report 2018. United Nations Children’s Fund, New York.

Vir, S.C., 2011. Public health and nutrition in developing countries, 1st ed. CRC Press, New Delhi.

WHO, 2007. Promoting safety of medicines for children. World Health Organization, Geneva, Switzerland.

World Health Organization, 2017. WHO Model List of Essential Medicines, 20th list. World Health Organization, Geneva.

World Health Organization, 2016. Guideline: daily iron supplementation in infants and children. World Health Organization, Geneva.

World Health Organization, 2015. WHO Model List of Essential Medicines for Children, 5th list. World Health Organization, Geneva.

Ziegler, E.E., Nelson, S.E., Jeter, J.M., 2009. Iron supplementation of breastfed infants from an early age. Am. J. Clin. Nutr. 89, 525–532. doi:10.3945/ajcn.2008.26591

Appendix A

<Include Figure A.1>

<Include Figure A.2>

Figure captions

Figure 1: Schematic of the Therapeutic Nipple Shield (TNS). The TNS consists of a) a silicon nipple shield device worn during breastfeeding, and b) a dosage form placed within the nipple shield’s teat.

Figure 2: In-vitro testing is performed by means of a breastfeeding simulation apparatus developed by Gerrard et al. (Gerrard et al., 2013). Image adapted from (Scheuerle et al., 2017a).

Figure 3: Schematic of frozen reverse spherification process for the manufacture of iron(III)sulphate pentahydrate liquid-core hydrogels. The gelation occurs by an exchange of sodium ions from the guluronic acid blocks of alginate with calcium cations from the frozen hemispheres, and the stacking of these guluronic acid blocks to form a characteristic “egg-box” structure. One alginate chain can be linked with several other chains through the calcium cations and form a three-dimensional gel network (Paques et al., 2014).

Figure 4: a) Illustration of the compression testing setup, applying vertical compression through the movement of the setup’s upper flat plate. b) Typical force-displacement graph for liquid-core sodium alginate hydrogels containing 29.59 mg ferric sulphate pentahydrate, manufacture by frozen reverse spherification.

Figure 5: Illustration of the liquid-core hydrogel’s deformation during compression testing. Rupture and release of the hydrogel’s liquid core occurs following the formation of a pinhole in image f).

Figure 6: Release from sodium alginate hydrogels into human milk. Cumulative normalised proportion of ferric sulphate pentahydrate released in each fraction over the amount of milk passed through the TNS. Release is represented as a percentage of the total amount loaded within the sodium alginate hydrogels to the total amount released. Each set of points represents the average of three experiments, using the mean of absorbance triplicate measurements for each fraction shown.

Figure A.1: a) Absorbance scan for iron(III)sulphate pentahydrate samples of known concentration at λ =328-1000 nm in human milk. The ferric salicylate's maximum absorbance was measured at λmax = 524 nm. b) Calibration curve of iron(III)sulphate pentahydrate in human milk at λmax =524 nm. All samples were pre-processed by adding hydrochloric acid to the sample to enable absorbance measurements following casein precipitation. Each data point represents the average of triplicate measurements.

Figure A.2: a) Absorbance scan for iron(III)sulphate pentahydrate samples of known concentration at λ =328-1000 nm in DDI water. The ferric salicylate's maximum absorbance occured at λmax = 524 nm. b) Calibration curve of iron(III)sulphate pentahydrate in DDI water at λmax =524 nm. All samples were pre-processed by adding hydrochloric acid to the sample (1:8) to enable absorbance measurements following casein precipitation. Each data point represents the average of triplicate measurements.