Supporting Information

Interface Instability in LiFePO4—Li3+xP1−xSixO4 All-Solid-State Batteries

Matthias F. Groh,‡,1 Matthew J. Sullivan,‡,1 Michael W. Gaultois,1 Oliver Pecher,1 Kent J. Griffith,1 and Clare P. Grey*,1

1 Department of Chemistry, University of Cambridge, Lensfield Road, Cambridge CB2 1EW, UK
*Email: cpg27@cam.ac.uk

‡ These authors contributed equally.

Table S1.	Lattice parameters (in Å) for all components in each Rietveld refinement with respect to literature values. Components with a phase fraction of less than 10 wt-% are greyed due to their higher susceptibility to inaccuracy. In general, all values and especially standard deviations should be taken with a grain of salt due to the abundance of closely related phases (cf. space group types and lattice parameters of references).

|  | A (SPS) | B (SPS) | B (Ampoule) | C (SPS) | C (Ampoule) | “Li1.9FeP0.1Si0.9O4” | reference |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Figures of merit | Rwp: 2.805 Rexp: 6.612 Rp: 2.022 GOF: 0.424 | Rwp: 1.907 Rexp: 1.063 Rp: 1.414 GOF: 1.793 | Rwp: 2.149 Rexp: 1.052 Rp: 1.513 GOF: 2.043 | Rwp: 1.978 Rexp: 1.079 Rp: 1.465 GOF: 1.833 | Rwp: 3.020 Rexp: 1.036 Rp: 1.794 GOF: 2.916 | Rwp: 1.705 Rexp: 0.967 Rp: 1.225 GOF: 1.763 |  |
| LiFePO4 |  | a = 10.3360(6) b = 6.0133(3) c = 4.6970(3) wt-% = 16.6(2) | a = 10.3772(7) b = 6.0247(4) c = 4.7169(3) wt-% = 21.5(3) | a = 10.321(3) b = 6.015(1) c = 4.695(1) wt-% = 5.7(2) |  |  | a = 10.332(4) b = 6.010(5) c = 4.692(2) Pnma3 |
| Li0.6Fe1.4P0.6Si0.4O4 | a = 10.474(4) b = 6.033(3) c = 4.743(3) wt-% = 5.5(2) | a = 10.405(1) b = 6.0297(7) c = 4.7343(6) wt-% = 24.1(3) | a = 10.3925(3) b = 6.0271(2) c = 4.7310(2) wt-% = 30.3(3) |  |  |  | a = 10.4240(1) b = 6.03937(7) c = 4.75676(7) Pnma4 |
| Fe2SiO4 |  |  |  | a = 4.8004(6) b = 10.475(1) c = 6.0782(6) wt-% = 16.8(2) | a = 4.8161(3) b = 10.4795(6) c = 6.0877(3) wt-% = 27.4(2) |  | a = 4.818(1) b = 10.470(2) c = 6.086(1) Pbnm5 |
| Li2FeSiO4 |  |  |  | a = 6.257(1) b = 10.680(2) c = 5.0194(8) wt-% = 6.7(2) | a = 6.220(4) b = 10.667(7) c = 4.941(4) wt-% = 4.5(4) |  | a = 6.2855(4) b = 10.6594(6) c = 5.0368(3) Pmnb2 |
| Li3–xFexP1–xSixO4 | a = 6.1772(3) b = 10.5537(5) c = 4.9540(2) x(Fe) = 0.080(2) wt-% = 61.7(4) |  |  |  |  | a = 6.2602(4) b = 10.6800(8) c = 5.0210(3) x(Fe) = 0.586(7) wt-% = 56.4(4) | cf. Li2FeSiO4 and γ-Li3PO4 |
| γ-Li3PO4 | a = 4.9306(4) b = 6.1233(6) c = 10.4849(8) wt-% = 32.8(3) | a = 4.9278(3) b = 6.1226(4) c = 10.4769(6) wt-% = 35.1(2) | a = 4.92440(9) b = 6.1214(1) c = 10.4805(2) wt-% = 44.6(3) | a = 4.9283(3) b = 6.1252(4) c = 10.4714(7) wt-% = 49.5(4) | a = 4.9278(2) b = 6.1234(3) c = 10.4869(5) wt-% = 66.4(4) | a = 4.92(1) b = 6.20(2) c = 10.48(2) wt-% = 1.8(4) | a = 4.926(3) b = 6.129(1) c = 10.483(4) Pcmn6 |
| Li3.75P0.25Si0.75O4 |  |  |  | a = 5.030(3) b = 6.138(4) c = 5.395(3)  = 91.76(7)° wt-% = 7.5(4) |  |  | a = 5.10536(11) b = 6.11225(12) c = 5.29671(11)  = 90.3692(8)° P21/m7 |
| Graphite |  | a = 2.4577(5) c = 6.7176(3) wt-% = 24.1(2) | a = 2.464(2) c = 6.701(1) wt-% = 3.6(2) | a = 2.455(2) c = 6.7110(7) wt-% = 8.6(2) | a = 2.455(7) c = 6.698(3) wt-% = 1.7(3) | a = 2.4688(7) c = 6.7175(6) wt-% = 27.6(3) | a = 2.464(2) c = 6.711(4) P63/mmc8 |
| FeO (Wuestite) |  |  |  | a = 4.2959(5) wt-% = 1.93(9) |  | a = 4.2625(5) wt-% = 8.1(2) | a = 4.326(2) Fm–3m9 |
| Li2SiO3 |  |  |  | a = 9.398(5) b = 5.326(5) c = 4.697(4) wt-% = 3.3(2) |  | a = 9.392(2) b = 5.392(2) c = 4.661(1) wt-% = 6.1(2) | a = 9.396(1) b = 5.396(1) c = 4.661(1) Cmc2110 |

In well refined cases such as B (SPS), the derived molar ratios of n(Fe):n’(Si) = 5.4 and n(P):n’(Si) = 8.3 agree with the ratios in the starting materials of 5.9 and 8.9, respectively. However, the abundance of closely related phases with small phase fractions as well as the ambiguity of phosphorus/silicon scattering factors lead to stronger deviations in other cases, especially with unaccounted minor by-phases like for case C (Ampoule). The compositions of the refined solid solutions should be viewed as indication of a trend.

Figure S1.	Rietveld refinement of a powder X-ray diffractogram (synchrotron radiation;  = 49.5178 pm) of a batch of C-LFP.

Figure S2.	Rietveld refinement of a powder X-ray diffractogram (synchrotron radiation;  = 49.5178 pm) of a batch of Li3.25P0.75Si0.25O4.

Figure S3.	Powder X-ray diffractograms (Cu-Kα radiation;  = 154.06 pm, 154.43 pm) of C-LFP/Li3.25P0.75Si0.25O4 composites mixed in a 1:2 mass ratio (A) before and after sintering at a range of SPS dwell temperatures. Reference patterns of the starting materials LFP and Li3.25P0.75Si0.25O4 are depicted beneath.

Figure S4.	Powder X-ray diffractograms (Cu-Kα radiation;  = 154.06 pm, 154.43 pm) of C-LFP/Li3.25P0.75Si0.25O4 composites mixed in a 2:1 mass ratio (B) before and after sintering at a range of SPS dwell temperatures as well as in a fused silica ampoule. Reference patterns of the starting materials LFP and Li3.25P0.75Si0.25O4 are depicted beneath. The main Bragg reflection of graphite from the SPS treatment as well from the coating inside the ampoule is marked with an asterisk.

Figure S5.	Comparison of PXRD patterns of C-LFP/Li3.25P0.75Si0.25O4 composites mixed in a 2:1 mass ratio (B), sintered via SPS or annealed in a fused silica ampoule at 800 °C with calculated reference patterns for γ-Li3PO4 and Li1–yFe1+yP1–ySiyO4 with x = 0.4. Graphite reflections from the SPS dies as well as the coating of the ampoule are denoted with an orange asterisk. Residual C-LFP is not marked. See Rietveld refinements in Figures 5 (main text) and S6.

Figure S6.	Rietveld refinement of a powder X-ray diffractogram (Cu-Kα radiation;  = 154.06 pm, 154.43 pm) of a C-LFP/Li3.25P0.75Si0.25O4 composite mixed in a 2:1 mass ratio (B) after annealing in a fused silica ampoule at 800 °C. The ratio of refined phases is indicated by weight percentage.

Figure S7.	Powder X-ray diffractograms (Cu-Kα radiation;  = 154.06 pm, 154.43 pm) of C-LFP/Li3.75P0.25Si0.75O4 composites mixed in a 2:1 mass ratio (C) before and after sintering at a range of SPS dwell temperatures as well as in a fused silica ampoule. Reference patterns of the starting materials LFP and Li3.75P0.25Si0.75O4 are depicted beneath. The main reflection of graphite from the SPS treatment as well from the coating inside the ampoule is marked with an asterisk.

Figure S8.	Comparison of PXRD patterns of C-LFP/Li3.75P0.25Si0.75O4 composites mixed in a 2:1 mass ratio (C), sintered in an SPS or annealed in a fused silica ampoule at 800 °C with reference patterns for γ-Li3PO4 and Fe2SiO4, representing the respective solid solutions. Refined phases with small phase fractions omitted. Graphite reflections from the SPS dies as well as the coating of the ampoule are denoted with an orange asterisk. Black crosses mark unknown phase(s). See Rietveld refinements in Figures 6 (main text) and S9.

Figure S9.	Rietveld refinement of a powder X-ray diffractogram (Cu-Kα radiation;  = 154.06 pm, 154.43 pm) of a C-LFP/Li3.75P0.25Si0.75O4 composite mixed in a 2:1 mass ratio (C) after annealing in a fused silica ampoule at 800 °C. An unrefined, unknown phase is marked with asterisks. The ratio of refined phases is indicated by weight percentage.

Figure S10.	Rietveld refinement of a powder X-ray diffractogram (Cu-Kα radiation;  = 154.06 pm, 154.43 pm) of a SPS-produced (800 °C) sample of the nominal composition of “Li1.9FeP0.1Si0.9O4”. The ratio of refined phases is indicated by weight percentage.

Figure S11.	 31P MAS NMR spectra recorded with a recycle delay of 15 ms for phosphorus-substituted Li2FeSiO4 synthesised in the SPS according to Arachi et al.1 (black, cf. Rietveld fit in Figure S10) and m(LFP):m’(Li3.25P0.75Si0.25O4) = 1:2 (A, red) after sintering at 800 °C. Spinning sidebands are denoted with asterisks. Note the strong signal of the LSPO by-product.

Figure S12.	Visualisation of the local environment of the phosphorus atoms in P-doped Li2FeSiO4 (Pmnb)2 (left) and in LiFePO4 (right)3. Note the additional iron atom (Fe1, shortest P–Fe distance) in the vicinity of the phosphorus atom in LFP while the overall geometric situation is otherwise closely related. Thus, Fe1 is most likely the cause for the difference in the 31P NMR shift of the two compounds and their respective solid solutions.

Figure S13.	 31P MAS NMR spectra recorded with a recycle delay of 15 ms and offset frequency of ~300 kHz for m(LFP):m’(Li3.25P0.75Si0.25O4) = 2:1 (red, B) and m(LFP):m’(Li3.75P0.25Si0.75O4) = 2:1 (blue, C) before and after sintering at 800 °C. The black arrow indicates the carrier frequency. Spinning sidebands are denoted with asterisks.

Figure S14.	Room temperature galvanostatic cycling profiles for thin pellets of sintered C-LFP Li3.25P0.75Si0.25O4 composite powders mixed with Ketjen carbon, Super P carbon, and PTFE binder (3:3:3:1 mass ratio). The C-LFP and Li3.25P0.75Si0.25O4 were mixed in a 1:2 mass ratio prior to sintering at a SPS dwell temperatures of 500 ºC (top; pellet thickness = 260 ± 20 μm) and 600 ºC (bottom; pellet thickness = 220 ± 30 μm). Both samples were cycled at a nominal C/10 cycling rate based on the initial mass of LFP prior to sintering i.e. assuming no reaction. Pellets were cycled against lithium metal anodes using LP30 liquid electrolyte.

Figure S15.	Room temperature galvanostatic cycling profile for a thin pellet (210 μm) of carbon coated LFP mixed with Ketjen carbon, Super P carbon and PTFE binder at a rate of C/10. The pellet was cycled against a lithium metal anode using LP30 liquid electrolyte.

(1) 	Arachi, Y.; Higuchi, Y.; Nakamura, R.; Takagi, Y.; Tabuchi, M. Synthesis and Electrical Property of Li2−xFeSi1−xPxO4 as Positive Electrodes by Spark-Plasma-Sintering Process. J. Power Sources 2013, 244, 631–635.

(2) 	Sirisopanaporn, C.; Masquelier, C.; Bruce, P. G.; Armstrong, A. R.; Dominko, R. Dependence of Li2FeSiO4 Electrochemistry on Structure. J. Am. Chem. Soc. 2011, 133, 1263–1265.

(3) 	Streltsov, V. A.; Belokoneva, E. L.; Tsirelson, V. G.; Hansen, N. K. Multipole Analysis of the Electron Density in Triphylite, LiFePO4, Using X-Ray Diffraction Data. Acta Crystallogr. B 1993, 49, 147–153.

(4) 	Recham, N.; Casas-Cabanas, M.; Cabana, J.; Grey, C. P.; Jumas, J.-C.; Dupont, L.; Armand, M.; Tarascon, J.-M. Formation of a Complete Solid Solution between the Triphylite and Fayalite Olivine Structures. Chem. Mater. 2008, 20, 6798–6809.

(5) 	Della Giusta, A.; Ottonello, G.; Secco, L. Precision Estimates of Interatomic Distances Using Site Occupancies, Ionization Potentials and Polarizability in Pbnm Silicate Olivines. Acta Crystallogr. B 1990, 46, 160–165.

(6) 	Bondareva, O. S.; Simonov, M. A.; Belov, N. V. Crystal Structure of the Synthetic Analog of Lithiophosphate, γ−LiPO4. Dokl. Akad. Nauk SSSR 1978, 240, 75–77.

(7) 	Deng, Y.; Eames, C.; Chotard, J.-N.; Lalère, F.; Seznec, V.; Emge, S.; Pecher, O.; Grey, C. P.; Masquelier, C.; Islam, M. S. Structural and Mechanistic Insights into Fast Lithium-Ion Conduction in Li4SiO4–Li3PO4 Solid Electrolytes. J. Am. Chem. Soc. 2015, 137, 9136–9145.

(8) 	Trucano, P.; Chen, R. Structure of Graphite by Neutron Diffraction. Nature 1975, 258, 136–137.

(9) 	Fjellvåg, H.; Grønvold, F.; Stølen, S.; Hauback, B. On the Crystallographic and Magnetic Structures of Nearly Stoichiometric Iron Monoxide. J. Solid State Chem. 1996, 124, 52–57.

(10) 	Völlenkle, H. Verfeinerung Der Kristallstrukturen von Li2SiO3 und Li2GeO3. Z. Für Krist. - Cryst. Mater. 1981, 154, 77–81.