Characterising Degradation of Perovskite Solar Cells through In-situ and Operando Electron Microscopy

Felix Utama Kosasiha,* and Caterina Ducatia

aDepartment of Materials Science & Metallurgy, University of Cambridge, 27 Charles Babbage Road, Cambridge CB3 0FS, United Kingdom

*Corresponding author. E-mail addresses: fuk21@cam.ac.uk, cd251@cam.ac.uk

Declarations of interest: none

Keywords: perovskite; photovoltaics; stability; degradation; electron microscopy; in-situ characterisation

Abstract: Organic-inorganic hybrid perovskite solar cells have exhibited power conversion efficiencies comparable to more established PV technologies thanks to their favourable optoelectronic properties, but low operational stability inhibits their commercialisation and widespread use. Many degradation pathways are possible and most of them are not currently well understood at the nanoscale due to the difficulty of characterising a perovskite solar cell’s complex nanostructure. This work reviews the application of in-situ and operando electron microscopy to visualise the dynamic processes that occur in perovskite solar cells as various stimuli are applied inside a microscope column. Additionally, potential challenges and an outlook on future uses of this technique are briefly discussed.

- Introduction

Through the past eight years, the rapid rise in performance of organometal halide perovskite solar cells (PSCs) has brought great interest from the scientific community. Since Kojima et al. reported a perovskite-sensitised cell with 3.8% power conversion efficiency (PCE) in 2009 [1], the record PCE for PSCs has multiplied almost sixfold to 22.1% [2]. This impressive feat is due to perovskite’s favourable optoelectronic properties, such as high optical absorption coefficient at the visible light region with sharp absorption onset and low Urbach energy [3–7], low exciton binding energy [7–10], tuneable band gap values [11–15], relatively benign trap states and grain boundaries [16–19], defect tolerance [17,20], and high carrier mobility and lifetime which translate to high carrier diffusion length [21–23]. These advantageous characteristics are further optimised through careful manipulation and selection of the perovskite crystal composition [2,11,12,24–27] and dimensionality [28–31], cell architecture [32–34], film synthesis and deposition process [35–38], charge-selective contacts [39–42], and interface passivation [43–45].

In PSCs, organometal halide is the most commonly used type of perovskite with a generic formula of ABX3 where A is a monovalent organic cation, B is a divalent metal cation, and X is a monovalent halide anion. A is usually either methylammonium (MA+, CH3NH3+), formamidinium (FA+, HC(NH2)2+), or a combination of the two. There have also been attempts to use larger organic cations such as n-butylammonium (BA+, C4H9NH3+) [28,31] or phenylethylammonium (PEA+, C6H5C2H4NH3+) [46,47], normally resulting in two-dimensional perovskites where the metal halide octahedra share corners and form planes sandwiching the large organic cations. B is almost always either lead (Pb2+) or tin (Sn2+), with lead being the preferred choice due to tin’s fast oxidation to its +4 state and consequent reduction in performance [48,49]. There have been numerous attempts to widen the range of potential B cations by forming non-traditional perovskite crystal structures, such as antimony (Sb3+) or bismuth (Bi3+) in a dimer perovskite (A3B2X9) and a combination of one monovalent cation (e.g. copper (Cu+) or silver (Ag+)) and one trivalent cation (Sb3+ or Bi3+) occupying unequal B positions in a double perovskite (A2BB’X6), but each one of these combinations currently has unresolved drawbacks in terms of PCE and stability [50–53]. Very recently, Chen et al. published an exciting work where Cs2TiBr6 is used for the first time in a solar cell. Their device reached a stabilised PCE of 3.3% and showed promising phase and environmental stability, opening the doors to a family of Ti-based perovskites for solar cell applications [54]. The X anion can be either chloride (Cl-), bromide (Br-), iodide (I-), or a mixture of them. Choice of composition will usually affect the cell’s band gap, crystallography, and stability [2,11,12,24–27].

Unfortunately, commercialisation of PSCs is currently inhibited by their poor operational stability in comparison with the market-dominating crystalline silicon solar cells. Whereas silicon cells can be guaranteed to last for 25 years in normal operating conditions, PSC degradation occurs in the timeframe of days to months at best. This low stability is mainly caused by hybrid perovskites’ sensitivity to various environmental factors, most importantly heat [55], moisture [56–58], light [59–66], and oxygen gas when under illumination [67–70]. Since these four factors will always be present in a terrestrial solar cell’s operating environment, developing perovskites with greater inherent resiliency against them is crucial if PSCs are to be used on a large scale. Contact with moisture and oxygen gas can be prevented by encapsulation of the cell [32,71–73], but this step adds to the cost of cell manufacture and cannot thoroughly protect the cell from thermal and light-induced degradation [55,74,75]. Based on previous studies, other techniques which have been proposed to ameliorate the effect of external factors on stability of PSCs include using hydrophobic and dopant-free contacts [38–40,76,77], cation/anion mixing [11–13,26,27], and adding an Al2O3 or Sb2S3 blocking layer between the perovskite and contacts [44,78–80].

In addition to external causes of degradation, internal factors may also contribute to PSCs’ poor stability. Internal degradation is primarily caused by structural instability and ion migration. Previous studies on the structural stability of perovskites have identified two key parameters calculated from the radii of perovskite-forming ions, known as octahedral factor μ and Goldschmidt’s tolerance factor t. The value of μ needs to be above 0.422 and t should be close to 1 in order to achieve a stabilised cubic phase [81,82]. These two factors are defined as follows, where rA, rB, and rX are the ionic radii of the elements composing ABX3.

μ=rBrX				t=rA+rX2(rB+rX)

A particularly well-known example of this requirement is FAPbI3’s spontaneous phase change from the optically active, black cubic α phase to inactive, yellow hexagonal δ phase in ambient conditions [21,25]. Changing a certain percentage of the FA+ cations with smaller ones, such as MA+ or caesium (Cs+), brings the overall tolerance factor closer to unity and preserves the α phase [27,83,84]. Ion migration is another major problem, with both electrical and structural implications. I- and MA+ ions can migrate with low activation energies through vacancies [85–87] and accumulate near the perovskite-contact interface, resulting in reduced photocurrent and, together with the presence of traps, hysteresis in the J-V curve [88,89]. In addition, photoinduced iodide migration has been proposed as the first step in the degradation of MAPbI3 to HI, CH3NH2, MAI, and PbI2 [85,86,90] and also the cause of phase segregation in mixed-halide perovskites [60–62].

It is difficult to accurately characterise PSC degradation due to its complex architecture and multi-layered structure. While a crystalline silicon solar cell is almost exclusively composed of silicon, an efficient PSC needs to have a perovskite layer as the light absorber, a hole transport layer (HTL), an electron transport layer (ETL), and top and bottom electrodes. Compounds commonly used for HTL include 2,2’,7,7’-tetrakis-(N,N’,di-p-methoxyphenylamine)-9,9’-spirobifluorene (spiro-OMeTAD), poly(3-hexylthiophene-2,5-diyl) (P3HT), polytriarylamine (PTAA), poly(3,4-ethylenedioxythiophene):polystyrenesulfonate (PEDOT:PSS), carbon, CuSCN, and NiO [91]. The range of ETL materials is no less diverse, for example TiO2, ZnO, SnO2, fullerene, and phenyl-C61-butyric acid methyl ester (PCBM) [92]. These carrier transporting layers may sometimes contain various dopants and additives, such as Li-bis(trifluoromethanesulfonyl)imide (Li-TFSI) and tert-butylpyridine (tBP), adding to the complexity of tracing the cause of cell degradation. Each layer’s thickness ranges from 50 to 500 nm, and they are often porous or nanostructured. Furthermore, there is currently a strong momentum in the direction of mixed-cation, mixed-halide perovskite due to the ions’ complementary nature in terms of enhancing efficiency and stability. PSCs can now contain a perovskite layer composed of up to 4 A cations, normally some combination of rubidium (Rb+), potassium (K+), Cs+, MA+, and FA+, and 2 X anions of either Cl-, Br-, or I-. Figure 1 shows an energy band diagram of most commonly used materials in PSCs.

Figure 1 | Energy band diagram of common PSC materials. The numbers are in eV and 0 eV refers to the vacuum level. [92–94]

In this work, we review the effort to characterise the degradation of PSCs by in-situ and operando scanning or transmission electron microscopy (SEM/TEM, henceforth referred simply as in-situ EM). Although Nanova et al. have pioneered the use of analytical TEM to characterise PSCs since 2014 [95], it took two years for the first in-situ EM study of PSC degradation to be published [96]. In-situ EM is an invaluable technique to gain a deeper understanding of PSC degradation mechanism as more advanced sample holders, data recorders, and data processing software now allow researchers to conduct a wide variety of experiments inside an SEM/TEM column with precisely calibrated stimulus, high spatial, temporal, and spectral resolutions, and real-time image and data acquisition followed by accurate data analysis. Currently, it is possible for cutting-edge TEMs to reach sub-Ångström spatial resolution [97], temporal resolution in the order of femtoseconds [98], and spectral resolutions of ~120 eV and ~10 meV for energy dispersive X-ray spectroscopy (EDX) and electron energy loss spectroscopy (EELS) respectively [99], although in most cases not all at the same time. For standard TEMs, the limits which still allow sufficient signal collection are about 1 nm for spatial resolution, microseconds for temporal resolution, and ~130 eV and ~1 eV for EDX and EELS spectral resolution [100].

Reliable in-situ TEM experiments are enabled primarily by the invention of sample holders capable of applying various kinds of stimuli on the sample through dedicated software programs created by the manufacturers. Older heating holders are not very reliable because the sample grid and the heating filament are separated, so temperature uniformity across the sample cannot be achieved. This imbalance, in turn, may distort the sample and exacerbate thermal drift. The advent of microelectromechanical system (MEMS) chips enable fast and uniform heating and quenching with high thermal and spatial stability. A high-end heating holder can reach 1,300oC with 0.005oC stability while maintaining the TEM’s native spatial resolution over a large viewing area [101]. Furthermore, the same MEMS chip technology can be used to electrically bias samples. Several holders can do heating and biasing simultaneously since the required components can be fitted into a single chip [102,103]. These chips can apply a DC or AC electric potential of up to ~100 volts and measure current down to the order of picoamperes. The holder itself is optimised to allow low drift rate, reduced membrane bulging, and high tilting range. Other than heating and biasing, TEM samples can be exposed to moisture and other gases through specialised gas holders designed as a reaction chamber [104–106]. These holders can accommodate pressures of up to ~1 atm in sealed chambers equipped with electron-transparent silicon nitride (SiNx) windows. These chambers are designed such that the gas volume is as thin as possible to minimise electron scattering by the gas particles, enabling atomic resolution even at high pressures. In-situ experiments can be run with a static volume of gas or with a dynamic, continuous flow through the sample holder. For the latter case, a gas supply system must be used. This system is responsible to measure and control the gas pressure and flow rate and also to mix different gases with user-specified compositions in systems with multiple inlets. It is now possible to integrate a heating MEMS chip into the gas chamber to enable simultaneous heating and gas exposure. One extremely important thing to remember is that the microscope’s vacuum integrity will be compromised if there is a leak in the gas holder, so a leak test procedure is necessary before inserting the holder into the microscope column. Other types of in-situ sample holders not relevant in the context of this review are also widely used in other experiments, such as liquid cell holder, straining holder, cooling holder, and magnetising holder. Holders with illumination systems are not yet commercially available and will be discussed separately in section 3 below.

Degradation characterisation was previously limited to post-mortem observations, in which a before-after comparison of the cell is made and the knowledge gap in between is filled by tracing back and interpolating the changes. With in-situ observations, we can see and measure dynamic processes on the cell as the stimulus is applied in the order that they happen, up to the microscope’s temporal resolution and minimum detection limit. Obtained data can include standard bright field or dark field images and spectrum images of EDX or EELS. The high sampling rate and resolutions result in very large datasets, especially when spectrum images are involved. Development of tools for big data analysis such as multivariate analysis algorithms and machine learning now allow scientists to extract meaningful patterns and information from these datasets with relatively short processing time. A particularly well-known algorithm is principal component analysis (PCA), which can be used to denoise the data and reduce its dimensionality according to principles of statistics, allowing us to obtain the details we need faster and more easily. However, in-situ EM also has its side effects, with cell damage from the high-energy electron beam being the most pressing. We will end this review with ways to minimise these side effects and a brief outlook on in-situ EM.

- Thermal Treatment

Within the wide range of temperatures that solar cells may be exposed to during operation, it is fortunate that most of the widely-studied perovskites do not undergo any performance-compromising phase change. While MAPbI3’s crystal structure is expected to change from tetragonal to cubic as its temperature rise above 55oC [107,108], both phases perform well as light absorbers and thus this transition does not have a significant impact on the PCE [109,110]. Both MAPbCl3 and MAPbBr3 have a stable cubic structure at room temperature and their transition temperature to tetragonal phase is below normal operating temperature range of a solar cell [107,108]. The problem of FAPbI3’s transition between its α and δ phase is already solved as mentioned above, while the α phase’s transition into β and γ phases occur only upon cooling to about -70oC and -140oC respectively [21]. While the phase transition temperatures of more exotic compositions have not been accurately determined, those which have stable cubic structures at room temperature are not expected to undergo any further phase change upon heating. The primary cause of thermal degradation, therefore, is not phase transition but thermal decomposition of the perovskite into its organic and inorganic components. Thermogravimetric analysis of MAPbI3 has actually shown that it is very stable, with sublimation of HI and CH3NH2 observed at 250oC [111]. However, there is still a possibility that sublimation may occur at lower temperatures, albeit at a much slower rate. For example, MAPbI3 decomposition into HI, CH3NH2, PbI2, and metallic lead has been shown by Conings et al. after heating to 85oC in an N2-filled glovebox for 24 hours [55].

Thermal treatment was the first kind of stimulus whose effect on degradation was investigated through in-situ EM. Divitini et al. heated mesosuperstructured MAPbI3 cells inside a TEM column and discovered that the degradation pathway is highly dependent on the cell’s fabrication route [96]. All four devices examined here share the same structure of fluorine-doped tin oxide (FTO)/compact TiO2/mesoporous TiO2/MAPbI3/spiro-OMeTAD/gold (Au), but each one has its MAPbI3 layer deposited with a different technique. The recorded EDX data were subsequently processed with PCA algorithm to maximise the signal-to-noise ratio and analysed in conjunction with high-angle annular dark field (HAADF) images. Iodine and lead migration was identified as the primary cause of perovskite degradation and a correlation was observed between migration of these two elements and exposure of the perovskite layer to ambient air during the synthesis step. In samples prepared either in vacuum or in a glovebox, lead and iodine migrated from the perovskite layer to the interface with FTO and formed PbI2 particles there. On the contrary, in a sample fabricated in air, iodine and lead migrated towards the gold electrode (Fig. 2). The authors concluded that migration of iodine and lead to FTO and its agglomeration into PbI2 there is preferred because FTO has a rougher surface introduced by the focused ion beam (FIB) milling sample preparation step. In the air-exposed sample, this preference was overridden because oxygen and water in the perovskite film introduced pinning sites which prevented elemental migration to FTO. Moreover, perovskite degradation was only observed when the samples were heated to beyond 150oC and it was suggested that PCE’s decrease at lower temperatures was related to heating response of the HTL and its dopants instead as the only other cell component vulnerable to heating, which agrees with literature [112]. Unfortunately, the mechanism of this HTL degradation was not further investigated because spiro-OMeTAD is entirely composed of light elements, resulting in TEM images with very low contrast. It also remains to be seen whether iodine and lead will still migrate to FTO if the sample was not prepared via FIB milling, and why the oxygen and water-induced pinning sites did not prevent diffusion to the gold electrode.

Figure 2 | Elemental migration inside a PSC upon heating. HAADF images (top row) and elemental EDX maps for lead (middle row) and iodine (bottom row) of a sample fabricated in air at set temperatures. Both elements can be seen migrating towards the HTL. Heating steps were conducted for 30 minutes from 50oC to 175oC and 15 minutes afterwards to accommodate the faster dynamics. Scale bar applies to all panels. Reprinted with authors’ permission from ref. [96].

Other in-situ TEM studies of MAPbI3 show that thermal decomposition can be accelerated when other stimuli are put on the cell. Yang et al. identified significant change in HAADF intensity from their FIB-milled sample device (indium-doped tin oxide (ITO)/TiO2/MAPbI3/spiro-OMeTAD/Ag) upon heating to 50-60oC, but only in areas which have already been damaged by the electron beam (Fig. 3) [113]. It was therefore proposed that thermal-induced elemental migration may be aided by defects in the crystal structure. This is in good agreement with the general consensus that both Schottky and Frenkel defects are effective migration channels [114,115]. It should be noted that heating in this study was done with a halogen lamp and the authors were not able to conclusively disentangle the effects of heat and light in the cell degradation.

Figure 3 | HAADF images of a PSC undergoing thermal degradation after beam damage. The cell was kept for 30 days in vacuum and subsequently heated at ~50-60oC. The dashed box in Day 30 image marked areas of beam damage. After heating, perovskite decomposition was only observed inside this box. Bright particles observed in Day 1 image were most likely caused by FIB milling and disappeared the next day. Adapted with permission from ref. [113]. Copyright 2016 American Chemical Society.

Unlike the previous two reports which used full devices for samples, Fan et al. heated an MAPbI3 film in vacuum and dry ambient air and observed similar decomposition pathways in both cases [116]. Upon heating at 85oC in a calibrated heating and gas reaction cell, MAPbI3 was shown to degrade to PbI2 as deduced from transformed lattice fringes and selected area electron diffraction (SAED) patterns (Fig. 4). By identifying a few unchanged diffraction spots in the otherwise altered SAED pattern, the degradation mechanism was revealed to be a sequential transition. Combining this discovery with DFT calculations, it was concluded that MAPbI3 decomposition proceeds through layer-by-layer decomposition to PbI2, with each decomposed layer exposing the next. The authors argued that this mechanism should be more likely compared to bulk decomposition given its lower activation energy. In fact, the difference in activation energy is sufficiently large that surface decomposition was calculated to be three orders of magnitude faster than bulk decomposition. Further, it was also shown that this decomposition could be decelerated by coating the surface of MAPbI3 with a thin layer of hexagonal boron nitride (hBN) which increased the energy barrier of MAPbI3 exfoliation.

Figure 4 | Real-time evolution of SAED pattern of MAPbI3 upon heating. After 400 s of heating at 85oC (top row), the symmetry changed from tetragonal to trigonal characteristic of PbI2. After coating with hBN, MAPbI3’s tetragonal symmetry did not change on heating (bottom row). Scale bar is 2 nm-1 and applies to all panels in the same row. Reprinted from ref. [116], copyright 2017 with permission from Elsevier.

Comparing the three in-situ works discussed above, the higher onset of thermal degradation observed in

Divitini et al.’s experiments [96] may be caused by the vacuum environment and the shorter heating period (c.f. Conings et al. [55]) or by other layers in the device protecting the perovskite and blocking the escape of sublimated HI and CH3NH2 (c.f. Fan et al. [116]). Taken together, these studies have shed light on how thermal decomposition occurs in PSCs and provided us with clues to engineer designs which are more robust towards it. It seems that the onset temperature for thermal decomposition can be significantly increased if the cell is in a vacuum environment, which may mean cells encapsulated in vacuum can last longer. Of course, the encapsulation must be completely leak-proof to prevent entry of atmospheric gases and to maintain vapour pressures of HI and CH3NH2 inside the sealing, thus preventing further sublimation of the perovskite. Suitable contacts should not only possess high electrical conductivity and favourable energy levels but also passivate and stabilise the surface of perovskite films such that layer-by-layer decomposition can be suppressed. Finally, further research should be conducted to investigate possible thermal degradation in non-perovskite layers, especially the HTL and gold contact.

- Illumination

It is arguable that light-induced degradation is the most worrying aspect of PSC stability, as a solar cell must be under illumination and the consequent electrical bias if it is to generate power. Unfortunately, there is a myriad of ways through which light can decrease the performance of PSCs. Light has been reported to cause formation of PbI2 from MAPbI3 [59], phase segregation in mixed-halide perovskites [60–62], gold and iodine diffusion across a cell [63,64], deterioration of interfacial chemical bonding between spiro-OMeTAD and Au [65], and creation of deep trap sites in the mesoporous TiO2 layer [66]. Although many mechanisms have been proposed in literature to explain various strains of light-induced degradation [117], this problem is still an open question for the photovoltaics community.

It is therefore regrettable that only one in-situ EM study has been conducted to investigate light-induced degradation in PSCs. Yuan et al. used a modified environmental SEM fitted with high-numerical aperture oil-immersion objective lens and laser illumination system to conduct simultaneous luminescence and high-resolution scanning electron microscopy. They observed changes in the morphology and photoluminescence (PL) spectra of a MAPbI3 film when a high-intensity monochromatic laser beam (I = 500 W/cm2, λ = 532 nm) was shone on it (Fig. 5) [118]. The authors concluded that photogenerated charges cause random currents of charged species. This randomised migration of ions means HI and CH3NH2 can sublimate from all surfaces, including surfaces of grain boundaries. The resulting reduction in perovskite film thickness caused a decrease in the PL intensity. Note that this importance of surfaces in degradation stressed by Yuan et al. agrees well with Fan et al.’s study covered in the previous section and reiterates the necessity of choosing surface-passivating contacts.

Figure 5 | Effect of laser illumination on a PSC. SEM micrograph acquired before illumination (a). PL image (b) and SEM micrograph (c) acquired after 500 W/cm2 laser illumination was applied for 12 s. Significant morphology change can be seen from the SEM images. The scale bar applies to all panels. Adapted with permission from ref. [118]. Copyright 2016 American Chemical Society.

Obviously, there are still many gaps in our understanding of light-induced degradation of PSCs. Future in-situ EM work should focus on trying to confirm degradation mechanisms which have been proposed in published literature. Therefore, observation of full devices in a TEM is needed as it can provide a more complete picture of all possible degradation pathways, both within and outside the perovskite film itself. Given the rising prominence of mixed-cation, mixed-halide perovskites in the race to ever-higher PCE, it is particularly important to visualise halide segregation in real-time and conclusively identify why and how it is triggered by light. To achieve these goals, an in-column illumination system allowing for precise control of emission spectrum will be needed, which should ideally be polychromatic and as close as possible to the AM1.5 solar spectrum to replicate a real-life cell’s operating conditions. Very recently, Domanski et al. have noted that white LEDs can be a feasible replacement to the AM1.5 spectrum [119]. This greatly ease the requirement for in-situ EM illumination study, but assumes that the cell will be protected with UV-proof encapsulation in real life. Additionally, extra care should be taken to minimise damage from the electron beam as it is especially difficult to decouple the effects of light-induced degradation and beam damage. Several techniques have been proposed to shine light on a TEM sample, either through the sample holder itself or an optical fibre, but so far these systems have never been used for PSC characterisation to the best of the authors’ knowledge [120–122]. In a system attached to a sample holder, the light source will be inside the microscope column during operation. Hence, changing light sources is not possible without breaking vacuum in the sample chamber. This design is preferred in terms of its portability and adaptability to different microscopes but the tiny available space inside a TEM column limits the type and number of feasible light source and some machining of the holder will be necessary. Moreover, sample holders which are already designed for other stimuli are unlikely to be compatible with this illumination system model, restricting researchers’ ability to apply multiple stimuli at a sample. Conversely, an optical fibre-based system is much more versatile as it can be coupled to any light source but the whole appendage will be fixed to a particular microscope. The fibre end must be carefully positioned inside the microscope column. Putting it too far from the sample will result in a large illumination cone at the sample, producing a beam with low intensity. If it is too close, it may disrupt the sample holder as it is tilted.

- Ambient Conditions

Atmospheric degradation is generally not considered a major cause of worry in PSC degradation as devices can always be encapsulated to prevent exposure to oxygen and water. Nonetheless, they can be very harmful to non-encapsulated cells and therefore increasing the stability of PSCs against degradation caused by these two compounds is still a priority. More robust cells would allow for simpler and cheaper encapsulation material and procedure, hopefully no more complicated than existing ones currently used for other thin-film solar cells.

It has been established that exposure to oxygen is harmless if the device is not under illumination, as perovskite is not oxidised in its ground state [32,123–125]. Unfortunately, oxygen-induced degradation has been observed when a perovskite film is exposed to light as excited electrons in the conduction band get oxidised by molecular oxygen [67–70,126]. Aristidou et al. have proposed a mechanism for this light-assisted degradation, in which molecular oxygen captures an excited electron to become a superoxide anion O2-, which subsequently deprotonates the MA cation in MAPbI3 to produce CH3NH2, PbI2, I2, and water [68]. The first step in this mechanism is key to minimising this form of degradation. If the excited electrons can be transferred to the ETL and contact before they react with oxygen, then perovskite decomposition can be prevented. Thus, an electron-selective layer possessing wide interfacial area with perovskite and excellent electronic coupling is required.

Unfortunately, atmospheric oxygen gas is not the only source of oxygen which can degrade PSCs. Jung et al. have investigated a PSC with a structure of glass/FTO/compact TiO2/mesoporous TiO2/MAPbI3/spiro-OMeTAD/Au in a TEM to discover that oxygen ions from the mesoporous TiO2 layer can diffuse into the perovskite film upon biasing (Fig. 6) [127]. The sample was forward biased at 1 V via an electrical biasing sample holder to mimic illuminated conditions, creating an operando scene inside the TEM column. Analysis of the features in EEL spectra revealed that the mesoporous TiO2 layer was transformed to Ti2O3, oxygen diffused into MAPbI3 region, and the bulk plasmon peak of MAPbI3 was changed to resemble that of metallic lead instead. Very recently, Dr. Jung informed the authors through personal communication that all Ti and O features in the EEL spectra changed back to their original conditions after the biasing was stopped. This study has significant importance because it potentially shows that even when a device is completely shielded from atmospheric oxygen through encapsulation, it can still be reversibly degraded by oxygen from TiO2.

Figure 6 | Effect of electrical biasing on the EEL spectra of TiO2 and MAPbI3. Core-loss EELS line profiles of TiO2 (a) and MAPbI3 (b) and low-loss line profiles of TiO2 (c) and MAPbI3 (d). Significant oxygen penetration into the capping MAPbI3 layer can be seen by comparing the spectra. Reprinted with permission from ref. [127]. Copyright 2017 Cambridge University Press.

Moisture degradation of PSCs is not a pressing topic for in-situ EM study because the mechanism has already been conclusively determined by Leguy et al. with ellipsometry and X-ray diffraction (XRD) [56]. The problem of moisture degradation is complicated by three factors. First, it is greatly accelerated if the cell is heated, a condition at which the degradation process also becomes completely irreversible [77]. Second, the decomposition also runs more rapidly when the cell is electrically biased, which is the normal condition of an illuminated solar cell [128]. Third, similar degradation mechanisms can also be brought about by other polar solvents, such as isopropanol and DMF [128]. This last factor stresses the importance of careful choice of solvents used in the film synthesis process and complete evacuation of solvent remnants. A summarised mechanism of moisture-induced MAPbI3 degradation, taking into account the effects of heat and electric field, has been proposed by Leijtens et al [128]. It is worth mentioning that even though FAPbI3 is not any more resistant to moisture compared to MAPbI3, mixing FA+ and Cs+ cations on the A site does show promising results in humidity tests due to weaker hydrogen bonding between them and water [26,83,129].

While observing in-situ crystallisation process of FAPbI3 in a low-energy STEM, Aguiar et al. used HAADF imaging and high-resolution valence EELS to discover adsorption of H+ and OH- ions at the grain boundaries (Fig. 7). The authors proposed that these ions may have come from residual water vapour trapped at the grain boundaries during film synthesis and speculated that the same process may also play a part in moisture degradation in normal operation [130]. This discovery prompted a follow-up in-situ study by the same group on FAPbI3-xClx sample inside an electron-transparent gas STEM cell equipped with a heating chip. The STEM probe was monochromated to maximise EELS energy resolution and set at a low beam current (< 86 pA) to minimise beam damage. Quantitative analysis of the EELS and EDX spectra found that the presence of water vapour during film synthesis either eliminates or at least reduces the amount of chlorine inside the perovskite crystals [131]. This study shows that chlorine bonds are easily broken by water vapour, raising the need to ensure that mixed-halide PSCs are synthesised in dry conditions in order to achieve the desired perovskite stoichiometry.

Figure 7 | STEM image and valence EELS spectra of a FAPbI3 cell. White arrow in (a) marks the acquisition direction for EEL spectra in (b). The raw spectra were then processed to subtract the silicon nitride window background, allowing comparison of the hydrogen, OH-, and lead peaks between grain interior and boundary regions (c). Reproduced with permission from ref. [130] with permission from the Royal Society of Chemistry.

To close this section, it is instructive to cover an experiment by Yang et al. where a cell was left in a TEM column with a vacuum level of ~ 10-7 Torr for 30 days straight [113]. Lead particles were observed near the perovskite’s top surface on the first day, but they disappeared on the following day. Surprisingly, additional lead particles created through electron beam-induced perovskite degradation also disappeared after storage in the vacuum condition. Yang subsequently concluded that the vacuum was unlikely to cause degradation in PSCs. This inference is counterintuitive because the TEM vacuum system’s pumps should have sucked away any CH3NH2 and HI vapour in the sample chamber, leading to further sublimation from the perovskite. Moreover, it is also non-trivial because a similar situation occurs in gloveboxes and other containers with continuous flushing of inert gases. A possible explanation for this observation is that the cell’s other layers were responsible to trap the vapour molecules inside the cell.

- Electrical Biasing

The response of PSCs to applied electrical bias has become a major topic of study due to perovskite’s high ionic conductivity and low formation energy of various Schottky and Frenkel defects. Previous theoretical works by Eames et al., Azpiroz et al., and Haruyama et al. have shown that vacancy-mediated migration of I-, MA+, and FA+ ions have low activation energies in the order of ~0.1-0.8 eV, comparable to ion conductors [85–87]. In biased conditions, these ions can migrate easily and accumulate at the perovskite/contact interfaces, screening the applied electric field and consequently altering the cell’s built-in voltage and charge collection efficiency [88]. This ion migration has a wide-ranging impact on the performance of PSCs, from contributing to the J-V curve hysteresis [89,132] to causing irreversible structural damage in ambient air [128]. Unger et al. have also suggested that the ionic conductivity of MAPbI3 may be increased even higher when it is illuminated, potentially exacerbating the problem [133].

Jeangros et al. conducted an in-situ biasing experiment with a cell architecture of n-type silicon/ITO/PCBM-polyethylenimine/MAPbI3/spiro-OMeTAD/Au [134]. They found that nanoparticles started to appear at the perovskite/HTL interface and at positions where there were structural defects within minutes of a +6 V bias being applied. The perovskite/HTL interface line was retracted towards the perovskite while the HAADF intensity in the HTL side of the interface grew brighter (Fig. 8). HAADF brightness is proportional to atomic number, so this observation signifies migration of either lead, iodine, or both from the perovskite into the HTL. When a negative bias was applied, the cell entered breakdown regime. Again, nanoparticles were visible at the perovskite/HTL interface, but this time voids were also formed at the perovskite/ETL interface. Subsequent HRTEM imaging and EDX analysis showed that the nanoparticles were PbI2, in good agreement with the HAADF intensity rise. Furthermore, combined EDX data of the perovskite and HTL layers revealed a decreased I/Pb atomic ratio compared to pre-bias condition, suggesting that some iodine have sublimated. Most of these observed changes were largely replicated in a parallel ex-situ experiment, showing that the effect of beam damage and vacuum conditions were minimal.

Figure 8 | Elemental migration induced by electrical bias. HAADF images (left) and intensity profile integrated over the green shaded area (right) for cells under forward bias (a) and reverse bias (b). Arrows and circles highlight the formation of PbI2 nanoparticles and the shrinking MAPbI3 layer. Arrowheads show a polarity-dependent increase in HAADF intensity at the charge transport layers. Reprinted with permission from ref. [134]. Copyright 2016 American Chemical Society.

It is also important to bear in mind that in PSCs, interfaces and defects may introduce localised aberrations in the electric field. A region of relatively higher concentration of charged point defects can act as local dopants, exerting its own electric field whose direction is not necessarily aligned to the cell’s built-in field [114]. Dangling bonds and other imperfections at the perovskite surface and grain boundaries may become sources of local trap states, enabling non-radiative charge recombination and decreasing the cell potential [43,86]. To properly account for the effects of these abnormalities, EMs can be used to map and even quantitatively measure the electric field in a sample through techniques such as electron holography, Lorentz TEM, and differential phase contrast imaging [135–138].

An interesting avenue of future research would be to combine in-situ illumination and electrical biasing to examine how pre-biasing affects the ion migration paths during illumination. Another promising direction is to conduct in-situ voltage sweep of cells with known degrees of J-V hysteresis, ranging from negligible to severe, and compare the speed and extent of ion migration across cells.

- Challenges

Although in-situ EM is a powerful technique to study degradation mechanisms in PSCs, it does have several complicating factors. The most harmful is a possibility that damage observed in the sample was actually caused or at least aggravated by the high-energy electron beam. Xiao et al. provided direct evidence that electron irradiation damage on perovskite worsens with increasing acceleration voltage, probe current, and exposure duration [139], while Yuan et al. spotted film thinning and band gap tuning in their perovskite sample after electron beam scanning [118]. Beam-induced iodide segregation, similar to photo-induced halide segregation reported in mixed-halide PSCs, has also been reported through SEM cathodoluminescence (Fig. 9) [140]. This scenario can never be eliminated as high-energy electrons are necessary to probe the sample, but the severity can be significantly minimised by cooling the sample and adopting low-dose microscopy techniques. The most helpful step is to operate in STEM mode, such that only the sample section currently being probed is exposed to the electrons. Minimise the current by using a small objective aperture and large spot size, while keeping it high enough to generate meaningful images and spectra. Always blank the beam or park it outside the sample while no measurement is being made, minimise dwell time, and try to use a lower acceleration voltage. Naturally, low-dose techniques result in lower signal-to-noise ratio and image contrast. These cannot be fixed by frame averaging as it defeats the very purpose of in-situ EM itself, which is to observe dynamic processes. Fortunately, more efficient detectors and data processing can help us ameliorate this problem. A method to check for beam effects is to subject a section of the sample to the same imaging/profiling procedure without applying the stimuli (heating, biasing, etc) and assess its conditions afterwards.

Figure 9 | Time evolution of SEM cathodoluminescence (CL) spectra of MAPbI3. Yellow arrows indicate quenching of the CL emission from the perovskite band gap with slight blue shifting while another high-energy peak appears and blue-shifts. A spectrum is obtained every 5 seconds for 255 seconds. Reprinted with permission from ref. [140]. Copyright 2016 American Chemical Society.

The next complicating factor is the high vacuum environment inside an EM. The decomposition products of PSCs, such as HI, CH3NH2, or MAI should have been sucked immediately by the EM’s pump system as soon as they are evolved in the EM column. This means the perovskite decomposition process will never reach equilibrium. However, Yang et al.’s experiment has proven that a complete cell can survive an EM vacuum for 30 continuous days, hinting that the decomposed gases may diffuse more slowly in the dark or were trapped inside the cell by the device layers [113]. An alternative method to prevent removal of the product gases is to use a gas cell with electron-transparent windows, but this usually comes at the price of reduced spatial resolution and possible outward bowing of the silicon nitride membrane causing increased gas path length at the centre of the cell, further compromising spatial resolution.

With regards to the EM hardware, particularly in TEM, an additional complication is the minimal space available within the sample chamber. The objective lens and apertures, cold-finger, and EDX detector(s) are normally very close to the sample holder, leaving almost no space to place an illumination system or other stimuli sources. Aberration correctors can be used to allow larger pole piece gaps without compromising spatial resolution, but so far the largest gap is only about 9 mm in size for TEMs with 200-400 kV of accelerating voltage [141]. Moreover, automated drift correctors can be very tricky to use as the sample itself undergo changes as it is being probed. Drift in in-situ EM can be particularly severe as there are many possible causes of it, such as expansion and contraction of the sample, temperature variations, chemical reactions, and electrical charging [141].

Finally, a classic issue with all EM experiments is a possibility that extremely thin samples may not accurately represent the bulk device. This is especially the case in TEM, where samples can only be about ~200 nm thick at most to get a meaningful spatial resolution. Furthermore, the large surface area to volume ratio for these samples may influence the rate of ion migration and degradation compared to bulk devices, especially when probing the mechanism of atmospheric degradation. One last thing to keep in mind is the effect sample preparation steps might have had on the samples, particularly FIB milling as it is still the best technique to obtain cross-section TEM samples. Modern FIB machines are conventionally operated in tandem with an SEM imaging system, in which the electron gun and the ion source are put at an angle to one another to allow visualisation of the sample as it is being milled. The ion beam can be operated at low power for imaging or at high power (~30 KeV) for milling. An FIB miller is also equipped with a gas injection system (GIS) and a micromanipulator used to transfer the milled lamella onto the TEM sample grid. The GIS channels gaseous precursors to deposit a protective layer on the specimen. These precursor molecules are cracked by the ion beam, thus producing a film of the desired material which can be either conducting (Pt or W) or insulating (SiO2).

To produce a solar cell lamella, first a ~2-μm thick platinum layer is deposited on top of the region of interest to block the Ga+ ions from damaging this area. Then, a pair of trenches are cut at the front and back side of the desired region. These trenches should be about 20 x 10 μm2 in size and its depth should decrease (i.e. shallower) as it moves further away from the specimen strip. Once this strip is only attached to the rest of the cell on one side, the micromanipulator is welded with platinum to the lamella and then it is completely cut away from the bulk sample. After it is attached to a TEM sample grid, additional milling is performed until the lamella’s thickness reaches electron transparency. To obtain a uniform thickness despite the ion beam’s Gaussian profile, a specific thinning procedure is usually recommended by the FIB manufacturer with precise tilt angles and beam currents. Gallium ions (Ga+) are normally used for the milling step due to their heavy atomic mass and low melting point so implantation of Ga+ ions is always a possibility, as is the case with surface amorphisation, preferential milling, redeposition of milled atoms, contamination by the protective / welding material, and other microstructural modifications [142]. Plasma FIB with Xe+ ions may be able to partially solve this problem as multiple studies have shown that it can mill sample lamellae faster and with less damage compared to Ga+ ions [143,144].

- Conclusion and Outlook

Only a handful of in-situ EM studies on PSC degradation has been conducted so far and there is certainly ample room for many more. Almost all published works were done on MAPbI3 and the promising discoveries made highlight the need to replicate them on other perovskite compositions, including mixed-cation, mixed-halide and fully inorganic ones. Future projects should experiment with applying multiple kinds of stimuli simultaneously, particularly pairings which have been reported to cause accelerated degradation in bulk devices such as light and oxygen or moisture and electrical bias. Another open question which also stands to benefit greatly from in-situ observations is the origin of hysteresis and why it tends to worsen during cell ageing [119], where real-time elemental mapping upon illumination and biasing would be most helpful. More generally, knowing the mechanism of various degradation pathways would help the perovskite photovoltaics community to design a series of accelerated ageing tests with sufficient predictive power to be used as a standard across research laboratories and industry.

To ensure that the findings from an in-situ EM study can be relied upon, ideally the results should always be compared with a parallel ex-situ experiment. This is important because in-situ EM studies can take a significant amount of time and resources, often allowing only a handful of sample to be observed. Comparison with ex-situ studies can compensate for inferior statistical significance arising from the low number of in-situ samples. Another way to validate the results is to cross-check them against other in-situ characterisation methods. In the context of PSC degradation, many such methods can be used to probe various PSC parameters. In-situ absorption spectroscopy monitors changes in light absorption as a PSC is degraded [58]. Since the photoactive perovskite and degradation products have different band gaps, formation of a new phase can be easily identified by shifts of the absorption onset. In-situ XRD, synchrotron XRD, and grazing-incidence wide-angle X-ray scattering (GIWAXS) reveal structural modifications in the perovskite [145–150]. More specifically, these methods can show changes in crystallinity, grain size, and phase by peak identification. Synchrotron XRD and GIWAXS are especially useful for in-situ observation as the fast 2D detector and high brightness X-ray source enable high temporal resolution. In-situ X-ray photoelectron spectroscopy (XPS) measure binding energies of elements located at the sample top surface to reveal changes in chemical bonding. By tracking changes in peak intensity and position, we can monitor the degradation speed of perovskite into other phases [151]. Alterations in the morphology of perovskite film surface can be observed using in-situ scanning force microscopy (SFM) [148]. This technique can tell us information about film roughness, crystallite size, and the presence of steps and grain boundaries. One of the more rarely used techniques is in-situ laser beam-induced current (LBIC), which takes advantage of perovskite’s photoluminescence properties to map its degradation and provide a measure of the performance reduction’s spatial homogeneity [152]. In-situ EM is complementary in many ways to the above techniques. The information produced by EM is not spatially averaged over the entire sample like it is in absorption spectroscopy, XRD, GIWAXS, and XPS, so we can see where certain ions migrate to and where new phases are formed. While SFM and LBIC also show localised information, an advantage of EM over these two methods and the rest is its ability to explain why and how certain things happen instead of showing what happens. Of course, this is not to say the above non-EM methods are not useful; indeed they supply various data which EM cannot. Combining multiple in-situ characterisation techniques with each one’s unique advantages will be key to conclusively determine degradation mechanisms in PSC.

In the future, further improvements in EM and its accessories would greatly enlarge the scope of in-situ microscopy. Invention of even more advanced sample holders and in-column illumination system with greater precision and accurate calibration would enable experiments with high degree of operator control. Higher-order aberration and drift correctors would improve spatial resolution, while direct detection cameras and pulsed electron sources would increase temporal resolution. Well-calibrated standards for elemental identification would provide a path towards more accurate quantification. Simultaneous acquisition of images and diffraction patterns can reduce beam exposure time, limiting beam damage on the sample. Sophisticated denoising and data processing algorithms such as PCA, non-negative matrix factorisation (NMF), independent component analysis (ICA), and singular value decomposition (SVD) and application of artificial neural networks can significantly improve the signal-to-noise ratio, allowing for lower electron dose and further minimising beam damage. Consequently, these automated procedures help us sieve through the massive amount of data that in-situ experiments produce through dimensionality reduction while maintaining statistically significant variance. After denoising, spectral characteristics of the elemental components can be extracted from the simplified data to obtain spatial distribution of detected elements, which would be extremely useful for mixed-cation, mixed-halide perovskite. A detailed explanation of PCA and related algorithms and examples of their use can be found in published literature [90,153–160]. All these developments will be beneficial for all researchers in the in-situ EM community, whose needs are no different with those of us investigating PSC degradation [161].

Vitae

Felix Utama Kosasih is a PhD candidate in the Department of Materials Science & Metallurgy at the University of Cambridge, where he works under the supervision of Dr. Caterina Ducati in the Electron Microscopy Group. He received his B.Eng.(Hons.) in Materials Science and Engineering from the National University of Singapore in 2017. His research focuses on investigating optoelectronic properties and degradation of perovskite solar cells with analytical transmission electron microscopy.

Caterina Ducati is a Reader in Nanomaterials in the Department of Materials Science & Metallurgy at the University of Cambridge. She is also a Tutor, Director of Studies in Materials Science, and Fellow of Trinity College Cambridge. Her research focuses on understanding the relationship between structure and optoelectronic properties of nanomaterials for applications in photovoltaics and photocatalysis. She received her undergraduate degree from Università Statale di Milano and PhD from the University of Cambridge.

Acknowledgment: FUK acknowledges support from the Jardine Foundation. The authors thank Giorgio Divitini for fruitful discussions.

References

[1]	A. Kojima, K. Teshima, Y. Shirai, T. Miyasaka, Organometal Halide Perovskites as Visible- Light Sensitizers for Photovoltaic Cells, J Am Chem Soc. 131 (2009) 6050–6051. doi:10.1021/ja809598r.

[2]	W.S. Yang, B. Park, E.H. Jung, N.J. Jeon, Iodide management in formamidinium-lead-halide – based perovskite layers for efficient solar cells, Science (80-. ). 356 (2017) 1376–1379. doi:10.1126/science.aan2301.

[3]	S. De Wolf, J. Holovsky, S.J. Moon, P. Löper, B. Niesen, M. Ledinsky, F.J. Haug, J.H. Yum, C. Ballif, Organometallic halide perovskites: Sharp optical absorption edge and its relation to photovoltaic performance, J. Phys. Chem. Lett. 5 (2014) 1035–1039. doi:10.1021/jz500279b.

[4]	A. Sadhanala, F. Deschler, T.H. Thomas, S.E. Dutton, K.C. Goedel, F.C. Hanusch, M.L. Lai, U. Steiner, T. Bein, P. Docampo, D. Cahen, R.H. Friend, Preparation of single-phase films of CH3NH3Pb(I1-xBrx)3 with sharp optical band edges, J. Phys. Chem. Lett. 5 (2014) 2501–2505. doi:10.1021/jz501332v.

[5]	W. Tress, Maximum Efficiency and Open-Circuit Voltage of Perovskite Solar Cells, in: N.-G. Park, M. Grätzel, T. Miyasaka (Eds.), Org. Halide Perovskite Photovoltaics, 1st ed., Springer International Publishing, 2016: pp. 53–77. doi:10.1007/978-3-319-35114-8.

[6]	P. Umari, E. Mosconi, F. De Angelis, Relativistic GW calculations on CH3NH3PbI3 and CH3NH3SnI3 Perovskites for Solar Cell Applications, Sci. Rep. 4 (2014) 1–7. doi:10.1038/srep04467.

[7]	Q. Lin, A. Armin, R.C.R. Nagiri, P.L. Burn, P. Meredith, Electro-optics of perovskite solar cells, Nat. Photonics. 9 (2015) 106–112. doi:10.1038/nphoton.2014.284.

[8]	V. D’Innocenzo, G. Grancini, M.J.P. Alcocer, A.R.S. Kandada, S.D. Stranks, M.M. Lee, G. Lanzani, H.J. Snaith, A. Petrozza, Excitons versus free charges in organo-lead tri-halide perovskites, Nat. Commun. 5 (2014) 1–6. doi:10.1038/ncomms4586.

[9]	A. Miyata, A. Mitioglu, P. Plochocka, O. Portugall, J.T.W. Wang, S.D. Stranks, H.J. Snaith, R.J. Nicholas, Direct measurement of the exciton binding energy and effective masses for charge carriers in organic-inorganic tri-halide perovskites, Nat. Phys. 11 (2015) 582–587. doi:10.1038/nphys3357.

[10]	K. Galkowski, A. Mitioglu, A. Miyata, P. Plochocka, O. Portugall, G.E. Eperon, J.T.-W. Wang, T. Stergiopoulos, S.D. Stranks, H.J. Snaith, R.J. Nicholas, Determination of the exciton binding energy and effective masses for the methylammonium and formamidinium lead tri-halide perovskite family, Energy Environ. Sci. 9 (2015) 962–970. doi:10.1039/C5EE03435C.

[11]	G.E. Eperon, S.D. Stranks, C. Menelaou, M.B. Johnston, L.M. Herz, H.J. Snaith, Formamidinium lead trihalide: a broadly tunable perovskite for efficient planar heterojunction solar cells, Energy Environ. Sci. 7 (2014) 982. doi:10.1039/c3ee43822h.

[12]	J.H. Noh, S.H. Im, J.H. Heo, T.N. Mandal, S. Il Seok, Chemical management for colorful, efficient, and stable inorganic-organic hybrid nanostructured solar cells, Nano Lett. 13 (2013) 1764–1769. doi:10.1021/nl400349b.

[13]	D.P. McMeekin, G. Sadoughi, W. Rehman, G.E. Eperon, M. Saliba, M.T. Horantner, A. Haghighirad, N. Sakai, L. Korte, B. Rech, M.B. Johnston, L.M. Herz, H.J. Snaith, A mixed-cation lead mixed-halide perovskite absorber for tandem solar cells, Science (80-. ). 351 (2016) 151–155. doi:10.1126/science.aad5845.

[14]	C.M. Sutter-Fella, Y. Li, M. Amani, J.W. Ager, F.M. Toma, E. Yablonovitch, I.D. Sharp, A. Javey, High Photoluminescence Quantum Yield in Band Gap Tunable Bromide Containing Mixed Halide Perovskites, Nano Lett. 16 (2016) 800–806. doi:10.1021/acs.nanolett.5b04884.

[15]	M.R. Filip, G.E. Eperon, H.J. Snaith, F. Giustino, Steric engineering of metal-halide perovskites with tunable optical band gaps, Nat. Commun. 5 (2014) 1–9. doi:10.1038/ncomms6757.

[16]	Y. Yan, W.-J. Yin, T. Shi, W. Meng, C. Feng, Defect Physics of CH3NH3PbX3 (X = I, Br, Cl) Perovskites, in: N.-G. Park, M. Grätzel, T. Miyasaka (Eds.), Org. Halide Perovskite Photovoltaics, 1st ed., Springer International Publishing, 2016: pp. 79–105. doi:10.1007/978-3-319-35114-8.

[17]	W. Yin, T. Shi, Y. Yan, Unusual defect physics in CH3NH3PbI3 perovskite solar cell absorber, Appl. Phys. Lett. 104 (2014) 63903. doi:10.1063/1.4864778.

[18]	J. Huang, Y. Yuan, Y. Shao, Y. Yan, Understanding the physical properties of hybrid perovskites for photovoltaic applications, Nat. Rev. Mater. 2 (2017) 17042. doi:10.1038/natrevmats.2017.42.

[19]	H. Oga, A. Saeki, Y. Ogomi, S. Hayase, S. Seki, Improved understanding of the electronic and energetic landscapes of perovskite solar cells: High local charge carrier mobility, reduced recombination, and extremely shallow traps, J. Am. Chem. Soc. 136 (2014) 13818–13825. doi:10.1021/ja506936f.

[20]	K.X. Steirer, P. Schulz, G. Teeter, V. Stevanovic, M. Yang, K. Zhu, J.J. Berry, Defect Tolerance in Methylammonium Lead Triiodide Perovskite, ACS Energy Lett. 1 (2016) 360–366. doi:10.1021/acsenergylett.6b00196.

[21]	C.C. Stoumpos, C.D. Malliakas, M.G. Kanatzidis, Semiconducting tin and lead iodide perovskites with organic cations: Phase transitions, high mobilities, and near-infrared photoluminescent properties, Inorg. Chem. 52 (2013) 9019–9038. doi:10.1021/ic401215x.

[22]	G. Xing, N. Mathews, S. Sun, S.S. Lim, Y.M. Lam, M. Grätzel, S. Mhaisalkar, T.C. Sum, Long-range balanced electron- and hole-transport lengths in organic-inorganic CH3NH3PbI3., Science (80-. ). 342 (2013) 344–7. doi:10.1126/science.1243167.

[23]	S.D. Stranks, S.D. Stranks, G.E. Eperon, G. Grancini, C. Menelaou, M.J.P. Alcocer, T. Leijtens, L.M. Herz, A. Petrozza, H.J. Snaith, Electron-Hole Diffusion Lengths Exceeding 1 Micrometer in an Organometal Trihalide Perovskite Absorber, Science (80-. ). 342 (2014) 341–344. doi:10.1126/science.1243982.

[24]	W. Rehman, D.P. McMeekin, J.B. Patel, R.L. Milot, M.B. Johnston, H.J. Snaith, L.M. Herz, Photovoltaic mixed-cation lead mixed-halide perovskites: links between crystallinity, photo-stability and electronic properties, Energy Environ. Sci. 10 (2017) 361–369. doi:10.1039/C6EE03014A.

[25]	T.M. Koh, K. Fu, Y. Fang, S. Chen, T.C. Sum, N. Mathews, S.G. Mhaisalkar, P.P. Boix, T. Baikie, Formamidinium-containing metal-halide: An alternative material for near-IR absorption perovskite solar cells, J. Phys. Chem. C. 118 (2014) 16458–16462. doi:10.1021/jp411112k.

[26]	Z. Wang, D.P. McMeekin, N. Sakai, S. van Reenen, K. Wojciechowski, J.B. Patel, M.B. Johnston, H.J. Snaith, Efficient and Air-Stable Mixed-Cation Lead Mixed-Halide Perovskite Solar Cells with n-Doped Organic Electron Extraction Layers, Adv. Mater. 29 (2017) 1–8. doi:10.1002/adma.201604186.

[27]	N.J. Jeon, J.H. Noh, W.S. Yang, Y.C. Kim, S. Ryu, J. Seo, S. Il Seok, Compositional engineering of perovskite materials for high-performance solar cells, Nature. 517 (2015) 476–480. doi:10.1038/nature14133.

[28]	Z. Wang, Q. Lin, F.P. Chmiel, N. Sakai, L.M. Herz, H.J. Snaith, Efficient ambient-air-stable solar cells with 2D–3D heterostructured butylammonium-caesium-formamidinium lead halide perovskites, Nat. Energy. 6 (2017) 17135. doi:10.1038/nenergy.2017.135.

[29]	G. Grancini, C. Roldán-Carmona, I. Zimmermann, E. Mosconi, X. Lee, D. Martineau, S. Narbey, F. Oswald, F. De Angelis, M. Graetzel, M.K. Nazeeruddin, One-Year stable perovskite solar cells by 2D/3D interface engineering, Nat. Commun. 8 (2017) 15684. doi:10.1038/ncomms15684.

[30]	I.C. Smith, E.T. Hoke, D. Solis-Ibarra, M.D. McGehee, H.I. Karunadasa, A Layered Hybrid Perovskite Solar-Cell Absorber with Enhanced Moisture Stability, Angew. Chemie - Int. Ed. 53 (2014) 11232–11235. doi:10.1002/anie.201406466.

[31]	H. Tsai, W. Nie, J.C. Blancon, C.C. Stoumpos, R. Asadpour, B. Harutyunyan, A.J. Neukirch, R. Verduzco, J.J. Crochet, S. Tretiak, L. Pedesseau, J. Even, M.A. Alam, G. Gupta, J. Lou, P.M. Ajayan, M.J. Bedzyk, M.G. Kanatzidis, A.D. Mohite, High-efficiency two-dimensional Ruddlesden-Popper perovskite solar cells, Nature. 536 (2016) 312–317. doi:10.1038/nature18306.

[32]	M.M. Lee, J. Teuscher, T. Miyasaka, T.N. Murakami, H.J. Snaith, Efficient Hybrid Solar Cells Based on Meso-Superstructured Organometal Halide Perovskites, Science (80-. ). 338 (2012) 643–647. doi:10.1126/science.1228604.

[33]	J.M. Ball, M.M. Lee, A. Hey, H.J. Snaith, Low-temperature processed meso-superstructured to thin-film perovskite solar cells, Energy Environ. Sci. 6 (2013) 1739–1743. doi:10.1039/c3ee40810h.

[34]	J.Y. Jeng, Y.F. Chiang, M.H. Lee, S.R. Peng, T.F. Guo, P. Chen, T.C. Wen, CH3NH3PbI3 perovskite/fullerene planar-heterojunction hybrid solar cells, Adv. Mater. 25 (2013) 3727–3732. doi:10.1002/adma.201301327.

[35]	W.S. Yang, J.H. Noh, N.J. Jeon, Y.C. Kim, S. Ryu, J. Seo, S.I. Seok, High-performance photovoltaic perovskite layers fabricated through intramolecular exchange, Science (80-. ). 348 (2015) 1234–1237. doi:10.1126/science.aaa9272.

[36]	N.J. Jeon, J.H. Noh, Y.C. Kim, W.S. Yang, S. Ryu, S. Il Seok, Solvent engineering for high-performance inorganic–organic hybrid perovskite solar cells, Nat. Mater. 13 (2014) 897–903. doi:10.1038/nmat4014.

[37]	J. Zheng, M. Zhang, C.F.J. Lau, X. Deng, J. Kim, Q. Ma, C. Chen, M.A. Green, S. Huang, A.W.Y. Ho-Baillie, Spin-coating free fabrication for highly efficient perovskite solar cells, Sol. Energy Mater. Sol. Cells. 168 (2017) 165–171. doi:10.1016/j.solmat.2017.04.029.

[38]	F. Zhang, W. Shi, J. Luo, N. Pellet, C. Yi, X. Li, X. Zhao, T.J.S. Dennis, X. Li, S. Wang, Y. Xiao, S.M. Zakeeruddin, D. Bi, M. Grätzel, Isomer-Pure Bis-PCBM-Assisted Crystal Engineering of Perovskite Solar Cells Showing Excellent Efficiency and Stability, Adv. Mater. 29 (2017). doi:10.1002/adma.201606806.

[39]	F. Zhang, X. Zhao, C. Yi, D. Bi, X. Bi, P. Wei, X. Liu, S. Wang, X. Li, S.M. Zakeeruddin, M. Grätzel, Dopant-free star-shaped hole-transport materials for efficient and stable perovskite solar cells, Dye. Pigment. 136 (2017) 273–277. doi:10.1016/j.dyepig.2016.08.002.

[40]	S.H. Chang, C.C. Chen, L.C. Chen, C.L. Tien, H.M. Cheng, W.C. Huang, H.Y. Lin, S.H. Chen, C.G. Wu, Unraveling the multifunctional capabilities of PCBM thin films in inverted-type CH3NH3PbI3 based photovoltaics, Sol. Energy Mater. Sol. Cells. 169 (2017) 40–46. doi:10.1016/j.solmat.2017.05.007.

[41]	K. Aitola, K. Domanski, J.P. Correa-Baena, K. Sveinbjörnsson, M. Saliba, A. Abate, M. Grätzel, E. Kauppinen, E.M.J. Johansson, W. Tress, A. Hagfeldt, G. Boschloo, High Temperature-Stable Perovskite Solar Cell Based on Low-Cost Carbon Nanotube Hole Contact, Adv. Mater. 29 (2017). doi:10.1002/adma.201606398.

[42]	J.H. Park, J. Seo, S. Park, S.S. Shin, Y.C. Kim, N.J. Jeon, H.W. Shin, T.K. Ahn, J.H. Noh, S.C. Yoon, C.S. Hwang, S. Il Seok, Efficient CH3NH3PbI3 Perovskite Solar Cells Employing Nanostructured p-Type NiO Electrode Formed by a Pulsed Laser Deposition, Adv. Mater. 27 (2015) 4013–4019. doi:10.1002/adma.201500523.

[43]	H. Tan, A. Jain, O. Voznyy, X. Lan, F.P. García de Arquer, J.Z. Fan, R. Quintero-Bermudez, M. Yuan, B. Zhang, Y. Zhao, F. Fan, P. Li, L.N. Quan, Y. Zhao, Z.-H. Lu, Z. Yang, S. Hoogland, E.H. Sargent, Efficient and stable solution-processed planar perovskite solar cells via contact passivation, Science (80-. ). 355 (2017) 722–726. doi:10.1126/science.aai9081.

[44]	M. Kot, C. Das, Z. Wang, K. Henkel, Z. Rouissi, K. Wojciechowski, H.J. Snaith, D. Schmeisser, Room-Temperature Atomic Layer Deposition of Al2O3: Impact on Efficiency, Stability and Surface Properties in Perovskite Solar Cells, ChemSusChem. 9 (2016) 3401–3406. doi:10.1002/cssc.201601186.

[45]	J.-P. Correa-Baena, W. Tress, K. Domanski, E.H. Anaraki, S.-H. Turren-Cruz, B. Roose, P.P. Boix, M. Grätzel, M. Saliba, A. Abate, A. Hagfeldt, Identifying and suppressing interfacial recombination to achieve high open-circuit voltage in perovskite solar cells, Energy Environ. Sci. 10 (2017) 1207–1212. doi:10.1039/C7EE00421D.

[46]	L.N. Quan, M. Yuan, R. Comin, O. Voznyy, E.M. Beauregard, S. Hoogland, A. Buin, A.R. Kirmani, K. Zhao, A. Amassian, D.H. Kim, E.H. Sargent, Ligand-Stabilized Reduced-Dimensionality Perovskites, J. Am. Chem. Soc. 138 (2016) 2649–2655. doi:10.1021/jacs.5b11740.

[47]	Y. Hu, J. Schlipf, M. Wussler, M.L. Petrus, W. Jaegermann, T. Bein, P. Müller-Buschbaum, P. Docampo, Hybrid Perovskite/Perovskite Heterojunction Solar Cells, ACS Nano. 10 (2016) 5999–6007. doi:10.1021/acsnano.6b01535.

[48]	N.K. Noel, S.D. Stranks, A. Abate, C. Wehrenfennig, S. Guarnera, A.-A. Haghighirad, A. Sadhanala, G.E. Eperon, S.K. Pathak, M.B. Johnston, A. Petrozza, L.M. Herz, H.J. Snaith, Lead-free organic–inorganic tin halide perovskites for photovoltaic applications, Energy Environ. Sci. 7 (2014) 3061–3068. doi:10.1039/C4EE01076K.

[49]	F. Hao, C.C. Stoumpos, D.H. Cao, R.P.H. Chang, M.G. Kanatzidis, Lead-free solid-state organic-inorganic halide perovskite solar cells, Nat. Photonics. 8 (2014) 489–494. doi:10.1038/nphoton.2014.82.

[50]	A. Abate, Perovskite Solar Cells Go Lead Free, Joule. 1 (2017) 659–664. doi:10.1016/j.joule.2017.09.007.

[51]	S. Chakraborty, W. Xie, N. Mathews, M. Sherburne, R. Ahuja, M. Asta, S.G. Mhaisalkar, Rational Design: A High-Throughput Computational Screening and Experimental Validation Methodology for Lead-Free and Emergent Hybrid Perovskites, ACS Energy Lett. 2 (2017) 837–845. doi:10.1021/acsenergylett.7b00035.

[52]	F. Giustino, H.J. Snaith, Toward Lead-Free Perovskite Solar Cells, ACS Energy Lett. 1 (2016) 1233–1240. doi:10.1021/acsenergylett.6b00499.

[53]	C.N. Savory, A. Walsh, D.O. Scanlon, Can Pb-Free Halide Double Perovskites Support High-Efficiency Solar Cells?, ACS Energy Lett. 1 (2016) 949–955. doi:10.1021/acsenergylett.6b00471.

[54]	M. Chen, M.-G. Ju, A.D. Carl, Y. Zong, R.L. Grimm, J. Gu, X.C. Zeng, Y. Zhou, N.P. Padture, Cesium Titanium(IV) Bromide Thin Films Based Stable Lead-free Perovskite Solar Cells, Joule. (2018) 1–13. doi:10.1016/j.joule.2018.01.009.

[55]	B. Conings, J. Drijkoningen, N. Gauquelin, A. Babayigit, J. D’Haen, L. D’Olieslaeger, A. Ethirajan, J. Verbeeck, J. Manca, E. Mosconi, F. De Angelis, H.G. Boyen, Intrinsic Thermal Instability of Methylammonium Lead Trihalide Perovskite, Adv. Energy Mater. 5 (2015) 1–8. doi:10.1002/aenm.201500477.

[56]	A.M.A. Leguy, Y. Hu, M. Campoy-Quiles, M.I. Alonso, O.J. Weber, P. Azarhoosh, M. Van Schilfgaarde, M.T. Weller, T. Bein, J. Nelson, P. Docampo, P.R.F. Barnes, Reversible hydration of CH3NH3PbI3 in films, single crystals, and solar cells, Chem. Mater. 27 (2015) 3397–3407. doi:10.1021/acs.chemmater.5b00660.

[57]	J.A. Christians, P.A. Miranda Herrera, P. V. Kamat, Transformation of the excited state and photovoltaic efficiency of CH3NH3PbI3 perovskite upon controlled exposure to humidified air, J. Am. Chem. Soc. 137 (2015) 1530–1538. doi:10.1021/ja511132a.

[58]	J. Yang, B.D. Siempelkamp, D. Liu, T.L. Kelly, Investigation of CH3NH3PbI3 degradation rates and mechanisms in controlled humidity environments using in situ techniques, ACS Nano. 9 (2015) 1955–1963. doi:10.1021/nn506864k.

[59]	G. Abdelmageed, C. Mackeen, K. Hellier, L. Jewell, L. Seymour, M. Tingwald, F. Bridges, J.Z. Zhang, S. Carter, Effect of temperature on light induced degradation in methylammonium lead iodide perovskite thin films and solar cells, Sol. Energy Mater. Sol. Cells. 174 (2018) 566–571. doi:10.1016/j.solmat.2017.09.053.

[60]	E.T. Hoke, D.J. Slotcavage, E.R. Dohner, A.R. Bowring, H.I. Karunadasa, M.D. McGehee, Reversible photo-induced trap formation in mixed-halide hybrid perovskites for photovoltaics, Chem. Sci. 6 (2015) 613–617. doi:10.1039/C4SC03141E.

[61]	D.J. Slotcavage, H.I. Karunadasa, M.D. McGehee, Light-Induced Phase Segregation in Halide-Perovskite Absorbers, ACS Energy Lett. 1 (2016) 1199–1205. doi:10.1021/acsenergylett.6b00495.

[62]	D.W. deQuilettes, W. Zhang, V.M. Burlakov, D.J. Graham, T. Leijtens, A. Osherov, V. Bulović, H.J. Snaith, D.S. Ginger, S.D. Stranks, Photo-induced halide redistribution in organic–inorganic perovskite films, Nat. Commun. 7 (2016) 11683. doi:10.1038/ncomms11683.

[63]	K. Domanski, J.P. Correa-Baena, N. Mine, M.K. Nazeeruddin, A. Abate, M. Saliba, W. Tress, A. Hagfeldt, M. Grätzel, Not All That Glitters Is Gold: Metal-Migration-Induced Degradation in Perovskite Solar Cells, ACS Nano. 10 (2016) 6306–6314. doi:10.1021/acsnano.6b02613.

[64]	S. Cacovich, L. Ciná, F. Matteocci, G. Divitini, P.A. Midgley, A. Di Carlo, C. Ducati, Gold and iodine diffusion in large area perovskite solar cells under illumination, Nanoscale. 9 (2017) 4700–4706. doi:10.1039/C7NR00784A.

[65]	D. Wei, T. Wang, J. Ji, M. Li, P. Cui, Y. Li, G. Li, J.M. Mbengue, D. Song, Photo-induced degradation of lead halide perovskite solar cells caused by the hole transport layer/metal electrode interface, J. Mater. Chem. A. 4 (2016) 1991–1998. doi:10.1039/C5TA08622A.

[66]	T. Leijtens, G.E. Eperon, S. Pathak, A. Abate, M.M. Lee, H.J. Snaith, Overcoming ultraviolet light instability of sensitized TiO2 with meso-superstructured organometal tri-halide perovskite solar cells, Nat. Commun. 4 (2013) 1–8. doi:10.1038/ncomms3885.

[67]	A.D. Sheikh, A. Bera, M.A. Haque, R.B. Rakhi, S. Del Gobbo, H.N. Alshareef, T. Wu, Atmospheric effects on the photovoltaic performance of hybrid perovskite solar cells, Sol. Energy Mater. Sol. Cells. 137 (2015) 6–14. doi:10.1016/j.solmat.2015.01.023.

[68]	N. Aristidou, I. Sanchez-Molina, T. Chotchuangchutchaval, M. Brown, L. Martinez, T. Rath, S.A. Haque, The Role of Oxygen in the Degradation of Methylammonium Lead Trihalide Perovskite Photoactive Layers, Angew. Chemie - Int. Ed. 54 (2015) 8208–8212. doi:10.1002/anie.201503153.

[69]	F.T.F. O’Mahony, Y.H. Lee, C. Jellett, S. Dmitrov, D.T.J. Bryant, J.R. Durrant, B.C. O’Regan, M. Graetzel, M.K. Nazeeruddin, S.A. Haque, Improved environmental stability of organic lead trihalide perovskite-based photoactive-layers in the presence of mesoporous TiO 2, J. Mater. Chem. A. 3 (2015) 7219–7223. doi:10.1039/C5TA01221J.

[70]	A.J. Pearson, G.E. Eperon, P.E. Hopkinson, S.N. Habisreutinger, J.T.W. Wang, H.J. Snaith, N.C. Greenham, Oxygen Degradation in Mesoporous Al2O3/CH3NH3PbI3-xClx Perovskite Solar Cells: Kinetics and Mechanisms, Adv. Energy Mater. 6 (2016) 1–10. doi:10.1002/aenm.201600014.

[71]	F. Bella, G. Griffini, J.-P. Correa-Baena, G. Saracco, M. Gratzel, A. Hagfeldt, S. Turri, C. Gerbaldi, Improving efficiency and stability of perovskite solar cells with photocurable fluoropolymers, Science (80-. ). 354 (2016) 203–206. doi:10.1126/science.aah4046.

[72]	I. Hwang, I. Jeong, J. Lee, M.J. Ko, K. Yong, Enhancing Stability of Perovskite Solar Cells to Moisture by the Facile Hydrophobic Passivation, ACS Appl. Mater. Interfaces. 7 (2015) 17330–17336. doi:10.1021/acsami.5b04490.

[73]	F. Matteocci, S. Razza, F. Di Giacomo, S. Casaluci, G. Mincuzzi, T.M. Brown, A. D’Epifanio, S. Licoccia, A. Di Carlo, Solid-state solar modules based on mesoscopic organometal halide perovskite: a route towards the up-scaling process, Phys. Chem. Chem. Phys. 16 (2014) 3918. doi:10.1039/c3cp55313b.

[74]	F. Matteocci, L. Cinà, E. Lamanna, S. Cacovich, G. Divitini, P.A. Midgley, C. Ducati, A. Di Carlo, Encapsulation for long-term stability enhancement of perovskite solar cells, Nano Energy. 30 (2016) 162–172. doi:10.1016/j.nanoen.2016.09.041.

[75]	B. McKenna, J.R. Troughton, T.M. Watson, R.C. Evans, Enhancing the stability of organolead halide perovskite films through polymer encapsulation, RSC Adv. 7 (2017) 32942–32951. doi:10.1039/C7RA06002E.

[76]	L. Zheng, Y.-H. Chung, Y. Ma, L. Zhang, L. Xiao, Z. Chen, S. Wang, B. Qu, Q. Gong, A hydrophobic hole transporting oligothiophene for planar perovskite solar cells with improved stability, Chem. Commun. 50 (2014) 11196–11199. doi:10.1039/C4CC04680C.

[77]	S.N. Habisreutinger, T. Leijtens, G.E. Eperon, S.D. Stranks, R.J. Nicholas, H.J. Snaith, Carbon nanotube/polymer composites as a highly stable hole collection layer in perovskite solar cells, Nano Lett. 14 (2014) 5561–5568. doi:10.1021/nl501982b.

[78]	S. Guarnera, A. Abate, W. Zhang, J.M. Foster, G. Richardson, A. Petrozza, H.J. Snaith, Improving the long-term stability of perovskite solar cells with a porous Al2O3 buffer layer, J. Phys. Chem. Lett. 6 (2015) 432–437. doi:10.1021/jz502703p.

[79]	G. Niu, W. Li, F. Meng, L. Wang, H. Dong, Y. Qiu, Study on the stability of CH3NH3PbI3 films and the effect of post-modification by aluminum oxide in all-solid-state hybrid solar cells, J. Mater. Chem. A. 2 (2014) 705–710. doi:10.1039/C3TA13606J.

[80]	S. Ito, S. Tanaka, K. Manabe, H. Nishino, Effects of surface blocking layer of Sb2S3 on nanocrystalline TiO2 for CH3NH3PbI3 perovskite solar cells, J. Phys. Chem. C. 118 (2014) 16995–17000. doi:10.1021/jp500449z.

[81]	V.M. Goldschmidt, Die Gesetze der Krystallochemie, Naturwissenschaften. 14 (1926) 477–485. doi:10.1007/BF01507527.

[82]	C. Li, X. Lu, W. Ding, L. Feng, Y. Gao, Z. Guo, Formability of ABX 3 (X = F, Cl, Br, I) halide perovskites, Acta Crystallogr. Sect. B Struct. Sci. 64 (2008) 702–707. doi:10.1107/S0108768108032734.

[83]	Z. Li, M. Yang, J.S. Park, S.H. Wei, J.J. Berry, K. Zhu, Stabilizing Perovskite Structures by Tuning Tolerance Factor: Formation of Formamidinium and Cesium Lead Iodide Solid-State Alloys, Chem. Mater. 28 (2016) 284–292. doi:10.1021/acs.chemmater.5b04107.

[84]	M. Saliba, T. Matsui, J.-Y. Seo, K. Domanski, J.-P. Correa-Baena, M.K. Nazeeruddin, S.M. Zakeeruddin, W. Tress, A. Abate, A. Hagfeldt, M. Grätzel, Cesium-containing triple cation perovskite solar cells: improved stability, reproducibility and high efficiency, Energy Environ. Sci. 9 (2016) 1989–1997. doi:10.1039/C5EE03874J.

[85]	C. Eames, J.M. Frost, P.R.F. Barnes, B.C. O’Regan, A. Walsh, M.S. Islam, Ionic transport in hybrid lead iodide perovskite solar cells, Nat. Commun. 6 (2015) 7497. doi:10.1038/ncomms8497.

[86]	J.M. Azpiroz, E. Mosconi, J. Bisquert, F. De Angelis, Defect migration in methylammonium lead iodide and its role in perovskite solar cell operation, Energy Environ. Sci. 8 (2015) 2118–2127. doi:10.1039/C5EE01265A.

[87]	J. Haruyama, K. Sodeyama, L. Han, Y. Tateyama, First-principles study of ion diffusion in perovskite solar cell sensitizers, J. Am. Chem. Soc. 137 (2015) 10048–10051. doi:10.1021/jacs.5b03615.

[88]	W. Tress, N. Marinova, T. Moehl, S.M. Zakeeruddin, M.K. Nazeeruddin, M. Grätzel, Understanding the rate-dependent J–V hysteresis, slow time component, and aging in CH3NH3PbI3 perovskite solar cells: the role of a compensated electric field, Energy Environ. Sci. 8 (2015) 995–1004. doi:10.1039/C4EE03664F.

[89]	S. Van Reenen, M. Kemerink, H.J. Snaith, Modeling Anomalous Hysteresis in Perovskite Solar Cells, J. Phys. Chem. Lett. 6 (2015) 3808–3814. doi:10.1021/acs.jpclett.5b01645.

[90]	S. Cacovich, G. Divitini, C. Ireland, F. Matteocci, A. Di Carlo, C. Ducati, Elemental Mapping of Perovskite Solar Cells by Using Multivariate Analysis: An Insight into Degradation Processes, ChemSusChem. 9 (2016) 2673–2678. doi:10.1002/cssc.201600913.

[91]	M.-H. Li, P.-S. Shen, K.-C. Wang, T.-F. Guo, P. Chen, Inorganic p-type contact materials for perovskite-based solar cells, J. Mater. Chem. A. 3 (2015) 9011–9019. doi:10.1039/C4TA06425A.

[92]	G. Yang, H. Tao, P. Qin, W. Ke, G. Fang, Recent progress in electron transport layers for efficient perovskite solar cells, J. Mater. Chem. A. 4 (2016) 3970–3990. doi:10.1039/C5TA09011C.

[93]	S. Ito, Inorganic Hole-Transporting Materials for Perovskite Solar Cells, in: N.-G. Park, M. Grätzel, T. Miyasaka (Eds.), Org. Halide Perovskite Photovoltaics, 1st ed., Springer International Publishing, 2016: pp. 343–366. doi:10.1007/978-3-319-35114-8.

[94]	C.-C. Chueh, C.-Z. Li, A.K.-Y. Jen, Recent progress and perspective in solution-processed Interfacial materials for efficient and stable polymer and organometal perovskite solar cells, Energy Environ. Sci. 8 (2015) 1160–1189. doi:10.1039/C4EE03824J.

[95]	D. Nanova, A.K. Kast, M. Pfannmöller, C. Müller, L. Veith, I. Wacker, M. Agari, W. Hermes, P. Erk, W. Kowalsky, R.R. Schröder, R. Lovrinĉić, Unraveling the nanoscale morphologies of mesoporous perovskite solar cells and their correlation to device performance, Nano Lett. 14 (2014) 2735–2740. doi:10.1021/nl5006838.

[96]	G. Divitini, S. Cacovich, F. Matteocci, L. Cinà, A. Di Carlo, C. Ducati, In situ observation of heat-induced degradation of perovskite solar cells, Nat. Energy. 1 (2016) 15012. doi:10.1038/nenergy.2015.12.

[97]	R. Erni, M.D. Rossell, C. Kisielowski, U. Dahmen, Atomic-resolution imaging with a sub-50-pm electron probe, Phys. Rev. Lett. 102 (2009) 1–4. doi:10.1103/PhysRevLett.102.096101.

[98]	L. Piazza, D.J. Masiel, T. LaGrange, B.W. Reed, B. Barwick, F. Carbone, Design and implementation of a fs-resolved transmission electron microscope based on thermionic gun technology, Chem. Phys. 423 (2013) 79–84. doi:10.1016/j.chemphys.2013.06.026.

[99]	O.L. Krivanek, T.C. Lovejoy, N. Dellby, T. Aoki, R.W. Carpenter, P. Rez, E. Soignard, J. Zhu, P.E. Batson, M.J. Lagos, R.F. Egerton, P.A. Crozier, Vibrational spectroscopy in the electron microscope, Nature. 514 (2014) 209–212. doi:10.1038/nature13870.

[100]	D. Williams, C.B. Carter, The Transmission Electron Microscope, 1996. doi:10.1007/978-1-4757-2519-3_1.

[101]	DENSsolutions, Wildfire In Situ TEM Heating, (n.d.). http://denssolutions.com/products/wildfire/ (accessed February 14, 2018).

[102]	DENSsolutions, Lightning In Situ TEM Biasing & Heating, (n.d.). http://denssolutions.com/products/lightning/ (accessed February 14, 2018).

[103]	Protochips, In Situ TEM Electrothermal Analysis: Fusion | Protochips, (n.d.). http://www.protochips.com/products/fusion/ (accessed February 14, 2018).

[104]	DENSsolutions, Climate In Situ TEM Gas & Heating, (n.d.). http://denssolutions.com/products/climate/ (accessed February 14, 2018).

[105]	Hummingbird Scientific, Gas Flow Holder for In-situ TEM | Hummingbird Scientific, (n.d.). http://hummingbirdscientific.com/products/gas-flow/ (accessed February 14, 2018).

[106]	Protochips, TEM Environmental Gas Cell: Atmosphere | Protochips, (n.d.). http://www.protochips.com/products/atmosphere/ (accessed February 14, 2018).

[107]	R.E. Wasylishen, O. Knop, J.B. Macdonald, Cation rotation in methylammonium lead halides, Solid State Commun. 56 (1985) 581–582. doi:10.1016/0038-1098(85)90959-7.

[108]	D.B. Mitzi, I.B.M.T.J. Watson, I. Box, Synthesis, Structure, and Properties of Organic-Inorganic Perovskites and Related Materials, 1999.

[109]	C. Quarti, E. Mosconi, J.M. Ball, V. D’Innocenzo, C. Tao, S. Pathak, H.J. Snaith, A. Petrozza, F. De Angelis, Structural and optical properties of methylammonium lead iodide across the tetragonal to cubic phase transition: implications for perovskite solar cells, Energy Environ. Sci. 9 (2016) 155–163. doi:10.1039/C5EE02925B.

[110]	R.L. Milot, G.E. Eperon, H.J. Snaith, M.B. Johnston, L.M. Herz, Temperature-Dependent Charge-Carrier Dynamics in CH3NH3PbI3 Perovskite Thin Films, Adv. Funct. Mater. 25 (2015) 6218–6227. doi:10.1002/adfm.201502340.

[111]	A. Dualeh, P. Gao, S. Il Seok, M.K. Nazeeruddin, M. Grätzel, Thermal behavior of methylammonium lead-trihalide perovskite photovoltaic light harvesters, Chem. Mater. 26 (2014) 6160–6164. doi:10.1021/cm502468k.

[112]	X. Zhao, H.-S. Kim, J.-Y. Seo, N.-G. Park, Effect of Selective Contacts on the Thermal Stability of Perovskite Solar Cells, ACS Appl. Mater. Interfaces. 9 (2017) 7148–7153. doi:10.1021/acsami.6b15673.

[113]	B. Yang, O. Dyck, W. Ming, M.-H. Du, S. Das, C.M. Rouleau, G. Duscher, D.B. Geohegan, K. Xiao, Observation of Nanoscale Morphological and Structural Degradation in Perovskite Solar Cells by in Situ TEM, ACS Appl. Mater. Interfaces. 8 (2016) 32333–32340. doi:10.1021/acsami.6b11341.

[114]	Y. Yuan, Q. Wang, J. Huang, Ion Migration in Hybrid Perovskite Solar Cells, in: N.-G. Park, M. Grätzel, T. Miyasaka (Eds.), Org. Halide Perovskite Photovoltaics, 1st ed., Springer International Publishing, 2016: pp. 137–162. doi:10.1007/978-3-319-35114-8.

[115]	Y. Yuan, J. Huang, Ion Migration in Organometal Trihalide Perovskite and Its Impact on Photovoltaic Efficiency and Stability, Acc. Chem. Res. 49 (2016) 286–293. doi:10.1021/acs.accounts.5b00420.

[116]	Z. Fan, H. Xiao, Y. Wang, Z. Zhao, Z. Lin, H.-C. Cheng, S.-J. Lee, G. Wang, Z. Feng, W.A. Goddard, Y. Huang, X. Duan, Layer-by-Layer Degradation of Methylammonium Lead Tri-iodide Perovskite Microplates, Joule. 1 (2017) 548–562. doi:10.1016/j.joule.2017.08.005.

[117]	G. Abdelmageed, L. Jewell, K. Hellier, L. Seymour, B. Luo, F. Bridges, J.Z. Zhang, S. Carter, Mechanisms for light induced degradation in MAPbI3 perovskite thin films and solar cells, Appl. Phys. Lett. 109 (2016) 233905. doi:10.1063/1.4967840.

[118]	H. Yuan, E. Debroye, K. Janssen, H. Naiki, C. Steuwe, G. Lu, M. Moris, E. Orgiu, H. Uji-I, F. De Schryver, P. Samorì, J. Hofkens, M. Roeffaers, Degradation of Methylammonium Lead Iodide Perovskite Structures through Light and Electron Beam Driven Ion Migration, J. Phys. Chem. Lett. 7 (2016) 561–566. doi:10.1021/acs.jpclett.5b02828.

[119]	K. Domanski, E.A. Alharbi, A. Hagfeldt, M. Grätzel, W. Tress, Systematic investigation of the impact of operation conditions on the degradation behaviour of perovskite solar cells, Nat. Energy. 3 (2018) 1. doi:10.1038/s41560-017-0060-5.

[120]	F. Cavalca, A.B. Laursen, B.E. Kardynal, R.E. Dunin-Borkowski, S. Dahl, J.B. Wagner, T.W. Hansen, In situ transmission electron microscopy of light-induced photocatalytic reactions, Nanotechnology. 23 (2012) 75705. doi:10.1088/0957-4484/23/7/075705.

[121]	B.K. Miller, P.A. Crozier, System for In Situ UV-Visible Illumination of Environmental Transmission Electron Microscopy Samples, Microsc. Microanal. 19 (2013) 461–469. doi:10.1017/S1431927612014122.

[122]	Q. Liu, L. Zhang, P.A. Crozier, Design and Application of an In Situ Illumination System for an Aberration-corrected Environmental Transmission Electron Microscope, Microsc. Microanal. 22 (2016) 730–731. doi:10.1017/S1431927616004505.

[123]	H.S. Kim, C.R. Lee, J.H. Im, K.B. Lee, T. Moehl, A. Marchioro, S.J. Moon, R. Humphry-Baker, J.H. Yum, J.E. Moser, M. Grätzel, N.G. Park, Lead iodide perovskite sensitized all-solid-state submicron thin film mesoscopic solar cell with efficiency exceeding 9%, Sci. Rep. 2 (2012) 1–7. doi:10.1038/srep00591.

[124]	J. Burschka, N. Pellet, S.J. Moon, R. Humphry-Baker, P. Gao, M.K. Nazeeruddin, M. Grätzel, Sequential deposition as a route to high-performance perovskite-sensitized solar cells, Nature. 499 (2013) 316–319. doi:10.1038/nature12340.

[125]	J. You, L. Meng, T. Bin Song, T.F. Guo, W.H. Chang, Z. Hong, H. Chen, H. Zhou, Q. Chen, Y. Liu, N. De Marco, Y. Yang, Improved air stability of perovskite solar cells via solution-processed metal oxide transport layers, Nat. Nanotechnol. 11 (2016) 75–81. doi:10.1038/nnano.2015.230.

[126]	D. Bryant, N. Aristidou, S. Pont, I. Sanchez-Molina, T. Chotchunangatchaval, S. Wheeler, J.R. Durrant, S.A. Haque, Light and oxygen induced degradation limits the operational stability of methylammonium lead triiodide perovskite solar cells, Energy Environ. Sci. 9 (2016) 1655–1660. doi:10.1039/C6EE00409A.

[127]	H. Joon Jung, D. Kim, S. Kim, B. Shin, V.P. Dravid, Operando Injection of Oxygen Ions to Organometal Halide Perovskite (CH3NH3PbI3) under In-Situ Electrical Biasing STEM-EELS, in: Microsc. Microanal., Cambridge University Press, 2017: pp. 1976–1977. doi:10.1017/S1431927617010546.

[128]	T. Leijtens, E.T. Hoke, G. Grancini, D.J. Slotcavage, G.E. Eperon, J.M. Ball, M. De Bastiani, A.R. Bowring, N. Martino, K. Wojciechowski, M.D. McGehee, H.J. Snaith, A. Petrozza, Mapping electric field-induced switchable poling and structural degradation in hybrid lead halide perovskite thin films, Adv. Energy Mater. 5 (2015) 1–11. doi:10.1002/aenm.201500962.

[129]	J.W. Lee, D.H. Kim, H.S. Kim, S.W. Seo, S.M. Cho, N.G. Park, Formamidinium and cesium hybridization for photo- and moisture-stable perovskite solar cell, Adv. Energy Mater. 5 (2015). doi:10.1002/aenm.201501310.

[130]	J.A. Aguiar, S. Wozny, T.G. Holesinger, T. Aoki, M.K. Patel, M. Yang, J.J. Berry, M. Al-Jassim, W. Zhou, K. Zhu, In situ investigation of the formation and metastability of formamidinium lead tri-iodide perovskite solar cells, Energy Environ. Sci. 9 (2016) 2372–2382. doi:10.1039/C6EE01079B.

[131]	J.A. Aguiar, N.R. Alkurd, S. Wozny, M.K. Patel, M. Yang, W. Zhou, M. Al-Jassim, T.G. Holesinger, K. Zhu, J.J. Berry, In situ investigation of halide incorporation into perovskite solar cells, MRS Commun. 7 (2017) 575–582. doi:10.1557/mrc.2017.52.

[132]	P. Calado, A.M. Telford, D. Bryant, X. Li, J. Nelson, B.C. O’Regan, P.R.F. Barnes, Evidence for ion migration in hybrid perovskite solar cells with minimal hysteresis, Nat. Commun. 7 (2016) 1–10. doi:10.1038/ncomms13831.

[133]	E.L. Unger, E.T. Hoke, C.D. Bailie, W.H. Nguyen, A.R. Bowring, T. Heumüller, M.G. Christoforo, M.D. McGehee, Hysteresis and transient behavior in current–voltage measurements of hybrid-perovskite absorber solar cells, Energy Environ. Sci. 7 (2014) 3690–3698. doi:10.1039/C4EE02465F.

[134]	Q. Jeangros, M. Duchamp, J. Werner, M. Kruth, R.E. Dunin-Borkowski, B. Niesen, C. Ballif, A. Hessler-Wyser, In Situ TEM Analysis of Organic-Inorganic Metal-Halide Perovskite Solar Cells under Electrical Bias, Nano Lett. 16 (2016) 7013–7018. doi:10.1021/acs.nanolett.6b03158.

[135]	B. Bauer, J. Hubmann, M. Lohr, E. Reiger, D. Bougeard, J. Zweck, Direct detection of spontaneous polarization in wurtzite GaAs nanowires, Appl. Phys. Lett. 104 (2014) 211902. doi:10.1063/1.4880209.

[136]	N. Shibata, S.D. Findlay, Y. Kohno, H. Sawada, Y. Kondo, Y. Ikuhara, Differential phase-contrast microscopy at atomic resolution, Nat. Phys. 8 (2012) 611–615. doi:10.1038/nphys2337.

[137]	N. Shibata, S.D. Findlay, H. Sasaki, T. Matsumoto, H. Sawada, Y. Kohno, S. Otomo, R. Minato, Y. Ikuhara, Imaging of built-in electric field at a p-n junction by scanning transmission electron microscopy, Sci. Rep. 5 (2015) 10040. doi:10.1038/srep10040.

[138]	M. Lohr, R. Schregle, M. Jetter, C. Wächter, T. Wunderer, F. Scholz, J. Zweck, Differential phase contrast 2.0—Opening new “fields” for an established technique, Ultramicroscopy. 117 (2012) 7–14. doi:10.1016/j.ultramic.2012.03.020.

[139]	C. Xiao, Z. Li, H. Guthrey, J. Moseley, Y. Yang, S. Wozny, H. Moutinho, B. To, J.J. Berry, B. Gorman, Y. Yan, K. Zhu, M. Al-Jassim, Mechanisms of Electron-Beam-Induced Damage in Perovskite Thin Films Revealed by Cathodoluminescence Spectroscopy, J. Phys. Chem. C. 119 (2015) 26904–26911. doi:10.1021/acs.jpcc.5b09698.

[140]	O. Hentz, Z. Zhao, S. Gradečak, Impacts of Ion Segregation on Local Optical Properties in Mixed Halide Perovskite Films, Nano Lett. 16 (2016) 1485–1490. doi:10.1021/acs.nanolett.5b05181.

[141]	K. Jungjohann, C.B. Carter, In Situ and Operando, in: C.B. Carter, D.B. Williams (Eds.), Transm. Electron Microsc., Springer International Publishing, Cham, 2016: pp. 17–74. doi:10.1007/978-3-319-26651-0_2.

[142]	J. Mayer, L.A. Giannuzzi, T. Kamino, J. Michael, TEM Sample Preparation and FIB-Induced Damage, MRS Bull. 32 (2007) 400–407. doi:10.1557/mrs2007.63.

[143]	R.D. Kelley, K. Song, B. Van Leer, D. Wall, L. Kwakman, Xe+ FIB Milling and Measurement of Amorphous Silicon Damage, Microsc. Microanal. 19 (2013) 862–863. doi:10.1017/S1431927613006302.

[144]	T.L. Burnett, R. Kelley, B. Winiarski, L. Contreras, M. Daly, A. Gholinia, M.G. Burke, P.J. Withers, Large volume serial section tomography by Xe Plasma FIB dual beam microscopy, Ultramicroscopy. 161 (2016) 119–129. doi:10.1016/j.ultramic.2015.11.001.

[145]	J. Zhao, B. Cai, Z. Luo, Y. Dong, Y. Zhang, H. Xu, B. Hong, Y. Yang, L. Li, W. Zhang, C. Gao, Investigation of the hydrolysis of perovskite organometallic halide CH3NH3PbI3in humidity environment, Sci. Rep. 6 (2016) 1–6. doi:10.1038/srep21976.

[146]	K.W. Tan, D.T. Moore, M. Saliba, H. Sai, L.A. Estroff, T. Hanrath, H.J. Snaith, U. Wiesner, Thermally induced structural evolution and performance of mesoporous block copolymer-directed alumina perovskite solar cells, ACS Nano. 8 (2014) 4730–4739. doi:10.1021/nn500526t.

[147]	X. Tang, M. Brandl, B. May, I. Levchuk, Y. Hou, M. Richter, H. Chen, S. Chen, S. Kahmann, A. Osvet, F. Maier, H.-P. Steinrück, R. Hock, G.J. Matt, C.J. Brabec, Photoinduced degradation of methylammonium lead triiodide perovskite semiconductors, J. Mater. Chem. A. 4 (2016) 15896–15903. doi:10.1039/C6TA06497C.

[148]	D. Li, S.A. Bretschneider, V.W. Bergmann, I.M. Hermes, J. Mars, A. Klasen, H. Lu, W. Tremel, M. Mezger, H.J. Butt, S.A.L. Weber, R. Berger, Humidity-Induced Grain Boundaries in MAPbI3Perovskite Films, J. Phys. Chem. C. 120 (2016) 6363–6368. doi:10.1021/acs.jpcc.6b00335.

[149]	V.L. Pool, B. Dou, D.G. Van Campen, T.R. Klein-Stockert, F.S. Barnes, S.E. Shaheen, M.I. Ahmad, M.F.A.M. Van Hest, M.F. Toney, Thermal engineering of FAPbI3perovskite material via radiative thermal annealing and in situ XRD, Nat. Commun. 8 (2017) 1–8. doi:10.1038/ncomms14075.

[150]	M.L. Petrus, Y. Hu, D. Moia, P. Calado, A.M.A. Leguy, P.R.F. Barnes, P. Docampo, The Influence of Water Vapor on the Stability and Processing of Hybrid Perovskite Solar Cells Made from Non-Stoichiometric Precursor Mixtures, ChemSusChem. 9 (2016) 2699–2707. doi:10.1002/cssc.201600999.

[151]	J. Chun-Ren Ke, A.S. Walton, D.J. Lewis, A. Tedstone, P. O’Brien, A.G. Thomas, W.R. Flavell, In situ investigation of degradation at organometal halide perovskite surfaces by X-ray photoelectron spectroscopy at realistic water vapour pressure, Chem. Commun. 53 (2017) 5231–5234. doi:10.1039/C7CC01538K.

[152]	Z. Song, A. Abate, S.C. Watthage, G.K. Liyanage, A.B. Phillips, U. Steiner, M. Graetzel, M.J. Heben, Perovskite Solar Cell Stability in Humid Air: Partially Reversible Phase Transitions in the PbI2-CH3NH3I-H2O System, Adv. Energy Mater. 6 (2016) 1–7. doi:10.1002/aenm.201600846.

[153]	P.G. Kotula, M.R. Keenan, J.R. Michael, Tomographic Spectral Imaging with Multivariate Statistical Analysis: Comprehensive 3D Microanalysis., Microsc. Microanal. 12 (2006) 36–48. doi:10.1017/S1431927606060193.

[154]	M.R. Keenan, P.G. Kotula, Accounting for Poisson noise in the multivariate analysis of ToF-SIMS spectrum images, Surf. Interface Anal. 36 (2004) 203–212. doi:10.1002/sia.1657.

[155]	N. Dobigeon, N. Brun, Spectral mixture analysis of EELS spectrum-images, Ultramicroscopy. 120 (2012) 25–34. doi:10.1016/j.ultramic.2012.05.006.

[156]	N. Bonnet, N. Bonnet, N. Brun, N. Brun, C. Colliex, C. Colliex, Extracting information from sequences of spatially resolved EELS spectra using multivariate statistical analysis, Ultramicroscopy. 77 (1999) 97–112. doi:10.1016/S0304-3991(99)00042-X.

[157]	F. de la Peña, M.H. Berger, J.F. Hochepied, F. Dynys, O. Stephan, M. Walls, Mapping titanium and tin oxide phases using EELS: An application of independent component analysis, Ultramicroscopy. 111 (2011) 169–176. doi:10.1016/j.ultramic.2010.10.001.

[158]	M. Duchamp, M. Lachmann, C.B. Boothroyd, A. Kov?cs, F.-J. Haug, C. Ballif, R.E. Dunin-Borkowski, Compositional study of defects in microcrystalline silicon solar cells using spectral decomposition in the scanning transmission electron microscope, Appl. Phys. Lett. 102 (2013) 1–3. doi:10.1063/1.4800569.

[159]	G. Lucas, P. Burdet, M. Cantoni, C. Hébert, Multivariate statistical analysis as a tool for the segmentation of 3D spectral data, Micron. 52–53 (2013) 49–56. doi:10.1016/j.micron.2013.08.005.

[160]	D. Rossouw, P. Burdet, F. De La Peña, C. Ducati, B.R. Knappett, A.E.H. Wheatley, P.A. Midgley, Multicomponent Signal Unmixing from Nanoheterostructures: Overcoming the Traditional Challenges of Nanoscale X-ray Analysis via Machine Learning, Nano Lett. 15 (2015) 2716–2720. doi:10.1021/acs.nanolett.5b00449.

[161]	M.L. Taheri, E.A. Stach, I. Arslan, P.A. Crozier, B.C. Kabius, T. LaGrange, A.M. Minor, S. Takeda, M. Tanase, J.B. Wagner, R. Sharma, Current status and future directions for in situ transmission electron microscopy, Ultramicroscopy. 170 (2016) 86–95. doi:10.1016/j.ultramic.2016.08.007.