Title: Impacts of lithium on Magnox waste glass dissolution.

Authors: Thomas L. Goût¹,*, Mike T. Harrison², Ian Farnan¹

¹Department of Earth Sciences, University of Cambridge, Downing Street, Cambridge, CB2 3EQ, UK.

²National Nuclear Laboratory, Central Laboratory, Sellafield, Seascale, Cumbria, CA20 1PG, UK.

*Corresponding author:

Email address: tlg29@cam.ac.uk (T. Goût).

Declarations of interest: none

Keywords

Lithium; boron; NMR; temperature; nuclear waste glass.

Abstract

The safe storage of vitrified waste demands a thorough understanding of the effects of wasteform composition on chemical durability. One of the major compositional differences between UK glass and international glasses is the presence of Li. Based upon a 25 wt.% loading UK Magnox waste glass, two seven-component analogues of molar Li:Na 1.0 and 1.5 were leached to investigate the effects of Li on chemical durability. A comprehensive 11B nuclear magnetic resonance study then took place to investigate the B network before and after dissolution.

Here we show that the proportion of IIIB to IVB units did not evolve as the Li:Na ratio was varied; suggesting that Na preferentially charge compensates the B network. However, the B network was shown to leach incongruently at 90 °C. Despite Li being shown to be detrimental to durability during the earlier dissolution regimes, the residual rates of alteration implied excess Li contents had no long-term effects on chemical durability. The observed incongruent dissolution of the B network and initially decreased chemical durability could be attributed to Li preferentially modifying the Si network, thereby promoting glass hydration and B network dissolution whilst the Na compensated IVB units were less affected than IIIB units.

# Introduction

Owing to the durable nature of vitrified waste products, vitrification is often internationally regarded as the best high level nuclear waste immobilisation method available [1–5]. In the UK, it is planned that these vitrified waste products will be permanently disposed of deep underground in a geological disposal facility (GDF). Although the precise depth and lifetime of a GDF will depend upon its’ location and inventory, in the UK a depth of 200 to 1000 m and vitrified waste package lifetime of at least one million years must be considered [6–8]. During this time, it is assumed that groundwater at 40 °C (post thermal pulse assuming a mean surface temperature above 10 °C [9] and geothermal gradient of over 26 °Ckm-1 ) will breach the GDF and contact the vitrified products [1,11,12]; corroding the glass and potentially resulting in radionuclides leaching out of the glass [13–15]. Therefore, the effects of vitrified product chemistry and environmental properties, such as leachant temperature, on the kinetics of aqueous glass dissolution must be well understood prior to their disposal [11,16–23].

Historically, a target Magnox waste loading of 25wt.% had been vitrified using a sodium-lithium borosilicate base glass frit to yield a vitrified product referred to herein as MW25 [24–26]. As in the vitrification process the Li content of the vitrified product is split equally between the base glass and LiNO3 added to the waste to reduce the formation of refractory oxides during calcination [24,27,28], this method has resulted in some vitrified products containing excess amounts of Li [29,30]. The addition of Li to MW25 has been shown to be detrimental to chemical durability [29]. However, adding Li to MW25 as in other studies, rather than substituting it for another alkali metal, convolutes the effects of Li on chemical durability as the total alkali metal content increases and the concentrations of elements beneficial to chemical durability decrease.

To isolate the effects of Li on chemical durability, in the experiments described herein, rather than being added to the glass Li was instead substituted in place of Na on an atom for atom basis. As simulant 27-component MW25 pours took place on a full-scale inactive replica of the vitrification process [24,31,32], fabricating MW25 at various molar Li:Na values would not be viable. Therefore, experiments were performed on two seven-component analogues of compositions based upon an existing Li-free six-component analogue of MW25, Mg-EM (Table 1) [33]. Additionally, experiments took place at 40 °C and 90 °C to assess whether these effects were consistent under both theoretical GDF and accelerated-leaching temperatures respectively.

Batches of Li-Mg-EM containing molar Li:Na ratios of 1.0 and 1.5 (herein referred to as Li50Na50 and Li60Na40 respectively) were aimed at providing a simplified Li-containing analogue of MW25 and investigating the effects of excess Li on MW25 respectively. The total alkali metal molar fraction and molar fractions of all other elements remained constant across all Li-Mg-EM batches and Mg-EM. In addition to inductively coupled plasma mass spectrometry (ICP-MS) of the glass leachates from the dissolution experiments, a comprehensive 11B magic angle spinning nuclear magnetic resonance (MAS NMR) study took place to investigate the effects of Li on chemical durability and the B network.

# Experimental

## Fabrication

Li50Na50 and Li60Na40 were produced in two batches each, with a number suffix denoting the batch number. The nominal compositions of Li50Na50 and Li60Na40 compared to Mg-EM are tabulated in Table 1. The dried and weighed precursors (Al2O3, B2O3, La2O3, LiCO3, MgO, Na2B4O7 and SiO2) were heated in a 90 %-Pt 10%-Rh 200 mL crucible to 750 °C (10 °Cmin-1), held for 3 hours, and then heated to 1500 °C for pouring. The glass was poured onto graphite-coated steel plates, cooled and crushed. This procedure was then repeated, but the steel plates were pre-heated to 250 °C and held for 2 hours. After cooling to room temperature, the glass was annealed at 550 °C for 2 hours and cooled in the furnace over 16 hours. All batches were optically clear.

Table.1: The nominal cation atomic percent (at.%) compositions of Li50Na50 and Li60Na40 compared with Mg-EM [33].

|  | Nominal at.% |  |  |
| --- | --- | --- | --- |
| Element | Mg-EM | Li50Na50 | Li60Na40 |
| Al | 4.87 | 4.87 | 4.87 |
| B | 27.58 | 27.58 | 27.58 |
| La | 1.72 | 1.72 | 1.72 |
| Li | 0.00 | 7.69 | 9.23 |
| Mg | 6.54 | 6.54 | 6.54 |
| Na | 15.38 | 7.69 | 6.15 |
| Si | 43.91 | 43.91 | 43.91 |

Pristine pieces of annealed glass were selected for density measurements and electron probe microanalysis (EPMA). The remaining glass was crushed in an agate mortar and pestle set and sieved using a nest of 75 µm and 150 µm stainless steel test sieves. The sized glass powders were then decontaminated of magnetic particles and washed using only absolute ethanol following the product consistency test type B (PCT-B) protocol [34] using ethanol for the steps which required deionised water (DI). The washed glass was dried at 90  2 °C for 16 hours before being weighed, checked with a magnet, and placed into clean sample vials.

## Dissolution and leachate characterisation

Static batch dissolution experiments took place using 0.390 to 0.400  0.001 g of washed and sized glass in 4.00 ± 0.08 mL of type 1 DI (18.2 MΩ.cm at 25.0 °C) per leaching vessel at 40 ± 0.1 °C and 90 ± 0.1 °C for 1, 2, 4 and 16 weeks ( 2% of each leaching duration). A leachant volume to sample mass ratio of 10.0 ± 0.5 mL/g was targeted, which yielded a surface area to volume ratio (SA/V) of 1948 to 2200 m-1 depending upon glass density assuming a geometric mean particle diameter of 112.5 µm. Leaching vessels consisted of a 5 mL polytetrafluoroethylene (PTFE) liner and lid inside a stainless-steel reaction vessel, which were placed into pre-heated aluminium block heaters. Each leaching duration at each temperature for each composition consisted of samples leached in triplicate alongside duplicate blanks. At the end of each leaching interval, leachates were filtered using 0.45 µm nylon filters (Whatman Puradisc) and a 1.00  0.02 mL aliquot from each filtered leachate was diluted 5 times with 4.00  0.08 mL Teflon double distilled 1 wt.% HNO3 for analysis on a Perkin-Elmer NexION 350D ICP-MS. Solid samples were dried at 90  2 °C for 16 hours. Separate aliquots of undiluted, filtered leachates had their pH measured using a Mettler Toledo LE438 pH electrode with FE20 FiveEasy benchtop pH meter. The pH meter was calibrated before the end of each sampling interval using NIST traceable buffer standards of 7.00 and 10.00 ± 0.01.

All glass species within the leachates were analysed using ICP-MS alongside Fe, Zn and Pb to check for contamination. All isotopes lighter than, and including, 57Fe were analysed in collision mode using kinetic energy discrimination with a He gas filled collision cell. Standard mode was used for all other elements. SPS-SW2 (Spectrapure Standards) and a 10 ng/ml standard (SCP Science) were used to verify the calibration standards. ICP data were corrected and treated following the calculations outlined in the PCT methodology [34], with normalised releases (NLi) calculated for each element from its’ blank and mass loss corrected concentration within solution (CiSample), its’ elemental mass fraction within the pristine glass (fi), and the SA/V for each leaching vessel following equation 1 below. The NLi measures the extent of glass dissolution and allows the concentrations to be accurately compared with other glass compositions.

NLi=CiSamplefi∙SAV      (1)

## Wasteform characterisation

### Compositional characterisation

EPMA was used to analyse the concentrations of Mg, La and Si within each glass batch using three glass pieces mounted in epoxy resin and polished using diamond pastes down to 3 µm. The polished stubs were carbon coated prior to analysis. A Cameca SX100 electron microprobe with a 10 µm beam diameter, 15 keV acceleration voltage, and beam current of 20 nA was used. Mineral standards were used to calibrate the instrument: periclase for Mg, diopside for Si, and lanthanum hexaboride for La. Each piece of glass was analysed using 12 randomly spaced spots. Acid digestion of the washed and sized glass batches in HF and HNO3 then solution-based inductively coupled plasma optical emission spectroscopy (ICP-OES, Department of Chemistry, University of Sheffield) were used to obtain the concentrations of Li, B, Na and Al. The digested samples were analysed alongside certified reference materials for all glass elements using a Spectro Ciros Vision ICP-OES.

### Physical characterisation

Archimedes’ principle was used to find the density of all four batches in triplicate using pristine glass pieces which contained no visible defects. An Ohaus Pioneer analytical balance with weigh-below hook mounted onto a steel frame was used for the density measurements with a piece of wire and beaker of room temperature DI (temperature recorded throughout).

The particle size distributions of the sized glasses were obtained through laser diffraction analysis on a Malvern Instruments Mastersizer E to ensure they were close to the geometric mean of 112.5 µm. An ethanol dispersant was used with 50 to 100 mg of sample (approximately 25000 to 55000 particles) inside a small enclosed cell with a PTFE magnetic stirrer. A beam length of 14.3 mm was used to analyse particles from 1.2 µm to 600 µm.

X-ray powder diffraction (XRD) took place to assess whether the pristine glass batches were amorphous and whether a detectable quantity crystalline alteration products had formed after 16 weeks of dissolution. For each batch and dissolution temperature, 20.00 ± 0.01 mg of washed and sized pristine glass or 16-week leached glass (one selected from each triplicate) was weighed onto a zero-background sample holder. Samples were analysed on a Bruker D8 Advance X-ray diffractometer with Cu Kα1 radiation. Angles between 10 ° and 60 ° (2θ) were analysed.

### 11B MAS-NMR

Room temperature 11B MAS NMR spectroscopy was carried out on all washed and sized pristine samples and one leached sample from each triplicate to provide insights into the effects of Li on the B network and its behaviour during dissolution. Single-pulse 11B Bloch decay experiments used a small pulse-angle at a spectrometer frequency of 160.32 MHz on a Varian Infinity Plus spectrometer with an 11.7 T magnet. Approximately 80 mg of sample was packed into 4.0 mm zirconia rotors and spun at 10 kHz. Final spectra were obtained by accumulating 240 Bloch decays following a  π14 pulse (0.4 µs) with a pulse delay of 6 s, after testing that these were non-saturating conditions. Spectra were referenced to the liquid scale (15% BF3.OEt2 in CDCl3) using a secondary reference of solid NaBH4 at -42.05 ppm.

### 7Li MAS-NMR

7Li MAS NMR spectroscopy took place on the four washed and sized Li-Mg-EM batches as well as one sample from each triplicate from the 112 day leached samples. Single-pulse 7Li Bloch decay experiments took place using the same spectrometer, rotors, spin speed and samples masses as the 11B experiments at a spectrometer frequency of 194.21 MHz. Spectra consisted of 30 Bloch decays following a π2 pulse (4.8 µs) with a pulse delay of 132.5 s. Spectra were referenced to the liquid scale using a 1.0 M LiCl in deionised water reference at 0.0 ppm.

# Results

## Wasteform compositions

Table 2 displays the nominal and measured compositions of the Li-Mg-EM batches. All oxide contents for all batches were within 7.5 % of their target value, with the exception of Li2O for Li50Na50-1; this lower Li concentration is compensated by lower B and Na concentrations, resulting in Li50Na50-1 having a similar Li:Na and B:Li+Na as Li50Na50-2. Therefore, these compositions were considered to be internally consistent.

Table 2: Table of the nominal and measured oxide weight percent (wt.%) compositions of the four Li-Mg-EM batches. For EPMA, errors are reported as ± one standard deviation calculated from the 36 points analysed. For ICP-OES, errors are conservatively reported as 5% of the measured value as all values reported RSD less than 5%.

|  |  | Nominal oxide wt.% |  | Measured oxide wt.% |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Technique | Oxide | Li50 Na50 | Li60 Na40 | Li50Na50 Batch 1 | Li50Na50 Batch 2 | Li60Na40 Batch 1 | Li60Na40 Batch 2 |
| ICP-OES | Al2O3 | 5.24 | 5.26 | 5.12 ± 0.26 | 5.10 ± 0.26 | 5.10 ± 0.26 | 5.10 ± 0.26 |
| ICP-OES | B2O3 | 20.24 | 20.34 | 19.45 ± 0.97 | 20.67 ± 1.03 | 20.25 ± 1.01 | 20.03 ± 1.00 |
| EPMA | La2O3 | 5.91 | 5.94 | 6.18 ± 0.50 | 6.12 ± 0.48 | 6.37 ± 0.77 | 6.16 ± 0.37 |
| ICP-OES | Li2O | 2.42 | 2.92 | 2.06 ± 0.10 | 2.39 ± 0.12 | 2.82 ± 0.14 | 2.76 ± 0.14 |
| EPMA | MgO | 5.56 | 5.59 | 5.55 ± 0.34 | 5.77 ± 0.34 | 5.92 ± 0.65 | 5.74 ± 0.29 |
| ICP-OES | Na2O | 5.02 | 4.04 | 4.65 ± 0.23 | 4.91 ± 0.25 | 3.98 ± 0.20 | 3.95 ± 0.20 |
| EPMA | SiO2 | 55.61 | 55.91 | 56.07 ± 1.99 | 56.11 ± 2.10 | 55.75 ± 3.63 | 56.00 ± 1.43 |

## Physical characterisation results

Densities were highly consistent across batches, with the Li50Na50 batches being within error of the Li60Na40 batches and an average density of 2.52 g/cm3 measured in both the Li50Na50 and Li60Na40 compositions (Supplementary table 1); demonstrating no measurable change in density with the Li:Na ratio. Laser scattering analysis demonstrated that all four batches were close to the geometric mean of 112.5 µm with uniform particle size distributions, confirming the effectiveness of the sieving and washing methodology (Supplementary table 1).

Initial XRD of the washed and sized pristine glass batches revealed a small peak characteristic of cristobalite in Li50Na50-1 (Fig. 1). However, characteristic cristobalite peaks of a similar size were also found to be present in a crushed and sieved pristine international simple glass sample (ISG) (Supplied by Savannah River National Laboratory) [1]. Additionally, re-running the XRD of the Li50Na50-1 sample showed it to be amorphous. Therefore, the quantity of this cristobalite was concluded to be negligible. All other batches were shown to be amorphous (Fig. 1). Analysis of Li50Na50 and Li60Na40 leached at 40 ºC and 90 ºC for 16 weeks revealed no detectable secondary alteration phases (Supp. Fig. 1).

Figure 1: X-ray diffractograms of the four washed and sized Li-Mg-EM batches alongside crushed and sieved international simple glass (ISG). The peaks labelled with "C" correspond to the characteristic peaks of synthetic α-cristobalite (ICDD card number [082-1408]).

## Characterisation of the boron network

11B MAS-NMR was used to probe how the B network changed with the Li:Na contents of the glass and whether selective dissolution of IIIB units or IVB units occurred. The differing electric field gradients associated with IIIB and IVB species results in a narrow Gaussian IVB peak centred at 0 ppm and a broad IIIB doublet centred at approximately 12 ppm; consisting of both ring and non-ring IIIB contributions at approximately 11 and 17 ppm respectively [33]. As the area under each peak is proportional to the number of atoms in that environment, quantitative comparisons of the number of IIIB relative to IVB species can be made. Spectra in the figures were normalised to their IVB peak so that changes in the proportions of IIIB to IVB species could be compared through the size of the IIIB doublet.

Comparisons of the spectra acquired for the pristine samples of the four Li-Mg-EM batches with Mg-EM (taken from another study [33]) demonstrated no significant change in the proportion of IIIB to IVB species with the changing Li:Na ratio (Fig. 2). Minor differences observed in the intensity of the IIIB doublets are within the range of the total alkali metal contents of the glasses, which varied slightly between batches. When the leached samples are considered, for Li50Na50 and Li60Na40 leached at 40 °C we observed a negligible change in the amount of IIIB relative to IVB between 0 and 112 days of dissolution (Fig. 3a and Fig. 3c). However, at 90 °C we observed a significant decrease in the fraction of IIIB relative to IVB after 112 days of leaching for both compositions (Fig. 3b and d).

Figure 2:11B MAS-NMR spectra acquired at 160 MHz for washed and sized pristine: Li50Na50-1 (Blue), Li50Na50-2 (Green), Li60Na40-1 (Orange), Li60Na40-2 (Red) and Mg-EM (Black; the signal to noise ratio for Mg-EM differs from the Li-Mg-EM samples as this spectrum was taken from another study for comparison [33]). Some spectra were shifted to correct for referencing errors (Li50Na50-1 +0.2 ppm, Li50Na50-2 -0.1 ppm, and Mg-EM -0.2 ppm). Spectra were normalised to the IVB peak as to compare changes in the proportion of IVB to IIIB through the IIIB peak.

Figure 3: 11B MAS-NMR spectra acquired at 160 MHz for Li50Na50 leached at 40 °C (a), Li50Na50 leached at 90 °C (b), Li60Na40 leached at 40 °C (c) and Li60Na40 leached at 90 °C (d). The coloured lines represent: the first respective pristine glass batch (Black), the second pristine glass batch (Blue), 7 days of dissolution (Green), 14 days of dissolution (Yellow), 28 days of dissolution (Orange), and 112 days of dissolution (Red). Spectra were normalised to the IVB peak as to compare changes in the proportion of IIIB to IVB through the IIIB peak. Some spectra were shifted to correct for referencing errors for the sake of comparison (Li50Na50-2 -0.3 ppm in (a) and Li50Na50-1 +0.3 ppm in (b)).

Quantification of the spectra took place through curve fitting the IVB peak and IIIB doublet (ring and non-ring structures) using DMFIT software [35]. It should be noted that the first-order satellite transition sidebands fall under the IVB peak due to the low electric field gradient of IVB units and therefore need to be considered during the quantification [33]. To this end, a first-order spinning sideband manifold based upon the profile of the observed sidebands was fitted alongside the Gaussian IVB peak and the IIIB quadrupole doublet. Ring and non-ring IIIB peaks were fitted using separate peaks that coincided with chemical shifts and quadrupole coupling constants previously reported for ring and non-ring resonances [36,37]. Owing to the observed asymmetry of the IVB peak, a satisfactory fit could not be attained using a single Gaussian, Lorentzian or Voigt peak alone (Example in Supp. Fig. 2); this was also the case for Mg-EM (Supp. Fig. 3, spectrum from [33]). This asymmetry likely arises due to asymmetric distribution resonances from IVB sites in the glass and was taken into account by adding another Voigt peak under the IVB peak (Example in Supp. Fig. 4). It should be noted that this second IVB peak was fit solely to account for the observed asymmetry and has no significant interpretation; both peaks simply represent IVB species and the area of this second peak was simply added to the area of the main IVB peak when calculating the relative proportions of IIIB and IVB species.

The relative areas of fitted peaks provide a measure of the fractions of IIIB and IVB within the glass which could be compared to quantitatively investigate how the B network evolves through dissolution. Table 3 shows the fractions of IIIB and IVB estimated in the pristine, 7 day and 112 day samples from the curve fitting alongside their respective calculated IIIB/IVB ratios and the difference in the fraction of IIIB relative to IVB between the leached and pristine samples. The analysed molar concentrations of B, Li and Na within the pristine glasses as well as the results from fitting the pristine Mg-EM spectrum [33] using two peaks to fit the IVB peak are also given for comparison.

Table 3: Measured elemental molar percentages of Li, Na and B in the pristine Li-Mg-EM samples alongside the fractions of IIIB and IVB estimated from quantifying the pristine, 7 d leached and 112 d leached (40 and 90 °C) 11B NMR spectra. For the sake of comparison, values for Mg-EM are given (Concentrations and spectrum taken from another study whilst the spectrum was quantified using two IVB peaks as in the Li-Mg-EM samples.) Errors given on the concentrations are conservatively reported as 5% of the measured value as all values reported RSD less than 5%, with the errors on the [B]/[Total alkali], [IIIB] and [IVB] propagated from these values.

|  |  | Li50Na50 |  |  |  |  |  | Li60Na40 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Pristine |  | 40 °C Leached |  | 90 °C Leached |  | Pristine |  | 40 °C Leached |  | 90 °C Leached |  |
|  | Mg-EM1 | Li50Na50-1 | Li50Na50-2 | 7 d | 112 d | 7 d | 112 d | Li60Na40-1 | Li60Na40-2 | 7 d | 112 d | 7 d | 112 d |
| [Li] (at.%) | - | 6.7 ± 0.6 | 7.5 ± 0.7 | - | - | - | - | 8.9 ± 1.0 | 8.8 ± 0.8 | - | - | - | - |
| [Na] (at.%) | 15.1 ± 0.8 | 7.3 ± 0.7 | 7.4 ± 0.7 | - | - | - | - | 6.1 ± 0.7 | 6.1 ± 0.5 | - | - | - | - |
| [B] (at.%) | 28.3 ± 3.6 | 27.2 ± 2.6 | 27.9 ± 2.7 | - | - | - | - | 27.5 ± 3.1 | 27.4 ± 2.4 | - | - | - | - |
| [B]/ [Total alkali] | 1.87 ± 0.34 | 1.94 ± 0.37 | 1.87 ± 0.36 | - | - | - | - | 1.84 ± 0.42 | 1.84 ± 0.33 | - | - | - | - |
| IIIB (%) | 61.7 | 63.5 | 62.9 | 63.5 | 62.7 | 61.2 | 61.0 | 62.6 | 62.9 | 63.2 | 62.9 | 62.8 | 60.5 |
| IVB (%) | 38.3 | 36.5 | 37.1 | 36.5 | 37.3 | 38.8 | 39.0 | 37.4 | 37.1 | 36.8 | 37.1 | 37.2 | 39.5 |
| [IIIB] (at.%) | 17.5 ± 2.2 | 17.3 ± 1.7 | 17.6 ± 1.7 | - | - | - | - | 17.2 ± 1.9 | 17.2 ± 1.5 | - | - | - | - |
| [IVB] (at.%) | 10.8 ± 1.4 | 9.9 ± 0.9 | 10.3 ± 1.0 | - | - | - | - | 10.3 ± 1.2 | 10.2 ± 0.9 | - | - | - | - |
| IIIB/IVB | 1.61 | 1.74 | 1.70 | 1.74 | 1.68 | 1.58 | 1.56 | 1.67 | 1.70 | 1.72 | 1.70 | 1.69 | 1.53 |
| Difference in IIIB from pristine (% points) | - | - | - | 0.6 | -0.8 | -1.7 | -2.5 | - | - | 0.3 | 0.3 | -0.1 | -2.1 |

When comparing spectra simply through normalising them to their IVB peaks, this neglects to consider that the intensity and position of the first-order satellite transition sidebands differed slightly between samples. As such, changes in the fraction of IIIB as alluded to through overlaying sample spectra normalised to their IVB peak (as in Fig. 2 and Fig. 3) can differ from those calculated from curve fitting the spectra (Table 3). However, in this instance, the overlaid spectra and integrated peak intensities seem to be in good agreement.

Minor differences between the fractions of IIIB in the four pristine glass batches may be attributed to small differences in their respective total alkali metal to B ratios. As the errors associated with the concentration measurements of the glasses are large, the exact cause of these subtle discrepancies could not be further investigated. For comparison, the quantification of the Mg-EM fit is also shown; these values were in very good agreement with the fit used in the original study [33]. The consistency of the IIIB fractions in the pristine Li-Mg-EM batches suggests that the discrepancy in the fraction of IIIB observed between Li-Mg-EM and Mg-EM can be explained by differences in the alkali metal to B ratios of Mg-EM and Li-Mg-EM. That is, if these changes were real we would expect to observe a similar effect between Li50Na50 and Li60Na40 as well.

As displayed in the spectra (Fig. 3) after 112 days of leaching at 90 °C, we observe a significant drop in the proportion of IIIB to IVB units in both compositions. Interestingly, whilst the majority of this drop appears to occur after just 7 days in Li50Na50 (-1.7%), there is a negligible change for Li60Na40 after 7 days (-0.1%). It should be considered that the errors associated with the differences calculated between the leached and pristine sample fits would be less than those associated with comparing the pristine sample fits as the starting B to total alkali metal ratio will not vary when comparing leached with pristine samples. After 7 days of leaching at 40 °C for both compositions we observed a very slight increase in the fraction of IIIB. Similarly, after 112 days of leaching there is no further change for Li60Na40 whereas for Li50Na50 there is a slight drop in the fraction of IIIB. However, it is unclear whether these increases are significant as they likely fall within the error of the fits.

Attempts to characterise the role of Li in the glass through 7Li MAS-NMR demonstrated no significant difference in chemical shift or peak width between the Li50Na50 and Li60Na40 batches (Supp. Fig. 5).

## Leachate compositions

Leachates were analysed for all the constituent elements of the Li-Mg-EM compositions and common contaminants. All glass constituents within the leachates were at concentrations well above detection limits, with the exceptions of La in the leachates at both temperatures and Al at 40 ºC. Average blank concentrations of less than 0.05 µg/ml were observed for all elements except Na and Si which were less than 0.5 µg/ml. Triplicate RSD values less than 7.5 % were observed for all elements except Al. For comparison, the normalised releases of mobile glass species (B, Li, Na) and Si were plotted alongside Mg-EM [33] and MW25 [Publication in preparation] (Fig. 4) which had been leached in similar dissolution experiments.

Using B as a tracer for glass dissolution (Fig. 4a), comparing the releases of B from Mg-EM with Li50Na50 and Li60Na40 at 90 °C it is clear that the substitution of Li for Na had a significant negative impact on the chemical durability of the glass. However, comparing Li50Na50 with Li60Na40 at both 40 and 90 °C demonstrates that despite having an initially higher rate of alteration, the higher Li:Na had no impact on the residual rate of alteration. That is, whilst the substitution of Li into Mg-EM had a long-term detrimental impact on chemical durability, the further substitution of more Li for Na had no long-term effect. The time taken for the NLB of Li50Na50 and Li60Na40 to converge was longer at 40 °C than at 90 °C, presumably as more time was required to reach the residual rate regime at 40 °C. As the total alkali metal contents of Li50Na50, Li60Na40, and Mg-EM were all equal, this effect could only be attributed to the change in Li:Na.

Interestingly, the same effect is also visible in the NLLi at 40 °C and 90 °C, with the exception of 112 days at 90 °C where the NLLi of Li60Na40 is insignificantly higher than that of Li50Na50 (Fig. 4b). Changing the Li:Na had a smaller effect on the NLNa (Fig. 4c): at 40 °C the NLNa of Li50Na50 and Li60Na40 were consistently within error of one another except at 14 days, whereas at 90 °C the NLNa of the Li50Na50 and Mg-EM remained equal for all leaching durations whilst that of Li60Na40 was higher than Mg-EM at 7 days. Whilst at 7 and 14 days at 90 °C the NLNa of Li60Na40 was higher than that of Li50Na50, the difference at 14 days was considered negligible as at this time the NLNa of both Li-Mg-EM batches were within error of that of Mg-EM. At 7 days of dissolution at 90 °C, the NLSi of Li50Na50 was marginally higher than that of Li60Na40 but after this time they converged to remain equal throughout dissolution; later also converging with the decreasing Mg-EM NLSi after 112 days of dissolution (Fig. 4d). At 40 °C, the NLSi of Li50Na50 and Li60Na40 follow an opposite, decreasing trend with time whilst the NLSi of Li50Na50 remained consistently higher than that of Li60Na40 throughout dissolution. Comparing the NLSi suggests that Si saturation conditions were achieved after 14 days at 90 °C and 7 days at 40 °C.

It was noted that the pH of the leachates were slightly higher at 40 °C than those at 90 °C. Further, the pH of the Li60Na40 and Li50Na50 leachates were noted to remain equal throughout dissolution except for the 112 day leachates at 40 °C (Supp. Fig. 6). However, as this difference was only 0.06 pH units, this was considered negligible.

Figure 4: Normalised releases of B (a), Li (b), Na (c) and Si (d). For comparison, normalised releases for Mg-EM at 90 °C [33] and MW25 at both 40 °C and 90 °C [publication in preparation] are also given. Errors are given to 1 standard deviation calculated from the triplicate values, with the exception of the Mg-EM releases which have been assigned a conservative 10 % error due to absence of available triplicate data from the original study.

# Discussion

## The pristine boron network

It has been demonstrated in other studies of Li-Na and Li-K borosilicate systems using 17O MAS-NMR that instead of being purely randomly mixed, network modifying cations of higher field strengths (Li) associate preferentially with non-bridging oxygen (NBO) in the Si network compared with those of lower field strengths (Na or K) [36,37]. Combined with observations of a larger number of Si-NBOs in Li, Li-Na or Li-K borosilicates compared with Na, K or Na-K borosilicates [37,38], it was suggested that Li preferentially modifies the Si network over Na. Similarly, using 11B MAS-NMR, comparable chemical shifts for a Li-Na borosilicate and a Na borosilicate have been observed for both IIIB ring and IVB peaks, showing preference for Na to charge compensate the B network over Li [37]. The authors suggested these preferences resulted in nanoscale heterogeneity in Li-Na borosilicates, with Li-Si-rich domains present in a Na-rich borosilicate host matrix [37]. Additional evidence for Na preferentially compensating the B network over Li has been provided in elemental profiles of leached glass, which have displayed similar sharp profiles for B and Na behind a wide Li interdiffusion layer [39]. The authors attributed this difference in behaviour to Na being more strongly bonded in its’ charge compensation role than Li in its’ NBO role [39].

The near-identical proportions of IIIB to IVB associated with pristine Mg-EM, Li50Na50 and Li60Na40 (Li:Na 0, 1.0 and 1.5 respectively) demonstrates that there is no measurable change in the coordination of the B network associated with the changing Li:Na ratio. This conclusion is justified not only by the visual similarity of the spectra (Fig. 2) but also the estimated concentrations of IIIB and IVB for these batches being within error of one another (Table 3). Further, the similar peak shapes for the IIIB doublets suggests there is also no change in the proportion of non-ring to ring IIIB structures.

As Li is expected to preferentially modify the Si network [37], Li will likely not compete with Na to compensate IVB units [40]. As a result, despite the Na contents of Li60Na40 being approximately 2.5 times less than that of Mg-EM, the majority of IVB in Li50Na50 and Li60Na40 would still be charge compensated by Na. This would contribute to the B spectra being similar between all samples, but in both Li50Na50 and Li60Na40 lower concentrations of Na than IVB were observed (Table 3). Therefore, when the concentration of Na is reduced to below that of IVB, another cation must be charge compensating the IVB in its’ place else the proportion of IVB to IIIB would reduce. It is therefore hypothesised that at higher Li:Na ratios a significant amount of Li compensates the B network in place of the removed Na. However, the preference of Li to continue modifying the Si network at higher Li:Na ratios may be reflected in the similarity between the 7Li MAS-NMR spectra of the two analogue types (Supp. Fig. 5); although this result may be questionable due to the small range of chemical shifts associated with 7Li spectra potentially meaning any subtle differences between analogues would be immeasurably small. Additionally, it should also be considered that whilst Li is preferentially modifying the Si network, even at lower Li:Na ratios a small fraction Li may also charge compensate IVB units. Some La and Mg may also fulfil a charge compensation role to the B network once there is insufficient Na. However, alkaline earths (in this case Mg) are expected to compensate IVAl over IVB units preferentially to alkali metals [36,41], suggesting Mg likely maintains its’ role compensating Al in the network as the Li:Na ratio changes.

## Lithium promoting glass dissolution

Using the releases of B as a measure of the extent of glass alteration [42,43], by comparing the NLB of Li50Na50 and Li60Na40 at 90 °C with Mg-EM (Fig. 4a) it is clear that substituting Li for Na had a notable detrimental impact on wasteform durability; with the NLB of the two Li containing glasses being similar and significantly higher than the Mg-EM glass (which contains no Li) by a factor approaching two at long dissolution times. Similarly, from comparing the NLB of Li50Na50 and Li60Na40 at both 40 and 90 ° (Fig 4a), it is clear that raising the Li:Na contents had a detrimental effect on chemical durability during the initial dissolution regimes but had no effect on the rate of residual alteration. Interestingly, at both temperatures the same effect is also visible in the NLLi, with only a minor difference between the two Li-Mg-EM compositions at 112 days at 90 °C (Fig. 4b). However, this effect is only partially observed in the NLNa at 90 °C and it is not observed at all in the NLNa at 40 °C (Fig. 4c) or the NLSi at either temperature (Fig. 4d).

Quantification of the spectra of the pristine glasses and their respective samples leached for 7 and 112 days at 40 °C displayed no significant evolution in the proportion of IIIB to IVB (Table 3) or visible change in the proportion of ring to non-ring IIIB structures. However, at 90 °C a significant drop in the proportion of IIIB to IVB was observed after 112 days in both Li50Na50 and Li60Na40. This demonstrates that at 90 °C preferential dissolution of IIIB units is taking place. It is hypothesised that similar incongruent boron dissolution is also taking place at 40 °C but due to the significantly lower rate of glass alteration compared with 90 °C this effect is immeasurably small. This effect cannot simply be the result of the IIIB units having lower chemical durability than IVB units, as no such incongruence was observed after leaching Mg-EM at 90 °C for 112 days [33]. It was therefore shown that substituting Li for Na promotes dissolution of IIIB units.

As previously discussed, Na in its’ charge compensation role is expected to be more strongly bonded than Li in its’ network modifying role [39]. In this view, it is hypothesised that the incongruent leaching of IIIB units after 112 days and the long-term decrease in chemical durability associated with the Li-Mg-EM analogues compared with Mg-EM arises due to a combination of the preference of Li to modify the Si network and due to network modifying Li leaching more readily.

As Li preferentially modifies the Si network, the Si network of the Li-Mg-EM analogues has a higher number of NBOs and is more depolymerised than that of Mg-EM. As water ingresses into the glass, the higher degree of depolymerisation may cause the Li-modified Si network to present less of a barrier to the inward diffusion of water species than a more polymerised network. This would result in more rapid hydration of the glass network in a composition containing Li. Further, as Li leaches more easily from its’ modifying role than Na from its’ compensating role, in the Li-Mg-EM analogues a nanoscale region denuded of alkalis with a more open depolymerised Si character is formed at a faster rate; also resulting in further and faster interdiffusion into the glass.

Although there is a preference for Na to charge compensate IVB, the higher concentration of Na than IVB in Mg-EM (Table 3) suggests that part of the excess Na concentration may be modifying the Si network. Further, it is reasonable to expect that a very small fraction of Na is also modifying the Si network in the Li-Mg-EM compositions. It is hypothesised that the smaller ionic radius of Li compared with Na and a preferential exchange of protonated water species for Li over Na may result in Li presenting less of a barrier to the hydration of the glass and leaching out earlier than Na to provide a more open glass structure respectively as compared with Mg-EM. Therefore, in addition to the effects of depolymerisation and cation preferences discussed in the previous paragraph, it is expected that having Li as a modifier to the Si network facilitates faster hydration of the glass than if Na were modifying it.

As a high amount of energy is required to break the bonds of the Si network [21], this enhanced degree of depolymerisation and rate of glass hydration brought about by Li has a negligible impact on the rate of dissolution of the Si network. The low energy barrier required to hydrolyse the B network bonds [21], however, means that there is an increased rate of B network dissolution; as is reflected by the NLB of Li-Mg-EM being higher than those of Mg-EM throughout dissolution (Fig. 4a). As Na preferentially compensates the B network, it remains largely unaffected by the effects of Li on the Si network; as is reflected by the NLNa of Li50Na50 and Mg-EM being within error of one another throughout dissolution. That is, the faster hydration of the glass may result in more rapid dissolution of the B network but charge compensating Na appears unaffected. Consequently, these effects cause IIIB units to leach at a faster rate whilst the Na compensated IVB units are less affected, resulting in incongruent dissolution of IIIB and IVB units.

Comparing the NLB and NLLi (Fig. 4a and 4b) of Li60Na40 and Li50Na50 at both temperatures, it could be expected that the initially increased rate of glass dissolution associated with Li60Na40 arises from the increased Li contents enhancing the previously discussed depolymerisation and hydration effects. The difference between the NLLi of Li50Na50 and Li60Na40 at 112 days could potentially be attributed to the precipitation of Li-bearing phases from solution, but this difference is small enough to be considered negligible. It should also be considered that these differences may be influenced by a lower concentration of Na in Li60Na40 available to compensate the B network, likely requiring Li in its’ place. The similarity between the residual rates of alteration of Li60Na40 and Li50Na50 for all releases at both temperatures suggests that despite an increased initial rate of dissolution brought about by a higher Li:Na ratio, in the later stages of dissolution a similar passivating altered layer structure is formed regardless of composition. After such a layer is formed, any hydration effects would be significantly less relevant. Therefore, raising the Li:Na ratio from a value of 1.0 to 1.5 was concluded to not impact the long-term chemical durability of the glass.

After just 7 days of leaching at 90 °C incongruent B network dissolution was observed in Li50Na50 but not in Li60Na40 (Table 3). However, there was a decrease in chemical durability associated with Li60Na40 compared with Li50Na50 during this time (Fig. 4a and 4b). When considering these results, it should be noted that at this time the NLNa of Li60Na40 was also slightly higher than that of Li50Na50 whilst the NLNa of Li50Na50 and Mg-EM were within error of one another (Fig. 4c). Due to there being less Na than IVB, a significant fraction of Li likely compensated the IVB units in place of Na at higher Li:Na ratios (Li60Na40). The fraction of IVB compensated by Li would likely be subject to the previously discussed effects, as would any Na and IVB compensated by Na which is closely neighboured by Li. Therefore, more of the Na and more IVB units in Li60Na40 compared with Li50Na50 were affected by these Li effects; resulting in higher IVB releases, virtually congruent dissolution of the B network, and a small increase in the NLNa at 7 days for Li60Na40 compared with Li50Na50. As the majority of the IVB in Li60Na40 is still compensated by Na, these differences appear to become more negligible over time such that the NLNa of Li50Na50 and Li60Na40 after 14 days remained within error of one another and similar magnitudes of incongruent B network dissolution are clearly visible after 112 days for Li50Na50 and Li60Na40. At 40 °C, no such incongruence or Na behaviour was visible, potentially due to the glass not being altered enough.

The small difference between the Li-Mg-EM NLSi at just 7 days at 90 °C and the consistently higher NLSi of Li50Na50 at 40 °C throughout dissolution coincide with Si saturating in solution after 7 days at 40 °C and 14 days at 90 °C.  The longer time taken to reach saturation at 90 °C may be attributed a higher apparent Si solubility limit at 90 °C than at 40 °C, also influenced by the higher in-situ pH at higher temperatures [44]. As such, it appears that the apparent Si solubility limits for Li50Na50 and Li60Na40 were very similar at 40 °C and the same at 90 °C.  At this steady state Si concentration, the rate of Si dissolution matches the rate of Si precipitation [43,45]; any subtle differences between the rates of Si network dissolution for Li50Na50 and Li60Na40 would therefore not be reflected in the NLSi. Consequently, for such subtle compositional changes, the NLSi cannot provide detailed information regarding the associated changes in the kinetics of dissolution of the Si network.

## Suitability as an analogue

For simplicity, the NLB were used to assess the suitability of the analogues as representations of MW25 (Fig. 4a). In this view, Li50Na50 was shown to be an excellent analogue of MW25 during the later dissolution regimes, with an NLB within error of MW25’s from 28 days onwards (112 day Li50Na50 being within error of the 126 day MW25 measurement). The 7 day 90 °C MW25 NLB was noted to be between those of Li50Na50 and Mg-EM. Whilst an intermediate Li:Na of 1.0 was shown to have a worse chemical durability than a Li:Na of 0.0 (Mg-EM), Li50Na50 better matched the chemical durability of MW25 than Mg-EM during the later dissolution regimes. However, at 40 °C the releases of all elements except Si from MW25 were significantly lower than from the Li-Mg-EM batches. The reasons for this remain unclear and potentially might have arisen due to differences in experimental conditions used.

It is expected that the presence of Li significantly affects the mechanical and structural properties of the glass, including chemical durability [26,46], in ways which would be difficult to simulate in a Li-free composition. Further, in atom probe analyses of interdiffusion in glasses, Li is seen to leach in a wide interdiffusion profile preceding the Na ion-exchange front [39]; consistent with the dissolution behaviour observed here of preferential release of Li over Na in the interdiffusion stage of glass dissolution. Consequently, representing Li in the simplified analogue composition better replicates the dissolution processes of MW25.

# Conclusions

It was shown that the proportion of IIIB to IVB remained constant in the pristine glasses regardless of the Li:Na ratio. This was consistent with Na preferentially charge compensating the B network and, when Li was substituted for Na, it preferentially modified the Si network. However, a lower concentration of Na than IVB in these glasses implied at higher Li:Na ratios Li also charge compensated the IVB network.

At 90 °C and long duration, IIIB units were shown to leach more readily than IVB units when the glass contained Li. Similar effects may be occurring at 40 °C, but may not be sufficiently different to be observed at lower temperature. During the initial stages of dissolution, a faster rate of Li releases and glass alteration (B release) was observed for Li containing glasses, as is consistent with Li preferentially depolymerising the Si network in the pristine glass and leaching more readily than Na in its’ charge compensation role.

Lithium increases the residual rate of dissolution at both 40 and 90 °C compared with a Na-only glass such that a similar passivating altered layer formed regardless of an increased initial rate of glass dissolution. As such, it was concluded that the increased Li:Na ratio had no impact on the long-term chemical durability of the glasses and that a simplified analogue of MW25 glass should contain Li to more accurately reflect the glass behaviour in solution.

Acknowledgements

The authors would like to thank: Jason Day (Earth Sciences, University of Cambridge) for running the ICP-MS analysis, Iris Buisman (Earth Sciences, University of Cambridge) for training and assistance throughout the EPMA analyses, Giulio Lampronti (Earth Sciences, University of Cambridge) for training and assistance throughout the XRD analyses, Rui Guo (Earth Sciences, University of Cambridge) for assistance in interpreting the NMR spectra, and Neil Bramall (Chemistry, University of Sheffield) for digesting the glass and running the ICP-OES analysis.

Funding

This work was supported by EPSRC under an Industrial CASE award (Grant Ref: EP/M507350/1).

References

[1]	S. Gin, A. Abdelouas, L.J. Criscenti, W.L. Ebert, K. Ferrand, T. Geisler, M.T. Harrison, Y. Inagaki, S. Mitsui, K.T. Mueller, J.C. Marra, C.G. Pantano, E.M. Pierce, J. V. Ryan, J.M. Schofield, C.I. Steefel, J.D. Vienna, An international initiative on long-term behavior of high-level nuclear waste glass, Mater. Today. 16 (2013) 243–248. doi:10.1016/j.mattod.2013.06.008.

[2]	L. Werme, I.K. Björner, G. Bart, H.U. Zwicky, B. Grambow, W. Lutze, R.C. Ewing, C. Magrabi, Chemical corrosion of highly radioactive borosilicate nuclear waste glass under simulated repository conditions, J. Mater. Res. 5 (1990) 1130–1146. doi:10.1557/JMR.1990.1130.

[3]	T. Ma, A.P. Jivkov, W. Li, W. Liang, Y. Wang, H. Xu, X. Han, A mechanistic model for long-term nuclear waste glass dissolution integrating chemical affinity and interfacial diffusion barrier, J. Nucl. Mater. 486 (2017) 70–85. doi:10.1016/j.jnucmat.2017.01.001.

[4]	A.J. Connelly, R.J. Hand, P.A. Bingham, N.C. Hyatt, Mechanical properties of nuclear waste glasses, J. Nucl. Mater. 408 (2011) 188–193. doi:10.1016/j.jnucmat.2010.11.034.

[5]	É. Vernaz, J. Bruezière, History of Nuclear Waste Glass in France, Procedia Mater. Sci. 7 (2014) 3–9. doi:10.1016/j.mspro.2014.10.002.

[6]	R. Shaw, C. a. Auton, B. Baptie, Potential natural changes and implications for a UK GDF, Br. Geol. Surv. (CR/12/127 (2012) 175. http://nora.nerc.ac.uk/500752/.

[7]	J.P. Busby, J.R. Lee, S. Kender, J.P. Williamson, S. Norris, Modelling the potential for permafrost development on a radioactive waste geological disposal facility in Great Britain, Proc. Geol. Assoc. 126 (2015) 664–674. doi:10.1016/j.pgeola.2015.06.001.

[8]	NDA (RWM) Report no. NDA/RWM/146, Geological Disposal: Review of Alternative Radioactive Waste Management Options., 2017. https://rwm.nda.gov.uk/publication/geological-disposal-review-of-alternative-radioactive-waste-management-options/.

[9]	MET office, Temperature, rainfall and sunshine time-series: Annual mean temperature in England., (2017). https://www.metoffice.gov.uk/climate/uk/summaries/actualmonthly (accessed March 5, 2018).

[10]	J. Busby, Geothermal prospects in the United Kingdom, Proc. World Geotherm. Congr. (2010) 25–29. http://www.geothermal-energy.org/304,iga_geothermal_conference_database.html.

[11]	P.K. Abraitis, F.R. Livens, J.E. Monteith, J.S. Small, D.P. Trivedi, D.J. Vaughan, R.A. Wogelius, The kinetics and mechanisms of simulated British Magnox waste glass dissolution as a function of pH, silicic acid activity and time in low temperature aqueous systems, Appl. Geochemistry. 15 (2000) 1399–1416. doi:10.1016/S0883-2927(99)00118-3.

[12]	P.K. Abraitis, B.P. McGrail, D.P. Trivedi, F.R. Livens, D.J. Vaughan, Single-pass flow-through experiments on a simulated waste glass in alkaline media at 40 °C. II. Experiments conducted with buffer solutions containing controlled quantities of Si and Al, J. Nucl. Mater. 280 (2000) 206–215. doi:10.1016/S0022-3115(00)00040-4.

[13]	J. Birkholzer, J. Houseworth, C.-F. Tsang, Geologic Disposal of High-Level Radioactive Waste: Status, Key Issues, and Trends, Annu. Rev. Environ. Resour. 37 (2012) 79–106. doi:10.1146/annurev-environ-090611-143314.

[14]	J. Sheng, S. Luo, B. Tang, Temperature effects on the leaching behavior of a high-level waste glass form, Nucl. Technol. 123 (1998) 296–303. doi:https://doi.org/10.13182/NT98-A2900.

[15]	D. Rebiscoul, P. Frugier, S. Gin, A. Ayral, Protective properties and dissolution ability of the gel formed during nuclear glass alteration, J. Nucl. Mater. 342 (2005) 26–34. doi:10.1016/j.jnucmat.2005.03.018.

[16]	S. Gin, X. Beaudoux, F. Angeli, C. Jegou, N. Godon, Effect of composition on the short-term and long-term dissolution rates of ten borosilicate glasses of increasing complexity from 3 to 30 oxides, J. Non. Cryst. Solids. 358 (2012) 2559–2570. doi:10.1016/j.jnoncrysol.2012.05.024.

[17]	E. Vernaz, S. Gin, C. Jégou, I. Ribet, Present understanding of R7T7 glass alteration kinetics and their impact on long-term behavior modeling, J. Nucl. Mater. 298 (2001) 27–36. doi:10.1016/S0022-3115(01)00643-2.

[18]	B.C. Bunker, Molecular mechanisms for corrosion of silica and silicate glasses, J. Non. Cryst. Solids. 179 (1994) 300–308. doi:10.1016/0022-3093(94)90708-0.

[19]	Y. Inagaki, T. Kikunaga, K. Idemitsu, T. Arima, Initial dissolution rate of the international simple glass as a function of ph and temperature measured using microchannel flow-through test method, Int. J. Appl. Glas. Sci. 4 (2013) 317–327. doi:10.1111/ijag.12043.

[20]	P.K. Abraitis, D.J. Vaughan, F.R. Livens, J. Monteith, D.P. Trivedi, J.S. Small, Dissolution of a complex borosilicate glass at 60 °C: The influence of pH and proton adsorption on the congruence of short-term leaching, in: Mater. Res. Soc. Symp. - Proc., 1998. doi:10.1557/PROC-506-47.

[21]	S. Gin, L. Neill, M. Fournier, P. Frugier, T. Ducasse, M. Tribet, A. Abdelouas, B. Parruzot, J. Neeway, N. Wall, The controversial role of inter-diffusion in glass alteration, Chem. Geol. 440 (2016) 115–123. doi:10.1016/j.chemgeo.2016.07.014.

[22]	S. Gin, P. Jollivet, M. Fournier, F. Angeli, P. Frugier, T. Charpentier, Origin and consequences of silicate glass passivation by surface layers, Nat. Commun. 6 (2015) 6360. doi:10.1038/ncomms7360.

[23]	R. Hellmann, S. Cotte, E. Cadel, S. Malladi, L.S. Karlsson, S. Lozano-Perez, M. Cabié, A. Seyeux, Nanometre-scale evidence for interfacial dissolution–reprecipitation control of silicate glass corrosion, Nat. Mater. 14 (2015) 307–311. doi:10.1038/nmat4172.

[24]	M.T. Harrison, Vitrification of High Level Waste in the UK, Procedia Mater. Sci. 7 (2014) 10–15. doi:10.1016/j.mspro.2014.10.003.

[25]	C.R. Scales, Characterisation of Simulated Vitrified Magnox product manufactured on the VTR. (2011) National Nuclear Laboratory Report NNL (10) 10929 Issue 6.

[26]	A.J. Connelly, K.P. Travis, R.J. Hand, N.C. Hyatt, E. Maddrell, Composition-structure relationships in simplified nuclear waste glasses: 1. Mixed alkali borosilicate glasses, J. Am. Ceram. Soc. 94 (2011) 151–159. doi:10.1111/j.1551-2916.2010.04066.x.

[27]	M.T. Harrison, The Effect of Composition on Short- and Long-term Durability of UK HLW Glass, Procedia Mater. Sci. 7 (2014) 186–192. doi:10.1016/j.mspro.2014.10.025.

[28]	B.F. Dunnett, Review of the Development of UK High Level Waste Vitrified Product, (2007) Report for Nexia Solutions (06) 7926 Issue 4.

[29]	M.T. Harrison, C.J. Steele, A.D. Riley, The effect on long term aqueous durability of variations in the composition of UK vitrified HLW product, Glas. Technol. Eur. J. Glas. Sci. Technol. Part A. 53 (2012) 211–216.

[30]	N.R. Gribble, Limit on lithium in HAL and impact on glass product quality (2008). Technical Memorandum: Nexia Solutions VTR 3569 - Issue 2.

[31]	A. Riley, S. Walker, N.R. Gribble, Composition Changes and Future Challenges for the Sellafield Waste Vitrification Plant, Mater. Res. Soc. 1193 (2009) 1–6. doi:https://doi.org/10.1557/PROC-1193-267.

[32]	N.E. Ahmad, S. Fearn, J.R. Jones, W.E. Lee, Preliminary Surface Study of Short Term Dissolution of UK High Level Waste Glass, Procedia Mater. Sci. 7 (2014) 230–236. doi:10.1016/j.mspro.2014.10.030.

[33]	R. Guo, C.T. Brigden, S. Gin, S.W. Swanton, I. Farnan, The effect of magnesium on the local structure and initial dissolution rate of simplified UK Magnox waste glasses, J. Non. Cryst. Solids. 497 (2018) 82–92. doi:10.1016/j.jnoncrysol.2018.03.002.

[34]	ASTM, Standard Test Methods for Determining Chemical Durability of Nuclear , Hazardous , and Mixed Waste Glasses and Multiphase Glass Ceramics : The Product Consistency Test ( PCT ) Designation: C1285-14, 2002. doi:10.1520/C1285-14.2.

[35]	D. Massiot, F. Fayon, M. Capron, I. King, S. Le Calvé, B. Alonso, J.O. Durand, B. Bujoli, Z. Gan, G. Hoatson, Modelling one- and two-dimensional solid-state NMR spectra, Magn. Reson. Chem. 40 (2002) 70–76. doi:10.1002/mrc.984.

[36]	F. Angeli, T. Charpentier, D. De Ligny, C. Cailleteau, Boron speciation in soda-lime borosilicate glasses containing zirconium, J. Am. Ceram. Soc. 93 (2010) 2693–2704. doi:10.1111/j.1551-2916.2010.03771.x.

[37]	L.S. Du, J.F. Stebbins, Site preference and Si/B mixing in mixed-alkali borosilicate glasses: A high-resolution 11B and 17O NMR study, Chem. Mater. 15 (2003) 3913–3921. doi:10.1021/cm034427r.

[38]	L.S. Du, J.F. Stebbins, Solid-state NMR study of metastable immiscibility in alkali borosilicate glasses, J. Non. Cryst. Solids. 315 (2003) 239–255. doi:10.1016/S0022-3093(02)01604-6.

[39]	S. Gin, J. V. Ryan, D.K. Schreiber, J. Neeway, M. Cabié, Contribution of atom-probe tomography to a better understanding of glass alteration mechanisms: Application to a nuclear glass specimen altered 25 years in a granitic environment, Chem. Geol. 349–350 (2013) 99–109. doi:10.1016/j.chemgeo.2013.04.001.

[40]	G. Calas, L. Galoisy, L. Cormier, G. Ferlat, G. Lelong, The Structural Properties of Cations in Nuclear Glasses, Procedia Mater. Sci. 7 (2014) 23–31. doi:10.1016/j.mspro.2014.10.005.

[41]	L. Cormier, D. Ghaleb, J. Delaye, Competition for charge compensation in borosilicate glasses: Wide-angle x-ray scattering and molecular dynamics calculations, Phys. Rev. B - Condens. Matter Mater. Phys. 61 (2000) 14495–14499. doi:10.1103/PhysRevB.61.14495.

[42]	B. Fleury, N. Godon, A. Ayral, S. Gin, SON68 glass dissolution driven by magnesium silicate precipitation, J. Nucl. Mater. 442 (2013) 17–28. doi:10.1016/j.jnucmat.2013.08.029.

[43]	P. Frugier, S. Gin, Y. Minet, T. Chave, B. Bonin, N. Godon, J.E. Lartigue, P. Jollivet, A. Ayral, L. De Windt, G. Santarini, SON68 nuclear glass dissolution kinetics: Current state of knowledge and basis of the new GRAAL model, J. Nucl. Mater. 380 (2008) 8–21. doi:10.1016/j.jnucmat.2008.06.044.

[44]	E. Vernaz, S. Gin, Apparent Solubility Limit of Nuclear Glass Étienne Vernaz and Stéphane Gin Commissariat à l’Énergie Atomique (CEA/Valrhô), DCC/SCD/LEAM BP 171, 30207 Bagnols-sur-Cèze Cedex, France, 663 (2001).

[45]	B. Parruzot, P. Jollivet, D. Rebiscoul, S. Gin, Long-term alteration of basaltic glass: Mechanisms and rates, Geochim. Cosmochim. Acta. 154 (2015) 28–48. doi:10.1016/j.gca.2014.12.011.

[46]	Subhashini, H.D. Shashikala, N.K. Udayashankar, Investigation of mixed alkali effect on mechanical, structural and thermal properties of three-alkali borate glass system, J. Alloys Compd. 658 (2016) 996–1002. doi:10.1016/j.jallcom.2015.11.014.