Molecularly engineered photocatalyst sheet for scalable solar formate production from carbon dioxide and water

Qian WANG,1 Julien WARNAN,1 Santiago RODRÍGUEZ-JIMÉNEZ,1 Jane J. LEUNG,1 Shafeer KALATHIL,1 Virgil ANDREI,1 Kazunari DOMEN,2,3 Erwin REISNER1,*

Affiliation and full postal address

1 Department of Chemistry, University of Cambridge, Lensfield Road, Cambridge CB2 1EW, UK

2 Office of University Professor, The University of Tokyo, 7-3-1 Hongo, Bunkyo-ku, Tokyo 113-8656, Japan

3 Research Initiative for Supra-Materials, Interdisciplinary Cluster for Cutting Edge Research, Shinshu University, 4-17-1 Wakasato, Nagano-shi, Nagano 380-8553, Japan

*Corresponding author

Professor Erwin REISNER

Department of Chemistry, University of Cambridge, Lensfield Road, Cambridge CB2 1EW, UK

Tel: +44-1223336323

E-mail: reisner@ch.cam.ac.uk

Abstract

Harvesting solar energy to convert CO2 into chemical fuels is a promising technology to curtail the growing atmospheric CO2 levels and alleviate the global dependence on fossil fuels. However, the assembly of efficient and robust systems for the selective photoconversion of CO2 without sacrificial reagents and external bias remains a challenge. Here, we present a photocatalyst sheet that converts CO2 and H2O into formate and O2 as a potentially scalable technology for CO2 utilisation. This technology integrates La and Rh-doped SrTiO3 (SrTiO3:La,Rh) and Mo-doped BiVO4 (BiVO4:Mo) light absorbers modified by phosphonated Co(II) bis(terpyridine) and RuO2 catalysts onto a gold layer. The monolithic device provides a solar-to-formate conversion efficiency of 0.08±0.01% with a selectivity for formate of 97±3%. As the device operates wirelessly and uses water as an electron donor, it offers a versatile strategy toward scalable and sustainable CO2 reduction using molecular-based hybrid photocatalysts.

Coordination complexes have long been explored for achieving the (electro)chemical CO2 reduction reaction (CO2RR) and high selectivity with good durability has been reported in homogenous solution.1, 2 Hybrid systems employ immobilised molecular catalysts on the surface of a semiconductor, which allows their use in a range of solvents for efficient photocatalysis, including an aqueous medium.3-8 Ultimately, CO2RR requires coupling with sustainable oxidation chemistry of an abundant electron source such as water for such technologies to satisfy global energy demands.9 Therefore, particular effort has been focused on the development of standalone hybrid photoelectrochemical (PEC) cells, which can also couple CO2RR with water oxidation.10-14 However, hybrid PEC cells suffer from scale-up problems due to the pH gradient and IR drops occurring during the PEC reaction.15

Colloidal systems using particulate photocatalysts are an emerging alternative to PEC configurations as they benefit from a simpler design and potentially lower cost.16 However, sacrificial reductants are commonly required for CO2 conversion using hybrid photocatalysts due to the low oxidising power of the utilised photosensitiser unit, which cannot catalyse water oxidation.7, 17-19 A nature-inspired artificial Z-scheme CO2 conversion system composed of a hybrid photocatalyst for CO2RR and a semiconductor photocatalyst for water oxidation could in principle cope with both the high selectivity of CO2RR and strong oxidation power. Nonetheless, the realisation of photosynthetic Z-scheme CO2RR systems remains a critical scientific challenge due to inefficient interparticle charge transfers as well as fiercely competitive side and back reactions such as proton reduction and oxidation of the products from CO2RR.20-22 To our knowledge, selective Z-scheme CO2RR system based on particulate hybrid photocatalysts has yet to be reported.23

Z-scheme-inspired photocatalyst sheets consist of two redox-complementary semiconductor particles fixed on a conductive layer that ensures charges relay while avoiding the side reactions associated with the use of redox mediators.24 As the reduction and oxidation reactions occur in close proximity to one another on the photocatalyst sheet, the pH gradient and IR drop are largely suppressed.15 The photosynthetic activity of the photocatalyst sheet is thus scalable and avoids PEC limitations.

Here, we report such a monolithic device, taking the SrTiO3:La,Rh|Au|RuO2-BiVO4:Mo sheet as an example, and immobilise a phosphonated cobalt(II) bis(terpyridine) molecular catalyst as CO2 reduction catalyst on the surface in a straightforward manner. Solar irradiation of the device delivered formate (HCOO‒) from aqueous CO2 with 97±3% selectivity, accompanied by a simultaneous O2 generation in a stoichiometric 2:1 ratio with a solar-to-formate conversion efficiency (STF) of 0.08±0.01%. When the sheet device is irradiated with simulated sunlight, electron-hole pairs are excited in both SrTiO3:La,Rh and BiVO4:Mo. Electrons are transferred from the conduction band of BiVO4:Mo to the donor levels of SrTiO3:La,Rh through the gold (Au) layer. Simultaneously, electrons in SrTiO3:La,Rh reduce CO2 to HCOO‒ with the aid of the molecular complex functioning as a CO2RR cocatalyst, and holes in BiVO4:Mo oxidise water to oxygen with RuO2 species serving as an oxygen evolution cocatalyst.

Device preparation and characterisation

The photocatalyst sheet, SrTiO3:La,Rh|Au|RuO2-BiVO4:Mo, consisting of SrTiO3:La,Rh and RuO2-modified BiVO4:Mo (RuO2-BiVO4:Mo) particles embedded into a Au layer, was prepared by a previously reported particle transfer method.25 RuO2-BiVO4:Mo is expected to provide strong water oxidation power under visible light irradiation,26 whereas SrTiO3:La,Rh was chosen as the light absorber for CO2RR owing to its relatively negative conduction band (‒1.1 V versus NHE at pH 7).27 The sheet was subsequently modified with the molecular CO2RR cocatalyst (CotpyP) by immersion from a methanolic solution. Fully assembled CotpyP-loaded SrTiO3:La,Rh|Au|RuO2-BiVO4:Mo sheets with relatively large active areas (ca. 5.7 cm× 6 cm) could be prepared (Figure 1a,b). Scanning electron microscopy and energy dispersive X-ray spectroscopy (SEM–EDX) mapping confirmed that a Au layer with a thickness of ca. 300 nm supports a particle layer composed of SrTiO3:La,Rh and RuO2-BiVO4:Mo particles (Figure 1c-h, Supplementary Fig. 1).

Precious-metal-free CotpyP was selected as the cocatalyst because this 3d transition metal-based complex can be easily prepared and readily immobilised on porous metal oxide scaffolds via its phosphonate anchoring groups, and was previously used for low-overpotential CO2RR on a p-type silicon photoelectrode (m-TiO2|p-Si) in an aqueous electrolyte solution.28 SEM–EDX and X-ray photoelectron spectroscopy (XPS) analyses (Co 2p and N 1s spectra; Supplementary Fig. 2) suggest that the CotpyP catalyst molecules were adsorbed on both SrTiO3:La,Rh and RuO2-BiVO4:Mo particles. No significant changes were observed in the attenuated total reflection infrared (ATR-IR) spectra of CotpyP powder and CotpyP grafted on the SrTiO3:La,Rh and RuO2-BiVO4:Mo particles (Supplementary Fig. 3 and Supplementary Table 1), indicating an unchanged core structure of the catalyst upon immobilisation. The loading amount of CotpyP was estimated via inductively coupled plasma optical emission spectrometry (ICP-OES) to be ~17 nmol cm‒2 (Supplementary Table 2).

Performance for photosynthetic CO2RR and water oxidation

Simultaneous production of HCOO‒ and O2 occurred over the CotpyP-loaded SrTiO3:La,Rh|Au|RuO2-BiVO4:Mo sheets (ca. 1 cm2) in a CO2-saturated KHCO3 aqueous solution (0.1 M, pH 6.7) under a CO2 atmosphere (1 atm) and simulated solar irradiation (AM 1.5G, 100 mW cm‒2), as shown in Figure 2a. The hybrid photocatalyst sheet enabled an STF of 0.08±0.01%, while attaining 97±3% selectivity for HCOO‒ formation. The pH of the reaction medium did not change after 6 hours of irradiation. No products were obtained in the absence of light or either of the semiconductor powders afforded under the same conditions (Supplementary Table 3). These results supported the occurrence of a Z-scheme mechanism in the sheet system, ruling out the possibilities of significant reduction/oxidation of impurities as sacrificial reagents.

During control experiments performed in an aqueous K2SO4 solution (0.1 M, pH 6.7) without CO2/HCO3‒ and purged with N2, no CO2RR products were detected. Continuous H2 and O2 with trace amounts were observed and the amount of H2 was similar to that produced in the presence of CO2/HCO3– (Supplementary Fig. 4 and Supplementary Table 3). These observations indicate that first the H2 detected from the present sheet was produced via water splitting rather than HCOO‒ decomposition and, second, highlight the modest catalytic activity of CotpyP for hydrogen production.28

Isotopic labelling experiments confirmed that HCOO‒ resulted from 13CO2/H13CO3‒ (a doublet attributable to the 13C-coupled proton (1JCH = 195 Hz) was observed by proton nuclear magnetic resonance (1H NMR) spectroscopy; Figure 2b). The amount of H13COO‒ was quantified as 5.3 μmol and comparable to that of the formate obtained from normal 12CO2/H12CO3‒ conditions (Supplementary Table 3). The evolution of O2 gas accompanied the reduction reactions in a stoichiometric ratio of (HCOO‒+H2+CO):O2 = 2.2±0.2 (HCOO‒:O2 = 2.1±0.3), demonstrating a clean conversion without the need of sacrificial reagents.

In agreement with absorption onsets of both SrTiO3:La,Rh and BiVO4:Mo in the diffuse reflectance spectra (DRS), HCOO‒ was produced up to λ ≤ 510 nm irradiation (Figure 2c), indicating that the photoreactions proceeded via bandgap transitions in the semiconductors. The apparent quantum yield (AQY) at 420±15 nm was 2.6%. A sheet with an active irradiated area of ca. 20 cm2 was prepared and produced HCOO‒ with an STF of 0.06% (Figure 3), which is comparable to those detected from the 1 cm2 samples (Figure 2a), demonstrating the scalability of our photocatalyst sheet system.

The photocatalyst particles covered more than 90% of the underlying Au layer (Figure 1h) and the exposed Au did not show significant activity for electrocatalytic CO2RR (Supplementary Fig. 5). Furthermore, the CotpyP-loaded Au film yielded no detectable products without applied potential, while the SrTiO3:La,Rh|Au|RuO2-BiVO4:Mo sheet without CotpyP produced negligible HCOO‒ (Supplementary Table 3). The Au layer is thus believed to serve only as an electron transfer medium between SrTiO3:La,Rh and BiVO4:Mo rather than as a catalyst for CO2RR.

Photocatalytic reactions over the colloidal systems, in which individual semiconductor powders were suspended in aqueous solution containing sacrificial reagents, were carried out to ascertain the function of CotpyP (Supplementary Table 4). Upon loading of CotpyP on SrTiO3:La,Rh, HCOO‒ production became evident in the presence of triethanolamine (TEOA) as an electron donor, confirming the function of CotpyP as the CO2RR cocatalyst. The turnover number (TON) for HCOO‒ was 305 after 4 hours. Likewise, photocurrent over the CotpyP-modified SrTiO3:La,Rh|Au photocathode for CO2RR increased remarkably compared to the pristine SrTiO3:La,Rh photocathode (Figure 4a). In contrast, O2 evolution showed no significant improvement after loading CotpyP on either SrTiO3:La,Rh or BiVO4:Mo in an aqueous solution containing Ag+ as electron acceptor (Supplementary Table 4). Similar photocurrents for the RuO2-BiVO4:Mo|Au photoanode were also observed with and without loading CotpyP on its surface in an electrolyte solution containing HCOO– (Supplementary Fig. 6). It can therefore be concluded that CotpyP serves as a CO2RR cocatalyst on SrTiO3:La,Rh, and not as an oxygen evolution or formate oxidation cocatalyst on BiVO4:Mo. In addition, the O2 evolution rate over RuO2-BiVO4:Mo sheet in a 0.1 M AgNO3 aqueous solution did not show significant change after loading CotpyP on its surface (1.2 μmol h–1 cm–2 and 1.3 μmol h–1 cm–2 obtained on RuO2-BiVO4:Mo and CotpyP/RuO2-BiVO4:Mo sheets, respectively), indicating the negligible impact of CotpyP on the O2 evolution rate over RuO2-BiVO4:Mo. Considering that BiVO4:Mo is unable to produce HCOO‒ from CO2 due to insufficient driving force from its conduction band,29-31 we propose that HCOO‒ and O2 were therefore generated by two-step photoexcitation over the SrTiO3:La,Rh and BiVO4:Mo particles (Figure 1a).

In order to investigate the robustness of CotpyP toward O2, the controlled potential electrolysis experiments (CPE) of CotpyP|m-TiO2|Ti electrode were performed with and without the presence of O2 (Figure 5). The Faradaic efficiency for HCOO– dropped from 83% to 40% when replacing the mixture of CO2 and N2 (CO2+N2, 50% each) with that of CO2 and O2 (CO2+O2, 50% each) due to cooccurrence of the oxygen reduction reaction (Figure 5b). However, the amount of HCOO– produced did not change substantially (16.1 and 13.7 μmol in 5h using a CO2+N2 and CO2+O2 atmosphere, respectively), implying substantial HCOO‒ production activity remained in the presence of O2 and the O2 reduction reaction occurred mainly on m-TiO2|Ti electrode, as evidenced by the red dashed curve in Figure 5a. After re-purging with CO2+N2 and repeating linear sweep voltammetry (LSV) scan, a significant drop in the CO2 reduction activity was not observed, which illustrated the O2 tolerance of CotpyP (Figure 5a).32

Device selectivity and stability

To date, reported photo(electro)chemical reduction of aqueous CO2 to a single product using molecular catalysts remains scarce, in particular due to the competing proton reduction reaction. For instance, CotpyP-loaded m-TiO2|p-Si poised at an applied potential of 0 V versus reversible hydrogen electrode (RHE) favoured PEC H2 production instead of CO2 reduction.28 To investigate the factors influencing the selectivity of CotpyP, the PEC performance of a CotpyP-loaded SrTiO3:La,Rh photocathode for CO2RR was studied in a CO2-saturated KHCO3 aqueous solution (0.1 M, pH 6.7) under a CO2 atmosphere (1 atm) and simulated solar irradiation (AM 1.5G, 100 mW cm‒2). Under 0.0 V versus RHE applied potential in the controlled potential photoelectrolysis (CPPE), more H2 than CO and HCOO‒ was produced over CotpyP-SrTiO3:La,Rh (Figure 4b and c), consistent with results on CotpyP-m-TiO2|p-Si. The CotpyP-SrTiO3:La,Rh|Au achieved a higher total TON and selectivity for CO and HCOO‒ (144 after 4 h CPPE, 47%) than CotpyP-m-TiO2|p-Si (20.8 after 8 h CPPE, 37%),28 presumably due to the more negative conduction band potential of SrTiO3:La,Rh than that of TiO2 (‒1.1 and ‒0.5 V versus NHE at pH 7 for SrTiO3:La,Rh and TiO2, respectively).

The shared electrode potential, at which the CotpyP-SrTiO3:La,Rh|Au and RuO2-BiVO4:Mo|Au photoelectrodes generate photocathodic and photoanodic currents without external bias, was estimated to be +0.45 V versus RHE (Supplementary Fig. 7). In contrast, HCOO‒ became the predominating product with a selectivity of 93±3% (Faradaic efficiency for HCOO‒ production was 83.9±5.8% over 4 hours) when the potential was increased to +0.5 V versus RHE (Figure 4b and c). The increasing dominance of hydrogen evolution at higher applied potentials has also previously been observed on CotpyP-m-TiO2|p-Si photocathode.28 The surface reaction pathways and rate-determining steps might change caused by a variation in the photo-charging rate and outer Helmholtz adsorption potential at different applied bias.33-36 Hence, the photocatalyst sheet can yield HCOO‒ with high selectivity. Additionally, a current-increasing effect (caused by the presence of formate as an electron donor) was not observed on a RuO2-BiVO4:Mo photoanode in the electrolyte containing 1.5 mM HCOO‒ (Supplementary Fig. 6), suggesting that the photogenerated holes in RuO2-BiVO4:Mo selectively oxidise water rather than HCOO‒ due to the high activity of RuO2 for water oxidation.11,37

The photosynthetic reaction over the CotpyP-SrTiO3:La,Rh|Au|RuO2-BiVO4:Mo sheet was carried out for 24 hours with the replacement of the reactant medium with a fresh solution and CO2 purging every 6 hours (Figure 4d). The HCOO‒ and O2 formation rates remained at 51% of the initial activity after 24 hours. The X-ray diffraction (XRD) patterns of the sheet before and after reaction (Supplementary Fig. 8) showed that the phases of SrTiO3:La,Rh, BiVO4:Mo and Au did not change notably. Additionally, no notable peak shift was observed in Co 2p and N 1s XPS spectra (Supplementary Fig. 2), suggesting that no significant heterogenisation of CotpyP occurred during the reaction. A small peak attributable to hydrous ruthenium oxide was observed along with the major peak of RuO2 after the 24-hour reaction conducted in aqueous solution.

While the amount of Ru remaining on the photocatalyst sheet did not remarkably decrease, that of Co dropped by half after the 24-hour reaction (Supplementary Table 2). Accordingly, the TONs for HCOO‒ in the first and fourth runs were calculated to be 428 and 447, respectively. Note that these values are conservative estimates for the TONs because the CotpyP deposited on BiVO4:Mo was inactive for the CO2RR and other leaching/inactive Co was not taken into account. The comparable TON in the last run compared with the initial one further confirmed that the function of the residual CotpyP cocatalyst was preserved.

Reported systems coupling CO2RR with water oxidation for formate production remain scarce, whether in powder suspension form or bias-free PEC cells. A wired system consisting of a ruthenium complex-modified N,Zn-Fe2O3 photocathode and a photoanode based on n-type SrTiO3-x single crystal was reported to produce 1.55 μmol HCOO‒ after 1 hour when the complex loading amount was 70 nmol, corresponding to a TON for HCOO‒ of 22.38 The reaction rate of the present sheet system was recovered to 80% of the initial rate by reloading the CotpyP cocatalyst, suggesting the decrease of the activity is attributable mainly to the drop in the number of active sites rather than the essential deterioration of the sheet structure. In the future, the efficiency and durability of the present sheet could be upgraded through improvement in the molecular cocatalyst, such as replacing phosphonate with a more robust anchoring group or constructing a polymeric matrix,39 and grafting the molecular cocatalysts on the surface of CO2RR photocatalysts selectively by photoreduction.40

Due to the unique structure of photocatalyst sheet, the pH gradient and IR drop between the SrTiO3:La,Rh and BiVO4:Mo generated during the redox reactions can be effectively suppressed.15 As a consequence, the photocatalyst sheet was five times more active than a conventional bias-free PEC parallel cell consisting of a CotpyP-SrTiO3:La,Rh photocathode and a RuO2-BiVO4:Mo photoanode under the same conditions (Supplementary Fig. 9). The photocatalyst sheet design is particularly beneficial to the molecularly-engineered system because it can be used in the aqueous solution with a wide range of pH (2.5–7.5).41 Therefore, various molecular catalysts could be applied to the photocatalyst sheet in future development. In addition, precious-metal-free photocatalyst sheets with a large area can be readily established by replacing the gold with sputtered carbon or indium tin oxide nanoparticles.15,24 Hence, this technology displays promising efficiency as well as advantageous versatility and scalability for combing molecular catalysts and semiconductors to achieve artificial photosynthesis.

Conclusions

We demonstrate a hybrid prototype photocatalyst sheet performing photosynthetic CO2RR to form HCOO‒ with a selectivity of 97±3% and an STF of 0.08±0.01% using water as the electron donor. This performance is achieved due to the combined high selectivity of an immobilised precious-metal-free molecular catalysts for CO2RR and the strong water oxidation power of the semiconductors. The present wireless and stand-alone device couples formate production with water oxidation using light as the sole energy source, a rarity in the field of wireless CO2 conversion. It also shows high stability during the photosynthetic reaction without sacrificial reagents and enables the scalability of the photocatalytic activity. This finding overcomes the hurdle of hybrid photocatalysts requiring sacrificial reagents in photocatalytic CO2RR constructs and provides the impetus to study other molecular catalysts for solar fuel production via artificial photosynthesis in such an architecture. Although here we focus on production of formic acid – a promising fuel and  H2 carrier –  the simplicity of the assembly process for immobilising molecular catalysts on the photocatalyst sheet allows the exploration of a wide range of catalysts for various photosynthetic reactions and products in the future.

Methods

Synthesis of SrTiO3:La,Rh and BiVO4:Mo powders

SrTiO3:La,Rh (La/(La + Sr) = Rh/(Rh + Ti) = 4 mol%) was synthesised by a two-step solid-state reaction according to a previously reported procedure.24 In the initial step, SrCO3 (Alfa Aesar, 99.99%, heated in air at 573 K for 1 h before use) and rutile-type TiO2 (Sigma-Aldrich, ≥99.98%) powders were mixed in a mortar at a Sr/Ti ratio of 1.05. The mixture was placed into an alumina crucible, heated up to 1473 K at 10 K min−1, and kept at the target temperature for 10 h. The sample was allowed to cool naturally to room temperature. Subsequently, the resulting SrTiO3 was mixed with La2O3 (La/(La + Sr) = 4 mol%; Fisher Scientific, 99.99%, freshly calcined in air at 1273 K for 12 h before use) and Rh2O3 (Rh/(Rh + Ti) = 4 mol%; Wako Pure Chemical, 98.0‒102.0%), and heated at 1373 K for 6 h. The heating and cooling procedures were carried out in the same way as the first step.

BiVO4:Mo (Mo/V = 0.05 mol%) was synthesised via a solid-liquid reaction.42 Layered Mo-doped K3V5O14 was prepared as a precursor by calcining a mixture of K2CO3 (Breckland Scientific, 99.5%), V2O5 (Fisher Scientific, 99.6%) and MoO3 (Mo/V = 0.05 mol%, BDH Chemicals, 99.5%) in air at 723 K for 5 h. Then, the obtained Mo-doped K3V5O14 was added to a suspension of BiONO3 (adding stoichiometric Bi(NO3)3·5H2O (Sigma-Aldrich, 98%) in 100 mL distilled water) and stirred mildly at 343 K for 10 h. The resulting powder was collected by filtration, washed with distilled water and then dried overnight in air before use.

Loading of RuO2 on BiVO4:Mo powders

RuO2, determined by XPS (Supplementary Fig. 2) as an oxygen evolution cocatalyst, was loaded on BiVO4:Mo particles in advance of the sheet preparation. RuO2 nanoparticles (1 wt%) were loaded on BiVO4:Mo by following an impregnation method.26 BiVO4:Mo powder (0.1–0.2 g) was immersed in an aqueous solution containing a given amount of RuCl3 (Acros Organics, 35‒40% Ru) and placed in a water bath. After evaporating the solution to dryness, the resulting powder was collected and calcined in air at 623 K for 1 h.

Fabrication of SrTiO3:La,Rh|Au|RuO2-BiVO4:Mo sheets

SrTiO3:La,Rh|Au|RuO2-BiVO4:Mo photocatalyst sheets were fabricated by a particle transfer method.24,25 First, a mixture of SrTiO3:La,Rh and RuO2-loaded BiVO4:Mo powders (10 mg each) was suspended in isopropanol (Sigma-Aldrich, ≥99.5%, 0.5 mL) by ultrasonication for 20 min and drop-cast on a glass substrate (3 cm × 3 cm). After drying at room temperature, a gold layer was deposited by thermal vacuum evaporation (Kurt J. Lesker) under a base pressure below 5 × 10−3 Pa. The thickness of ca. 300 nm of the gold layer was controlled by a crystal sensor and a thickness monitor. The obtained sample was placed on an alumina plate, heated to 573 K under air at a rate of 10 K min−1, and kept at the target temperature for 20 min to form good contact between gold and semiconductors.24 This process would damage the CotpyP and thus the molecular cocatalyst was deposited on the surface after the assembly of the photocatalyst sheet. The Au film supporting the particulate photocatalysts was then bonded to a second glass plate (1 cm × 1 cm unless otherwise noted) with adhesive carbon tape and then lifted off the primary glass plate. Finally, the photocatalyst sheet obtained was ultrasonicated twice, for 2 min each time, in distilled water to remove excess particles piling up on the particle layer.

Assembly of CotpyP on SrTiO3:La,Rh|Au|RuO2-BiVO4:Mo sheets

A methanolic solution of CotpyP (0.25 mM) was prepared by the dropwise addition of a methanol solution of tpyP (2,2':6',2''-terpyridine-4'-phosphonic acid, HetCat) to a methanol solution of Co(BF4)2·6H2O (Sigma Aldrich, >99%).28 Ultraviolet-visible (UV-Vis), and 1H NMR spectra are presented in Supplementary Figs. 10 and 11. Immobilisation of CotpyP on the SrTiO3:La,Rh|Au|RuO2-BiVO4:Mo photocatalyst sheet was performed by soaking the sheet in the methanolic solution of CotpyP for 10 h. The CotpyP-loaded SrTiO3:La,Rh|Au|RuO2-BiVO4:Mo photocatalyst sheet was then rinsed with methanol and dried for ca. 16 h in air before use.

Fabrication of photoelectrodes and PEC parallel cell

Photoelectrodes of SrTiO3:La,Rh|Au and RuO2-BiVO4:Mo|Au were prepared by the particle transfer method similar to the fabrication of the photocatalyst sheet. SrTiO3:La,Rh or RuO2-BiVO4:Mo powder (20 mg) was dispersed in isopropanol (0.5 mL) by ultrasonication for 20 min. The suspension was deposited on a glass substrate (3 cm × 3 cm). Au layers 1.5 μm in thickness were deposited on the semiconductor particles by vacuum evaporation. The resulting Au film holding the photocatalyst powder was annealed at 573 K for 20 min and then transferred to another glass plate (1 cm × 1 cm). Loading of CotpyP on SrTiO3:La,Rh|Au and RuO2-BiVO4:Mo|Au electrodes was carried out by soaking the electrode in the methanolic solution of CotpyP as described above for 10 h. The CotpyP-loaded photoelectrodes were then rinsed with methanol and dried for ca. 16 h in air. Electrical contact was established by embedding a copper wire in indium at the bottom of the sample. The copper wire and indium were encapsulated with epoxy (Araldite, Rapid 5-Minute Epoxy). The exposed active area of the photoelectrode after the insulation was ~0.2 cm2.

The CotpyP-SrTiO3:La,Rh|Au and RuO2-BiVO4:Mo|Au electrodes were connected using indium solder to form PEC parallel cells with side-by-side placement of the electrodes. The indium was subsequently covered with epoxy and the exposed area after packaging was about 0.8 cm2.

Characterisation

XRD patterns of the samples were measured with a PANalytical Empyrean Series 2 instrument using Cu Kα source operated at 40 kV and 40 mA. The DRS were recorded using an ultraviolet-visible-near-infrared spectrometer (Varian Cary 50 Bio). The SEM-EDX element mapping images were obtained using a TESCAN MIRA3 FEG-SEM instrument with an Oxford Instruments Aztec Energy X-maxN 80 system at an acceleration voltage of 15 kV. XPS analysis was carried out at the EPSRC National Facility for Photoelectron spectroscopy (‘HarwellXPS’) using a Kratos Axis SUPRA XPS fitted with a monochromated Al kα X-ray source (1486.7 eV), a spherical sector analyser, 3 multichannel resistive plate and 128 channel delay line detectors. All data were recorded over a spot size of 700 × 300 µm and at 150 W under a pressure below 10-8 Torr and a room temperature of 294 K. Electronic charge neutralisation was achieved using a magnetic immersion lens. Filament current, charge balance and filament bias was 0.27 A,  3.3 V and 3.8 V, respectively. ICP-OES measurements were recorded on a Thermo Scientific iCAP 7400 ICP-OES DUO spectrometer. Analyte solutions for ICP-OES were obtained by digesting the sheets in aqueous HNO3 (>68%) overnight and dilution to 2% vol/vol with Milli-Q water. FT-IR spectra were collected on a Thermo Scientific Nicolet iS50 FT-IR spectrometer in ATR-IR mode. The 1H NMR spectra of CotpyP were recorded in a Bruker 500MHz DCH cryoprobe spectrometer at room temperature. Chemical shifts are given in ppm and are referenced relative to residual protium in the deuterated methanol and deuterium oxide (Eurisotop). Solution UV-vis spectra were collected using an Edinburgh Instruments FS5 spectrofluorimeter with a quartz cuvette (Starna Scientific) at room temperature.

Photocatalytic reactions

Z-scheme photosynthetic reactions were carried out in a closed system with side illumination from Newport Oriel 67005 solar light simulators with Air Mass 1.5 Global (AM 1.5 G) solar filters, which were calibrated to 100 mW cm−2 (1 Sun) using a certified Newport 1916-R optical power meter. A LOT-QD LS0816-H large area solar simulator was employed for the scalability tests. The photocatalyst sheet samples (ca. 1 cm2) were attached to a steel rod and inserted into the reaction cell containing an aqueous solution of 0.1 M KHCO3 (12 mL) unless otherwise noted. The photosynthetic reactions over the photocatalyst sheet with an active irradiated area of ca. 20 cm2 were carried out in a custom-built reactor (Figure 3a). Before performing the photosynthetic reaction, the reactant in the cell was purged for 30 min with CO2 containing 2% CH4 as an internal standard for gas chromatography (GC) measurements. The pH of the reactant after CO2 purging was 6.7. CO and H2 quantification were executed by manual sampling from the headspace of the reaction cells into a Shimadzu GC-2010 Plus gas chromatograph with a barrier discharge ionisation detector. The GC-2010 Plus was equipped with a ShinCarbon micro ST column (0.53 mm diameter) kept at 313 K using a helium carrier gas. Aliquots (50 µL) of the headspace gas were removed from the sealed cell using a gastight syringe (Hamilton, GASTIGHT) for GC analysis. The error for the integrated CH4 peak area in all injections was 2-3%. In addition, no trend (increase or decrease) was observed on the peak areas during the reaction, indicating that the amount of CH4 did not undergo significant changes. Formate was analysed by ion chromatography (IC) using a Metrohm 882 Compact IC plus ion chromatography system with a solution of carbonate (4 mM) containing acetone (50 mL L−1) as the eluent. 1H NMR spectroscopy was conducted on a Bruker 400 MHz NMR spectrometer in D2O. The O2 evolution was traced using a NeoFox-GT fluorometer and Fospor-R fluorescence oxygen sensor probe from Ocean Optics inside a glove box with an O2 concentration of less than 3 ppm. The analytical errors are <5% for quantifying HCOO‒, H2 and CO, and <10% for O2.

In the colloidal systems for photocatalytic CO2RR, TEOA was used as an electron donor. SrTiO3:La,Rh powder (2 mg) was added to Pyrex glass photoreactor vials containing an aqueous solution of TEOA (0.1 M, 2 mL) and capped with rubber septa. For the water oxidation reaction, BiVO4:Mo powder (2 mg) was dispersed in 2 mL of an AgNO3 (0.1 M) aqueous solution in the same vials, where Ag+ cations acted as sacrificial electron acceptors. For the CotpyP-SrTiO3:La,Rh and CotpyP-BiVO4:Mo samples, 65 μL methanolic solution of CotpyP (0.25 mM) was added to the reactant. After briefly vortexing, the samples were purged with CO2 (for CO2RR) or N2 (for water oxidation reaction) containing 2% CH4 as an internal standard at ambient pressure for 30 min and then irradiated by a solar light simulator (AM 1.5G, 100 mW cm−2).

Error bars in the figures and tables correspond to the standard deviation (n = 3). The source data containing the individual data points used for the statistical analysis are available from the Cambridge data repository.43

Photoelectrochemical measurements

The CotpyP-SrTiO3:La,Rh|Au and (CotpyP/)RuO2-BiVO4:Mo|Au electrodes were characterised in a three-electrode configuration using a Ag/AgCl reference electrode (in saturated KCl aqueous solution, Basi MW-2030) and a platinum mesh counter electrode. A Selemion (AGC Engineering) was used as the ion-exchange membrane separating the anodic and cathodic compartments. The potential of the working electrode was controlled by a potentiostat (Ivium CompactStat). 0.1 M KHCO3 aqueous solution purged with CO2 containing 2% CH4 for 30 min was used as the electrolyte (pH 6.7) under stirring unless otherwise noted. The photoelectrode was irradiated with a solar simulator (AM 1.5G, 100 mW cm−2). Current-potential curves were measured at a scan rate of 10 mV s‒1.

O2-inhibition of CotpyP catalyst

The preparation of the m-TiO2|Ti electrode (TiO2 layer thickness of ~6 µm) was performed following a previously reported procedure.28 The Ti foil (10 × 20 × 0.25 mm) was sonicated sequentially in isopropanol and ethanol for 30 min, and dried under a flow of N2. The mesoporous TiO2 (m-TiO2) scaffold was deposited on Ti foil by slot-coating commercial Ti-nanoxide pastes (15-20 nm particles, 100 % anatase, Solaronix) over a defined area (0.7 cm × 0.7 cm). The electrodes were then sintered in a Carbolite furnace under atmospheric conditions at 598 K for 5 min, followed by annealing at 648 K for 5 min, and lastly by annealing at 723 K for 5 min.

Immobilisation of CotpyP on m-TiO2|Ti electrode was carried out by soaking the electrodes in a methanolic solution of CotpyP (0.25 mM, same solution as that used for photocatalyst sheet) for 16 h.28 Subsequent electrical contact was established in the same manner used on CotpyP-SrTiO3:La,Rh|Au and RuO2-BiVO4:Mo|Au photoelectrodes.

LSV experiments were carried out in the same three-electrode configuration described above in aqueous KHCO3 solution (0.1 M, pH 6.7) purging with CO2+N2 (50% each) or CO2+O2 (50% each) for 30 min. The LSV scans were recorded at a scan rate of 50 mV s‒1 from positive to negative potential. CPE experiments were performed at an applied potential of ‒0.3 V versus RHE.

Isotopic labelling

The photocatalytic reaction over CotpyP-SrTiO3:La,Rh|Au|RuO2-BiVO4:Mo was performed in 0.1 M NaH13CO3 (Sigma-Aldrich, 98 atom% 13C, 99% (CP)) aqueous solution with 13CO2 (Sigma-Aldrich, 99.0 atom % 13C, 99% (CP)) as the headspace gas. The amount of HCOO‒ produced in 6 h was analysed by both IC and 1H NMR spectroscopy on a Bruker 500 MHz DCH cryoprobe spectrometer at room temperature.

Quantum yield measurements

The AQY of the Z-scheme photocatalytic reaction was calculated using

AQY = (4R/I) × 100%

Where R and I denote the HCOO‒ production rate and the photon flux of monochromatic light, respectively. The present system is based on a two-step photoexcitation mechanism. To produce one formate molecule, two electrons in SrTiO3:La,Rh are consumed in the CO2 reduction reaction, whereas the two electrons are needed in BiVO4:Mo to combine with the holes in SrTiO3:La,Rh to complete the reaction. Therefore, four electrons are required to produce one formate molecule.44 The AQYs were determined using a LOT MSH-300 monochromator, the power at different wavelengths of which was measured using a Thorlabs PM100D power meter with a Thorlabs S302C thermal power sensor. The wavelength λ with a full width at half maximum of 15 nm was varied between 390 and 540 nm in 30 nm steps.

Solar-to-formate conversion efficiency

The STF is given as

STF (%) = (R(HCOO‒) ×∆Gr) / (P × S) × 100

where R(HCOO‒), ∆Gr, P and S indicate the rate of HCOO‒ formation during the Z-scheme reaction, the reaction Gibbs energy of the CO2 reduction reaction (238 kJ  mol−1),31 the energy intensity of the AM 1.5G solar irradiation (100 mW cm−2) and the irradiated sample area, respectively.

Data Availability

The data supporting the findings of the study are available in the paper and its supplementary materials. Source data for the main figures (Figs. 2, 3, 4 and 5) are provided with the paper. Other source data supporting the findings of this study are available from the Cambridge data repository (https://doi.org/10.17863/CAM.54840).

Acknowledgements

We thank Constantin Sahm and Dr. Annika Eisenschmidt at the University of Cambridge for assisting with the isotopic labelling experiment, Dr. Souvik Roy and Dr. Motiar Rahaman at the University of Cambridge for helpful discussions, Stephen Young at the University of Cambridge for performing ICP-OES analysis, and Mark Isaacs at HarwellXPS for carrying out XPS. This work was supported by Marie Sklodowska-Curie individual Fellowships European (to Q.W., GAN 793996 and to S.K., GAN 744317), European Commission Future and Emerging Technologies (FET) Open programme project SoFiA (to S.R.-J. and E.R., GAN 828838), Christian Doppler Research Association (Austrian Federal Ministry for Digital and Economic Affairs and the National Foundation for Research, Technology and Development) and the OMV Group (to J.W. and E.R.). V.A. is grateful for the financial support from the Cambridge Trusts (Vice-Chancellor’s Award) and the Winton Programme for the Physics of Sustainability. J.J.L. is supported by the Woolf Fisher Trust in New Zealand. The XPS data collection was performed at the EPSRC National Facility for XPS (“HarwellXPS”), operated by Cardiff University and University College London, under Contract No. PR16195.

Author contributions

Q.W. and E.R. conceived the idea. E.R. supervised the project. J.W., J.J.L. and S.R.-J. synthesised and characterised CotpyP. Q.W. prepared the photocatalyst sheet and photoelectrodes and conducted physical characterisations and photo(electro)chemical experiments. S.K. carried out NMR spectroscopy, V.A. assisted with O2 quantification and scalability tests. All authors analysed the data, discussed the results and assisted with manuscript preparation.

Competing interests

The authors declare no competing interests.

References

- Costentin, C., Robert, M. & Savéant, J.-M. Catalysis of the electrochemical reduction of carbon dioxide. Chem. Soc. Rev. 42, 2423‒2436 (2013).

- Francke, R., Schille, B. & Roemelt, M. Homogeneously catalyzed electroreduction of carbon dioxide—methods, mechanisms, and catalysts. Chem. Rev. 118, 4631‒4701 (2018).

- Sato, S., Morikawa, T., Saeki, S., Kajino, T. & Motohiro, T. Visible-light-induced selective CO2 reduction utilizing a ruthenium complex electrocatalyst linked to a p-type nitrogen-doped Ta2O5 semiconductor. Angew. Chem. Int. Ed. 49, 5101‒5105 (2010).

- Wang, W.-H., Himeda, Y., Muckerman, J. T., Manbeck, G. F. & Fujita, E. CO2 hydrogenation to formate and methanol as an alternative to photo- and electrochemical CO2 reduction. Chem. Rev. 115, 12936‒12973 (2015).

- Kuriki, R. et al. Nature-inspired, highly durable CO2 reduction system consisting of a binuclear ruthenium(II) complex and an organic semiconductor using visible light. J. Am. Chem. Soc. 138, 5159‒5170 (2016).

- Liu, X., Inagaki, S. & Gong, J. Heterogeneous molecular systems for photocatalytic CO2 reduction with water oxidation. Angew. Chem. Int. Ed. 55, 14924‒14950 (2016).

- Kuriki, R. et al. Robust binding between carbon nitride nanosheets and a binuclear ruthenium(II) complex enabling durable, selective CO2 reduction under visible light in aqueous solution. Angew. Chem. Int. Ed. 56, 4867‒4871 (2017).

- Dalle, K. E. et al. Electro- and solar-driven fuel synthesis with first row transition metal complexes. Chem. Rev. 119, 2752‒2875 (2019).

- Tu, W., Zhou, Y. & Zou, Z. Photocatalytic conversion of CO2 into renewable hydrocarbon fuels: state-of-the-art accomplishment, challenges, and prospects. Adv. Mater. 26, 4607‒4626 (2014).

- Sato, S. et al. Selective CO2 conversion to formate conjugated with H2O oxidation utilizing semiconductor/complex hybrid photocatalysts. J. Am. Chem. Soc. 133, 15240‒15243 (2011).

- Arai, T., Sato, S., Kajino, T. & Morikawa, T. Solar CO2 reduction using H2O by a semiconductor/metal-complex hybrid photocatalyst: enhanced efficiency and demonstration of a wireless system using SrTiO3 photoanodes. Energy Environ. Sci. 6, 1274‒1282 (2013).

- Sahara, G. et al. Photoelectrochemical reduction of CO2 coupled to water oxidation using a photocathode with a Ru(II)–Re(I) complex photocatalyst and a CoOx/TaON photoanode. J. Am. Chem. Soc. 138, 14152‒14158 (2016).

- Kumagai, H. et al. Hybrid photocathode consisting of a CuGaO2 p-type semiconductor and a Ru(II)–Re(I) supramolecular photocatalyst: Non-biased visible-light-driven CO2 reduction with water oxidation. Chem. Sci. 8, 4242‒4249 (2017).

- Nakada, A. et al. Solar water oxidation by a visible-light-responsive tantalum/nitrogen-codoped rutile titania anode for photoelectrochemical water splitting and carbon dioxide fixation. ChemPhotoChem 3, 37-45 (2019).

- Wang, Q. et al. Particulate photocatalyst sheets based on carbon conductor layer for efficient Z-scheme pure-water splitting at ambient pressure. J. Am. Chem. Soc. 139, 1675‒1683 (2017).

- Pinaud, B. A. et al. Technical and economic feasibility of centralized facilities for solar hydrogen production via photocatalysis and photoelectrochemistry. Energy Environ. Sci. 6, 1983‒2002 (2013).

- Lian, S., Kodaimati, M. S., Dolzhnikov, D. S., Calzada, R. & Weiss, E. A. Powering a CO2 reduction catalyst with visible light through multiple sub-picosecond electron transfers from a quantum dot. J. Am. Chem. Soc. 139, 8931‒8938 (2017).

- Rao, H., Schmidt, L. C., Bonin, J. & Robert, M. Visible-light-driven methane formation from CO2 with a molecular iron catalyst. Nature 548, 74–77 (2017).

- Cometto, C. et al. A carbon nitride/Fe quaterpyridine catalytic system for photostimulated CO2-to-CO conversion with visible light. J. Am. Chem. Soc. 140, 7437‒7440 (2018).

- Li, P. et al. All-solid-state Z-scheme system arrays of Fe2V4O13/RGO/CdS for visible light-driving photocatalytic CO2 reduction into renewable hydrocarbon fuel. Chem. Commun. 51, 800‒803 (2015).

- Iwase, A. et al. Water splitting and CO2 reduction under visible light irradiation using Z-scheme systems consisting of metal sulfides, CoOx-loaded BiVO4, and a reduced graphene oxide electron mediator. J. Am. Chem. Soc. 138, 10260‒10264 (2016).

- Suzuki, T. M. et al. Z-schematic and visible-light-driven CO2 reduction using H2O as an electron donor by a particulate mixture of a Ru-complex/(CuGa)1−xZn2xS2 hybrid catalyst, BiVO4 and an electron mediator. Chem. Commun. 54, 10199‒10202 (2018).

- Li, X., Yu, J., Jaroniec, M. & Chen, X. Cocatalysts for selective photoreduction of CO2 into solar fuels. Chem. Rev. 119, 3962‒4179 (2019).

- Wang, Q. et al. Scalable water splitting on particulate photocatalyst sheets with a solar-to-hydrogen energy conversion efficiency exceeding 1%. Nat. Mater. 15, 611‒615 (2016).

- Minegishi, T., Nishimura, N., Kubota, J. & Domen, K. Photoelectrochemical properties of LaTiO2N electrodes prepared by particle transfer for sunlight-driven water splitting. Chem. Sci. 4, 1120‒1124 (2013).

- Lin, F. et al. Photocatalytic oxidation of thiophene on BiVO4 with dual co-catalysts Pt and RuO2 under visible light irradiation using molecular oxygen as oxidant. Energy Environ. Sci. 5, 6400‒6406 (2012).

- Ma, X. et al. Surface photovoltage spectroscopy observes sub-band-gap defects in hydrothermally synthesized SrTiO3 nanocrystals. J. Phys. Chem. C 123, 25081‒25090 (2019).

- Leung, J. J. et al. Solar-driven reduction of aqueous CO2 with a cobalt bis(terpyridine)-based photocathode. Nat. Catal. 2, 354‒365 (2019).

- Kudo, A., Omori, K. & Kato, H. A novel aqueous process for preparation of crystal form-controlled and highly crystalline BiVO4 powder from layered vanadates at room temperature and its photocatalytic and photophysical properties. J. Am. Chem. Soc. 121, 11459‒11467 (1999).

- Chang, X. et al. Enhanced surface reaction kinetics and charge separation of p−n heterojunction Co3O4/BiVO4 Photoanodes. J. Am. Chem. Soc. 137, 8356−8359 (2015).

- Bassegoda, A., Madden, C., Wakerley, D. W., Reisner, E. & Hirst. J. Reversible interconversion of CO2 and formate by a molybdenum-containing formate dehydrogenase. J. Am. Chem. Soc. 136, 15473‒15476 (2014).

- Wakerley, D. W. & Reisner, E. Oxygen-tolerant proton reduction catalysis: Much O2 about nothing? Energy Environ. Sci. 8, 2283‒2295 (2015).

- Ryu, J., T. N. Andersen, T. N. & Eyring, H. The electrode reduction kinetics of carbon dioxide in aqueous solution. J. Phys. Chem. 76, 3278–3286 (1972).

- Akira, M. & Yoshio, H. Product selectivity affected by cationic species in electrochemical reduction of CO2 and CO at a Cu electrode. Bull. Chem. Soc. Jpn. 64, 123‒127 (1991).

- Pérez-Gallent, E., Marcandalli, G., Figueiredo, M. C., Calle-Vallejo, F. & Koper, M. T. M. Structure- and potential-dependent cation effects on CO reduction at copper single-crystal electrodes. J. Am. Chem. Soc. 139, 16412‒16419 (2017).

- Feng, S. et al. Enriched surface oxygen vacancies of photoanodes by photoetching with enhanced charge separation. Angew. Chem. Int. Ed. 59, 2044–2048 (2020).

- Hykaway, N., Sears, W. M., Morisaki, H. & Morrison, S. R. Current-doubling reactions on titanium dioxide photoanodes. J. Phys. Chem. 90, 6663‒6667 (1986).

- Sekizawa, K., Sato, S., Arai, T. & Morikawa, T. Solar-driven photocatalytic CO2 reduction in water utilizing a ruthenium complex catalyst on p‑type Fe2O3 with a multiheterojunction. ACS Catal. 8, 1405−1416 (2018).

- Leung, J. J., Vigil, J. A., Warnan, J., Edwardes Moore, E. & Reisner, E. Rational design of polymers for selective CO2 reduction catalysis. Angew. Chem. Int. Ed. 58, 7697‒7701 (2019).

- Belanger, D. & Jean Pinson, J. Electrografting: a powerful method for surface modification. Chem. Soc. Rev. 40, 3995–4048 (2011).

- Q. Wang, et al. Z-scheme water splitting using particulate semiconductors immobilized onto metal layers for efficient electron relay. J. Catal. 328, 308–315 (2015).

- Iwase, A., Ng, Y. H., Ishiguro, Y., Kudo, A. & Amal, R. Reduced graphene oxide as a solid-state electron mediator in Z-scheme photocatalytic water splitting under visible light. J. Am. Chem. Soc. 133, 11054‒11057 (2011).

- Reisner E., et al. Data set for Molecularly engineered photocatalyst sheet for scalable solar formate production from carbon dioxide and water. Cambridge Data Repository https://doi.org/10.17863/CAM.54840 (2020)

- Sasaki, Y., Iwase, A., Katoa, H. & Kudo, A. The effect of co-catalyst for Z-scheme photocatalysis systems with an Fe3+/Fe2+ electron mediator on overall water splitting under visible light irradiation. J. Catal. 259, 133–137 (2008).

Figure 1 | CotpyP-loaded SrTiO3:La,Rh|Au|RuO2-BiVO4:Mo photocatalyst sheet. a, Energy diagram depicting photosynthetic CO2RR coupled with water oxidation. b, Photograph of a 6 cm × 5.7 cm CotpyP-loaded SrTiO3:La,Rh|Au|RuO2-BiVO4:Mo photocatalyst sheet prepared by the particle transfer method. c–h, Top-view SEM–EDX elemental mapping images showing a superimposition (c) of the distributions of Sr (d), Bi (e), Co (f), Ru (g), and Au (h).

Figure 2 | Photosynthetic activity of the CotpyP-loaded SrTiO3:La,Rh|Au|RuO2-BiVO4:Mo sheet for CO2RR coupled to water oxidation under AM 1.5G irradiation. a, A typical time course of the photosynthetic HCOO‒, O2, H2 and CO production on a CotpyP-loaded SrTiO3:La,Rh|Au|RuO2-BiVO4:Mo sheet (ca. 1 cm2). The dashed lines are guides to the eye. b, 1H NMR spectra (D2O, 500 MHz) of the solution after 6-hour irradiation using 12CO2/H12CO3‒ (orange line, top) and 13CO2/H13CO3‒ (green line, bottom) as reactants. c, Dependence of AQY for HCOO‒ production over the sheet on incident light wavelength, along with DRS of SrTiO3:La,Rh (green line) and BiVO4:Mo (orange line) for comparison. The blue dots indicate the AQYs of the system at various incident light wavelength. The error bars indicate the incident wavelength with a full width at half maximum of 15 nm.  The reactions were carried out in a CO2-saturated KHCO3 aqueous solution (0.1 M, pH 6.7) under a CO2 atmosphere (1 atm).

Figure 3 | CotpyP-loaded SrTiO3:La,Rh|Au|RuO2-BiVO4:Mo photocatalyst sheet with an active irradiated area of ca. 20 cm2 for photosynthetic CO2RR coupled with water oxidation. a, Photograph of the sheet illuminated with simulated sunlight (AM 1.5G, 100 mW cm−2). b, Time course of the photosynthetic CO2RR and water oxidation over the sheet. The dashed lines are guides to the eye. The reaction was carried out in a CO2-saturated 0.1 M KHCO3 aqueous solution (180 mL, pH 6.7) without sacrificial reagents.

Figure 4 | Selectivity and stability of the CotpyP-loaded SrTiO3:La,Rh|Au|RuO2-BiVO4:Mo sheet for CO2RR coupled with water oxidation. a, Typical current-potential curves for a bare SrTiO3:La,Rh|Au photoelectrode (orange curve) and a CotpyP-SrTiO3:La,Rh|Au photoelectrode (green curve). b, Typical chronoamperometric curves of the CotpyP-SrTiO3:La,Rh|Au photoelectrodes at an applied potential of 0.0 V (red line) and +0.5 V (blue line) versus RHE. The active areas of the photoelectrodes are ~0.2 cm2. c, Dependence of the product distribution on CotpyP-modified and bare SrTiO3:La,Rh|Au photocathodes on the applied potential after an experimental runtime of 4 h. The active areas of the photoelectrodes are ~0.2 cm2. Error bars correspond to the standard deviation (n = 3). d, Time course of CO2RR on a sheet for 30 hours, with complete replacement of the reactant media and CO2 purging every 6 hours (dash-dotted black lines) and reloading of the CotpyP cocatalyst in the last run. The “1st, 2nd, 3rd and 4th” indicate the number of reaction cycles. The dashed lines are guides to the eye. All the above experiments were carried out in a CO2-saturated KHCO3 aqueous solution (0.1 M, pH 6.7) under a CO2 atmosphere (1 atm) under simulated solar irradiation (AM 1.5G, 100 mW cm‒2).

Figure 5 | O2-tolerance of CotpyP catalyst. a, LSV scans of a CotpyP|m-TiO2|Ti electrode under CO2+N2 atmosphere (dark blue and dark red solid lines). The dark blue and dark red solid lines indicate the LSV recorded before and after 5 h of CPE carried out in CO2+O2, respectively. LSV scans of CotpyP|m-TiO2|Ti recorded under CO2+O2 atmosphere (orange solid line), along with LSV scans of m-TiO2|Ti under CO2+N2 atmosphere (black dash line) and CO2+O2 atmosphere (red dash line) are presented for comparison. The scans were recorded in an aqueous KHCO3 solution (0.1 M, pH 6.7) and dark condition at a scan rate of 50 mV s-1. b, J-t traces from the first 5 hours of CPE with CotpyP|m-TiO2|Ti under a CO2+N2 atmosphere (red trace) and CO2+O2 atmosphere (blue trace) at an applied potential of –0.3 V versus RHE.