Avalanches and Mixing behavior of Porous 316L Stainless Steel under Tension

Yan Chen1,2, Qiangbing Wang3, Xiangdong Ding1,a, Jun Sun1 and Ekhard K.H. Salje1,2,a

1 State Key Laboratory for Mechanical Behavior of Materials, Xi’an Jiaotong University, Xi’an 710049, China

2 Department of Earth Sciences, University of Cambridge, Cambridge CB2 3EQ, United Kingdom

3 Guangzhou Sailong Additive Manufacturing Co., Ltd., Guangzhou 510700, China

a) E-mail addresses: ekhard@esc.cam.ac.uk (Ekhard K.H. Salje)

dingxd@mail.xjtu.edu.cn (Xiangdong Ding)

Abstract

The investigation of acoustic emission (AE) reveals mixing of avalanche processes in porous 316L stainless steel. One avalanche mechanism relates to the movement of dislocations, the other to crack propagation. Both mechanisms occur under different external tensions: small tension dislodges dislocations while crack propagation occurs at much higher tension close to the mechanical failure point. In an intermediate overlap regime, both effects occur simultaneously. The avalanche related power laws show a mixing behavior where the higher avalanche exponents form an upper limit for the mixing curve and the lower exponent is approached asymptotically for strong AE signals. The power law probability distribution functions, PDF, shows a characteristic upwards bend near the crossover between the two mechanisms. The three regimes, namely the dislocation movement, mixing, and crack propagation, are confirmed by other avalanche characteristics: the sparseness of the AE spectra, the avalanche exponents of energy, amplitude and duration. Only the crack propagation follows mean field predictions, while the dislocation movements (in confined spaces) deviates significantly from mean field behavior with much greater exponents than predicted in this approximation. We demonstrate that apparent deviations from scale invariance are, in reality, the result of two superimposed avalanche processes whereby each of them remains scale invariant. The seeming deviations from scale invariance are actually superposition effects.

Crackling noise is the manifestation of avalanches, which are commonly observed under divers scenarios like magnetization processes [1], martensitic transitions [2], crystal plasticity [3-4], stellar evolution [5], ferroelectric switching [6] and material failure [7-10]. A quantitative analysis is commonly undertaken under external forcing with constant rates, with the known highest experimental resolution for the collapse of porous materials [11-16], ferroelastic crystals [4, 17-19] and nano pillars [20-22].

Experimentally, one of the most accurate methods for the observation of crackling noise is the measurement of acoustic emission (AE). AE is associated with rapid changes of the strain field in an externally forced material. Detection of AE is a very sensitive technique adequate to detect local changes that occur at length scales ranging from nanometers to micrometers. It has been widely used to monitor crackling noise in materials subjected to an external stress whereby several competing processes can combine to generate AE spectra [23]. As an example, we found that a MgHo binary displays such kind of mixing characteristics. Collapsing holes and movements of dislocations compete under external forcing during acoustic emission experiments [24].

A major objection to the idea of scale invariance of avalanches is related to deviations from the required scale invariance: avalanches signals are power law distributed with trivial deviations for small length scales (~ the atomic cut-off) and large length scales (~ the sample size cut-off). Such wide ranges for power law distributions were indeed observed in some cases. Good experimental data were shown, e.g. over ca. 7 orders of magnitude of scale invariance with very little indication of any sample size cut-off in [11]. Nevertheless, other distributions show apparently non-power law distributions were the deviations from the scale invariances appears as deviations from a power law distributions somewhere in the middle of the distribution function. These deviations are unrelated to trivial cut-off effects. They are often observed as an upwards bend of the distribution functions [24] which defines a typical scale [25]. This problem was treated theoretically in [23] where it was argued that such upwards bends and their statistical consequences in the shape of the maximum likelihood curves [26] are due to the coincidence of separate physical processes, whereby each process is leading to scale invariant avalanches. With other words, the proposed solution is that several avalanche processes coexist with each individual avalanche process being scale invariant. The apparent deviation from the scale invariance of the observable total avalanche stems simply from the superposition of different avalanche mechanisms. This idea was tested previously [12, 24] where several mechanisms were identified. In this paper we report significant further progress: we designed an experiment where the mixing of the two processes is controlled experimentally. By doing so we generate three regimes, namely two regimes with a first ‘pure’ mechanism and a second ‘pure’ mechanism, and the mixing regime where both mechanisms coincide.

Our experiment became possible because we found that porous 316L stainless steel under uniaxial tension shows two different deformation mechanisms depending on the magnitude of the applied tension. Porous 316L stainless steel is probably one of the most common alloys due to its exceptional mechanical properties and a wide range of applications in chemical and petrochemical industry, wastewater treatment, and aerospace. We show that 316L displays indeed two AE mechanisms in tensile experiments and that we can distinguish between the two mechanisms in time sequences where one mechanism relates to moving dislocations and other to crack propagation. Our observations then prove that different scale invariant power laws and their mixing can be distinguished when the sample emits AE under different tensile strengths.

The porous 316L SS samples were produced by powder metallurgy. The average grain diameter of the powder is ca. 20μm. Fig.1 shows a scanning electron microscopy (SEM) image of a virgin sample after sintering, showing a large number of pores with size ranging from 10μm-200μm. Porosity of the sample is about 35%, which is determined by relative density measurements. Composition of the porous 316L SS has shown in Table 1.

Table1 Element composition of porous 316L stainless steel.

| Mass Fraction | Fe | Cr | Ni | Mo | Si | P | C | Mn |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Porous (%) | 61.26 | 15.65 | 11.05 | 2.48 | 0.78 | 0.008 | 8.67 | 0.1 |

The samples were cut into dog-bone specimens with a gauge range of 25mm×4mm×1.37mm. Uniaxial tensile experiments were performed at room temperature with a rate of 10-2mm/min on an Instron5969 Universal Testing System. We collected acoustic signals through a piezoelectric sensor, which is tied directly onto the surface of the sample. The signals from the sensor are first pre-amplified at 49dB over a frequency range between 95 kHz and 850 kHz, and transferred to the AMSY-6 AE-measurement system (Vallen-Systeme GmbH) with a time resolution of 20 MHz. An AE signal is defined as a ‘burst’ in the noise spectrum. A threshold of 20 dB was determined by an control experiment to evaluate the internal random noise of the experimental arrangement.

Time sequences of stress and acoustic signals during tension up to the sample fracture are shown in Fig. 2(a). Two sets of data are collected simultaneously. The porous sample is much softer than ordinary stainless steel [27-28] and can only reach 45 MPa as a peak stress value beyond which the stress slowly decreases instead of suffering a break after the maximum tensile strength. Figures 2(b)-(d) show time sequences of average energy (E, time integral of the squared AE-signal), duration (D, the time between the first and last threshold crossing one signal) and risetime (R, the time between the first threshold crossing and the first peak detected in one signal), respectively. All average values are obtained as summation of the AE parameters divided by the number of hits during intervals of 10s. From these results we find three different stages shown in Fig.2: stage 1 shows a high density of AE signals, stage 2 shows sparse signals with higher intensities, and stage 3 shows sparse and very intense AE signals. We then divide the data into these three groups for subsequent analysis.

The probability distribution functions (PDF) of the AE energy (E), amplitude (A), and duration (D) after separation into three regimes are shown in Fig. 3. They follow power law behavior, P(x)=x-a, with exponents for E, A, D denoted by ε, τ’, α. The PDF (Fig.3a) of regime 1 shows an exponent ε=2.34±0.03, regime 3 shows an exponent ε=1.52±0.03, whereas regime 2 shows power low mixing between regime 1 and regime 3. Maximum likelihood (ML) curves [23] in Fig.3(b) reveal that both regime 1 and regime 3 show a plateau which corresponds to their PDF exponents, while the ML of regime 2 shows a sharp decrease at low energies which is an indicator for the predicted mixing of avalanche mechanisms [23]. Figures 3(c-d) show PDFs of amplitude and duration, which also show mixing behavior. The power law exponent τ’ of amplitudes in regime 1 and regime 3 are 3.59 and 2.31 and mixing occurs in regime 2. The duration exponent  is 4.53 and 2.91 for regimes 1 and 3. Exponent mixing of avalanche populations leads indeed to non-universal power-law distributions while each primary avalanche in regimes 1 and 3 is scale invariant. The ML maxima and minima in the mixing regime are upper and lower bounds close the true exponents of the two pure mechanisms. This is demonstrated in Fig.3(b) where regime 1 shows a plateau at ε=2.4, regime 3 shows a plateau at ε=1.5 and regime 2 combines both exponents between these two extremes. A direct analysis is possible by inspection of the PDF of the AE energy, amplitude and duration in Figs.3(a,c-d), where the upward bend of the power-law curves indicates mixing. This result shows that the superposition of two power law distributed processes do not, in general, lead to an overall power law behavior. This superposition mimics a scale dependence, which, in fact does not exist. It is simply an artifact of the numerical superposition of two scale invariant distributions. To disentangle these two distributions from the experimental results is often difficult if the two competing processes cannot be identified, as we did in this work. The two sources of AE in our spectra are very easy to separate as they are associated with two different power law exponents. For more complex AE spectra, pattern recognition analyses, e.g. k-means algorithm has been successfully applied to AE monitoring to 304L stainless steel to distinguish between dislocation avalanches, microcracking and martensitic transformations [29]. We will report a similar approach in a forthcoming paper.

The correlations functions of energy versus amplitude E~Ax, amplitude versus duration A~Dχ, and energy versus duration E~Dγ equally follow power law distributions (Fig.4). The three regimes show power laws with exponents x=2.07±0.01, χ=1.53±0.01 and γ=2.94±0.02.

Fig.S1 in the supplementary material shows the distribution of waiting times (inter-event times) for three regimes. A Poisson distribution may be valid for small waiting times. For longer waiting times a power law distribution is found with an exponent near 2.3. The Poisson distribution for short waiting times may be caused by signal overlap and the spatial confinement of the avalanches [30]. The Omori law of three regimes shown in Fig.S2, from which we can see that the correlation between mainshock and aftershocks in regime2 is close to regime3. The Bath law in Fig.S3 also shows that regime1 fluctuates sharply around 1.2 while regime2 and 3 are close to the theoretical value 1.2.

In order to confirm the different origins of the two avalanches processes, we observed the tensile fracture morphology by comparison of the AE spectra with scanning electron micrograph (Fig.1(b-c)). We observed a large number of dimples distributed at the joints of the powders at the fractures in the vertical direction (Fig.1(b)). These dimples show typical plastic deformation characteristics of traditional 316L stainless steel. Meanwhile, they also have the unique morphology of powder metallurgy materials. The fracture surface in the horizontal direction shows a large number of macro-cracks in Fig.1(c). The density of the cracks increases when it is closer to the fracture surface. The different crack density is a good illustration of the uneven deformation of the sample due to the existence of a large number of holes and micro-cracks occurred in many places during the stretching process. As the tensile force increases, the micro-cracks gradually form macro-cracks and cause sample failure. This is also the reason why the stress-strain curve in Fig.2(a) reaches the maximum stress does not break immediately but slowly drops in regime 3.

By comparing the microscopic images and mechanical properties, we find that the porous 316L stainless steel prepared by powder metallurgy retains dislocation motions of traditional cold-rolled steel [31-32] at the beginning of the tension experiment. A new mechanism occurs at a later stage of deformation, namely crack propagation initiated by the high porosity. The exponent ε=2.24 in regime 1 correlates with dislocation motions. Crack propagation reveals typical exponents around ε=1.6 in regime 3, whereas in regime 2 both mechanisms coexist and show mixing behavior. Previously, Ma°løy et al. [33] studied the propagation of an interfacial crack along a heterogeneous transparent Plexiglas block and obtained a similar exponent around 1.7. Theory of crackling dynamics in material failure also shows an exponent of 1.65 [34]. The mixed regime may contain trigger events [35]. In [36] it was reported that dislocations induce crack propagation and the reverse mechanism. The statistical analyses of interevent times and of the Bath law (see supplementary Fig.S1-S3) do not imply trigger events with only two significant time correlations, namely that of dislocations and crack propagation, but no obvious cross correlations.

The values of experiment and the theoretical force integrated mean field (MF) model are compared in Table 2. The relationship between exponents of crack propagation and the theoretical values agree very well in regime 3. The values of the dislocation motion are much higher than the force integrated MF value. These results may be caused by the high porosity, which makes the sample easy to generate a large number of dislocations but makes it difficult to cause long-range dislocation movement.

Table2 Scaling consistency of three regimes.

|  | ε | τ’ | α | x | χ | γ | τ’-1 | (ε-1)x | (α-1)/χ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| regime1 | 2.24 | 3.59 | 4.53 | 2.07 | 1.53 | 2.94 | 2.59 | 2.77 | 2.31 |
| regime2 | mix | mix | mix | 2.07 | 1.53 | 2.94 | mix | mix | mix |
| regime3 | 1.62 | 2.31 | 2.91 | 2.07 | 1.53 | 2.94 | 1.31 | 1.28 | 1.25 |
| Theoretical value | 1.67 | 2.33 | 3.0 | 2.0 | 1.5 | 3.0 | 1.33 | 1.34 | 1.33 |

In summary, we showed experimentally that ‘complex’ crackling noise in steel under tension stems from the superposition of two different structural events, namely the nucleation/movement of dislocations and crack propagation. The AE spectra are fully explained by these effects. Each type of event leads to a power law distributions and, thus, scale invariance. The overall distributions are not scale invariant, however. Weak tension leads to a prominence of dislocation movements while stronger tension relates to crack propagation. The cross-over between the dislocation and crack propagation regime is characterized by the position of the upwards bend of the energy distribution.

Supplementary Material

See the supplementary material for waiting time distribution of the sample.

Acknowledgements

Financial support from the Natural Science Foundation of China (51931004, 51621063) and 111 project 2.0 (BP2018008) are gratefully acknowledged. E.K.H.Salje is grateful to EPSRC (EP/P024904/1). Y. Chen is supported by a scholarship from the China Scholarship Council to visit the University of Cambridge.

Reference

[1]	J. P. Sethna, K. A. Dahmen, and C. Myers, Nature 410, 242 (2001).

[2]	E. Vives, J. Ortín, L. Mañosa, I. Ràfols, R. Pérez-Magrané, and A. Planes, Physical Review Letters 72, 1694 (1994).

[3]	F. F. Csikor, C. Motz, D. Weygand, M. Zaiser, and S. Zapperi, Science 318, 251 (2007).

[4]	J. Weiss, W. B. Rhouma, T. Richeton, S. Dechanel, F. Louchet, and L. Truskinovsky, Physical Review Letters 114, 105504 (2015).

[5]	M. A. Sheikh, R. L. Weaver, and K. Dahmen, Physical Review Letters 117, 261101 (2016).

[6]	E. Salje, D. Xue, X. Ding, K. A. Dahmen, and J. Scott, Physical Review Materials 3, 014415 (2019).

[7]	E. K. Salje and K. A. Dahmen, Annual Review of Condensed Matter Physics 5, 233 (2014).

[8]	S. Zapperi, A. Vespignani, and H. Stanley, Nature 388, 658 (1997).

[9]	H. Ribeiro, L. Costa, L. Alves, P. Santoro, S. Picoli, E. Lenzi, and R. Mendes, Physical Review Letters 115, 025503 (2015).

[10] T. Mäkinen, A. Miksic, M. Ovaska, and M. Alava, Physical Review Letters 115, 055501 (2015).

[11] J. Baró, Á. Corral, X. Illa, A. Planes, E. K. Salje, W. Schranz, D. E. Soto-Parra, and E. Vives, Physical Review Letters 110, 088702 (2013).

[12] D. Soto-Parra, X. Zhang, S. Cao, E. Vives, E. K. Salje, and A. Planes, Physical Review E 91, 060401 (2015).

[13] G. F. Nataf, P. O. Castillo-Villa, J. Baró, X. Illa, E. Vives, A. Planes, and E. K. Salje, Physical Review E 90, 022405 (2014).

[14] G. F. Nataf, P. O. Castillo-Villa, P. Sellappan, W. M. Kriven, E. Vives, A. Planes, and E. K. Salje, Journal of Physics: Condensed Matter 26, 275401 (2014).

[15] T. Beirau and E. K. Salje, Applied Physics Letters 115, 071902 (2019).

[16] J. Baró, K. A. Dahmen, J. Davidsen, A. Planes, P. O. Castillo, G. F. Nataf, E. K. Salje, and E. Vives, Physical Review Letters 120, 245501 (2018).

[17] J. Weiss and J. Grasso, The Journal of Physical Chemistry B 101, 6113 (1997).

[18] V. Taupin, T. Richeton, J. Chevy, C. Fressengeas, J. Weiss, F. Louchet, and M. Miguel, Acta Materialia 56, 1555 (2008).

[19] J. Weiss, Philosophical Transactions of the Royal Society A 377, 20180260 (2019).

[20] N. Friedman, A. T. Jennings, G. Tsekenis, J.-Y. Kim, M. Tao, J. T. Uhl, J. R. Greer, and K. Dahmen, Physical Review Letters 109, 095507 (2012).

[21] G. Sparks and R. Maaß, Physical Review Materials 2, 120601 (2018).

[22] X. Ni, H. Zhang, D. B. Liarte, L. W. McFaul, K. A. Dahmen, J. P. Sethna, and J. Greer, Physical Review Letters 123, 035501 (2019).

[23] E. K. Salje, A. Planes, and E. Vives, Physical Review E 96, 042122 (2017)

[24] Y. Chen, X. Ding, D. Fang, J. Sun, and E. K. Salje, Scientific Reports 9, 1330 (2019)

[25] E. Faran, E. K. Salje, and D. Shilo, Applied Physics Letters 107, 071902 (2015)

[26]J. Baro ́ and E. Vives, Physical Review E 85, 066121, (2012)

[27]	S. Kheiri, H. Mirzadeh, M. Naghizadeh, Materials Science and Engineering: A 759, 90 (2019).

[28]	W. Qin, J.Li, Y. Liu, J. Kang, L. Zhu, D. Shu, P. Peng, D. She, D. Meng, and Y. Li, Materials Letters 254, 116 (2019).

[29] M. Shaira, N. Godin, P. Guy, L Vanel and J. Courbon, Materials Science and Engineering: A,   492, 392 (2008)

[30]	P. Zhang, O. U. Salman, J.-Y. Zhang, G. Liu, J. Weiss, L. Truskinovsky, and J. Sun, Acta Materialia 128, 351 (2017).

[31]	T. Mayama, K. Sasaki, and M. Kuroda, Acta Materialia 56, 2735 (2008).

[32]	M. Pham, C. Solenthaler, K. Janssens and S. Holdsworth, Materials Science and Engineering: A 528, 3261 (2011).

[33]	K. J. Måløy, S. Santucci, J. Schmittbuhl, and R. Toussaint, Physical Review Letters 96, 045501 (2006).

[34] D. Bonamy, S. Santucci, and L. Ponson, Physical Review Letters 101, 045501 (2008)

[35] T. Richeton, P. Dobron, F. Chmelik, J. Weiss, F. Louchet, Materials Science and Engineering: A,  424, 190 (2006).

[36] E. K. Salje, H. Liu, Y. Xiao, L. Jin, A. Planes, E. Vives, K. Xie, and X. Jiang, Physical Review E, 99, 023002 (2019).

Figure Captions

Fig.1 (a) Microstructure of initial porous 316L sample with porosity of 35%. (b)Dimples in the vertical direction of fracture zone. (c) Macro-cracks in the horizontal direction of fracture zone.

Fig.2 Strain stress curve and time sequence of AE (~jerk) spectra (a), average energy (b), duration (c), and risetime (d) of AE signals in porous 316L SS steel.

Fig.3 (a) Probability distribution function (PDF) of AE energy (E) for three regimes. Regime 1 shows an exponent 2.34±0.03, regime 3 shows an exponent 1.52±0.03 whereas regime 2 shows mixing of two exponents. (b) Maximum likelihood curves of three regimes confirm these results. (c) PDF of AE amplitude (A) for three regimes. Regime 1 shows an exponent 3.59±0.07, regime 3 shows an exponent 2.31±0.05 whereas regime 2 shows mixing of two exponents. (d) PDF of AE duration (D) for three regimes. Regime1 shows an exponent 4.53±0.03, regime 3 shows an exponent 2.91±0.24 whereas regime 2 shows mixing of two exponents.

Fig.4 (a) Energy versus amplitude correlations for three regimes follow a power law with an exponent x=2.07±0.01. (b) Amplitude versus duration power laws for three regimes with exponent χ=1.53±0.01. (c) Energy versus duration power laws for three regimes with exponent γ=2.94±0.02.